## Slide 1
Prof. Olivia Reinaud
Group of Supramolecular Bioinorganic Chemistry
Université Paris Descartes – CNRS UMR 8601
Metal ions in Biomimetic Cavities
Mn+

## Slide 2: Cu-Peptidylglycyl a-Hydroxylating Mono-oxygenase

## Slide 3
Classical strategy
Modeling the active site of non-heme metallo-enzymes
A supramolecular
approach
A precatalytic complex :
Amzel et al., Science, 2004

## Slide 4: Cu(II) complexes
TREN
TMPA
EtOH
MeCN
The Metal-Ligand interaction is fully controlled by the calix-cryptand
Open access to the metal center
No exo-binding
Well-defined second coordination sphere
PNAS, 2005, 102, 6831 - Chem Commun. 2007, 810 - J. Am. Chem. Soc. 2009, 131, 17800
Notes: Week interactions can have big (major) consequenses

## Slide 5: Functionalization of electroactive surfaces

## Slide 8
Electro-grafting a Funnel complex
H2O/KNO3 0.1 M + HEPES 0.05 M (pH = 9.4)
v = 0.1 V/s
E /V vs Ag/AgCl
30 cycles

## Slide 9
CVs (v = 0.1 V/s, E /V vs Ag/AgCl) in H2O/KNO3 0.1 M + HEPES buffer 0.1 M at different pH values
B) Plots of Epa (red circles) and Epc (black squares) vs pH.
CV (v = 0.05 V/s) in H2O/KNO3
0.1 M + HEPES 0.05 M (pH = 9.4)
B) CVs (v = 0.1 V/s)
in CH2Cl2/NBu4PF6 0.2 M (black)
in CH3CN/NBu4PF6 0.1 M (blue)
in H2O/KNO3 0.1 M (red, pH = 9.4)
Grafted decanethiol modified gold electrode

## Slide 10
in H2O/KNO3 0.1 M + HEPES buffer 0.1 M (pH = 9.4)
Response to i-PrNH2
[iPrNH2]: 2.5 µM < C < 35 µM.

## Slide 11
CVs in H2O/KNO3 0.1 M + HEPES buffer 0.1 M
pH = 9.4 for A, B, and C, pH = 10.4 for D
before (a, black) and after addition of amine (b, colored)
Selective detection of primary alkylamines in water
20 µM
n-OctNH2
20 µM
2-aminomethyl-
butane
50 µM
2-amino-
6-methylpyridine
50 µM
dopamine

## Slide 12
Selective detection of primary alkylamines in water

## Slide 13
Schematized strategies based on thiols and diazoniums for grafting organic layers onto surfaces
Dream :
Compact
Robust
Functional
Mono-layer

## Slide 14
Solid
Rigid
Functional
Radical-proof
Nature comm. 2012

## Slide 15
Cyclic voltammetry of glassy carbon electrodes modified with calixarenes and post-functionalized with ferrocene . CH2Cl2 + 0.2 M NBu4PF6 Scan rate varied from 0.1 to 3 V. s-1.
Robust mono-layer, very few defects
High density of functional groups, homogeneous

## Slide 16
Postfunctionalization of mixed monolayers
Mixed monolayers
J. Phys. Chem. C 2014, 118, 15919

## Slide 17: Perspectives
Patent + Spin off ULB, A. Matuzzi IJ,PH, OR
Cu+
Cu+
Poster
A. Brugnara (PhD)

## Slide 18
ANR « Calixzyme » 2005‐09, ANR « Cavity‐zyme (Cu) » 2010‐14
Y. Le Mest, P. Hapiot, I. Jabin, O. Reinaud
1998
2000
2005
Gael de Leener
Diana Over
Nicolas Le Poul
Corinne Lagrost

## Slide 20
Cyclic voltammetry in CH2Cl2 containing 0.2 M Bu4NPF6 of gold electrodes modified with calix[4]arenes and postfunctionalized with Fc-C5H10-NH2. The modified surfaces were obtained from the electrografting of diazonium cations in situ generated from (a) a pure solution of 3, (b) a pure solution of 4, (c) a 50/50 mix solution of 2 and 4, and (d) a 90/10 mix solution of 2 and 4.

## Slide 21
Strategy for electroclick grafting of [3.Cu(H2O)]2+ as monolayers on alkyne-terminated calix[4]arene modified gold electrodes.

## Slide 22
A ) CVs (v = 0.1 V/s, E /V vs Ag/AgCl, 25 cycles) obtained during the grafting of [3.Cu(H2O)]2+ on an alkyne-terminal calix[4]arene modified gold electrode in CH2Cl2/NBu4PF6 0.1 M + 18 µM [Cu(6-BrTMPA)(H2O)]2+ + 6 µM of [3.Cu(H2O)]2+. B) CVs (v = 0.1 V/s, E /V vs Ag/AgCl) at a [3.Cu(H2O)]2+-grafted calix[4]arene modified gold electrodes in CH2Cl2/NBu4PF6 0.2 M upon successive addition of acetonitrile (blue to red, max 4% vol.). Pas cité dans le texte ?

## Slide 23
Grafting of [3.Cu(H2O)]2+ on an alkyne-terminal decanethiol modified gold electrode under Ar) in H2O/KNO3 0.1 M + HEPES 0.05 M (pH = 9.4) + 20 µM [Cu(6-BrTMPA)(H2O)]2+ + 20 µM of [3.Cu(H2O)]2+. A) Successive CVs during the grafting process (v = 0.1 V/s, E /V vs Ag/AgCl, 30 cycles). B) Monitoring of the surface coverage q as a function of time obtained during the grafting: experimental (red) and simulated (blue and black) plots for: n = 1 (black) and n = 2.8 (blue) with k = 1.35 10-4 s-1.

## Slide 24
Figure 6. A) CV (v = 0.05 V/s) of the [3.Cu(H2O)]2+ decanethiol modified electrode in H2O/KNO3 0.1 M + HEPES 0.05 M (pH = 9.4). B) CVs (v = 0.1 V/s, E /V vs Ag/AgCl) at a [3.Cu(H2O)]2+ decanethiol modified electrode in CH2Cl2/NBu4PF6 0.2 M (black), CH3CN/NBu4PF6 0.1 M (blue) and in H2O/KNO3 0.1 M (red, pH = 9.4)
Experimental surface concentration was determined by integration of the current signal at low scan rates (G = 1.3 × 10-10 mol/cm2). For comparison, theoretical surface concentration (G = 8.8 × 10-11 mol/cm2) value was calculated by assuming an optimized compact alignment of the molecules onto the surface with the complex being an ellipse of S = 188 Å2 surface area