## Slide 1
Tesla Technology Collaboration Meeting, Saclay
July 5, 2016
LCLS-II CM Ambient Magnetic Field Management

## Slide 2: Magnetic scope, specifications & sources
First large CW project where magnetic shielding being analyzed stringently, especially longitudinal component of magnetic field
  Bavg ↓ → Rs ↓ → Q0 ↑ → Pdiss↓ → $capital & oper ↓
LCLS-II specification [1]:
  Bavg<5 mG to reach Q >2.7E10 at 2 K, 16 MV/m
Major magnetic field sources: vacuum vessel, components, earth
  Bvessel< 3 G [2]
  Bcomponents~ 1 G
  Bearth≈ 483 mG at SLAC [3]
  B//,beamline≈ 150 mG [4]
Most analyses done assuming SLAC tunnel magnetic fields
[1] “1.3 GHz Superconducting RF Cryomodule,” Functional Requirements Document, LCLSII-4.5-FR-0053.
[2] A. Crawford, arXiv:1507.06582v1.
[3] National Oceanic and Atmospheric Administration, 2014--2019 World Magnetic Model.
[4] S. Anderson, ”Tunnel Background Field Measurement in Linac Sectors 2-10 and in the LCLS Undulator Hall.”

## Slide 3: Trapped Magnetic Flux & Q0
Smaller ambient magnetic fields beneficial
  For high Q & for low flux expelling material
Q0>2.7 x 1010 may be realized for trapped B<3 mG
  For N-doped
↓B  ↑ ↑Q0
M. Martinello et al., IPAC 2016
S. Posen et al., J. Appl.
Phys. 119, 213903 2016

## Slide 4: Ambient Magnetic Field Management Methods
2-layer passive magnetic shielding
  Manufactured from Cryoperm 10
Strict magnetic hygiene program
  Material choices
  Inspection & demagnetization of components near cavities
  Demagnetization of vacuum vessel
  Demagnetization of assembled cryomodule / vessel
Active longitudinal magnetic field cancellation

## Slide 5: Fluxgates in pCM cavities
4 cavities instrumented with fluxgates inside helium vessel
  Cavities 1, 4, 5, 8
2 fluxgates per cavity
  #1: 45°to cavity axis, in vertical plane of cavity
  #2: 90°to cavity axis

## Slide 6: Longitudinal fluxgates outside cavities
5 fluxgates
  Cavities 1, 2, 5, 7, 8
  Mounted between the two layers of magnetic shields
  Parallel to cavity axis

## Slide 7: 2-layer magnetic shields
Manufactured from Cryoperm 10

## Slide 8: Magnetic hygiene program - Components
Materials in close proximity to cavities controlled
  Non magnetic materials preferred
  If stainless steel needed, 316LN or 316L preferred
All stainless steel & other magnetic components checked for residual magnetic fields
  Residual fields at cavity RF surface distance should be ≤5 mG
  Invar rod subject to this requirement too
    Checked & demagnetized after final welding & grinding

## Slide 9: Magnetic hygiene program – Vacuum Vessel
Helmholtz coils wound onto vessel directly
Residual mag field at beamline, top & bottom equators
Bavg > 500 mG
↓
<50 mG & uniform
Bz > 300 mG
↓
<50 mG & uniform

## Slide 10: Magnetic fields as assembly progresses
Fields up to 46 mG discovered after major assembly work
  Cryo-piping welds, warm coupler install, etc.
Investigation performed & ruled out several sources
  Vacuum vessel deduced to be magnetized
Cryomodule successfully demagnetized using in-place coils

## Slide 11: Summary
First large scale project where
  Magnetic hygiene very strictly enforced
  Cryomodule instrumented to monitor magnetic environment
2-layer magnetic shielding of cavities
Fluxgates monitored during cryomodule assembly
Helmholtz coils outside vacuum vessel
  Able to demagnetize vessel & cryomodule in-situ