## Slide 1: Ultimate gradient limitation in Nb SRF cavities: the bi-layer model and prospects for high Q at high gradient
Mattia Checchin
TTC Meeting, CEA Saclay, Paris
07 JUL 2016

## Slide 2: What is the ultimate gradient limitation for bulk Nb cavities?
Penetration of magnetic flux quanta in the superconductor
Vortexes can penetrate when the applied magnetic field approaches the field of first penetration. This latter falls in between two limits:
The lower critical field :
    Field at which a vortex far from a surface and not interacting with other vortices is stable in the superconductor
The superheating field :
    Highest field H for which the G-L free energy still posses a local minimum as a function of the order parameter
Analytical formulas of and for of our interest do not exist – we need numerical calculations!
  → A self-consistent code was developed

## Slide 3
Hc1 calculation

## Slide 4: Hc1 from the Gibbs free energy
The lower critical field corresponds to the H value at which the non-interacting-vortex Gibbs free energy is equal to zero.
Therefore:
Where:
1
The lower critical field is then defined as:
1 A. A. Abrikosov, Zh. Eksp. Teor. Fiz. 32, 1442 (1957), [Soviet Phys.—JETP 5, 1174 (1957)]

## Slide 5: Numerical calculation of GL equations in a vortex
Order parameter
Vector potential
Magnetic field
The adimensional GL equations in cylindrical coordinates are:
Boundary conditions:

## Slide 6
Hsh calculation

## Slide 7: Hsh calculation
The superheating field corresponds to the highest field H for which the G-L free energy still posses a local minimum as a function of the order parameter
Numerically, Hsh can be calculated as the highest field for which a valid solution () to the G-L equations still exist
The self-consistent code increases H iteratively till the previous statement is verified

## Slide 8: Numerical calculation of GL equations at the surface
The adimensional GL equations in 1 dimension are:
Boundary conditions:
Order parameter
Vector potential
Magnetic field

## Slide 9: Simulations Summary
The simulation are in agreement with previous calculations.
The analytical formulas that best fit the simulated points between are:

## Slide 10: Experimental data vs Theory
1
2
2
1 S. Casalbuoni et al., Nucl. Instr. Meth. Phys. Res. A 583, 45 (2005)
2 B. W. Maxfield and W. L. McLean, Phys. Rev. 139, A1515 (1965)
The parameters used in the simulation are experimental values from bibliography:

## Slide 11: Quench fields summary
N-doped cavities so far quench below Bc1
→ statistically, N-doped cavities are quenching close or below the lower critical field
120 C baked cavities quench always above Bc1
→ 120 C baked cavities can reach the metastable Meissner state above the lower critical field
EP cavities seem to quench at Bc1, but because of the HFQS we cannot conclude that Bc1 is the limitation
→ the dissipation regime is different
The Bean-Livingston barrier may give us more insight on what’s going on…

## Slide 12
Bean-Livingston barrier calculation

## Slide 13: Bean-Livingston Barrier
C. P. Bean and J. D. Livingston, Phys. Rev. Lett. 12, 14 (1964)
Bulk

## Slide 14: Bean-Livingston Barrier – Forces in play
Vortex – Field interaction
Vortex – Anti-Vortex interaction

## Slide 15: Bean-Livingston barrier
The cleaner the material (low k) the higher the barrier and the stronger the attractive force
Why 120 C baked cavities overcome Bc1 if they have the shortest barrier?
NB: the Bean-Livingston barrier represents the energy cost a vortex has to spend to penetrate the superconductor.
Gibbs free energy
Force per unit of length

## Slide 16: Experimental data vs Theory
N-doped possess higher barrier (stronger attractive force) than 120 C baked cavities
Why 120 C baked cavities, that should have lower quench field, are quenching instead at larger field than N-doped cavities?
Why only 120 C baked cavities can systematically overcome Bc1?

## Slide 17: Experimental data vs Theory
A. Romanenko et al., Appl. Phys. Lett. 104, 072601 (2014)
Constant
inside the penetration depth
Non-constant inside the penetration depth

## Slide 18
Bean-Livingston barrier with a dirty layer on the surface

## Slide 19: K profile
I assumed an analytical sigmoidal profile that represents a dirty layer on the surface of the superconductor:
Where:
surface
bulk
dirty layer thickness
penetration depth
profile steepness

## Slide 20: Attractive force enhancement
constant
,

## Slide 21: Attractive force enhancement
constant
,
3 times larger attractive force!!

## Slide 22: Force enhancement at the interface
attractive force
repulsive force
The force is enhanced by the presence of the dirty-clean interface

## Slide 23: Dependence on the layer’s
The dirtier the layer, the stronger the attractive force

## Slide 24
Prospects for High Q0 at High Gradient

## Slide 25: The path for high Q0 at high gradients
Dirty layer at the rf surface:
Enables high gradients (e.g. 120 C baked cavities)
Nitrogen doping:
Enables high Q-factors

## Slide 26: The path for high Q0 at high gradients
Let’s merge together the two effects
Dirty layer at the rf surface:
Enables high gradients (e.g. 120 C baked cavities)
Nitrogen doping:
Enables high Q-factors
Nitrogen infusion:
Enables high Q-factors at high gradients!

## Slide 27: Experimental results
The new Fermilab’s results show high Q0 at high gradient
The presence of a dirty doped layer at the surface might explain such results!

## Slide 28: Conclusions
A dirty layer at the surface seems beneficial in order to increase the quench field above
The magnetic field profile is perturbed by the dirty layer
The attractive force is enhanced at the layer-bulk interface
The smart tuning of the very surface might increase both and the maximum gradient
Tenths of nanometers doped layer
High at high field are possible!
Low cryogenic cost at high fields
Higher duty-cycle ILC?

## Slide 29
Thank you

## Slide 30
Backup Slides

## Slide 31: Shooting Method
Lets assume the following BVP
The correspondent IVP would be:
Solving the IVP we can get the solution at the position .
So, we can define the function as:
If such function has a root , then is solution of the BVP as well.

## Slide 32: Hc1 calculation code flow chart
BVP
GL equations
Shooting Method
f(r0), f’(r0)
a(r0), a’(r0)
Solution
f(r0), f’(r0)
a(r0), a’(r0)
k=kmax
Final
Solution
ε, Hc1
Print
STOP
R = R + Rstep
k = k + kstep
R=Rmax ||
f(R)>1 || f’(R)<0 ||a’(R)>0 ||
a’(R)<-1/(k R2)
yes
yes

## Slide 33: Hsh calculation code flow chart
BVP
GL equations
Shooting Method
f(0), a(0)
Solution
f(0), a(0)
k=kmax
Hsh
Print
STOP
Z = Z + Zstep
k = k + kstep
Z=Zmax ||
f(Z)>1 || f’(Z)<0
Flag=true
f(0)<0.0001
H = H + Hstep
Flag=true
yes
yes
yes
yes
no solution

## Slide 34: Why does the dirty layer enhance the force?
DIRTY LAYER ()
CONSTANT
zoom
zoom

## Slide 35: Why does the dirty layer enhance the force?
DIRTY LAYER ()
CONSTANT
zoom
zoom

## Slide 36: LE-SR results
A. Romanenko et al., Appl. Phys. Lett. 104, 072601 (2014)