## Slide 1: MPGDs
Bordeaux 11/10/2018
CERN MPT workshop
Rui De Oliveira

## Slide 2: Outline
Simplified TPC field-cage production
Existing MPGDs
Resistive detectors
  Micro Resistive well and resistive MicroMegas
  Advanced DLC coated material possibilities
How can we improve energy resolution
Dynamic range

## Slide 3: TPC fieldcage

## Slide 4: Possibilities of this technique
PCB material self sustaining
Single wall
Double wall
Dismountable field-cage
Double wall with potting in between
Square TPCs with flexible angles.
Resistor assembly on rigid board.
Plated edges to simplify connections .
Resistive layer deposition to create uniform fields may be possible.

## Slide 5: Existing MPGD structures
GEMs
  uWells
  uRwells
    Single resistive layer
    Double resistive layer
Micromegas
  BULK
  Micro BULK
  Floating mesh
  Resistive Micromegas
    Single resistive layer
    Double resistive layer
THGEM
  ML THGEM
  THwell
  R THwell
  MM THGEM

## Slide 6: Resistive detectors
Why resistive layers
  Spark energy reduction ( 600 uJ in a GEM , 30uJ in a classical MM , 10 nJ in a protected device)
  Charge spreading for better spacial resolution
  Electronic front end protection not needed
Optimal resistive value for spark damage control
  The highest the better
  Below 10M there is some risks of microscopic damages (can always be cured but need new cleaning)
Optimal values for charge sharing
  For 10mm x 10mm pads  500K/square typ
  For 0.4mm lines pitch  80M/square typ
Optimal value for rate capability
  Depends a lot on the structure (single or double layers)
  Single layers up to 100Kevents/cm2 typ with one 10Mohms layer (be careful : detector size dependent).
  Double layers above 10Mevents/cm2 typ with two 10Mohms layers
Existing resistive layers
  Polymer paste 10Kohms to 100K/Square too low
  Thickfilm paste (high temp only on ceramic substrates) 10K to 100M/square limited detector size
  Resistive kapton 5M/square single value
  Disipative films 1G/square and above too high
  DLC 100K to 1G/square perfect in theory

## Slide 7: Resistive detectors
Why resistive layers
  Spark energy reduction ( 600 uJ in a GEM , 30uJ in a classical MM , 10 nJ in a protected device)
  Charge spreading for better spacial resolution
  Electronic front end protection not needed
Optimal resistive value for spark damage control
  The highest the better
  Below 10M there is some risks of microscopic damages (can always be cured but need new cleaning)
Optimal values for charge sharing
  For 10mm x 10mm pads  500K/square typ
  For 0.4mm lines pitch  80M/square typ
Optimal value for rate capability
  Depends a lot on the structure (single or double layers)
  Single layers up to 100Kevents/cm2 typ with one 10Mohms layer (be careful : detector size dependent).
  Double layers above 10Mevents/cm2 typ with two 10Mohms layers
Existing resistive layers
  Polymer paste 10Kohms to 100K/Square too low
  Thickfilm paste (high temp only on ceramic substrates) 10K to 100M/square limited detector size
  Resistive kapton 5M/square single value
  Disipative films 1G/square and above too high
  DLC 100K to 1G/square perfect in theory

## Slide 8: Resistive detectors
Why resistive layers
  Spark energy reduction ( 600 uJ in a GEM , 30uJ in a classical MM , 10 nJ in a protected device)
  Charge spreading for better spacial resolution
  Electronic front end protection not needed
Optimal resistive value for spark damage control
  The highest the better
  Below 10M there is some risks of microscopic damages (can always be cured but need new cleaning)
Optimal values for charge sharing
  For 10mm x 10mm pads  500K/square typ
  For 0.4mm lines pitch  80M/square typ
Optimal value for rate capability
  Depends a lot on the structure (single or double layers)
  Single layers up to 100Kevents/cm2 typ with one 10Mohms layer (be careful : detector size dependent).
  Double layers above 10Mevents/cm2 typ with two 10Mohms layers
Existing resistive layers
  Polymer paste 10Kohms to 100K/Square too low
  Thickfilm paste (high temp only on ceramic substrates) 10K to 100M/square limited detector size
  Resistive kapton 5M/square single value
  Disipative films 1G/square and above too high
  DLC 100K to 1G/square perfect in theory

## Slide 9: Resistive detectors
Why resistive layers
  Spark energy reduction ( 600 uJ in a GEM , 30uJ in a classical MM , 10 nJ in a protected device)
  Charge spreading for better spacial resolution
  Electronic front end protection not needed
Optimal resistive value for spark damage control
  The highest the better
  Below 10M there is some risks of microscopic damages (can always be cured but need new cleaning)
Optimal values for charge sharing
  For 10mm x 10mm pads  500K/square typ
  For 0.4mm lines pitch  80M/square typ
Optimal value for rate capability
  Depends a lot on the structure (single or double layers)
  Single layers up to 100Kevents/cm2 typ with one 10Mohms layer (be careful : detector size dependent).
  Double layers above 10Mevents/cm2 typ with two 10Mohms layers
Existing resistive layers
  Polymer paste 10Kohms to 100K/Square too low
  Thickfilm paste (high temp only on ceramic substrates) 10K to 100M/square limited detector size
  Resistive kapton 5M/square single value
  Disipative films 1G/square and above too high
  DLC 100K to 1G/square perfect in theory

## Slide 10: Resistive detectors
Why resistive layers
  Spark energy reduction ( 600 uJ in a GEM , 30uJ in a classical MM , 10 nJ in a protected device)
  Charge spreading for better spacial resolution
  Electronic front end protection not needed
Optimal resistive value for spark damage control
  The highest the better
  Below 10M there is some risks of microscopic damages (can always be cured but need new cleaning)
Optimal values for charge sharing
  For 10mm x 10mm pads  500K/square typ
  For 0.4mm lines pitch  80M/square typ
Optimal value for rate capability
  Depends a lot on the structure (single or double layers)
  Single layers up to 100Kevents/cm2 typ with one 10Mohms layer (be careful : detector size dependent).
  Double layers above 10Mevents/cm2 typ with two 10Mohms layers
Existing resistive layers
  Polymer paste 10Kohms to 100K/Square too low
  Thickfilm paste (high temp only on ceramic substrates) 10K to 100M/square limited detector size
  Resistive kapton 5M/square single value
  Disipative films 1G/square and above too high
  DLC 100K to 1G/square perfect in theory

## Slide 11: Diamond Like Carbon base material vacuum deposition on 1m x 0.6m foils
DLC/Polyimide
DLC/Polyimide/Cu
Polyimide 50 um
APICAL NP
Kapton HN
DLC 0.1 to 1um
100K to 1G/square
Polyimide 50 um
APICAL NP
DLC 0.1 to 1um
Copper 5um

## Slide 12: Single uRwell structure
Pick up pads/lines
PCB support

## Slide 13: Single uRwell structure
Copper 5um
Polyimide 50um
DLC 0.1um typ
Pick up pads/lines
Glue 75um

## Slide 14: Single uRwell structure
+
Only 1 gluing + 1 patterning + 1 etching
Probably the simplest MPGD
Flexible detectors can be produced
Low mass detectors (rare event search)
mass production compatible
Top electrode fully supported
Patterned Copper
Etched Polyimide
DLC
Pick up pads/lines
-
Lateral current evacuation
Rate limitation 10 to 100K depending on size
Only 50um amplification gap (today)

## Slide 15: Single resistive MicroMegas structure
Pick up pads/lines
PCB support

## Slide 16: Single resistive MicroMegas structure
Polyimide 50um
DLC 0.1um
Pick up pads/lines
Glue 25um

## Slide 17: Single resistive MicroMegas structure
+
Only 1 gluing + 1 Bulk
Single piece
different gaps possible
different meshes possible
SS Mesh 400 to 700 LPI
Polyimide 50um
DLC 0.1um
Pick up pads/lines
-
Lateral current evacuation
Rate limitation 10 to 100K depending on size
Not Flexible
BULK steps are still manually performed

## Slide 18: Advanced DLC materials
Cu/DLC/Polyimide
Cu/Polyimide/DLC/Cu
Polyimide 50 um
APICAL NP
Kapton HN
DLC 0.1 to 1um
100K to 1G/square
Polyimide 50 um
APICAL NP
DLC 0.1 to 1um
Copper 5um
Copper 5um
Copper 5um

## Slide 19: High rate uRwell with 2DLC layers !
Base PCB

## Slide 20: High rate uRwell with 2DLC layers !
Cu/PI/DLC/Cu  bot Cu patterning + gluing

## Slide 21: High rate uRwell with 2DLC layers !
Microvia drilling + plating + top Cu patterning

## Slide 22: High rate uRwell with 2DLC layers !
New CU/PI/DLC/Cu gluing
+ microvia drilling
+ Cu Plating

## Slide 23: High rate uRwell with 2DLC layers !
Top Cu patterning + PI etching
-Rate above 10M events/cm2.s possible
-Spark protected
-full construction with std PCB processes

## Slide 24: High rate MM with 2DLC layers
Base PCB

## Slide 25: High rate MM with 2DLC layers
PI/DLC/Cu foil gluing

## Slide 26: High rate MM with 2DLC layers
Micro via drilling + Cu plating + top Cu patterning

## Slide 27: High rate MM with 2DLC layers
New PI/DLC/Cu gluing
+ microvia drilling
+ Cu Plating
+ Cu Patterning

## Slide 28: High rate MM with 2DLC layers
Bulk creation on top of the structure
-Rate above 10M events/cm2.s possible
-Pillars should hide the Microvias
-Spark protected
-BULK step still manually performed

## Slide 29: Can we get better energy resolution in MM detectors ?
Pad polishing
  Glass substrates give even better results
Improve amplification gap uniformity
  BULK : Hard to do better than what we have today
Mesh type
  Woven ( some field variations in the holes)
  Electro-formed
  Chemical etching (round shape seems to be the best)
Resistive layer
  Cancel the high fields at the edges of the pads
Remove Pillars
  Great contributor in field distortion

## Slide 30: Interesting to know concerning energy resolution
What is the field variation if we do a scan following the blue arrow?
Constant?
Scan at mid height

## Slide 31
Extensive studies have
been done by ATLAS NSW on:
-Meshes
-HV stability
-Operational margins

## Slide 32: Best MPGD concerning Energy resolution: Micro BULK MM
  -11.2% FWHM measured (Fe55)
  -Round holes
  -No Pillars modifying fields
  -Electrodes have a mirror like finishing by process
  -Really precise gap define by base material less than 1% error
  -No pad edges in the amplification region (in the holes)

## Slide 33: Dynamic range
Micromegas and micro-wells
  In Ar/Co2 mixtures with cosmic muons
  Average minimum gas gain for good efficiency : 3000 to 5000
  Sparks or instabilities at gas gain of 10 000 to 20 000
In similar conditions a triple GEM detector can reach gas gains above 100 000 before having instabilities.
It seems that only multi amplification gap devices can reach higher dynamic range.
  Triple or quadruple GEM detectors (THGEM also)
  Or may be multimesh structure

## Slide 34: Multi Mesh device: MM THGEM Marco Cortesi Rui De OLiveira
-Self supporting panel no frames no pillars
-large size compatible
-Mass production compatible
-See Marco’s talk for performances

## Slide 35
Future tests
- 2 and may be 3 stage MM-THGEM directly mounted on a simple PCB read-out
-triple GEM principle in a single object
-ultra Low IBF expected
-ultra High gain expected (high dynamic range)
-High rate by construction
-Efficiency/energy resolution needs to be studied?
-A multitude of possible configuration !
changing gaps, meshes, hole size, materials

## Slide 36: Other possibility : special uRwell device
High ionising part
low ionising part
Can do both

## Slide 37: Similar but with pad voltage control possible
High ionising part
low ionising part
Can do both

## Slide 38: Thank you

## Slide 39: Back slides

## Slide 40: Multi-Mesh Thick GEM – MM-THGEM

## Slide 41: simulations results
Garfield and Megaboltz qualitative Ion/Electron transport
and avalanche simulation
Map of electric field strength

## Slide 42: Gain MM-THGEM alone
-Maximum achievable gains (>105 and >104 for He/CO2 and Ar/CH4 respectively)
-Best configuration: High electric field strength in the avalanche gap and low dipole field at the extremities of the MM-THGEM holes.
-The avalanche processes are largely confined in the small volume between the two meshes, with small or no significant contribution from the pre- and post-amplification volumes.

## Slide 43: IBF study

## Slide 44: IBF versus MM-THGEM gain
-Different MM-THGEM bias configurations tested (expressed in term of the parameter α).
-The WELL-THGEM electrode was kept at 900 Volt, corresponding to a gas gain of around 20.
-Most of the gas gain is delivered by MM-THGEM
-High capability of the MM-THGEM to trap ions generated by its own avalanches.

## Slide 45: IBF versus Well THGEM gain
-MM-THGEM is efficient in trapping ions coming from the beneath transfer field also.
-lower IBF (ranging from 1.5-2%) is attained when the contribution of the WELL-THGEM to the total gain is the higher .
-ions drifting from the underneath multipliers are also trapped in the bottom mesh.

## Slide 46: uRwell High rate with 2 DLC layers
+
-High rate
-Single piece
-Flexible
DLC
-
-Silver interconnects must be printed
-Accurate Screen printing difficult with large size
-Back build up process increasing seriously the complexity
Silver connection in yellow

## Slide 47: High rate Micromegas with 2 DLC layers
+
-High rate
-Single piece
DLC 0.1um
-
-Silver interconnects must be printed
-Pillars should hide silver connections
-Accurate Screen printing difficult with large size
Silver connection