## Slide 1
L’ordre amorphe dans les verres dévoilé par les réponses non linéaires.
G. Biroli (CEA/IPhT-ENS), J.-P. Bouchaud (CFM)
Perpignan Univ.: P. M. Déjardin
Albert et al. Science (2016).
Started the 11/09/2004 thanks to:
Since then:
CEA/SPEC: D. L’Hôte, R. Tourbot, F.L. + C. Crauste, C. Brun, S. Albert, P. Gadige
Augsburg Univ.: P. Lunkenheimer, A. Loidl + Th. Bauer, M. Michl
For a review see "Nonlinear Dielectric Spectroscopy" Springer series ArXiv : 1807.03984

## Slide 2
Glasses : the simplest experiment…
Since 1927: 9 drops !!!
The physicist who started this experiment deceased after 2 drops …
Glasses would be both solid AND liquid. There are long time scales
A hammer breaks it…
And yet … it flows !!!...
Bitumen :
http://en.wikipedia.org/wiki/Pitch_drop_experiment

## Slide 3
Glasses: two key observables (ta and Sc)
tα
ta~10-12s
T
Tm
Tg
Liquid
Supercooled liquid
Glass (out of Eq.)
ta=100s
(Crystal)
T0
Would there be an underlying critical point driving the glass transition ?
Sc(T)=S(T)-Scryst(T)
 Supercooled dynamics is (would be?) related to thermodynamics :
 + other (semi)-universal features…
W. Kauzmann (1948)
←Adam Gibbs (1965)

## Slide 4
Theories:
S(q) [a.u.]
Polybutadiene, Tg 180K
Criticality ? Nothing is obvious …!
The glass looks like the liquid
Dynamical Heterogeneities (DH)
Kinetic theories:
 Kinetically Constrained Models (Garrahan, Chandler, et al…): Trivial thermo., only kinetic rules matter.
Glasses  ultra viscous liquids at any T
Thermodynamic theories:
Hurley, Harowell, PRE, 52, 1694, (1995)
Ncorr
Glasses  driven by a thermo. critical point
 RFOT (Wolynes etc…) : Amorphous order
 Frustration (Tarjus, Kivelson, etc…) : locally prefered structure
Can we test the existence of a thermodynamic critical point (Ncorr  at low T) ?

## Slide 5
Outline:
Why measuring c3 and c5 in glasses.
  A long story
  Dimensional analysis
  Bouchaud Biroli’s predictions
Orders of magnitude.
  Definition of c3 and c5
  Worst case analysis
Results & interpretations.
  w and T behavior of c3 and c5
  Discussion.
Summary and Perspectives.

## Slide 6
3rd and 5th order responses in glasses: a long story
 contrarily to c1, c3 (and c5 …) are predicted to reveal collective effects in glasses
Spin glasses
Molecular glasses
Colloïdal glasses
Frequency (Hz)
c3 (a.u.)
Frequency (Hz)
Frequency (a.u.)
Cu: Mn (1% at.),
Levy PRL (1986)
Crauste, PRL (2010)
Seybolt, Soft Mat. (2016)
Glycerol,
PNIPAM,
Frozen disorder ? YES Detailed balance ? YES
Even though these 3 glasses are different: anomalous features in c3 reveal Lglassy
Frozen disorder ? NO Detailed balance ? YES
Frozen disorder ? NO Detailed balance ? NO
Tests of predictions
P = c1 E+ c3 E3+ c5 E5 +…

## Slide 7
The interest of X3 and X5 in a nutshell: a dimensional analysis
Amorphous ordering phase transition :
The higher the order k ≥ 3, the stronger the divergence in T.
Thermodynamics of independent dipoles:
Independent « paquets » of Ncorr Ld dipoles
0
1
1
----- k=1 (linear resp.)
----- k=3
----- k=5
If  thermod. amorphous ordering: c1 is blind to it, contrarily to c3, c5…
Ld/2p
+ +…
t =
L
If

## Slide 8
Bouchaud-Biroli’s prediction [PRB, (2005)] for c3 at any frequency:
Because of Sc, the spin glass (increasing) plateau of X3 becomes an (increasing) peak
If Ncorr~ Ldf is large enough
X3, sing
wta
« 1 »
X3,
X3 = X3, sing+ X3, trivial
The higher the order k≥3, the more anomalous the w and T dependences.
Generalizing to c5: Albert et al. Science (2016)
X5, sing
wta
« 1 »
X5
X5 = X5, sing+ X5, trivial
where:
Peak at similar wta
These predictions can be tested experimentally…

## Slide 9
Outline:
Why measuring c3 and c5 in glasses.
  A long history
  Dimensional analysis
  Bouchaud Biroli’s predictions
Orders of magnitude.
  Definition of c3 and c5
  Worst case analysis
Results & interpretations.
  w and T behavior of c3 and c5
  Discussion.
Summary and Perspectives.

## Slide 10
Safer to detect ck at the kth harmonics
Definitions of c3 and of c5:
P
e
Supercooled liquid, controled T
VS (t)
For “low enough” E
+even harmonics

## Slide 11
Which sensitivity/field values are needed ? A worst case analysis
For an ideal gaz, |X1|, |X3| and |X5 | have no hump in w
 do not depend on T
Ideal gaz of dipoles:
…
for {p=4D; 10MV/m; 200K}
[W. Coffey et al, P. R. I. A.(1978) and P. M. Déjardin (2016)]
Which frequency dependence ?
Measuring c3 (or c5) is (very) difficult
0.2
N.B.: fa  peak of c1’’(w), as in supercooled liquids
wta  f/fa
The Xn(k) are dimensionless
Contrasts with BB close to Tg

## Slide 12
Outline:
Why measuring c3 and c5 in glasses.
  A long history
  Dimensional analysis
  Bouchaud Biroli’s predictions
Orders of magnitude.
  Definition of c3 and c5
  Worst case analysis
Results & interpretations.
  w and T behavior of c3 and c5
  Discussion.
Summary and Perspectives.

## Slide 13
Behavior of X3(w,T):
 Crauste-Thib., Brun, L’Hôte, F.L., PRL (2010), PRL (2012)
 3w susceptibility measured on many liquids:
 Bauer, Michl, Lunkenheimer, Loidl, PRL (2013), PRL(2015)
 Casalini, Fragiadakis, Roland, JCP (2015), (2017)
Richert, Kim, Young-Gonzales, JCP(2016)
Young-Gonzales, Adrjanowicz, Paluch, Richert, JCP(2017)
Contrary to X1, X3 has qualitative anomalies in {w,T}
 Main features of X3(3) :
 Humped shape for |X3(3)|, for a fixed value of f/fa
 Arg [X3(3)] depends only on f/fa
 Low frequency plateau does NOT depend on T
All these features are consistent with B&B’s prediction  Ncorr(T)  TcT
Bauer, PRL (2013)
Brun PRB (2011)
 The hump increases as

## Slide 14
The three X3’s:
Strongly suggests a common physical origin for the three X3’s : OK with B&B
Striking similarities for the moduli and for the phases
for f > 0.5 fa
for f > 5 fa
f/fa
f/fa

## Slide 15
How much is the increase of Ncorr upon cooling ?
X3max~ Ncorr(T)  very slowly in T :
See criticality see x10 on X3,max
|X3(3)(w,T)|
t0= 10-14 s and ta, min = 10-4 s  ta, max = 1018 s … !!!  Age of the Universe
Alternative way to test criticality: compare c3, c5, c7
Tg
ta
Tinitial
Tfinal
ta=0
Aging: observables depend on ta
Ncorr /Ncorr(eq)
ta, [s]
Brun et al. PRL 109, 175702 (2012)

## Slide 16
The interest of X3 and X5 in a nutshell: a dimensional analysis
Amorphous ordering phase transition :
The higher the order k ≥ 3, the stronger the divergence in T.
Thermodynamics of independent dipoles:
Independent « paquets » of Ncorr Ld dipoles
0
1
1
----- k=1 (linear resp.)
----- k=3
----- k=5
If  thermod. amorphous ordering: c1 is blind to it, contrarily to c3, c5…
Ld/2p
+ +…
t =
L
If

## Slide 17
c5 behaves as predicted by B&B
 2  compact amorphous domains
Propylene Carbonate  Glycerol
Behavior of c5(w,T):
, µ 2
 At the peak:
At fixed T: |c5(w)| has a « super peak »

## Slide 18
Outline:
Why measuring c3 and c5 in glasses.
  A long history
  Dimensional analysis
  Bouchaud Biroli’s predictions
Orders of magnitude.
  Definition of c3 and c5
  Worst case analysis
Results & interpretations.
  w and T behavior of c3 and c5
  Discussion.
Summary and Perspectives.

## Slide 19
Which kind of length in X3 and X5 : dynamic or static ?
There exists a thermodynamic critical point (static length) driving the physics around Tg
Our experimental results
 Theories with non trivial thermodynamics (Tc drives the physics around Tg):
  RFOT (Tc=TK)
  Frustration (TcTM)
 Theories where only dynamical rules matter:
  Standard version of Kinetically Constrained Models (KCM) seem unable to account for c5 and c3.
Consistent with…
NOT consistent with…
 The hump lies at f  fa so the length should be considered as dynamic
BUT:  dSc works quite well for X3(3) and X2;1(1) [see Richert et al. (2015)-(2016)].
 … and something more can be drawn from available theories of glasses…

## Slide 20
How to define thermodynamic amorphous order ? The Point to Set length LPS:
(Extensive) Monte Carlo simulations do show LPS increasing upon cooling.
 compare two states at a given T.
R
Frozen in a
Not frozen in R3
sa = <occupation of ■>a
sR,a = <occupation of ■>R,a
q = <sa sR,a>a
State a
■ molecular volume
 qEA  R<LPS
 0  R>LPS
R [in molecular diameters]
q(R)
G. Biroli, J.-P. Bouchaud, A. Cavagna, et al., Nat Phys. (2008)
Bidisperse soft-spheres (d=3)

## Slide 21
Does LPS diverge or not ?
Do glasses tend towards a genuine solid state or are they very peculiar liquids ???
Our c3-c5 experimental results are consistent both with :
  RFOT (Tc=TK)
  FLD (TcTm)
 The growth of LFS is frustrated: avoided critical point at Tc  Tm
G. Tarjus, Kivelson et al. J.Phys.CondensMat (2005)
 Sconf vanishes at TK (): Ideal Glass
TK
a
----- FLD
----- RFOT
T
Tg
LPS
  is exponentially large above TK  unreachable critical point at Tc = TK
Wolynes, Kirkpatrick, Thurumalai et al (1989)…(2012)
 T>TK: mosaic state (because of Sconf >0)
  Locally Favored Structure (e.g. icosaedron)

## Slide 22
Fraction “c” of pinned molecules
T
C. Camarota, G. Biroli PNAS (2012)
...ta increases…
...ta decreases…
Random pinning changes ta  critical point at c=0 and ideal glass phase.
Random pinning as a way to test the ideal glass phase.
Random Pinning decreases Sconf without changing the structure
(...Sc decreases…)
Sc =0 Ideal glass phase
c > 1/(LPS)3
Theoretical seminal work:
Numerical works:
L. Berthier, W. Kob PRE (2012)
M. Ozawa, W. Kob, A. Ikeda, K. Myazaki PNAS (2015)

## Slide 23
Summary:
→ X3, as well as X5, has anomalous features in w and T
Where is Tc ?  Do glasses tend towards a solid state ? … :
    X3,max(T) has been measured only for 6 glass formers : do more ?
    Investigate X3 around TMCT ?
    Find a way to measure directly the static length LPS ?
Colloids: on going work by Fuchs et al.
What about polymers ?
→ Striking similarities (modulus and phase) of the X3’s
Perspectives:
BB’s prediction is consistent with the X3’s and X5 data
µ = 2 + inspection of theories: suggests that there is a thermodynamic critical point driving the glass transition.
For molecular glasses: X3 captures Lglassy(T).
Amorphous domains are  compact

## Slide 24
The nonlinear team (2014-2018):
S. Albert
R. Tourbot
F. Ladieu
C. Wiertel
-Gasquet
CEA Saclay
(SPEC/SPHYNX)
Augsburg Univ.
CEA (IPhT) and ENS Paris(LPS)
CFM
G. Biroli
J.-P. Bouchaud
Theorists:
Th. Bauer
M. Michl
P. Lunkenheimer
A. Loidl
P. Gadige
Perpignan Univ
P.-M. Déjardin

## Slide 25
Phenomenological approaches of nonlinear responses:
compatible with BB’s general theory
 Each domain  µ = µm
Oversimplified energy landscape
 Toy model (Ladieu et al. (2012))
 Pragmatical model (Buchenau (2017))
 Entropy effects (Johari JCP (2013), Richert et al. (2015),(2016))
 Box model (Schiener et al. (1996))
Energy « absorption »
The various interpretations are (or so) reunified (Gadige PRE (2017))

## Slide 26
Is there a hump for | YES | NO
¦X3(3)¦ ? | Gly, FAN, SNGN, c-Oct, 2E1H, PC*,PG*, vinyl-PC | 2PC derivatives, 1Prop.
¦X2;1(1)¦ ? | Gly, NMEC, MTHF, SAL, c-Oct, PVac, CPDE, PC,PG, vinyl-PC, 6Me3H, 2E1H, 2E1B | 2PC derivatives
¦X3(1)¦ ? | All –or so- of the tested liquids | No exception (?)
At least 6 groups involved: Arizona, Augsburg, Gottingen, Katowice, Saclay, Washington DC.
This hump at wta  1 in the various |c3| seems generic
Genericity of the peak in w and of its T behavior ?
 6 liquids including 2 plastic crystals (SNGN, c-oct)
 33  fragility  110
Augsburg group :Bauer et al PRL (2013), Michl et al JCP(2015), (2016)
The T increase of the hump upon cooling seems generic, as mainly goes as TcT

## Slide 28
Saclay setup :
ILin+I3+I5
2 ILin +8 I3
+ 32 I5
Z2 = thick
capacitor (2×thin)
Z1 = thin
capacitor
rB
rA
Vscos(wt)
VA
VB
Kill linear and cubic signals before measuring
 Passive notch filters
Filters killing 1w and 3w
3 Lockin detectors in // measuring UA; UB and UA-UB
Filters killing 1w and 3w
UA
UB
dVs and c5(5) are the same for the two samples
 We can extract automatically the c5(5) signal
Does it work ?
(See C. Thibierge et al, RSI 79, 103905 (2008))

## Slide 29
Does our experiment work ?
 It works
Saclay, glycerol, 199K, f = 0.15Hz

## Slide 31
Spin Glasses … (1/3)
For Spin Glasses at Tc : clin does NOT diverge contrarily to c3
L. Levy, T. Oglieksi PRL57, 3288 (1986), L.Lévy, PRB, 38, 4963 (1988)
with
P(J)
J
0
Anti-Ferro
Ferro
Frustration AND quenched disorder [e.g. Cu: Mn (1% at.)]
T (K)
clin (a.u.)
c3 (a.u.)
Frequency (Hz)
c3 (@10mHz)
T (K)

## Slide 32
Spin Glasses (2/3): scaling relations between c3, c5, c7…
L. Lévy, PRB, 38, 4963 (1988):
|c3| (a.u.)
Frequency (Hz)
The best evidence of criticality  Plot one critical quantity vs another one
Tc determination is no longer an issue
|c3| (other a.u.)
|c7|h²/|c5|
|c5|h²/|c3|

## Slide 33
S.G. (3/3): Spin glasses versus structural glasses (Si  dri):
1
c3 , c5, c7 … related to Ncorr  xdf
Spin glasses ARE different from structural glasses
1
1
1
clin is blind to x
Thermodynamical Amorphous ordering:

## Slide 35
What about c3 in the excess wing regime ?
The break in the slope seen in c1’’ is not seen in |c3(3)|
Excess wing regime : local relaxation. Contrary to the a relaxation (collective)
Augsburg group :Bauer et al PRL (2013)

## Slide 37
Tg
ta
Tinitial
Tfinal
ta=0
Aging: observables depend on ta
X1 and X3 do not age similarly.
Aging of X3(3) [Brun et al PRL (2012)]

## Slide 38
Aging of X3(3) (continued):
Ncorr /Ncorr(eq)
ta, [s]
Brun et al. PRL 109, 175702 (2012)
Ncorr increases during aging.

## Slide 40
High order susceptibilities close to a standard para/ferro phase transition
Standard para/ferro phase transition :
The higher the order k, the stronger the divergence in Temperature.
For independant dipoles:
L() - + …
Independant « paquets » of Ncorr~ Ld dipoles
0
1
1
----- k=1 (linear resp.)
----- k=3
----- k=5
L
Another test of criticality: compare all the various ck.

## Slide 42
E
µ
 Each domain  µ = µm
« Toy » (Ladieu et al 2012) and « Pragmatical » models (Buchenau,2016)
Two phenomenological approaches yielding X3 ~ Ncorr
 Crossover to Trivial is enforced at f<<fa
 Ncorr , d=Tanh(D/T) and tex/ta  three free parameters
Good fits for X3(1) (phase+modulus). Ncorr is reasonnable, but model dependent.
…with a link to viscous flow
q2-q1 << p
Ncorr=15@Tg+17K; d=0.60; tex/ta = 7
Buchenau, ArXiv:1512.00188v2, Prop. Carbonate
Ncorr  100 @ Tg+9K

## Slide 43
Ncorr=10; d, tex/ta unchanged
Ncorr=5 ; d, tex/ta unchanged
« Toy » and « Pragmatical » models (2/2):
 (Partially) answered questions :
 Fit ALL the X3’s with a single mechanism involving Ncorr?
 Remaining questions :
Are there subdominant terms in X3 ?
 The link between Ncorr(T) and  Ln(ta)/  Ln(T) is missing : can we recover it ?
 Similarities between the various H3(k) (modulus AND phase) ?
 Bad point : Ncorr should be the same for all X3’s  these models are too naive.
 Yes, with Ncorr = 10-100

## Slide 45
An idea of G. Johari (JCP (2013)) for X2,1(1) (Est+Eaccos[wt]).
dS  dSc
 Adam Gibbs:
JCP (1965)
 RFOT :
Wolynes et al
 More generally
B&B JCP (2004) and d=3
 Amplitude and w dependence

## Slide 46
Unification of different perspectives:
glycerol
Est = 40kV/m
Samanta, Richert JCP (2015)
L’Hôte et al. PRB (2014)
f/fa
f/fa
218K
197K
 Unification provided Ncorr(T) ~  Ln(ta)/  Ln(T)

## Slide 47
Extending entropy effects to pure ac cubic responses :
Richert (2016), Kim, Young-Gonzales, Richert JCP (2016)
dS depends on time …
+ argument to kill dS at f>fa
yields c3(3),dS
(with no subdominant term
and with fS=0.64)
Good fits for X3(3) (modulus) with the same model fitting X2;1(1)
c3(3),dS (+c3(3),trivial )

## Slide 48
Summarizing :
Striking similarities (phase and modulus) between all the X3’s in w and T
BB’s prediction (the most general)
Toy and pragmatical phenomenological models
Johari: dSdSc and Ln(ta)~1/TSc
Richert et al (2016): extension to X3(3) and X3(1)
Ncorr is the origin of (the dominant part of) all X3’s
Ncorr increases upon cooling

## Slide 50
Box Model (Schiener et al. Science (1996)):
 Each DH « k » has a Debye dynamics: {tk} chosen to recover clin(w) at each given T.
→ Designed to account for NHB experiments:
 Applying E: each DH « k » is heated by dTk (ttherm) with ttherm  tk.
→ Box model:
c3 does NOT contain Ncorr
Works well for X3(1) above fa:
 as{tk}  ta heat diffusion over one DH takes a macroscopic time close to Tg.
e.g. R.Richert’s group: PRL (2006); PRB (2007); EPJB (2008); PRL (2010)…
Small contribution to X3(3)
Negligible contribution for X2;1(1)
Richert et al. PRL (2006)
Which relation with other approaches ??

## Slide 51
Box Model (2/2):
 BM has nothing to do with homogeneous heatings (heat propagation eq. Brun JCP(2010))
 Box Model: {dTk} are « fictitious temperatures »
A « hard task for physical intuition » since at Tg: xglassy 3 nm and ta = 100s
 Two remarks:
 T dependence:
 w dependence of X3(1) :
  A (real) constant !
For X3(1) above fa : we propose to recast the Box model in the {Ncorr; Sc} langage.
fictitious ?

## Slide 54
wta  f/fa
fa peak of clin’’(w)
|clin(w)| has no peak
Definition of fa:
Chart: Frequency [Hz]
Chart: Frequency [Hz]

## Slide 55
How to measure cubic susceptibilities
Vmeas
r1
Z2 = thick
capacitor
(2×thin)
Z1 = thin
capacitor
r2
Vac e j w t + Vst
Either push E as high as possible OR use a bridge with 2 samples of different thicknesses
C. Thibierge et al, RSI 79, 103905 (2008))
DV~ Vst2 Vac
Phase (DV) = cte
 when r1Z1=r2Z2 : Plin cancels
ILin +
INonlLin
2 ILin +
8 INonlLin
DV = Vmeas(Vac,Vst)
- Vmeas(Vac,0)
gives PNonLin