## Slide 1: CMS Tracker Upgrade France Tests mécaniques et thermiques d’un prototype d’un Dee
Nick Lumb
Institut de Physique Nucléaire de Lyon
05/12/2018

## Slide 2
PS modules
Glued directly to carbon fiber skins above carbon foam thermal contacts
Inserts in Dee for 3x positioning screws per module

## Slide 3
2S modules
5x aluminium inserts per module
For positioning and thermal contact

## Slide 4: Objectifs des tests
Tests mécaniques
  Planéité globale
  Epaisseur du sandwich
  Précision en XYZ des inserts PS et 2S
Tests thermiques
  ∆T de 10°C entre fluide de refroidissement (CO2) et les modules
  Variation entre modules

## Slide 5: Mechanical precision

## Slide 6
Overall flatness: laser scan (M3Axes)
Measurements performed with no constraints on prototype

## Slide 7: Overall flatness: laser scan
+3.5mm
-3.5mm
+3.5mm
-3.5mm
-0.4mm
+0.4mm
+0.4mm
-0.4mm

## Slide 8: IPNL measurements
Romer measurement arm, ruby tip (3mm/6mm); prototype minimally constrained in vertical position

## Slide 9: Measurement points - PS
CF skin height
local to inserts
CF skin height
above C-foams
Insert center and height (6mm ruby measurement tip in 3mm hole)

## Slide 10: Measurement points - 2S
CF skin height
local to inserts
CF skin height at module center
Height of module mounting surface
Center of circle reconstructed from points on insert nipple (3mm ruby tip)

## Slide 11: Meshed measurement points on CF skin (Z+ side)

## Slide 12: Surface deviation from nominal: Z+ side
Third party laser scan (M3Axes)
IPNL measurements
+0.4mm
-0.4mm
80% of surface within +/- 160 microns of nominal
But some zones with deviations of up to 0.4mm
OK for planarity spec. but could cause problems for PS module mounting – see later

## Slide 13: Distance between Z+ and Z- meshes
3 distinct zones:
2S region: 9.7-9.8mm
PS region: 9.6-9.7mm
Regions without inserts or C-foams: 9.3-9.4mm
Target thickness: 9.8mm
(9.0mm Airex + 2x 0.4mm skins)

## Slide 14: Insert XY precision within modules
Chart: Fits to modules - DeltaX all PS
| -0.14 | -0.12 | -0.1 | -0.08 | -0.06 | -0.04 | -0.02 | 0 | 0.02 | 0.04 | 0.06 | 0.08 | 0.1 | 0.12 | 0.14 | ou plus...
Fréquence | 0 | 0 | 0 | 0 | 2 | 1 | 3 | 28 | 23 | 3 | 1 | 1 | 0 | 1 | 0 | 0
Chart: Fits to modules - DeltaY all PS
| -0.14 | -0.12 | -0.1 | -0.08 | -0.06 | -0.04 | -0.02 | 0 | 0.02 | 0.04 | 0.06 | 0.08 | 0.1 | 0.12 | 0.14 | ou plus...
Fréquence | 0 | 0 | 0 | 1 | 1 | 2 | 6 | 20 | 24 | 6 | 2 | 1 | 0 | 0 | 0 | 0
Chart: Fits to modules - DeltaX all 2S
| -0.14 | -0.12 | -0.1 | -0.08 | -0.06 | -0.04 | -0.02 | 0 | 0.02 | 0.04 | 0.06 | 0.08 | 0.1 | 0.12 | 0.14 | ou plus...
Fréquence | 0 | 0 | 0 | 0 | 0 | 2 | 9 | 49 | 50 | 9 | 0 | 0 | 0 | 0 | 0 | 0
Chart: Fits to modules - DeltaY all 2S
| -0.14 | -0.12 | -0.1 | -0.08 | -0.06 | -0.04 | -0.02 | 0 | 0.02 | 0.04 | 0.06 | 0.08 | 0.1 | 0.12 | 0.14 | ou plus...
Fréquence | 0 | 0 | 0 | 0 | 0 | 2 | 10 | 46 | 52 | 9 | 0 | 0 | 0 | 0 | 0 | 0
Groups of inserts for each module individually fitted to CAD model
Spec. limits

## Slide 15: Z precision within modules – 2S
Chart: 2S DeltaZ by module
| -0.22 | -0.18 | -0.14 | -0.1 | -0.06 | -0.02 | 0.02 | 0.06 | 0.1 | 0.14 | 0.18 | 0.22 | ou plus...
Fréquence | 2 | 4 | 0 | 0 | 5 | 30 | 69 | 23 | 4 | 0 | 0 | 0 | 0
For each of the groups of 5 inserts, calculate mean Z and bin offset of each insert from mean
6 inserts on ‘step’

## Slide 16: Absolute Z positions – 2S
Chart: Z_2S_Z+_side
| -0.2 | -0.16 | -0.12 | -0.08 | -0.04 | 0 | 0.04 | 0.08 | 0.12 | 0.16 | 0.2 | ou plus...
Fréquence | 4 | 2 | 0 | 0 | 4 | 18 | 24 | 14 | 7 | 1 | 0 | 0
Chart: Z_2S_Z-_side
| -16.7 | -16.66 | -16.62 | -16.58 | -16.54 | -16.5 | -16.46 | -16.42 | -16.38 | -16.34 | -16.3 | ou plus...
Fréquence | 2 | 0 | 5 | 6 | 7 | 17 | 12 | 7 | 5 | 0 | 1 | 1
Mean | +0.014
RMS | 0.059
Mean | -16.514
RMS | 0.082
Distance between mounting surfaces on the two sides of the prototype should be difference between the means of the distributions: = 16.53 +/- 0.10mm
Target was 16.44 +/- 0.10mm

## Slide 17: Thermal tests

## Slide 18: Prototype equipped with dummy modules
Dummy modules: 1.5mm thick aluminium plates equipped with Minco heating foils
2x cooling inlet/outlet blocks

## Slide 19: Fridge installation
1x pt100 per dummy module reads temperature on plate surface
Fridge air temp. set to target module temp. (-20°C for CO2 @ -30°C)
Air temp. monitored
Pre-heaters on inlets (8W per inlet)
Module average powers
  2S: 5.5W
  PS: 7.8W
All tests performed for CO2 temp. of -30°C max.

## Slide 20: Module naming and cooling segmentation
Z+ side
Z- side
Black = S1
White = S2

## Slide 21: Baseline* results (all modules)
PS modules
2S modules
*Best overall results obtained in a single run (no averaging), after system optimisation
(Red cross used in all following plots to display same baseline data)

## Slide 22: PS modules
DeltaT on the Dee carbon fiber skin

## Slide 23: PS modules
Chart: deltaT Dee surface
| 4.7720447532801913 | 5.2146950458715606 | 6.1810986322323034 | 6.901417981651373 | 6.9077629635637372 | 5.7738749600228658 | 5.4875889908256905 | 6.6212822972260197 | 4.952976146788993 | 6.8182786487936697 | 5.8212282654184708 | 6.0274348623853191 | 5.4982175170196141 | 5.2800000000000011 | 6.1341042390890506 | 5.870000000000001 | 6.709606360534428 | 6.5485937614678909 | 6.7722479890735725 | 7.5802260550458715 | 7.3420034792632203 | 6.1099999999999994 | 8.0023429691872696
 | 9.5008 | 9.2728 | 9.6001 | 12.4287 | 9.6374 | 9.696 | 9.6744 | 11.0332 | 9.0822 | 10.0773 | 10.1348 | 12.3928 | 10.6983 | 10.4823 | 10.8281 | 10.3832 | 10.0134 | 10.8047 | 10.9509 | 11.6721 | 11.4384 | 8.7167 | 10.5252
 | 9.5008 | 9.2728 | 9.6001 | 9.696 | 9.6744 | 11.0332 | 9.0822 | 10.1348 | 10.6983 | 10.4823 | 10.8281 | 10.3832 | 10.0134 | 10.8047 | 10.9509 | 11.6721 | 11.4384
Correlation ∆T-module / ∆T-skin

## Slide 24: 2S modules
Effect of washer type (plastic or SS)

## Slide 25: 2S modules
Effect of thermal paste on inserts (2 modules only)
Before thermal paste added
All other modules without themal paste

## Slide 26: 2S modules
Chart: Module no. vs deltaT
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 11 | 13 | 15
Dummy modules | 10.2227 | 10.4893 | 9.356 | 9.2841 | 8.7406 | 10.4031 | 10.006 | 8.5363 | 9.881 | 9.6128 | 9.3351 | 12.8338 | 12.2252 | 8.0458 | 9.1526 | 8.7156 | 8.2196 | 8.1325 | 8.8063 | 8.1234 | 9.0621
Inserts - no thermal paste | 7.6403 | 8.1285 | 8.2928 | 8.214 | 8.2221 | 8.2651 | 7.2653 | 7.596 | 8.1086 | 7.974 | 6.9128 | 7.492 | 7.3703 | 7.9726 | 7.967
NP MIN | 6.3361 | 7.2986 | 7.6017 | 6.86 | 7.6575 | 7.9634 | 6.4731 | 6.7779 | 6.9915 | 7.0974 | 5.5834 | 7.32 | 6.5711 | 6.948 | 7.4183
NP MAX | 8.7129 | 9.6818 | 9.1664 | 8.9188 | 8.7866 | 8.5765 | 8.6952 | 8.7288 | 8.8524 | 9.4274 | 7.7581 | 7.84 | 8.3768 | 9.6872 | 8.7491
Inserts - with paste | 7.0092 | 6.9173 | 7.8174 | 7.3741 | 7.029 | 7.0708 | 7.3318 | 7.5675 | 7.26 | 7.2714 | 6.8319 | 6.1919 | 7.2645 | 7.0039 | 7.0933
WP MIN | 6.0698 | 6.0734 | 6.6493 | 6.5299 | 5.9289 | 5.6454 | 6.5004 | 6.9001 | 6.8907 | 6.6502 | 6.1127 | 5.6647 | 6.9089 | 6.6071 | 6.7731
WP MAX | 7.8025 | 7.723 | 8.6907 | 7.9963 | 8.3071 | 7.8572 | 8.1934 | 7.9933 | 7.9846 | 8.0559 | 7.3767 | 6.9221 | 7.5951 | 7.5887 | 7.2984
Measurements on individual inserts
1x small copper plate/ insert
Pt100 on plate
1.1W / insert
Open diamonds: MIN/MAX of group of 5

## Slide 27: Conclusions + perspectives
Globalement:
  Précision mécanique: OK 
  Performance thermiques: OK 
Des améliorations à faire mais on sait comment procéder
Prochain étape: prototype Dee entier
  Commandes déjà placées
  Construction Q2 2019

## Slide 28: Perspectives 2019-2025
2019:
  Fabrication d’un prototype « Dee » entier
  Construction centre d’assemblage des « Dees »
  Mise en place équipe technique pour l’assemblage des Dees
2020:
  Pré-production: 4 « Dees » entiers
  Tests mécanique et thermique
  2021-25:
  Production en série des 24 « Dees »
  Intégration des modules en silicium
  Tests système
  Installation bouchon dans CMS