## Slide 1: Mechanical Activities at CPPM S. Beurthey - P. Karst - April 2019 Measure of the 200 mm discs Investigation of the laser welding of the LaAlO3

## Slide 2: Setup : measure with stylus
Maximum Estimated displacement under contact = 5 µm
Accuracy of the measurement < 5 µm
Contribution :
Fabrice Gallo
Supporting tool

## Slide 3: Disc 1 - 200mm Rough surface Horizontal position
Planarity = 26 µm
Distribution RMS = 5 µm

## Slide 4: Disc 1 - 200mm Rough surface Vertical position
Planarity = 27 µm
Distribution RMS = 4 µm

## Slide 5: Disc 1 - 200 mm Rough surface Comparison Vertical/Horizontal

## Slide 6: Disc 1 - 200 mm Rough surface Comparison Vertical/Horizontal

## Slide 7: Disc 1 - 200 mm Rough surface Difference Horizontal-Vertical

## Slide 8: Disc 2 - 200mm transparent surface – Down side Measure with contact
Planarity = 53 µm
Distribution RMS = 11 µm

## Slide 9: Disc 2 - 200mm transparent surface – Up side Measure with contact
Planarity = 63 µm
Distribution RMS = 10 µm

## Slide 10: Setup Optical Measurement Disc 2
Transparent Sapphire
Stil Optical Pen
on a 3D measuring machine
Accuracy of the measure < 2 µm in depth of focus
Contributions :
Eric Vigeolas
Mathieu Niclas
Stephan Beurthey

## Slide 11: Disc 2 - 200mm transparent surface – Down side Scan with Stil
Planarity = 56 µm
Distribution RMS = 9 µm

## Slide 12: Disc 2 - 200mm transparent surface – Down side Comparison ScanStil/Contact
Planarity = 53 µm
Distribution RMS = 11 µm
Planarity = 56 µm
Distribution RMS = 9 µm
Note : the boundary conditions were not the same

## Slide 13: Disc 2 - 200 mm transparent surface – Up side Scan with Stil
Planarity = 75 µm
Distribution RMS = 13 µm

## Slide 14: Disc2 - 200 mm transparent surface – Up side Comparison ScanStil/Contact
Planarity = 63 µm
Distribution RMS = 10 µm
Planarity = 75 µm
Distribution RMS = 13 µm

## Slide 15
Measure with a double camera scanner

## Slide 16: Measure with a double camera scanner
Measurement accuracy < 7 µm in depth of focus

## Slide 17: Laser welding of LaAlO3 samples
Collaboration with the laboratory LP3 at Marseille
LP3 = the Lasers, Plasmas and Photonic Processes
First meeting CPPM/LP3 in March for defining what could be done in the next year :
  few welding tests
  1 mm seems to be thick for this process, try to weld on both faces
  Need a straightness less than 5 µm (laser beam = 20 µm)
Purchasing of 6 samples 10x10x1 mm (expected in April)

## Slide 18: Further Work
Complete the measure with the optical scan of the rough surface disc with and without the supporting tool.
Carry out laser welding tests
Implement the strength tests of the welding

## Slide 19: Spares

## Slide 20: Mesure Stylet Disque Opaque Horizontal

## Slide 21
Mesure Stylet Disque Poli face up Horizontal

## Slide 22: Mesure Stylet Disque Opaque Vertical

## Slide 23
Mesure Stylet Disque Poli face down Horizontal

## Slide 24: Mesure Crayon Stil : face down
Planéité = 51 µm

## Slide 25: Mesure Crayon Stil : face up
Planéité = 74 µm

## Slide 26
Planéité = 51 µm
Planéité = 53 µm