## Slide 1
| Avignon | ARIS2023 | June 09 |
Material science with radioactive isotopes - results from emission Mössbauer Spectroscopy
Hilary Masenda
School of Physics
University of the Witwatersrand
Johannesburg
Outline
Overview – materials, defects and radioactive isotopes, techniques
Emission Mössbauer Spectroscopy @ ISOLDE
Highlights
  Search for dilute magnetism in ZnO
  Lattice site and charge states in ternary nitrides: AlGaN and InGaN
Future work/concluding remarks

## Slide 2
e-ms.web.cern.ch
Collaborators
Linz
A. Bonanni, A. Tarazaga, R. Adhikari. A. Ernst
Lisbon
U. Wahl
Milan
R. Mantovan, M. Fanciulli
Reykjavík
S. Ólafsson, H. P. Gíslason, B. Qi,
H. P. Gunnlaugsson
Roskilde
T. E. Mølholt
Sofia
P. Krastev
Aarhus
G. Weyer
Berlin
R. Sielemann
Bilbao
F. Plazaola, I. Unzueta
CERN
K. Johnston, J. Schell, A. M. Gerami
Durban
K. Bharuth-Ram,
Johannesburg
D. Naidoo, O. Mpatani
Leuven
A. Vantomme, L. M. Pereira,
G. Langouche

## Slide 3
Material Science and Functional Materials
Wikipedia
encompasses a wide range including inorganic, organic, hybrids and nano-materials, soft matter and interfaces
“… are selected… for the nature of their response to electrical, magnetic, optical and chemical stimuli.” - R.W. Cahn
Functional Materials
The Coming of Materials Science
Scopus
Nov 2022
0.66M publications
Notes: Inter-disciplinary field that cuts across the different field of physical sciences – mainly solid state physics and chemistry and linking with processing engineering
The synergy between the different disciplines is motivated by the quest for a more holistic approach to understanding the complex nature of materials….
Understanding materials requires knowledge of the different aspects…
Central to these is the ability characterise these attributes - to investigate using spectroscopic and chemical analysis techniques
Functional materials – Cahn

## Slide 4
…modify structure of materials…
….enhance electrical, optical, magnetic properties….
… to realize functional materials …
…dopants …
During material growth
Diffusion
Ion implantation
Nuclear reaction
via proton or neutron irradiation
…for optoelectronic, spintronic, photovoltaic, quantum … applications
Ion implantation
smaller
faster
more efficient
new functionalities
Devices
Material Modification: Doping (Semiconductor) Materials
…..for tomorrow and the day after
During material growth
Notes: The drive of science and technology has been to design or develop new materials with novel properties …. for devices
this requires in some cases modification of existing materials
Modify existing…
On of the main way is doping (e.g. Si), the introduction of foreign atoms in the materials
There are several ways in which this can be achieved….
Define - Ion implantation …. bombarding material with high energetic ions
Advantages of ion implantation:
Precise control of the depth distribution and concentration
By pass solubility and diffusion limits

## Slide 5
Defects in Semiconductors/Materials
Notes: Not particular to ion implantation, defects can be observed
…also available in as-grown materials …
even in as-grown samples.
– antisites are also common defects in compound semiconductors.
The native point defects in GaN are isolated vacancies (VGa, VN), interstitials (Gai,
Ni), and antisites (GaN, NGa), as well as their complexes, such as Vga-VN,
NGaVN, GaN
VGa, Gai
VGa, etc

## Slide 6
To have quantitative control of the electrical, magnetic, optical properties of materials
structure of the host material and properties
chemical identity of a defect or impurity atom
thermal properties of defects (diffusion, binding)…..
lattice site of a dopant and interaction with host atoms
interaction between impurity atoms and other defects
optical, magnetic or electrical properties of a specific defect and its effect on the host materials….
....we should know the....
Defects in Semiconductors/Materials

## Slide 7
The half life of nuclear decay provides an opportunity of identifying the origin of conventional spectroscopic signals.
Radiotracer Deep Level Transient Spectroscopy (DLTS) [1990 Petersen+Nielsen]
Radiotracer Hall effect (HE) [1992 Gwilliam et al]
Radiotracer Photoluminescence (PL) [1965 Broser+Franke]
Nuclear radiation can easily be detected with high sensitivity i.e. very low concentrations of radioactive impurity atoms in a material can be quantified.
Radiotracer Diffusion depth profiling [1920 G. v. Hevesy]
Courtesy U. Wahl
Unstable isotopes as “spies” transmitting information with atomic resolution via the particles they emit in their decay.
beta-Nuclear Magnetic Resonance (β-NMR) [~1959 D. Connor]
Perturbed Angular Correlation (PAC) [1951 Frauenfelder et al]
Emission Channeling (EC) [1965 B. Domeij]
Mössbauer Spectroscopy (eMS) [1958 R.L. Mössbauer]
Materials Science with Radioactive Isotopes: Exploits 3 principle
Notes: Diffusion
radiotracer techniques allow for a very direct measurement of the diffusion proﬁle which is strongly indicative of the diffusion mechanism of the species of interest.
The increase in sensitivity—due to the ease of detecting radioactive decay—also allows for a clearer interpretation of data than is the case for non-tracer methods
DLTS
enables the observation of the charging and discharging of deep levels in a semiconductor through the measurement of capacitance transients.
Three properties of deep levels can be determined: concentration, position in the band gap, and capture cross section for free carriers.
PL –
widely used in semiconductor physics in order to detect optical transitions involving electronic energy levels in or near the band gap.
highly sensitive to low concentrations of optically active defects
HOWEVER,
it does not provide direct microscopic information about the chemical identity of the optical centers responsible for the signals.
Correlating the intensity of PL lines with the radioactive decay of implanted isotopes in the sample allows such an identification..
Beta-NMR
provides information on the microscopic environment of the probe nucleus, based on the measured shift in the Larmor frequency (chemical shift), or relaxation time.
In material science the common probe is 8Li, since it's light and relatively easy to polarize, it has spin I=2, so quadrupole interaction is present.
PAC
experiments require probe atoms which decay by a γ–γ cascade via an isomeric nuclear state.
By measuring the two γ-quanta (γ1, γ2) in coincidence, an anisotropic angular distribution of the γ2 radiation is observed,
PAC allows the measurement of the local EFG and the magnetic ﬁeld that a probe nucleus experiences when embedded in matter, independent of its physical state, i.e., solids, liquid, amorphous materials and molecules can be studied.
EC
used to determine the lattice location of impurities in crystalline materials
During decay, the nuclei emit charged particles i.e. α, β+/− and conversion electrons.
As they travel through the crystal they experience either channelling or blocking effects.
The resulting anisotropic particle emission yield in the vicinity of major crystallographic directions depends in a characteristic way on the lattice sites occupied by the emitter atoms and is recorded with the aid of position sensitive detectors.

## Slide 8
Rudolf L. Mössbauer
Nobel Prize in Physics in 1961 for his 1957 discovery of the Mössbauer effect.
Fujita
Z,N
γ
Er
Free Nucleus
1
2
Mössbauer Effect
Notes: A boy jumping from a boat on the water would fail to land on the shore because of an energy deficiency rising from the recoil of the boat. Likewise, a gamma ray emitted from a nucleus would not be absorbed by another nucleus due to a recoil reaction in emission.

## Slide 9
Fujita
1
2
Mössbauer Effect
Notes: The same boy jumping from a boat frozen in ice can easily land on the shore, because no recoil reaction takes place. Likewise, a recoil-free emission and absorption of a nuclear gamma ray can be observed in solids, i.e. the Mössbauer effect (Fujita 1999).

## Slide 10
Observing Mössbauer Effect

## Slide 11
ME has been observed in > 40 elements
P. Gütlich‘s Lecture slides
> 90% of all applications use 57Fe
Mössbauer Active Isotopes
Notes: The observation of resonance in Mössbauer spectroscopy for a particular nuclide is governed by the mean lifetime (τN) of the excited state and the transition energy EO.

## Slide 12
Fen+/Snn+
...sensitive to charge density distribution at the nucleus and symmetry around the probe…
Emission Mössbauer Spectroscopy @ ISOLDE
Notes: Hyperfine interactions are interactions between the nucleus and its surrounding electrons which cause nuclear energy levels changes of the order of 10-7-10-8 eV

## Slide 13
Hyperfine Interactions
Lattice asymmetry,
Clustering of atoms...
Chemical bonding, Charge states...
Electric monopole interaction
Electric quadrupole interactions
Magnetic dipole interactions
Size and Direction of Beff
Beff = Bext + Bhf
Notes: Hyperfine interactions are interactions between the nucleus and its surrounding electrons which cause nuclear energy levels changes of the order of 10-7-10-8 eV

## Slide 14
Fen+/Snn+
Charge and spin state of probe atom: Fen+, Snn+
Symmetry of lattice site (Vzz)
Binding properties (Debye-Waller factors)
Magnetic interactions (ferro/para)
Paramagnetic relaxation (~107-108 Hz) ...plus...
...sensitive to charge density distribution at the nucleus and symmetry around the probe…
Beam production at ISOLDE
Detect and distinguish up to 4-5 spectral components:
substitutional, interstitial, damage, vacancy-defects,…
Implantation angle = 30o w.r.t. c-axis
Emission angle = 60o w.r.t. c-axis
Fluence = ~ 3×1012 ions/cm2
Emission Mössbauer Spectroscopy @ ISOLDE

## Slide 15
| Avignon | ARIS2023 | June 09 |
Search for dilute magnetism in ZnO

## Slide 16
But
Different Crystal Structures
Conductivity mismatch
semiconductor materials → information processing
metallic magnetic materials → data storage.
Desired
both properties in one material
BUT
TC < 100 K
chromium spinels
europium chalcogenides
Semiconductor
DMS
Furdya: J. Appl. Phys. 64(1988) R29.
Dietl et al, Science 287 (2000) 1019
Nature and origin of magnetism
Example - Physics Case Motivation
Notes: Results from emission Mössbauer Spectroscopy studies revealed that Fe/Mn implanted ZnO and GaN shows slow paramagnetic relaxation.

## Slide 17
Dietl et al, Science 287 (2000) 1019
Possible origin…
[1]
[2]
[3]
[4]
Motivation
Notes: Results from emission Mössbauer Spectroscopy studies revealed that Fe/Mn implanted ZnO and GaN shows slow paramagnetic relaxation.

## Slide 18
If the spin is stable for longer than 140 ns – Sextet is observed
Ferromagnetic material
Relative line ratios:
3:4:1 (90o)  3:0:1 (0o)
Magnetic order
Bext
Sample
g
3 4 1 1 4 3
3 0 1 1 0 3
DmI = 0
Ferromagnetic/Paramagnetic?
eMS Spectra
Zinc Oxide
Notes: If the 57Fe probe interacts with a magnetic field it will cause a Zeeman splitting and the energy level of the nucleus split - resulting in six lines (due to the selection rule) – called a sextet.
--In the case of no external magnetic field and a sextet is observed… we know the spin alignment is stable for longer then 140 ns. Which is the measuring time of the experiment.
- if the material is magnetic
- or if the probe exhibit slow relaxing paramagnetism (but then more than one sextet is observed)
mean life time of the excited nuclear state (140 ns for 57Fe)

## Slide 19
If the spin is stable for longer than 140 ns – Sextet is observed
Slow relaxing paramagnetism
  (not only one sextet)
SZ = ±5/2
SZ = ±3/2
SZ = ±1/2
DmI = 0 from SZ = ±3/2
Paramagnetism
Bext
Sample
g
Relative line ratios:
3:4:1 (90o)  3:0:1 (0o)
57*Fe
Ferromagnetic/Paramagnetic?
Zinc Oxide
Notes: In a crystal field potential, the 6S ground state of Fe3+ splits into three Kramers spin doublets with Sz ±5/2, ±3/2, and ±1/2, and in the limit of low spin relaxation rates each doublet produces its own Mössbauer magnetic hyperfine spectrum and experimentally a superposition of the three sextets is observed.
Here a simulation of a single sextet originating from ordered magnetism like ferromagnetism
--Pay attention to the relative line intensities of the sextet as the angle between the external magnetic field and the gamma direction change.
*Characteristic is that line 2 and 5 (from the ΔmI=0) goes to zero when the external magnetic field is parallel to the gamma emission
-As mentioned earlier – in the case of slow relaxing paramagnetism – it will give rice to 3 sextet (or actually 6 sextets). They originate from the three Kramers doublets.
--Important is that the three sextet exhibits the same angular dependence.!
Characteristic is the at 0 deg – the line 2 and 5 from the ΔmI=0 also becomes ZERO.
This is best observed for the Sz = 3/2 states

## Slide 20
NO ordered magnetism
But Paramagnetism 
Magnetic structure – complex originates form more than one
Fe3+ (Sz = 5/2)
DmI → 0 from SZ = ±3/2
Zinc Oxide
Notes: in the case of slow relaxing paramagnetism – it will give rice to 3 sextet (or actually 6 sextets). They originate from the three Kramers doublets.
--Important is that the three sextet exhibits the same angular dependence.!
Characteristic is the at 0 deg – the line 2 and 5 from the ΔmI=0 also becomes ZERO.
This is best observed for the Sz = 3/2 states

## Slide 21
Temperature dependent Bhf
Bhf
TC or TN
T   Bhf 
No line broadening
Cold
Hot
Temperature Series
Zinc Oxide
Notes: Spin-lattice relaxation between a paramagnetic ion and a crystal lattice occurs when energy transfer takes place between the electronic spin of the ion and phonons of the lattice vibrations which are responsible for a fluctuating crystalline electric field generated by neighbouring ligands at a central paramagnetic ion.

## Slide 22
τ > 200 ns (slow)
τ = 100 ns
τ = 30 ns
τ = 13 ns
τ = 6 ns
τ = 3 ns
τ = 2 ns (fast)
Collapse of inner lines 3 and 4
Collapse of inner lines 2 and 5
Total collapse of all spectral lines
1 2 3 4 5 6
1 2 3/4 5 6
1 2/3/4/5 6
1/2/3/4/5/6
Simulation
[Blume M. and Tjon J.A.:
Phys. Rev. 165, 446 (1968)]
T   ΓΔ 
line broadening
then collapse
Temperature Series
Zinc Oxide
Notes: The Larmor precession time gives the minimum time required for the nucleus to sense the hyperfine field and is defined as the time taken for a nuclear spin state, I to split into (2I+1) sub-states under the influence of the hyperfine field.
As the relaxation rate increases, the sextets start to collapse in pairs beginning with the inner most lines. This is because the Larmor precession time for the outer lines is shorter than that for the inner lines, since (τl) is proportional to the energy difference between spectral lines.

## Slide 23
Masenda et al., Hyp. Int. 237 (2016) 40
Mantovan et al Adv. Electron. Mater. 1 (2015) 1400039
Implantation damage
→ Fe3+ (S=5/2) decreases
Zinc Oxide: 57Mn + 56Fe
Spin-spin
relaxation
contributes
Notes: Spin-spin relaxation involves energy transfer between neighbouring spins through magnetic dipole and/or exchange interactions
This spin-spin interaction is influenced by the distance between the ions and hence depends on the concentration of paramagnetic ions in the sample. For very low concentration of Fe ions (<10-4 at.%) the spin-spin relaxation is negligible since the ions are widely spaced.

## Slide 24
ZnO : Summary
Using eMS with short-lived radioactive 57Mn* with fluence ~ 31012 ion.cm-2
No dilute ferromagnetic behaviour is observed in the ZnO, ..... (<10-3 at. %)
Instead, paramagnetism in Fe implanted ZnO (and other oxides)
→ Slow paramagnetic relaxation of Fe3+
Leading candidate → Ga(Mn)As with current Tc = 185 K

## Slide 25
| Avignon | ARIS2023 | June 09 |
Lattice site and charge states in ternary nitrides

## Slide 26
“a0 engineering”
...tuning…
band-gap energy: 0.7 – 6.2 eV
magnetism (p-d hybridization)
effective masses of holes and electrons
dielectric constants
InN and GaN  InxGa1-xN
AlN and GaN  AlxGa1-xN
+ Mn doping → IS576
Grown by MOVPE
Linz, Austria
….from Binary to Ternary Systems

## Slide 27
BT sextets - Fe3+ (S=5/2)
→ paramagnetic
→ slow spin-lattice relaxation
[Blume M. and Tjon J.A.:
Phys. Rev. 165, 446 (1968)]
Mølholt et al., Phys. Scr. T148 (2012) 014006
Masenda, H. et al: J. Magn. Magn. Mater. 401 (2016) 1130
……different behaviour in 57Fe eMS on GaN (AlxGa1-xN)
→ suggests different physics between the AlN and GaN which is not well understood
…..to gain essential insight into the role played by Mn dopants
….Motivation - Binary to Ternary Systems

## Slide 28
….AlGaN: Virgin and Pre-Doped with Mn
…with Mn doping;
Magnetic contribution decreases
New Single line like (SLL) feature

## Slide 29
Seems area of Fe4+ decrease significantly with higher Al concentration at the expense of Fe3+
Area of Fe2+??
….Higher Al Concentration
Notes: Room temperature angular dependence for 40% and 80% Al in both doped virgin and Mn doped AlGaN

## Slide 30
… higher Al content samples → have less Fe4+ and more Fe3+ → the Fe2+ fraction fairly constant
…. Experiment + DFT
~ 47%

## Slide 31
….AlGaN
The completely-filled spin-up orbitals in Mn2+ (3d5)
Expected to enhance magnetic exchange interactions

## Slide 32
….Si Doping
Fe3+ fraction decreases
New single line (SL) appears
Fe4+
SL
...presents Fe3+ and no SLL…
…intentional doping with donor…
Al0.25Ga0.75N:Si
Preliminary results
Notes: Implant (and measure) at elevated temperatures (RT-1000 K)
Remove the sample from vacuum, quench in LN, measure off-line

## Slide 33
Temperature dependence
does not follow the expect SOD at temperatures < 250 K
 suggest Fe2+ and Fe3+
Large EQ identify doublet as due to Fe2+
additional broadening is due to isolated defects.
….from Temperature Dependence

## Slide 34
Fe2+ associated with defects
Presence of implantation induced isolated defects at low temperatures
Literature
VN main native defect in GaN [Many authors]
Stable up to very high temperature [Some authors]
….Fast cooling experiments
Notes: Implant (and measure) at elevated temperatures (RT-1000 K)
Remove the sample from vacuum, quench in LN, measure off-line

## Slide 35
Paramagnetic Fe2+ on Al/Ga sites associated with a nitrogen vacancy or vacancies,
…in AlxGa1-xN samples (similar results to GaN) …
Paramagnetic Fe3+ on Al/Ga sites,
Fast cooling measurements confirmed the presence of isolated defects below 250 K
Fe4+ concentration decreases with increasing Al content due enhanced hybridization effects
… when AlxGa1-xN doped with Mn (1 %) …
Favour Fe4+ state on Al/Ga sites,
… stabilized by Mn2+
….AlGaN – Summary
Notes: Unique charge states with co-doping

## Slide 36
No magnetic feature, no Fe3+
....but single line (SL)….
→ Fe4+ as in Mn doped AlxGa1-xN
FeX...not consistent with Fe2+-VN as in GaN → δRT ~ 0.27 mm/s – too low
Fast relaxing high-spin Fe3+?
Low spin Fe2+ or Fe3+?
Interstitial Fe?
Fe2+-VN, still a possibility?
Alternative interpretation
…spin relaxation rates as a function of x
... quadrupole interaction with temperature
…determine Debye temperatures
…apply theoretical calculations
FeY… Fe2+-VN → δRT ~ 0.83 mm/s
→ low intensity, VN mobile in InN?
…temperature series and rapid cooling
InN and GaN  InxGa1-xN
...development SL as a function of x …
….IS630 - InGaN
Notes: InN did not reveal any magnetic behaviour and this could be explained by the absence of high spin Fe3+?

## Slide 37
….Prospects for Unstable Isotopes - Halides
Notes: Chalcogenide materials are characterized by fast and reversible phase transitions, which are typically accompanied
by orders of magnitude variations in their electrical resistivity, as well as by large differences in their optical
reflectivity, making them extraordinarily important for non-volatile memory applications.

## Slide 38
Multiferroics + magnetoelectric
S. Dong et al., Advances in Physics 64 (2015) 519 - 626
2D materials + their hetero/hybrid structures
A. K. Geim and I. Grigorieva, Nature 499, 419 (2013)
Chalcogenides
…plus more …
Topological Insulators
Nitrides
….Ongoing and Prospects for Unstable Isotopes with EMS
Notes: Chalcogenide materials are characterized by fast and reversible phase transitions, which are typically accompanied
by orders of magnitude variations in their electrical resistivity, as well as by large differences in their optical
reflectivity, making them extraordinarily important for non-volatile memory applications.

## Slide 39
Thank You!!!
| hilary.masenda@wits.ac.za |
Acknowledgements
Linz
A. Bonanni, A. Tarazaga, R. Adhikari
A.Ernst
Lisbon
U. Wahl
Milan
R. Mantovan, M. Fanciulli
Reykjavík
S. Ólafsson, H. P. Gíslason, B. Qi,
H. P. Gunnlaugsson
Roskilde
T. E. Mølholt
Sofia
P. Krastev
Aarhus
G. Weyer
Berlin
R. Sielemann
Bilbao
F. Plazaola, I. Unzueta
CERN
K. Johnston, J. Schell, A. M. Gerami
Durban
K. Bharuth-Ram,
Johannesburg
D. Naidoo, O. Mpatani
Leuven
A. Vantomme, L. M. Pereira,
G. Langouche