## Slide 1: « Next » Generation of Targets
B. Jurado, CENBG; C. Cannes, IJCLab; B. Gall, O. Dorvaux, M. Kerveno, IPHC; M. Dubois, O. Bajat, X. Ledoux, G de France, B. Jacquot, J. Piot, D. Ackermann, H. Savajols, G. Frémont, J.-C. Foy, Ch. Stodel, GANIL

## Slide 2
2
Beam
Nout
Target
Spectrometer
Beam Dump
Detector
GT02 – A. Lopez-Martens « Heavy and super_heavy nuclei »
L. Caceres « Prospectives ISOL, Spectroscopie des états fondamentaux »
B. Jurado « Comment arriver à une description complète de la fission nucléaire? »
GT10 – G. de France “Une plateforme interdisciplinaire pour la R&D production de radioéléments innovants »
GT11 – M. Kerveno « Données nucléaires »
……………………
µm-mm
N*mm
~ dam/hm
~ m/dam
~ cm/dm
GT07
I Stefan, G de France « Possibles développements autour de SPIRAL2 »
P. Jardin, C. Barué, L. Maunoury « Ambitions à long terme de la production de faisceaux d’ions à GANIL »
……………
GT08
A transversal activity
Notes: Positionner cette thématique dans le contexte des prospectives

## Slide 3
Nbeam
Nout
 (cm²)
Target
Successful experiment
= Accurate measurements + low background + safe conditions
 Need of high quality targets with known properties at any time
Areal density
Homogeneity == spatial distribution (to be verified experimentally) (e.g. ensure that all detected neutrons have traversed the same path lenght in the target (no hole) for a correct interpretation of capture and transmission cross-section in resonance regions).
Effective area
Quantification & identification of contaminants and impurities, uncertainty depends on their impact on the measurement.
Requirements & constraints
D. Sapundjiev et al., Nucl. Instr. Meth. A 686 (2012) 75-81 “Preparation and characterization of thin film nuclear targets for neutron physical measurements”
p/d (Li/Be, conv) n
n (act* , Fission) FF
LP (Bi , fus) radio-isotopes
HI (targ , fus-evap)
HI (act* , fus-evap)
HI (targ , frag)
Hiq+ (C , stripping)
Characterization techniques not developed here
Notes: Exigences sur la qualité des cibles pour les résultats
Uncertainties expected to be < 0.5%

## Slide 4
Nbeam
Nout
Target
Requirements & constraints
ILP, HI 
Temptar
Radiation damage
 
p/d (Li/Be, conv) n
n (act* , Fission) FF
LP (Bi , fus) radio-isotopes
HI (targ , fus-evap)
HI (act* , fus-evap)
HI (targ , frag)
Hiq+ (C , stripping)
Plunger targets
Courtesy of A. Stolarz, A. Mitu
targets mounted on the wheel for TASCA
S3 Targets Station
Designed for 10pµA
IS3 = 1-1.5 pµA à 5 (existing)
10 (estimated)
20 pµA???
Notes: Etat des lieux et diversité des cibles.
Problématique de l’augmentation d’intensité / quelques solutions sur les stations
Aller plus loin

## Slide 5
Requirements & constraints
Layout
p/d (Li/Be, conv) n
n (act* , Fission) FF
LP (Bi , fus) radio-isotopes
HI (targ , fus-evap)
HI (act* , fus-evap)
HI (targ , frag)
Hiq+ (C , stripping)
ISOL targ : from beam to target fragmentation to explore new isotopes temperature stability and release time ?
Act* : backings, activity, limited laboratories, Chemical reaction (backing/layer)
 R&D on deposition & backings
Thin layer deposited on substrate (backing)
Backing must not interfere with the nuclear reaction used  Use high purity material
Backing must not interact with the target material
Stripper : induced damages with HI, fragile
 liquid or gaseous targets ?
Li or Bi : Tfus low, thin, fragile  liquid targets ?
*[] hidden slides 8, 9, 10
Notes: Sujets à présenter
Trop large  on va se concentrer sur les Bi liquide, actinides et ISOL targets

## Slide 6: Thin targetsfor nuclear physics experiments
p/d (Li/Be, conv) n
n (act* , Fission) FF
LP (Bi , fus) radio-isotopes
HI (targ , fus-evap)
HI (act* , fus-evap)
HI (targ , frag)
Hiq+ (C , stripping)

## Slide 7
7
Liquid Targets
Li or Bi : Tfus low, thin, fragile  liquid targets ?
p/d (Li/Be, conv) n
LP (Bi , fus) radio-isotopes
HI (targ , fus-evap)
LIEBE EMIS 2018
No backing material
Complex system
Homogeneity? Stability of the thickness ?
Higher dP/V
Design proposed by E. Noah and all, EURISOL 100 kW Target Stations Operation and Implications for its Proton Driver Beam, EPAC,2006
Images from Melanie Delonca CERN Ph.D thesis
LIquid Eutectic lead Bismuth loop targEt
D. Houngbo et al, Nucl. Instr. Meth. B 376 (2016) 57-59 “Develoment of a liquid Pb-Bi target for high-power ISOL facilities”
252Rf
256Sg
257Sg
268Sg
272Hs
276Ds
276Cn
people.physics.anu.edu.au/
272Ds
HI(209Bi, xn)
20xPb?
ANR REPARE : Research and dEvelopements for the Production of innovAtive RadioElements
WP3: High power liquid target (ARRONAX, SUBATECH, CERN, GANIL)
4He(209Bi, 2n)211At
Notes: REPARE: The goal of this work package is to design a high power rotating system able to sustain possibly 10kW beam power on a bismuth target including the extraction method and radioprotection aspects

## Slide 8
8
Liquid Targets
Li or Bi : Tfus low, thin, fragile  liquid targets ?
p/d (Li/Be, conv) n
LP (Bi , fus) radio-isotopes
HI (targ , fus-evap)
1. S. Halfon et al, Rev. Scient. Inst. 84 (2013) 123507 “High power liquid-lithium jet target for neutron production”
2. I. Mardor et al, Eur. Phys. J. A 54 (2018) 91 “The Soreq Applied Research Accelerator Facility (SARAF): Overview, research programs and future plans”
from [2]
Challenges @ SARAF:
Large volume power density > 1MW/cm3 (>> NFS 3kW/cm3)
Keeping stable temperature, vacuum conditions
Complex system, operation and maintenance

## Slide 9: Liquid or Gaseous targets
Strippers Foils
F. Marti, Proc. HIAT2015, pp.134-138, « Development of a liquid lithium charge stripper for FRIB »
P. Scharrer et al, Proc. HIAT 2015 pp. 144-147, « A pulsed-gas stripper for stripping high-intensity, heavy ion beams at 1,4 MeV.u at the GSI UNILAC »
H. Imao et al., Proc. Cyclotrons 2013, pp. 265-268, « R&D of helium gas stripper for intense uranium beams »
from [1]
Hiq+ (C , stripping)
from [2]
from [3]

## Slide 10: Gaseous equilibrium foils for S3 ?
Strippers Foils
Hiq+ (C , stripping)
Carbon foils for charge equilibraiton of evaporation residues
presently mounted on the wheel able to sustain 10pµA
Gas helps in cooling by convection
Complex system ? Dimensions for equivalent 30µg/cm²?

## Slide 11: Actinide Targets
Constraints:
Limited availability
high specific activity
Backing : material, thickness, roughness
High chemical purity
large surface/numerous
Fragile for transportation
Few expertise in the world
Actinide Targets
n (act* , Fission) FF
HI (act* , fus-evap)
Complementary developments:
backings (material + thickness)
characterization techniques
Methods:
High yield
reliability/reproducibility
control of dimensions and thickness
Electro-precipitation
Drop-on-Demand
intermetallic targets

## Slide 12: Actinide Targets
Actinide Targets
Applications
n (act* , Fission) FF
HI (act* , fus-evap)
Actinide targets for SHE:
  200 – 500 µg/cm²
  Homogeneous
  Numerous
  Minimizing Eloss in backing
  (now 1,5 µm Ti : dE=2/3dEtot)
people.physics.anu.edu.au/
238U
243Am
248Cm
242,4Pu
GT02 – A. Lopez-Martens « Heavy and super_heavy nuclei »
24xBk
252Cf
Courtesy of K. Eberhardt
242Pu / 110 µg/cm2
75 mm
GT02 – B. Jurado « Comment arriver à une description complète de la fission nucléaire? »
GT11 – M. Kerveno « Données nucléaires »
Actinide sample:
  1501000 µg/cm²
  Active diameter 40-80 mm
  Homogeneous
  Surface roughness as low as possible
  On ultra-thin backing: Ni (250 nm) or PL (220 nm)
Spectrometer for surrogate studies
Yu. T. Oganessian (JINR), “production of new target materials and development of techniques for making targets with high thermal and radiation stabilities “
J.B. Roberto (ORNL), “progress in the development of heavy actinide targets […] They depend on a robust infrastructure of actinide production, chemical processing, and heavy ion accelerator facilities. Continued scientific progress will require further advances in actinide production, processing, and target technology to enable experiments essential for ………………..;.” Nuclear Physics A 944 (2015)

## Slide 13
 
Actinide compound, dissolved in isobutanol
Ultrasonic stirrer
A
N
O
D
E
C
A
T
H
O
D
E
Cooling water
Backing: 2μm Ti-foil
Voltage: 100 V - 1500 V
PEEK-cell
Deposition time:
3-6 hours
Supporting frame with Ti-backing foil (2 µm)
Electrochemical cell assembly (26 ml)
Deposition yield: up to 90%
Target thickness: mg/cm2 in a single deposition step
Actinide Targets
Molecular Plating (JGU, IJCLab)
R&D
Courtesy of K. Eberhardt
Notes: For MP the compound, typically the chloride or nitrate is dissolved in a small amount of volume of nitric acid and the aqueous phase is mixed with a surplus of an organic solvent(few ml), they are isopropanol, isobutanol or acetone.Under these conditions no electrolytic dissociations occurs by applying an electric current at voltages up to 3000V.
It is assumed that the dissolved molecules form clusters that migrate in the electric field towards the cathode. However the deposition process is not yet well understood.
The composition of the deposit is complex and contains possibly fragments of the solvent

## Slide 14
I. Usoltsev et al, “Preparation and high intensity heavy ion irradiation tests of intermetallic 243Am/Pd targets” Nucl. Instr.Meth. B 318, pp. 297-305, 2014
1/Electro-deposition by molecular plating
Oxyde  Metallic state superior for electric & heat conductance, mechanical stability
2/Reduction
MP +red
MP +red
MP +red
MP
Actinide Targets
Intermetallic Targets (JINR Dubna, PSI)

## Slide 15
140La, 198gAu tracers as natural nitrate solution
on graphene 12 µm or Ti 50µm diam 25 mm
Organic solvents
Other substrate, thickness
Diam = 100 mm
Study of drop formation
Printing of JGU-Logo with NaCl-solution on Ti-surface
Stroke: 16.25 µm
Stroke velocity: 150 µm/ms
Droplet size: 15 ± 5 nL
4 mm
5 mm
330 µm
Courtesy of K. Eberhardt, D. Renish
R. Haas et al, “Development and characterization of a Drop-on-Demand inkjet printing system for nuclear target fabrication” Nucl. Instr. Meth. A 874, pp. 43-49, 2017
1st application: preparation of a 252Cf fission fragment source for JRC Geel. Very thin backing: Polyamide foil (24 µg/cm²) and graphite foil (10 µg/cm²)
Multi geometry of targets + no backing constraint / reduced volume of An*
Actinide Targets
Drop-on-Demand technique (JGU)

## Slide 16: Comparisons
Drop-on Demand | Molecular Plating | Intermetallic
 | Reliable technique Long-term experience | 
Quantitative yield | High yields possible (> 90%) | 
Fast method |  | 
Less homogeneous, uniform layer from aqueous solution | Homogeneous layer | 
Flexible target geometry | 1cell per geometry and actinide | 
No restrictions for the substrate (metal, polymer, C; ultra thin) | Conductive substrate necessary + tension resistant+ tight(==thick) | ++ Stability of An/substrate
Influence of certain parameters (pH, viscosity, surface roughness, hydrophobicity, …) | Chemical form undefined | - pinhole formation - Broad distribution  not all An efficient & attenuation and scattering of products
Potential for more chemical flexibility (non-aquaeous solvent) ? | Impurities from organic solvent | 
Performance to be studied | R&D on going IJCLab/GANIL | Higher maximum beam intensities
R. Haas et al, “ODIn – a setup for Off-line Deposit Irradiations of thin layers for nuclear physics applications” Nucl. Instr. Meth. A , available online 26/12/19
Actinide Targets

## Slide 17: Activités de recherche groupe radiochimie, C. Cannes Electrodépôt d’actinides et lanthanides en milieux non-aqueux
Actinide Targets
Molecular Plating @IJCLab
Projet en collaboration avec l’ICSM (Marcoule), l’IPNO-groupe PACS, CENBG (Bordeaux), Ganil (Caen)
CDD Ingénieur, David Rodrigues
Thèse de Lu Jin
Projet soutenu par Needs (2016 et 2017)
Anode (substrat)
[M]
Cathode (Pt)
Générateur haute tension
DE : 100 à 1000 V
ou I : 1 à 10 mA/cm2
Paramètres ajustables pour optimiser la qualité des dépôts :
La composition de l’électrolyte : choix du solvant et des additifs ;
La tension ou l’intensité imposée ;
Le temps d’électrolyse ;
La température d’électrolyse ;
Le traitement thermique du dépôt ;
L’état de surface du substrat.
Systèmes étudiés dans l’isobutanol :
Ce, Pr, Nd, U et Pu
U sur Al mince
Pu sur C mince
Ex. cibles réalisées :

## Slide 18: Electrodépôt de Nd sur Al : Concentration de l’eau et tension imposée
300 V
500 V
900 V
[H2O] = 0.22 M
[H2O] = 1.1 M
Avantage des images 3 D : informations sur la rugosité des dépôts.
On observe des « rubans » composés principalement de C et O (analyse EDX).
La quantité de ces rubans diminue quand DE ou la concentration en eau augmente.
Le dépôt est plus couvrant quand DE augmente et quand la concentration en eau augmente.
[Nd] = 5 10-4 M
[HNO3] = 10-3 M
Actinide Targets
Molecular Plating @IJCLab

## Slide 19
Conclusions et perspectives sur ce projet
Conclusions :
Des conditions opératoires optimales ont été définies pour le dépôt de Nd sur Al.
Le travail a permis d’établir une démarche expérimentale pour comprendre le rôle de chaque paramètre sur la qualité des dépôts. Ceci est mis à profit pour les dépôts de U sur Al dans le cadre de la thèse de Lu Jin.
Une étude par MEBE sur le traitement thermique des dépôts de U montre que sur Al, les dépôts ont tendance à former des craquelures quand la température augmente et sur C, ils se décollent dès 150°C.
Perspectives :
Comprendre les mécanismes de dépôt de l’uranium pour optimiser la qualité des cibles : Définir les conditions optimales de dépôt, améliorer l’adhérence des dépôts et caractériser les dépôts.
Projet en collaboration avec l’ICSM (Marcoule) et le Ganil (Caen).
Etablissement d’un protocole générique de définition de certaines conditions optimales ? Protocole de suivi de la croissance des couches ?
Préparer une cible de 242Pu pour des mesures de données nucléaires réalisées par le CENBG (Bordeaux) sur l’installation ALTO en 2022.
Travail réalisé dans le cadre du projet structurant Nacre (projet soumis à Needs en octobre 2019).
Actinide Targets
Molecular Plating @IJCLab
On going studies
Expertise in deposition,
Backings, characterization….

## Slide 20: New targets for SPIRAL1
O. Bajeat, Groupe Cibles Sources GANIL
ISOL Targets
p/d (Li/Be, conv) n
n (act* , Fission) FF
LP (Bi , fus) radio-isotopes
HI (targ , fus-evap)
HI (act* , fus-evap)
HI (targ , frag)
Hiq+ (C , stripping)
ECS Febiad existant avec cibles graphite
Fragmentation du projectile
New isotopes 
Target fragmentation ?

## Slide 21: Nouvelles cibles épaisses pour Spiral 1
Sous forme de feuilles métalliques (Nb), de céramiques poreuses (SiC, Al2O3, MgO…) ou de mousse de graphite imprégnée.
Cible de fragmentation | Faisceau d’intérêt | Estimation de l’intensité accélérée faisceau primaire 12C 95 A.MeV 2.1013 PPS /3600 W
Nb | 60Zn | 1,5.104
 | 64Ge | 1,5.103
 | 63Ga | 6,7.104
 | 67As | 2,7.103
 | 72,74,76Kr | 4,9.102/1,4.105/3,1.106
 | 79Se | 4,5.104
SiC | 21-22Mg | 8,2.102/2.105
 | 25Al | 7,9.104
Al2O3 | 10-11-15-16C | 
CaO | 28Mg, 30P, 32-33Ar | 
MgO |  | 
F. Ditroi et al, “Study of proton induced reactions on niobium targets up to 70MeV” Nucl. Instr. Meth. B 266, pp. 5087-5100, 2008
M. Barbui et al, “Calculations and first results obtained with a SiC prototype of the SPES direct target” Nucl. Instr. Meth. B 266, pp. 4289-4293, 2008
V. Hanemaayer et al, “Composite ceramic targets for high power proton irradiation” ” Nucl. Instr. Meth. B 266, pp. 4334-4337, 2008
ISOL Targets
Temperature stability ?
nacelle chauffante
Détecteur Ge
Faisceau d’ions radioactifs
Enceinte sous vide
Échantillon
collimateur
Release time ?
Test @LISE

## Slide 22
TATOO (Thin Actinide Target Cooperation) Work Program defined in PRCI (not accepted) IPNO, JGU, GSI, ICSM, GANIL
Stable
Radioactive
Conclusions & Perspectives
1- Opportunities with Bi liquid targets: design for radio-isotopes +SHE, feasibility, tests…..
2- Keeping expertise on actinides: R&D on deposition, backings, characterization, exploring new methods (DoD, intermetallic), reinforce collaboration between experts, knowledge transfer - R&D @IJCLab & SANDA EU-Project (h2020-nfrp2018)
3 – For exotic beams, studies on new materials
+++ mutual work with safety and design departments for thermal, mechanical issues with advanced simulations and prototypes + tests in real conditions
Multi-Physics disciplinary

## Slide 24
A TRAVAILLER
Prospectives à 10 ans
Bilan/demande forces ?
Multi-Physics disciplinary
 | Liquid Bi | Actinides | New targets for SPIRAL1
 | REPARE 2020-2023 | IJC Lab U 2021 Pu:2022 | 1 material/beam*/3 years?
 | Année Objectif* | Remarques
238U | 2021+1 | S3, composé et métallique
232Th | 2022+1 | S3
243Am | 2024+1 | S3
248Cm autres isotopes de Cm ? | 2024+1 | S3
242,244Pu | 2024+1 | S3
autres isotopes de Cm, Pa, Np** | > 2024 | S3
* Les années sont définies en considérant les premières expériences de S3 possibles en 2021.
** Au-delà de 2024, le programme expérimental sur S3 sera complété, on peut envisager des cibles de 1/ curium avec des isotopes autres que 248 (244 ?), 2/protactinium, neptunium, en fonction des capacités de fabrication et de disponibilité des isotopes.

## Slide 25
One of the major common concerns for all projects is the development of target technology which will meet the needs of the high intensity beams expected from the new projects.
This is underlined in the papers of Yu. T. Oganessian (JINR) [1] and J.B. Roberto (ORNL)[2] by the followings sentences:
-“In some laboratories, work has already started on developing accelerator complexes and new experimental facilities with the aim of the synthesis and study of nuclear and atomic properties of the new superheavy elements. Among these is the experimental complex under construction at FLNR (JINR) named the “SHE Factory [..]. Ideas incorporated in the design of the SHE Factory assume the development of the future experimental base in several ways: […] –production of new target materials (running and designed nuclear reactors and enrichment facilities) and development of techniques for making targets with high thermal and radiation stabilities “
“In the past decade, progress in the development of heavy actinide targets has contributed to the discovery of six new elements, elements 113–118, and more than 50 new isotopes. […] They depend on a robust infrastructure of actinide production, chemical processing, and heavy ion accelerator facilities. Continued scientific progress will require further advances in actinide production, processing, and target technology to enable experiments essential for exploring the limits of nuclear stability, heavy element chemistry, and the Periodic Table.”
[1] Yu. T. Oganessian et al, Nuclear Physics A 944 (2015) 62-98
[2] J.B. Roberto et al, Nuclear Physics A 944 (2015) 99-116

## Slide 26: Si besoin

## Slide 27
27
Nbeam
Nout
Spectrometer
Beam Dump
Detector
Thickness & homogeneity  ions Kinematics
 Optimal tuning of the spectrometer :
transmission of desired residues
and control of unwanted particles
 Accuracy (< 5%)
Requirements
Why characterization is important ?

## Slide 28: Characterisation
characterization
TARGET
thickness
thickness uniformity
identification of impurities
surface roughness
surface morphology
Isotopic abundances
Scanning Electron Microscpe (SEM)
AFM
X-ray diffractometer (XRD)
Optical microscope
Energy loss
Precise analytical balance
Spectrophotometry
*Low geometry a-particle (LGA)
*Radiographic Imaging (RI)
Rutherford Back Scattering (RBS)
PhotoElectron Spectroscopy (XPS)
Energy Dispersive X-Ray Spectroscopy (EDS)
Particle Induced X-ray Emission (PIXE)
Particle Induced g-ray Emission (PIGE)
Thermal Ionization Mass Spectroscopy (TIMS)
Neutron Activation Analysis (NAA)
Destructive/non destructive
Locally or over the surface

## Slide 29
Summary on thin layers characterization & Monitoring
X-ray
PIXE
MeV Ions
RBS / EBS
neutrons
g-ray
NAA
a
LGA
a
RI
X-ray
e-
e-
XPS
e-
e-
e-
e-
e-
e-
e-
e-
a
a
a
a
a
a
a
a
a
a
a
T
X-ray
EDS

## Slide 30
Gaseous or liquid
- gas or liquid flow (the melted metals as well)
- material closed in the chamber kept in the low temperature
- in case of gaseous target: implantation into the solid backing/carrier (D in PE)
The apparatus used in 1919 by Rutherford’s team
14N + α → 17O + p
Requirements
How does a target look like ?
Design proposed by E. Noah and all, EURISOL 100 kW Target Stations Operation and Implications for its Proton Driver Beam, EPAC,2006
Images from Melanie Delonca CERN Ph.D thesis
LIEBE
EMIS 2018
Notes: Rutherford transmutation „An anomalous effect in nitrogen,”
the alpha particle (from Polonium), which passed through the container with nitrogen gas, and nitrogen nucleus stuck together with a proton flying loose.

## Slide 31
MagIc Numbers Off Stability
Liquid H2 target
http://minos.cea.fr
Obertelli et al, Eur. Phys. J. A 50, 8 (2014)
AX (p , 2p) A-1Y proton knockout
Projectile
i
AX
p

Fragment
f
A-1Y
g
H2 target
100 - 200 mm
q
p
vacuum
Gas, P=1 atm.
E
300 mm
e-
e-


e-
e-
e-



drift
e-
e-
e-




e-
e-
e-


Requirements
How does a target look like ?

## Slide 32
Application – 3 bis
Actinide sample:
  500 - 1000 µg/cm²
  Active diameter 40-80 mm
  Homogeneous
  Surface roughness as low as possible
  On ultra-thin backing (low surf roughness)
242Pu / 110 µg/cm2
75 mm
Backing: Si-wafer, sputtered with thin Ti-layer. In total: 37 mg 242Pu for 8 targets
Layer homogeneity by Radiographic Imaging
Courtesy of K. Eberhardt
Actinide Targets

## Slide 33: Application - 2
Nature Vol. 533, pp. 47-51, 2016
233U-source:
  Thin (11µg/cm²)
  Homogeneous
  Low surface roughness
7.6(5) eV  163 nm (deep UV)
233U
229mTh
2 %
98 %
Laser excitation of a
nuclear level possible
229mTh might serve as „nuclear clock“
Courtesy of K. Eberhardt

## Slide 34: Contexte
Besoin de cibles d’actinides et autres radionucléides dans différents domaines de physique
Données nucléaires
L’étude de systèmes innovants pour le nucléaire du futur nécessite des données neutroniques des radionucléides. Ceci est essentiel pour établir l’inventaire des radionucléides, pour simuler le fonctionnement du réacteur ou pour dimensionner les installations.
Besoin de cibles minces (300 µg/cm2 ), de grande surface (d : 8 cm) sur Al ( 2 µm) :
232Th ; 233,234,235,238U ; 237Np ; 241,234Am ; 242,244Pu
Atome de petite taille Z1
Cible d’actinide
Z2
Élément
super lourd
Z = Z1 + Z2
L’atome de petite taille, accéléré par un
cyclotron, bombarde une cible d’actinide
Fusion des 2 noyaux
Désintégration du noyau en quelques
secondes
Synthèse et étude d’éléments superlourds (Z > 104)
Besoin de cibles minces (200 à 500 µg/cm2), sur Al, Ti ou C ( 2 µm) :
238U pour la synthèse de Hassium, Darmstadium et Copernicium
248Cm ; 243Am ; 242,244Pu pour la synthèse de Nihonium

## Slide 35: Méthode utilisée : Electroprécipitation
Electrolyte :
Solvant : isobutanol, isopropanol, Diméthylformamide (milieux visqueux)
Additif : HNO3, HF, HCl, Me4NCl (pour stabiliser l’élément en solution et pour augmenter la conductivité de l’électrolyte)
Montage à 2 électrodes :
Cathode : support de la cible, substrat de Z léger (Al, C, Ti)
Anode : métal inerte (Pt)
anode
[M]
cathode
Générateur haute tension
DE : 100 à 1000 V
ou I : 1 à 10 mA/cm2
Pour préparer des cibles minces d’actinides de grande surface, méthode la plus adaptée :
électroprécipitation

## Slide 36: Electroprécipitation : Principe
1. Réduction de l’eau :
2H2O + 2e H2 (g) + 2OH-
Modification du pH à la surface du substrat
Bleu de bromophénol : jaune à pH acide et violet à pH basique
avant électrolyse
pendant l’électrolyse
Electrolyte :
Solvant : isobutanol, isopropanol, DMF
Additif : HNO3, HF, HCl, Me4NCl
Montage à 2 électrodes :
Cathode : support de la cible, substrat de Z léger (Al, C, Ti)
Anode : métal inerte (Pt)
anode
[M]
cathode
Générateur haute tension
DE : 100 à 1000 V
ou I : 1 à 10 mA/cm2
2. Diffusion de l’élément à la cathode
3. Formation d’hydroxydes et précipitation à la surface du substrat :
[M] + x OH- M(OH)x

## Slide 37: Electroprécipitation : Optimisation des conditions de dépôt
Paramètres ajustables pour optimiser la qualité des dépôts :
La composition de l’électrolyte : choix du solvant et des additifs ;
La tension ou l’intensité imposée ;
Le temps d’électrolyse ;
La température d’électrolyse ;
Le traitement thermique du dépôt ;
L’état de surface du substrat.
Electrolyte :
Solvant : isobutanol, isopropanol, DMF
Additif : HNO3, HF, HCl, Me4NCl
Montage à 2 électrodes :
Cathode : support de la cible, substrat de Z léger (Al, C, Ti)
Anode : métal inerte (Pt)
anode
[M]
cathode
Générateur haute tension
DE : 100 à 1000 V
ou I : 1 à 10 mA/cm2
Systèmes étudiés dans l’isobutanol :
Ce, Pr, Nd, U et Pu
U sur Al mince
Pu sur C mince
Exemples de cibles réalisées :

## Slide 38: Electroprécipitation : Cas du néodyme
Electrolyte :
Solvant : isobutanol, isopropanol, DMF
Additif : HNO3, HF, HCl, Me4NCl
Montage à 2 électrodes :
Cathode : support de la cible, substrat de Z léger (Al, C, Ti)
Anode : métal inerte (Pt)
anode
[M]
cathode
Générateur haute tension
DE : 100 à 1000 V
ou I : 1 à 10 mA/cm2
Dépôt de Nd
sur Al dans l’isobutanol

## Slide 39: Electrodépôt de Nd sur Al : Choix de l’électrolyte
 | Concentration (M) dans l’isobutanol |  |  |  | Conditions d’électrolyse | 
 | Nd(NO3)3.5H2O | HNO3 | H2O | Me4NCl | E (V) | t
D1 | 5.5e-4 | 0 | 0 | 0 | 600 | 15 min
D2 | 5.5e-4 | 0 | 0.22 | 0 | 600 | 15 min
D3 | 5.5e-4 | 0 | 0.22 | 1e-3 | 600 | 15 min
D4 | 5.5e-4 | 1e-3 | 0.22 | 0 | 600 | 15 min
D5 | 5.5e-4 | 1e-3 | 0.22 | 0 | 250 | 1h30
D6 | 5.5e-4 | 1e-3 | 0.44 | 0 | 600 | 15 min
D7 | 5.5e-4 | 2e-3 | 0.44 | 0 | 600 | 15 min
D8 | 5.5e-4 | 1e-3 | 1,1 | 0 | 600 | 15 min
D9 | 5.5e-4 | 2e-3 | 0.22 | 0 | 600 | 15 min
D10 | 7.5e-4 | 1e-3 | 0.22 | 0 | 600 | 15 min
D11 | 1e-3 | 1e-3 | 0.22 | 0 | 600 | 15 min
Meilleurs dépôts

## Slide 40: Electrodépôt de Nd sur Al : Choix de l’électrolyte, concentration de l’eau
La valeur absolue du courant augmente avec la tension.
La valeur absolue du courant augmente avec la concentration en eau.
Le signal est perturbé quand la tension imposée est élevée. Ceci est dû est à la production de H2(g).
2H2O + 2e H2 (g) + 2OH-
[H2O] = 0.22 M
[Nd(NO3)3.5H2O] = 5 10-4 M [HNO3] = 10-3 M

## Slide 41: Electrodépôt de Nd sur Al : Concentration de l’eau et tension imposée
300 V
500 V
900 V
[H2O] =
0.22 M
[H2O] =
1.1 M
On observe des « rubans » composés principalement de C et O (analyse EDX).
La quantité de ces rubans diminue quand DE ou la concentration en eau augmente.
Le dépôt est plus couvrant quand DE augmente et quand la concentration en eau augmente.
[Nd] = 5 10-4 M
[HNO3] = 10-3 M

## Slide 42: Electrodépôt de Nd sur Al : Effet du temps d’électrolyse
20 min
10 min
30 min
[Nd] = 5 10-4 M [HNO3] = 10-3 M [H2O] = 1.1 M DE = 900 V
Le dépôt est le plus couvrant et le plus homogène pour un temps d’électrolyse de 20 min.
A 30 min d’électrolyse, on observe des trous, certainement formés par le dégagement des bulles de H2(g).
On obtient dans ces conditions un film de 15 µm d’épaisseur.

## Slide 43: Electrodépôt de Nd sur Al : Cinétique de dépôt
[Nd] = 5 10-4 M [HNO3] = 10-3 M [H2O] = 1.1 M DE = 900 V
Les rendements de dépôt (mesurés par ICP/AES) sont supérieurs à 90% à partir de 12 min d’électrolyse environ.
Le rendement d’électrolyse est le meilleur pour 20 min d’électrolyse.
L’intensité diminue puis atteint une valeur plateau après 10 min :
la formation du dépôt pourrait être suivie in situ par la mesure de l’intensité du courant.

## Slide 44: New targets for SPIRAL1
O. Bajeat, Groupe Cibles Sources GANIL
ISOL Targets
p/d (Li/Be, conv) n
n (act* , Fission) FF
LP (Bi , fus) radio-isotopes
HI (targ , fus-evap)
HI (act* , fus-evap)
HI (targ , frag)
Hiq+ (C , stripping)

## Slide 45
ECS Febiad existant avec cibles graphite
Fragmentation du projectile
ISOL Targets
New isotopes 
Target fragmentation ?

## Slide 46: Nouvelles cibles épaisses pour Spiral 1
Sous forme de feuilles métalliques (Nb), de céramiques poreuses (SiC, Al2O3, MgO…) ou de mousse de graphite imprégnée.
Cible de fragmentation | Faisceau d’intérêt | Estimation de l’intensité accélérée faisceau primaire 12C 95 A.MeV 2.1013 PPS /3600 W
Nb | 60Zn | 1,5.104
 | 64Ge | 1,5.103
 | 63Ga | 6,7.104
 | 67As | 2,7.103
 | 72,74,76Kr | 4,9.102/1,4.105/3,1.106
 | 79Se | 4,5.104
SiC | 21-22Mg | 8,2.102/2.105
 | 25Al | 7,9.104
Al2O3 | 10-11-15-16C | 
CaO | 28Mg, 30P, 32-33Ar | 
MgO |  | 
F. Ditroi et al, “Study of proton induced reactions on niobium targets up to 70MeV” Nucl. Instr. Meth. B 266, pp. 5087-5100, 2008
M. Barbui et al, “Calculations and first results obtained with a SiC prototype of the SPES direct target” Nucl. Instr. Meth. B 266, pp. 4289-4293, 2008
V. Hanemaayer et al, “Composite ceramic targets for high power proton irradiation” ” Nucl. Instr. Meth. B 266, pp. 4334-4337, 2008
ISOL Targets
Temperature stability ?

## Slide 47: Cibles ISOL Spiral 1 Projet de tests sur LISE
nacelle chauffante
Détecteur Ge
Faisceau d’ions radioactifs
Enceinte sous vide
Échantillon
collimateur
But: qualifier le relâchement des nouvelles cibles en implantant des atomes radioactifs d’intérêt dans des échantillons chauffés.
1ère application pour la cible niobium.
Les ions radioactifs implantés doivent avoir la bonne énergie pour être arrêtés dans la feuille.
L’activité de l’échantillon en fonction du temps permettra de déduire le temps de relâchement.
ISOL Targets
Release time ?

## Slide 48: Etude d’une cible Niobium
60Zn, 64Ge, 63Ga, 67As, 72,74,76Kr, 79Se …
La cible à l’étude est constituée de disques de faible épaisseur : 0,1 ou 0,05 mm.
Les distances seront optimisées pour obtenir une température uniforme.
Le pic de Bragg est déposé dans le fond refroidi.
Étude en cours
Simulation ANSYS

## Slide 49: Actinide Targets
Actinide Targets
Applications
n (act* , Fission) FF
HI (act* , fus-evap)
Actinide targets for SHE:
  200 – 500 µg/cm²
  Homogeneous
  Numerous
  Minimizing Eloss in backing
  (now 1,5 µm Ti : dE=2/3dEtot)
people.physics.anu.edu.au/
238U
243Am
248Cm
242,4Pu
GT02 – A. Lopez-Martens « Heavy and super_heavy nuclei »
Courtesy of K. Eberhardt
242Pu / 110 µg/cm2
75 mm
GT02 – B. Jurado « Comment arriver à une description complète de la fission nucléaire? »
GT11 – M. Kerveno « Données nucléaires »
Actinide sample:
  1501000 µg/cm²
  Active diameter 40-80 mm
  Homogeneous
  Surface roughness as low as possible
  On ultra-thin backing: Ni (250 nm) or PL (220 nm)
FALLSTAFF spectrometer
http://irfu.cea.fr/en/Phocea/Vie_des_labos/Ast/ast_technique.php?id_ast=4216
24xBk
252Cf