## Slide 1
High Field Magnet R&D
for the Next-generation Accelerators
Qingjin XU
for the Superconducting Magnet Group
Accelerator Division, IHEP-CAS
Apr 10 2024

## Slide 2
High Energy Circular Colliders for next decades | SPPC | FCC
Proposed institution | IHEP-CAS, China | CERN, Europe
Proposed dates | 2012 | 2013
Site of the project | China | Europe
Baseline technology | IBS 20~24 T to reach 125-150 TeV, Nb3Sn etc as options | Nb3Sn 16 T to reach 100 TeV
Timeline | Construction at 2040s | Construction at 2050-60s
Cost | * | **
Design Scope for Next-generation Accelerators

## Slide 3
Roadmap of the High Field Magnet R&D at IHEP
Challenges: Stress control, quench protection, field quality control,……
2018-2021, 12.47T @4.2K
NbTi + Nb3Sn
2021-2024 16T @ 4.2K
Nb3Sn + HTS

## Slide 4
16 T Model Dipole LPF3: Nb3Sn 13 T (Common Coil with 55 mm gap) + HTS 3 T inserts (Block & CCT)
Development of the 16-T Model Dipole LPF3

## Slide 5
The Nb3Sn coils for LPF3
Chengtao Wang et al
Development of the 16-T Model Dipole LPF3

## Slide 6
The ReBCO block insert coils for LPF3
Parameters | Values
L0 | 409.6 mm
L1 | 540.2 mm
Rhard | 800 mm
Aend | 6 °
R1 | 9.5 mm
Z1 | 120 mm
Ze Feng et al
Development of the 16-T Model Dipole LPF3

## Slide 7
The ReBCO CCT instert coils for LPF3
典型CCT线圈结构示意
“斜螺线管”型CCT线圈结构示意
Rui Kang et al
Development of the 16-T Model Dipole LPF3

## Slide 8
2023.8.29 Assembly completed
Stress monitoring during
assembly with FBG
Pre-stress applied with commercial hydraulic jack
Pre-stress and assembly of LPF3
Yingzhe Wang et al
Development of the 16-T Model Dipole LPF3

## Slide 9
Current decay curve at the operating current
Varistor plus CLIQ to protect the Nb3Sn coils. The maximum hot spot is ~ 230 K
NI configuration plus dump resistor to protect the 2 HTS insert coils
Quench protection of LPF3
Development of the 16-T Model Dipole LPF3
Jinrui Shi et al

## Slide 10
Performance test ongoing from Sep 2023
The Nb3Sn coils were trained firstly, maximum current reached ~85% of Iop in Dec 2023, but showed an unstable plateau at 11 T due to one of the outmost Nb3Sn coil, probably due to insufficient pre-stress during assembly
HTS block coil was ramped independently to 100% of Iop with negligible terminal voltage
Wei Li et al
Development of the 16-T Model Dipole LPF3
55 mm 双孔径

## Slide 11
Reassembly of the magnet with enhanced pre-stress
Xin Chen et al
Development of the 16-T Model Dipole LPF3
应变片监测磁体组装、降温、励磁过程
光栅光纤监测磁体组装及测试过程
2024 年 1 月

## Slide 12
The 2nd Performance test in Feb 2024
Development of the 16-T Model Dipole LPF3
The Nb3Sn coils showed very unstable performance in the 6300-7000 A region due to one of the inner most coils, but finally passed this region and reached ~87% of Iop in the beginning of March 2024
HTS block coil was ramped independently to 120% of Iop to test its ultimate performance, but one of the lead was damaged due to the quench.

## Slide 13
Accident in Mar 14 2024
Development of the 16-T Model Dipole LPF3
The operator forgot to follow the most important step of the test manual: turn on the quench detection system, and powered the Nb3Sn coils to high current directly. 2 of 6 Nb3Sn coils were serious damaged during a quench
Plan for next months: establish a hardware interlock protection system, and re-fabricate 2 new Nb3Sn coils and 2 HTS coils, to reach 16 T by the end of 2024

## Slide 14
Chart: Applied Magnetic Field (T)
| 0 | 5 | 15 | 20 | 25 | 30
REBCO: B ∥ Tape plane | 4144.6766 | 3507.9375 | 3148.3332 | 2909.0554 | 2090.4933 | 1888.9952
REBCO: B ⊥ Tape plane, 45 μm sub | 5478.1345 | 5053.3515 | 4372.0346 | 3812.2534 | 3348.8068 | 3146.724 | 2964.7726 | 2801.365 | 2663.2305 | 2530.35 | 2415.161 | 2307.3222 | 2215.5971 | 2121.427 | 2046.7953 | 1970.1838 | 1905.1216 | 1841.6283 | 1784.4676 | 1729.8653 | 1682.3664 | 1631.1403 | 1591.3007
REBCO: B ⊥ Tape plane | 4144.6766 | 1445.8386 | 975.0997 | 767.7508 | 655.6687 | 571.6114 | 526.7777 | 481.944 | 442.7183 | 428.1462 | 403.4904 | 386.6773 | 364.2626 | 341.8457 | 328.3952 | 319.4289 | 318.3073
Bi-2212: OST NHMFL 50 bar OP | 1243.4169 | 1159.7904 | 1097.571 | 1051.5861 | 1014.8275 | 981 | 955.0755 | 928.7776 | 905.6283 | 884.9933 | 865.478 | 846.7181 | 827.3047
Nb₃Sn: Internal Sn RRP® | 1754.8557 | 1454.9349 | 1190.9814 | 1072.6374 | 957.7741 | 855.0933 | 757.6336 | 268.0143 | 190.8587 | 118.9241 | 65.5533 | 28.3097
Nb₃Sn: High Sn Bronze | 166.6431 | 137.8146 | 111.0954 | 84.3762 | 60.8212 | 40.0788 | 19.3362 | 8.0861
Nb-Ti: LHC 4.2 K | 5106.8846 | 4054.1538 | 3180.5962 | 2710.2269 | 2217.4577 | 1724.6885 | 1411.1115 | 1187.1231 | 918.3423
Nb-Ti: Iseult/INUMAC MRI 4.22 K | 393.4783 | 291.3043 | 194.203 | 104.3478
Exponential Y-axis Labels | 10 | 100 | 1000 | 10000
Nb-Ti midrange maximal | 971.9231 | 687.3077 | 448.4615 | 393.4783
2212 Fitted Line for 50bar ASC'16 | 1381.5217 | 1248.5735 | 1162.079 | 1099.1369 | 1050.2486 | 1010.6145 | 977.4929 | 949.1799 | 924.5486 | 902.818 | 883.4258 | 865.9547 | 850.0872 | 835.5764 | 777.6921 | 691.6232
YBCO B perp linear extrap | 312.7055 | 264.5487 | 240.4379
IBS 2016
IBS 2019
IBS 2022
IBS 2025
IBS Technology: Status and Outlook
90% Stainless-steel & 10% Sliver stabilized IBS tape achieved the highest Je in 2022!
Significantly reduced the cost and raised the
mechanical properties.

## Slide 15
IBS Technology: Status and Outlook
Ic of Φ34mm-17 turns-DPC reached 60 A at 4.2 K and 32 T, world’s highest record up to now
The First IBS Solenoid Coil at 32 T background field
Chunyan Li et al
2024 Supercond. Sci. Technol. 37 015001
Successfully fabricated double pancake coils and a series-connected coil consisting of six DP coils

## Slide 16
IBS Technology: Status and Outlook
Quench propagation study of the IBS tapes and coils
Chunyan Li et al

## Slide 17
IBS Technology: Status and Outlook
Quench propagation study of the IBS tapes and coils
Chunyan Li et al
In 15~17K, when the transmission current of iron-based superconductor is 14-179A, the corresponding NZPV value is 0.4– 7cm/s

## Slide 18
IBS Technology: Status and Outlook
2008.02
2008.09
2016
2018
Discovery of IBS
2008.04
Discovery of
122 phase IBS
2020
100-m 7-core IBS tape fabricated
Je= 100 A/mm2
@ 10 T, 4.2 K
IBS solenoid at 24 T
Racetrack at 8 T
Je= 300 A/mm2
@ 10 T, 4.2 K
IBS solenoid at 32 T
Racetrack at 10 T
1.3 kA transposed cable
Je > 450 A/mm2
@ 10 T, 4.2 K
2022
H. Hosono
IBS (Tc 26K)
Z. Zhao
IBS (Tc 55K)
Je of IBS expected to be similar as ReBCO in 5 years with better mechanical properties and lower cost

## Slide 19
Milestone of the HL-LHC CCT Magnet Project
Development of CCT Magnets for HL-LHC
Agreement signed
btw IHEP and CERN
The qualified prototype delivered to CERN
The CCT magnet from China under test at CERN
All the 12 series CCT magnets delivered to CERN
Installation to tunnel
HL-LHC commissioning

## Slide 20
Development of CCT Magnets for HL-LHC
Successful design upgrade to solve the “long training problem”, significantly reduced the times of quench during training, ensured the project progress “on track”.

## Slide 21: Training of MCBRD02 & MCBRD03
Development of CCT Magnets for HL-LHC
AP1(CB12，25 quenches 526A) reached ±422A after 11 quenches.
AP2(CB09, 33 quenches 530A; after thermal cycle ＞500A) reached ±422A without any quenches.

## Slide 22: Training of MCBRD04
Development of CCT Magnets for HL-LHC
Satisfying performance at 4 K for both apertures, tested at IMP-CAS

## Slide 23
4 series CCT magnets have been fabricated, successfully reached the design target and delivered to CERN
Components for 2 series magnets being shipped to CERN
Production rate for the rest of series magnets: every 3 month per magnet; to be completed by Oct 2025
Development of CCT Magnets for HL-LHC
 | Coil name | Winding method | Location | Coil stand-alone performance (4.2 K) | Magnet performance at 4.2 K
MCBRD01 | MCBRD_CB01 | Wet wind | CERN | 530 A | Both apertures reached ultimate current 422 A, and passed 4-hour stability test at 4.2 K
 | MCBRD_CB03 | Direct wind |  | 410 A (training stopped due to the availability of the test station) | 
 | MCBRD_CB02 | Direct wind | CERN | Failed to reach the design current | 
MCBRD02 | MCBRD_CB04 | Wet wind | CERN | 422 A (training stopped due to the availability of the test station) | Both apertures reached ultimate current 422 A, and passed 4*1 hour stability test at 4.2 K
 | MCBRD_CB06 | Wet wind |  | 530 A | 
MCBRD03 | MCBRD_CB09 | Direct wind with new channel size | CERN | 530 A | Both apertures reached ultimate current 422 A, and passed stability test at 4.2 K
 | MCBRD_CB12 | Direct wind with new channel size |  | 526 A (25 quenches) | 
 | MCBRD_CB14 | Direct wind with new channel size | BAMA | 530 A (30+34 quenches), put in quarantine | 
MCBRD04 | MCBRD_CB13 | Direct wind with new channel size | IMP | 530 A (20+33 quenches) | Both apertures reached ultimate current 422 A, and passed stability test at 4.2 K
 | MCBRD_CB17 | Direct wind with new channel size |  | 524 A (47 quenches) | 
MCBRD05 | MCBRD_CB18 | Direct wind with new channel size | IHEP | 530 A (43 quenches) | To be assembled
 | MCBRD_CB19 | Direct wind with new channel size | IHEP | 530 A (63 quenches) | 
 | MCBRD_CB20 | Direct wind with new channel size | IHEP | To be stand-alone tested | 
MCBRD_CB10, 11, 15, 16 |  | Shipped to CERN for fabrication |  |  | 

## Slide 24
Summary
Long-term advanced superconducting magnet R&D for future high-energy accelerators is ongoing at IHEP-CAS
16 T (Nb3Sn+HTS) model dipole has been fabricated at IHEP-CAS and under performance test at 4.2 K. Re-fabrication of damaged coils to be done in the next months，aiming to reach 16 T in 2024
Strong domestic collaboration for the advanced superconductor R&D (HTS & Nb3Sn): Stainless-steel-Silver stabilized IBS tape achieved the highest Je in 2022! Significantly reduced the cost and raised the mechanical properties
HL-LHC CCT magnets going well, to be installed in the tunnel in 2026
Thanks for your attention!