## Slide 1: Alkaline Etching of silicon
Igor Ozerov / PLANETE /
Aix-Marseille Univ, CNRS, CINAM 13009 Marseille France
28/01/2020 meeting at CPPM

## Slide 2: Principles of anisotropic wet etching of Silicon
Parallel vertical walls with high aspect ratio for {110} wafers !

## Slide 3: Alcaline Wet Etching of Silicon at CINaM
J. Proust, F. Bedu, S. Chenot, I. Soumahoro, I. Ozerov, B. Gallas, R. Abdeddaim, and N. Bonod, Advanced Optical Materials, vol. 3, pp. 1280-1286, 2015.
Selective chemical etching, Cr/Au mask
KOH or TMAH ?
KOH {110}>{100}>{111}
TMAH {100}>{110}>{111}

## Slide 4: Preliminary results on Si (110) nov.-dec. 2019
Sample B: etching in KOH solution for 1 hour
Contact mechanical profilometer measurements: Channel depth ~27-30 µm
Technological steps:
Plasma cleaning of Si(110)/ SiO2
UV lithography (channel definition)
Reactive Ion Etching of SiO2 (channel opening)
Wet etching of Si in KOH solution
(Removal of the remaining SiO2 mask)
After lithography
After RIE
After lithography : Channel width 300 µm, photoresist thickness 1.5µm

## Slide 5: Preliminary conclusions
Proof of concept – Ok.
Need to get Si (110) wafers thicker SiO2 layer mask for deeper etching.
Roughness of the obtained surface (along the channel direction)