## Slide 1
Direct ultratrace and isotopic analysis in solids by femtosecond LA-ICPMS.
Christophe Pécheyran, IPREM, Université de Pau et des Pays de l’Adour Fanny Claverie, Université de Pau et des Pays de l’Adour
Frédéric Perrot, CENBG, Gradignan
Bertrand Thomas, CENBG, Gradignan
Cédric Cerna, CENBG, Gradignan
Fabrice Piquemal, CENBG, Gradignan

## Slide 2
A laser to dig, an ICPMS to count…
  Alternative to wet chemistry:
    Direct analysis
    Very limited sample preparation
    Very limited risk of contamination
    Refractory matrices anaysis
  Tool of choice for micro-analysis:
    Quasi non destructive
    Micro analyses (µm – hundreds µm)
    Depth profiling (< µm resolution)
    High sensitivity
ICPMS
Ablation Cell
He 

Scan
Inclusion analysis
Imaging, bulk analysis
Laser
LA-ICPMS :

## Slide 3
LA– ICPMS applied to challenges of societyles
Environment
Health
Archaeology
Forensic science
Inter/national security
Fight against counterfeiting
Energy,
etc...
ICPMS
He 

Scan
Laser
Ablation Cell
Scan
Inclusion analysis
Imaging, bulk analysis

## Slide 4
1983
1985
1990
1995
2000
2010
Big Bang
(First ICPMS)
2005
2015
Laser ablation over time
1064 nm, Nanoseconde, 10 Hz, (Arrowsmith et al, 1987)
266 nm, Nanoseconde, 20 Hz (Chenery et al, 1993 )
213 nm, nanoseconde, 20 Hz (Jeffries et al, 1998
193 nm nanoseconde , 20 Hz (Geertsen et al, 1994)
785 nm Femto, 10 Hz (Russo et al 2002)
266, 196 nm, Femto, 20 Hz (Poitrasson et al 2003)
1030 nm, Femto, 10 kHz (Pécheyran et al 2005)
257 nm, Femto, 100 kHz, (Pécheyran et al, 2013)
694 nm, Nanoseconde, 10 Hz, (Gray et al,1985)
2020

## Slide 5
Nanosecond pulses
Femtosecond pulses
Thermal effects= accuracy bias
(preferential evaporation, large particles)
Limited termal effects =
better accuracy, precision and sensitivity
Ultra short pulses for better analytical performances

## Slide 6
Small laser beam
(≈ 10 μm)
Adjusting the laser beam shape to the sample morphology to :
1/ improve the detection sensitivity
2/ high spatial resolution
Galvanometric scanners
HR-fs LASER
High repetition rate(<100 kHz)
Fast movement
(<2 m/s)
IPREM : HR femtosecond laser with virtual beam shapping

## Slide 7
HR-ICPMS jet interface, Thermo
High Rep-
UVfs-LA
MC-ICPMS, Nu Plasma
ICPMS/MS Agilent 8900 (semi-conductor config)
High Rep-
IRfs-LA
HR-MCICPMS Nu1700 (Nu Instruments/Cameca), EQUIPEX MARSS
PLATEFORME PAMAL (Pau-UPPATech) : Laser-ICPMS imaging
(unsurpassed limits of detection)
(Ultimate isotope precision)
(Fast and sensitive multielement imaging)

## Slide 8
Estuaire aval
Extracting the most relevant information from few nanograms of matter=> detecting few pico, femto and even attograms
ORIGIN
INTENTION
U Civilian
U Military
Nuclear forensic science at the particle scale
Collaboration with F. Pointurier, CEA

## Slide 9
INTENTION => precise U isotope ratio
HR-ICPMS
HR-UVfs-LA
MC-ICPMS
 | fsLA-MCICPMS |  |  | fsLA-HRICPMS |  | 
 | 235/238U | 234/238U | 236/238U | 235/238U | 234/238U | 236/238U
Ecart à la valeur vraie % | 1% | -1,6% | - | 1% | 3% | 4%
Précision interne (RSD) | 0,32% | 0,68% | - | 1% | 2% | 1%
Précision externe (RSD) | 1,8 % | 2,4% | - | 5% | 13% | 12%
F. Claverie et al, Anal. Chem, 2016 – A. Donard et al, JAAS, 2016
TIMS results
LA-ICP-SF-MS results
Nuclear forensic science at the particle scale
Collaboration with F. Pointurier, CEA

## Slide 10
Time (s)
Intensity (cps)
139La | 140Ce | 141Pr | 143Nd | 147Sm | 153Eu | 157Gd | 159Tb | 163Dy | 165Ho | 166Er | 169Tm | 172YB | 175Lu
105 ag (34 ag)0 | 127 ag (35 ag)0 | 80 ag (31 ag)0 | 707 ag (246 ag)0 | 388 ag (223 ag)0 | 173 ag (173 ag)0 | 633 ag (265 ag)0 | 85 ag (43 ag)0 | 276 ag (183 ag)0 | 95 ag (48 ag)0 | 277 ag (145 ag)0 | 114 ag (50 ag)0 | 555 ag (258 ag)0 | 113 ag (61 ag)0
Nuclear forensic science at the particle scale
One micron particle = few hundreds nanogrammes
UvFsLA – HR-ICPMS
(jet interface)
Detection Limit : ∑Counts < 70 => Poisson’ s law : LD =(2,71 + 3,29√B)/S
A. Donard et al, JAAS, 2015
ORIGIN => lanthanides pattern
Collaboration with F. Pointurier, CEA

## Slide 11
238U
234Th
234Pa
234U
230Th
214Bi
214Pb
210Bi
210Pb
206Pb
214Po
210Po
226Ra
222Rn
218Po
238U
238U
234U
238U
234U
238U
238U
234U
238U
234U
230Th
Carbonate formation
230Th Production
time
Chart: 230Th/234U as a function of time
Direct dating of archaeological objects by fsLA-ICPMS imaging
Very low 238U, 234U and 230Th levels:
      If T≈ 100ky and [238U]≈1 ng/g (10-9g/g)  [230Th]≈10 fg/g (10-14g/g)

## Slide 12
(cps)
(cps)
(cps)
Isotopic mapping shows different levels and types of alteration at the micron scale (here 1pixel = 30µm)
Allows to consider only the most relevant zones for dating.
Ostrich eggshell
Direct dating of archaeological objects by fsLA-ICPMS imaging
 | LA-Fs-HR-ICP-MS Protocol
Sampling mass (6 analysis) | 1 mg (238U≈1-15 ppb)
Analysis time | 3 days (6 images accumulated)
Sample preparation | Fragments embedded in epoxy
Age | 51±16 ky (115 ions of 230Th measured  ~20 ag in the sample)
Chart: Ages comparison
| U/Th mapping | Tribolo et al. 2013 | Jacobs and Robert 2015
 | 51 | 52 | 55
230Th instrumental background as low as 0,02 ion/s
Collab. N Mercier, C Tribolo, Univ Bx Montaigne

## Slide 13: Nesher Ramla : archaic Homo
Well preserved sample
Enamel : 230Th detectable  U-series usable
Each tissue processed separately incorporation kinetic of U after death
Tissu | Masse ablatée | Age (ka)
Enamel | 0,86 mg | 73,4±6,5
Dentine | 6,42 mg | 86,8±3
Cement | 0,55 mg | 99,1±4,5
Auroch tooth

## Slide 14: Nesher Ramla
Minimum age
= 99,06±4,5 ky
Science, 372(6549), 1429-1433, 2021

## Slide 15: Application to material purity assessment for rare events experiments
CENBG is involved for many years in neutrino physics and double beta decay experiments
Using UVfsLA-ICPMS analytical methodology measurements for quantitative ultra-low background measurements and U/Th mapping of materials used in rare event experiments

## Slide 16: Material purity assessment for rare events experiments : µ-coaxial cable
LASER Operating Conditions for IMAGING
λ=257 ns
Pulse duration : 360 fs
Energy per pulse: 5 µJ
Repetition rate: 50 Hz
Spot size: 8 µm
Speed of the scan: 10 µm/s
Distance between 2 lines: 5 µm
D~400 µm

## Slide 17: 2D-FsLA-ICPMS mapping of µ-coaxial cable
13C
65Cu
238U
Cu contamination in some of the copper wires.
Complementarity with conventional ICPMS :
  fsLA HR-ICPMS is able to locate contamination
  Quantitative analysis (with fit for purposes standards)

## Slide 18
232Th
13C
80µm
2D-FsLA-ICPMS mapping of the acrylic sample
25 mm
25 mm
Acrylic sample (C5O2H8)
238U
80 µm
Counts/s
Counts/s
Notes: On a pas mesuré le socncentration sur cette image, mais la distribution spatiale.

## Slide 19: FsLA-ICPMS for FAST surface analysis of acrylic samples
25 mm
25 mm
600 µm
2D scan of a square of 600x600 µm2
µm in 30 s only.
UV fs laser operating conditions :
λ=257 ns
Energy: 5 µJ/pulse
Frequency: 400 Hz
Spot size: 8 µm
Scan velocity: 2 mm/s
Acrylic sample (C5O2H8)
sample
background
Laser ON
Laser OFF

## Slide 20: Acrylic : Polished or not polished ?
Two acrylic samples have been measured:
one with polishing process applied on the top surface
one without polishing
→ Very efficient tool to measure the U/Th contamination and to choose the best surface treatment of a critical material!
232Th
One order of magnitude!

## Slide 21: Depth profile (Z axis) of U/Th level
Laser
shots
600 µm
Acrylic
surface
1 scan
4 µm depht
2 scans
8 µm depht
3D profile
Bulk contamination
Several 2D laser scans to explore the Z-axis
Mass of ablated acrylic per scan ~1.7 μg with a 10% uncertainty
Most of U and Th contamination of the acrylic is located on the surface in the first 4 μm
Surface contamination

## Slide 22: Conclusion
→ Overall efficiency of 0.20% of the LA-ICPMS has been derived for 238U and 232Th (tune condition U/Th=1,00 +/- 0,01 on NIST 612)
→ Very low background
→ Detection at the ppt level (and even lower) for U and Th with less than 10 μg of sample ablated !
→ Sensitivity competitive with Neutron Activation Analysis
Need to have a reference material for U and Th concentration
A home-made acrylic standard at the ppb level has been designed (to be published/pattented)
Quantitative analysis
Notes: La sensibilité n’est pas la limite de detction qui doit etre utilisée ici

## Slide 23
Contact Organisation
Nicolas TASTET
Tél. 07 82 45 08 27
contact@spectratom.fr
Comité d’Organisation
www.spectratom2022.sciencesconf.org
Dr. Christophe PECHEYRAN (Président) IPREM - UMR 5254, Université de Pau et des Pays de l'Adour/CNRS
Dr. Olivier DONARD (co-président) IPREM - UMR 5254, Université de Pau et des Pays de l'Adour/CNRS
Dr. Fanny CLAVERIE UPPA-Tech, Université de Pau et des Pays de l'Adour/CNRS
Dr. Pascale LOUVAT IPREM - UMR 5254, Université de Pau et des Pays de l'Adour
Pr. Florence PANNIER IPREM - UMR 5254, Université de Pau et des Pays de l'Adour
Gaëlle BARBOTIN UPPA-Tech, Université de Pau et des Pays de l'Adour
Dr. Hugues PAUCOT UT2A formation, Université de Pau et des Pays de l'Adour
Dr. Fabienne SEBY UT2A, Université de Pau et des Pays de l'Adour
Géraldine BOURGUET UPPATECH - Université de Pau et des Pays de l'Adour
Antonia TOSKA IPREM - UMR 5254, Université de Pau et des Pays de l'Adour
Matthieu BOCCAS IPREM - UMR 5254, Université de Pau et des Pays de l'Adour
Asmodée GALY IPREM - UMR 5254, Université de Pau et des Pays de l'Adour
L’EVÈNEMENT DE L’ANALYSE
INORGANIQUE FRANCOPHONE
Nous sommes particulièrement heureux de vous accueillir de nouveau à Pau pour l’édition 2022.
BIENVENUE !