## Slide 1
Plasma cleaning for SRF needs
at IJCLab
O. Hryhorenko (post-doc), E. Mistretta, B. Mercier, D. Longuevergne
Equipe MAVERICS – Plateforme Vide et Surfaces
Pôle Physique des Accélérateurs - IJCLAB
FCCee SRF IN2P3 collaboration meeting – 9th November

## Slide 2: Test bench
f = 13.56 MHz
P = 100 W
Window
Way of gas injection

## Slide 3: Before/after plasma cleaning
Before cleaning:
deposition of the C layer
(40-50 nm)
After cleaning:
No C-layer

## Slide 4
Plan and collaboration
4
Apply to low beta cavities (Spiral2 QWR)
Starting collaboration :
GANIL : apply in-situ plasma cleaning in Spiral2 cryomodules
LPP : experts in plasma diagnostics
INSP : expertise in surface oxide and decontamination by plasma