## Slide 1
Meeting FCC-ee
Vacuum
Suheyla BILGEN – Bruno MERCIER – Gaël SATTONNAY
MAVERICS team at IJCLab / IN2P3
November 16, 2021
Réunion R. Kersevan 16/11/2021

## Slide 2: Plan
Contexte équipe MAVERICS-IJCLAB/IN2P3
Présentation plateforme Vide&Surfaces
Exemple : NEG
Collaboration CERN 2018-2020 : mesures VPS+désorption ionique
Simulation Vide dynamique DYVACS
Propositions
Réunion R. Kersevan 16/11/2021

## Slide 3
Réunion R. Kersevan 16/11/2021

## Slide 4
MAVERICS : Thématiques de recherche
Propriétés supraconductrices des surfaces (résistance de surface et blindage magnétique des cavités SRF)
Vide Dynamique
  désorption stimulée
  phénomènes collectifs (nuages d’électrons dans le LHC)
Modifications par irradiation (électrons, photons, ions) des propriétés de surface des matériaux (émission électronique secondaire, désorption moléculaire, chimie de surface)
→ Analyses de surface des matériaux → Plateforme Vide et Surfaces
But : Améliorer les performances des accélérateurs de particules de haute énergie
 | Cavités SRF |  | Lignes faisceaux / chambres à vide |  | 
 | Augmenter les gradients accélérateur Réduire les pertes RF | Limiter le multipacting |  | Limiter les augmentations de pression | 
Traitements de surface | Niobium massif : thermique, dopage/ infusion N, polissage (Projets HELOISE et PACCAS du MP SRF) | Traitements thermiques Conditionnement des surfaces Nettoyage plasma, UV |  |  | Traitements de surface
Couches minces | Matériaux alternatifs : multicouches supraconductrices S-I-S (Projet AXE SRF du MP SRF) | TiN, Carbone amorphe, NEG (Projet MULTIPAC du MP SRF + CNRS 80PRIME) |  |  | Couches minces
-Participation à des projets de conception / construction d'accélérateurs du Pôle (ESS, MYRRHA, PIP2)
-Participation au Groupe Transverse FATI (fabrication additive métallique) / Projet FABBAC
Réunion R. Kersevan 16/11/2021

## Slide 5: Plan
Réunion R. Kersevan 16/11/2021
Contexte équipe MAVERICS-IJCLAB/IN2P3
Présentation plateforme Vide&Surfaces
Exemple : NEG
Collaboration CERN 2018-2020 : mesures VPS+désorption ionique
Simulation Vide dynamique DYVACS
Propositions

## Slide 6
Secondary Electron Yield (SEY)
Thèse S. Bilgen
Confocal Microscope
    Compact SIMS Hiden Analytical
Secondary Ion Mass Spectrometry (SIMS)
Profile of bi-layer TiN/Al2O3/Nb
NEG coating chamber (Ti,Zr,V)
X-ray difractometer
Heat treatment (H2)
dedicated to characterization and surface analysis of materials used in accelerator technology
outgassing rate
scanning electron microscope
Composition (EDS)
Structural (EBSD)
VKX200 de Keyence
molecular desorption energy
surface roughness
Surface Structure and Texture
Equipment of the V&S Platform (some Examples)
Pôle accélérateurs
Thèse S. Birra
Accelerator Department
Réunion R. Kersevan 16/11/2021

## Slide 7: Emission électronique secondaire / Analyses de surfaces
Bâti mesure SEY
ISIS (ICMMO)
SEY
+Analyse de surfaces/XPS
+ mesures haute T
+Conditionnement NEG in situ
e
Bâti multitechnique
SEY
+Analyse de surfaces (XPS)
+mesures basse T (10K)
Analyse de surfaces
XPS de routine
EQUIPEX PACIFICS
2022/2023
Réunion R. Kersevan 16/11/2021

## Slide 8: Plateforme ANDROMEDE IJCLab : TOF-SIMS
SuperACO
3 MV
Sample
12MeV – Au4004+ nanoparticle beam
Carbon on the surface of a fully conditioned Cu
Graphene reference sample
TOF-SIMS : a graphitic (graphene) carbon layer is formed on the surface of the fully conditioned sample (with a large amount of H).
Analysis of contaminants
Réunion R. Kersevan 16/11/2021

## Slide 9: Plan
Réunion R. Kersevan 16/11/2021
Contexte équipe MAVERICS-IJCLAB/IN2P3
Présentation plateforme Vide&Surfaces
Exemple : NEG
Collaboration CERN 2018-2020 : mesures VPS+désorption ionique
Simulation Vide dynamique DYVACS
Propositions

## Slide 10: NEG coating – preliminary results
Réunion R. Kersevan 16/11/2021
270 nm
25,4at% Zr
39,5at% Ti
35,1at% V
XPS
SEM
XRD

## Slide 11: Plan
Réunion R. Kersevan 16/11/2021
Contexte équipe MAVERICS-IJCLAB/IN2P3
Présentation plateforme Vide&Surfaces
Exemple : NEG
Collaboration CERN 2018-2020 : mesures VPS+désorption ionique
Simulation Vide dynamique DYVACS
Propositions

## Slide 12: Collab CERN – V. Baglin – Thèse S. Bilgen
Réunion R. Kersevan 16/11/2021
Vacuum Pilot Sector
Vacuum port
Vacuum port
Instruments
Liner
Vacuum
enveloppe

## Slide 13: Collab CERN – V. Baglin – Thèse S. Bilgen
Réunion R. Kersevan 16/11/2021
Set up : Ion stimulated desorption
base pressure: 5x10-10 mbar
Gases used: Ar, H2, CO
Continuous beam
Beam current: pA up to 300 nA
Beam energy: 200 eV to 5keV

## Slide 14: Plan
Réunion R. Kersevan 16/11/2021
Contexte équipe MAVERICS-IJCLAB/IN2P3
Présentation plateforme Vide&Surfaces
Exemple : NEG
Collaboration CERN 2018-2020 : mesures VPS+désorption ionique
Simulation Vide dynamique DYVACS
Propositions

## Slide 15: DYVACS - Gas density profiles in presence of e-cloud
15
Analytical model of the dynamic pressure – DYVACS – DYnamic VACuum Simulation code
ions
e-
e-
p+
p+
p+
Photo e-
e- accelerated
multipacting
e _
Electron cloud
Secondary e-
Synchrotron
Radiation
DYVACS is based on the gas balance differential equation (VASCO)
It is used to compute the gas density nj
for j= H2, CH4, CO, CO2
Evolution of the e-cloud is explicitly taken into account
Boundary conditions: continuity of flux and pressure between each segment
For the LHC
Réunion R. Kersevan 16/11/2021

## Slide 16: DYVACS - Gas density profiles
16
ions
e-
p+
p+
p+
e- accelerated
e _
Secondary e-
Synchrotron
Radiation
for i= H2, CH4, CO, CO2
Electron cloud
Analytical model of the dynamic pressure – DYVACS – Dynamic VACuum Simulation code
Inputs: Cj,,, , ,, , , Sj , σp→i, σe→i , Ibeam , , ,
by the p beam
by the EC
Residual gas ionization
Réunion R. Kersevan 16/11/2021

## Slide 17: DYVACS - Gas density profiles
17
ions
e-
e-
p+
p+
p+
e- accelerated
e _
Secondary e-
Synchrotron
Radiation
Electron cloud
Analytical model of the dynamic pressure – DYVACS – Dynamic VACuum Simulation code
Inputs: Cj,,, , ,, , , Sj , σp→i, σe→i , Ibeam , , , a, b, c, size of the segment, radius BP, Ebeam, time of one turn, etc.
* density computed with « the map model »
T. Demma et al. Model
depends on : - SEY (surface properties) ,
- beam parameters (nppb, bunch length, beam size, etc.) and
- on vacuum chamber dimensions, etc.
Réunion R. Kersevan 16/11/2021

## Slide 18: DYVACS - Gas density profiles in presence of e-cloud
18
ions
e-
e-
p+
p+
p+
e- accelerated
e _
Secondary e-
Synchrotron
Radiation
Inputs: Cj,,, , ,, , , Sj , σp→i, σe→i , Ibeam , , , a, b, c, size of the segment, radius BP, Ebeam, time of one turn, etc.
Electron cloud
Many inputs are necessary → measurements in laboratory are needed!
It is possible to play with all phenomena independently!
Analytical model of the dynamic pressure – DYVACS – DYnamic VACuum Simulation code
Réunion R. Kersevan 16/11/2021

## Slide 19: DYVACS - Gas density profiles
Comparison between in situ measurements in the LHC and the DYVACS simulation
In situ pressure measurement (VPS Station N°4)
In situ beam intensity and energy evolution
Réunion R. Kersevan 16/11/2021

## Slide 20: DYVACS - Gas density profiles
Experimental pressure (pink line)
computed pressure using DYVACS with EC (blue line)
and without EC (green line)
A good agreement was observed in a short computation time, between the in situ pressure measurements and DYVACS simulation
Comparison between in situ measurements in the LHC and the DYVACS simulation
For a=1,4 (SEY=1,6); b=[0; -5] variation of the b factor by DYVACS; c=0
Réunion R. Kersevan 16/11/2021

## Slide 21: DYVACS - Gas density profiles
Pressure time evolution measurements vs DYVACS simulations
All calculations reproduce with a good agreement the in situ pressure evolution measured in station 4 (unbaked copper) of VPS in the LHC.
inputs:
Same ESD,PSD and ISD used.
a fixed for a constant SEY
b is computed as a function of nppb.
Réunion R. Kersevan 16/11/2021

## Slide 22: DYVACS - Gas density profiles
DYVACS reproduces the evolution of the partial pressures for H2, CO2, CO and CH4 during beam operation
H2 has the highest partial pressure
Distribution of partial pressures for H2, CO2, CO and CH4 along the Cu station 4
Distribution of partial pressures along the pipe
Vacuum port
Vacuum port
Instruments
Liner
Vacuum
enveloppe
V. BAGLIN, meeting, CERN, 5th Dec. 2017
Réunion R. Kersevan 16/11/2021

## Slide 23: DYVACS - Gas density profiles
DYVACS reproduces the evolution of the partial pressures for H2, CO2, CO and CH4 during beam operation
Distribution of partial pressures for H2, CO2, CO and CH4 along the Cu station 4
Réunion R. Kersevan 16/11/2021

## Slide 24: Propositions
Réunion R. Kersevan 16/11/2021
Four main axes:
measurement of the Secondary Emission Yield (SEY) a fundamental parameter for multipacting + influence of the surface chemistry+ conditioning
    Characterization of materials in the Vide&Surfaces platform + ANDROMEDE
    Thin films of NEG (influence of thickness)
(ii) the Ion Stimulated Desorption (ISD) focused in FCCee (ion cloud for e- beam)
    qualification/validation of the set up : ISD measurements on copper / C-coating
    Set up improvement : implementation of a protocol to perform measurements on activated NEG (activation in situ in the set up)
(iii) New measurements in the VPS during the next LHC RUN : NEG behaviour in the VPS (study of the e-cloud for the FCC e+ ring)
(iv) the dynamic pressure simulation code development (DYVACS)+comparison with measurements
    Consolidate the DYVACS model by comparing it with new measurements in the VPS during the next RUN