## Slide 1
Elise Guerinoni, Sandrine Dourdain, Zijun Lu, Stéphane Pellet-Rostaing
23-25/05/2022
LTSM – Laboratoire Tri ionique par les Systèmes Moléculaires auto-assemblés
FORMICA 3D
FORmulation et MécanIsmes d’un système d’extraCtion de l’uranium par des Amines tertiaires pour minimiser les verrous de 3ème phase et de Dégradation des extractants
NEEDS Ressources

## Slide 2: Uranium production & AMEX process
https://assets.rte-france.com/prod/public/2020-06/bilan-electrique-2019_1_0.pdf
IAEA, “Uranium 2018: Resources, Production and Demand.”
Ore extraction
Mined ore
COMMINUTION
PRE-CONCENTRATION
LEACHING
Oxidant
Lixiviant
SOLVENT EXTRACTION
ION-EXCHANGE RESIN
YELLOW CAKE PRECIPITATION AND DRYING
SOLID/LIQUID SEPARATION
Wash water
TAILS TO WASTE

## Slide 3: AMEX process and solvent extraction
C. Boirie, “Extraction of uranyl sulfate with amines,” Bull. soc. chim. France, vol. No. 8-9, 1958
A. Chagnes et.al., Solvent Extraction and Ion Exchange, vol. 30, no. 1, pp. 67–76, 2012
Common Name | Composition |  | Nature of the amine
Alamine 336 | Di-n-octyl monodecylamine | 44 % | R1, R2 R3
 | Tri-n-octyl-amine | 28 % | R1, R2, R3
 | Mono-octyl di-decyl-amine | 23 % | R1 R2, R3
 | Tri-n-decyl-amine | 3 % | R1, R2, R3
Alamine 308 | Tri-isooctyl-amine | 100 % | R1, R2, R3
Alamine 304 | Tri-n-dodecyl-amine | 95-100 % | R1, R2, R3
Extractant : tertiary amine
Diluent : linear alcane
Phase modifier : 1-octanol
Leaching containing :
Uranium sulfate
Impurities : Fe, Zr, Mo, V
Sulfurique acid
Ammonium sulfate
Problem:
Non selective extraction
3rd phase formation
Amines degradation due to combined presence of octanol and vanadium
Notes: Purifier l’urnanium et on fait de l’extraction liquide liquide
Et amex description
Premier etape est la protonation et comparable aun ammonium quaternaire

## Slide 4
1 Sato, T., Watanabe, H., & Suzuki, H. (1986). Liquid-liquid extraction of molybdenum(VI) from aqueous acid solutions by high-molecular weight amines Solvent Extraction and Ion Exchange, 4(5), 987‑998.
2 Chagnes, A., & Cote, G. (2018). Chemical Degradation of a Mixture of tri-n-Octylamine and 1-Tridecanol in the Presence of Chromium(VI) in Acidic Sulfate Media. Metals, 8(1), 57.
Polar head
Apolar chain
Extractant = Amphiphilic molecule
Aggregate
FORMICA 3D
FORmulation et MécanIsmes d’extraCtion de l’uranium par des Amines tertiaires pour minimiser les verrous de 3ème phase et de Dégradation des extractants
Polar core
Apolar shell
Extractant : tertiary amine
Diluent : linear alcane
Phase modifier : 1-octanol
Notes: A l’echelle moléculaire on considère que c’est que la complexation qui joue selon le mécanisme d’extration echnage anionique

## Slide 5
Formulating new systems to optimize the AMEX process and to avoid 3rd phase problems:
    Effect of extractant alkyl chains
    Effect of diluent alkyl chains
Objectives
5
Aggregate
Polar core
Apolar shell

## Slide 6: Effect of extractant alkyl chains length
C6 THA
C7 THA
C8 TOA
C9 TNA
C10 TDA
Increasing
On phase stability?
On extraction?
On extraction mechanisms?

## Slide 7: Effect of extractant alkyl chains length
C6 THA
C7 THA
C8 TOA
C9 TNA
C10 TDA
Increasing
[amine] = 0.2 M
[1-octanol] = 0.316 M
dodecane
[U] = 10.5 M
[H2SO4] = 0,1 M
[(NH4)2SO4] = 1 M
On extraction?
On phase stability?

## Slide 8
Effect of extractant alkyl chains length
C6 THA
C7 THA
C8 TOA
C9 TNA
C10 TDA
Increasing
No effect of alkyl chain on chelation mechanisms
On extraction mechanisms? Chelation
On extraction mechanisms? Aggregation
EXAFS
SANS
Presence of aggregates – differents shape, size & interactions

## Slide 9
SANS fitting Core shell model + Sticky hard Sphere
Supramolecular scale
Effect of extractant alkyl chain on aggregation
C6
C7
C8
C9
C10
N° C | 6 | 7 | 8 | 9 | 10
(Å) | 6.1 | 5.9 | 5.8 | 5.6 | 5.5
 | 4.3 | 4.2 | 4.0 | 3.7 | 3.4
(Å) | 2.8 | 3.2 | 3.4 | 3.6 | 3.7
τ-1 (kBT) | 10.0 | 9.1 | 8.3 | 7.3 | 5.0
N° C | 6 | 7 | 8 | 9 | 10
 | 6.1 | 5.9 | 5.8 | 5.6 | 5.5
 | 4.3 | 4.2 | 4.0 | 3.7 | 3.4
 | 2.8 | 3.2 | 3.4 | 3.6 | 3.7
τ-1 (kBT) | 10.0 | 9.1 | 8.3 | 7.3 | 5.0
Aggregates with smaller polar core;
Aggregates with thicker apolar shell;
Attractive interactions between aggregates less important less 3rd phase.
With increasing
Notes: 2 échelle rond vert et rond gris
Modifier configuration chaines alkylesmais même tete polaire pour montrer que agrégation est importante et pas seulment complexation
Pourquoi la tete polair ec’est l’amine et les premiers carbones et pas autre chose ?

## Slide 10: Aggregation and 3rd phase formation mechanism
Supramolecular scale
All data was rationalized with the thermodynamic ienaic approach
Less 3rd phase
More 3rd phase
Z. Lu, S. Dourdain, B. Demé, J.F. Dufrêche, T. Zemb, S. Pellet-Rostaing, Journal of Molecular Liquids, 349, 118409, 2022
Z. Lu, S. Dourdain, B. Demé, J.F. Dufrêche, T. Zemb, S. Pellet-Rostaing, Journal of Molecular Liquids, Journal of Molecular Liquids, 349, 118487, 2022
Notes: 2 échelle rond vert et rond gris
Modifier configuration chaines alkylesmais même tete polaire pour montrer que agrégation est importante et pas seulment complexation
Pourquoi la tete polair ec’est l’amine et les premiers carbones et pas autre chose ?

## Slide 11: Thermodynamic balance of the extraction – Ienaic
To avoid 3rd phase, optimal system: long or branched chains !
Less 3rd phase
More 3rd phase
Notes: Bulk : mettre en paquet les cations stoechimoetrique de chacun des composé hydrophiles
Micellisation ; mettre en paquet les agregats
Rayon cœur de cœur et de couronne necessaire pour calculer l’energie de courbure
Energie de courbure la plus impacté
Packing de la molécule equation à mettre dans diapo
V is the volume of the hydrophobic part of the extractant, lc the alkyl chains length (which
is usually 80 % of the extended chains length) and a the area per head group.

## Slide 12
Formulating new systems to optimize the AMEX process and to avoid 3rd phase problems:
    Effect of extractant alkyl chains
    Effect of diluent alkyl chains
Objectives
12
Aggregate
Polar core
Apolar shell

## Slide 13: Effect of diluent chain length
C5 C6 C7 C8 C10 C12 C14 C16
Effect of diluent chain length
Increasing
[amine] = var
[1-octanol] = var
alkane
[U] = 10.5 M
[H2SO4] = 0,1 M
[(NH4)2SO4] = 1 M
On extraction?
On phase stability?

## Slide 14
Effect of diluent chain length
On aggregation:
C5 C6 C7 C8 C10 C12 C14 C16
Effect of diluent chain length
Increasing
SAXS
Aggregates with smaller polar core;
But with more 3rd phase ?
 origin of interaction ?
With increasing
Notes: Modele de baxter
Mecanimse de foramtion de troisème phase

## Slide 15: Origin of the third phase ?
Extractant
Diluent
Less 3rd phase
With bigger core??
Less 3rd phase
with smaller core
New mechanism for third phase formation ?
Hypothesis: depletion forces generated by diluent around agregates to be studied with neutron scattering
More 3rd phase
with bigger core
More 3rd phase
with smaller core

## Slide 16: Perspectives
Motokawa, R., Kobayashi, T., Endo, H., Mu, J., Williams, C. D., Masters, A. J., Antonio, M. R., Heller, W. T., & Nagao, M. (2019). ACS Central Science, 5(1), 85‑96.
Understanding diluent effect and origin of the third phase formation:
- Full characterization of the third phase
- SANS of the extraction to test new structure factors
taking into account depletion effects
Proposal submission for SANS measurement on JRR-3 in Japan in 2022 with Ruihey MOTOKAWA
2FDN funding
NEEDS project : FORMICA
JSPS fellowship application
NEEDS
Framework of Elise Guerinoni Thesis: ILL

## Slide 17: Selectivity
Chart: Selectivité diluent + select new
| SU/Zr | SU/Mo | SU/V | SU/Fe
C5 | 5.1611 | 1.2046 | 968.0476 | 600.9415
C6 | 0.9065 | 0.95979 | 2152.7085 | 997.8402
C7 | 0.39916 | 0.96918 | 1436.4111 | 841.0909
C8 | 0.25358 | 0.89335 | 1015.0763 | 672.8428
C10 | 0.13161 | 0.87548 | 2353.4879 | 1045.0736
C12 | 0.08249 | 0.87055 | 3678.8073 | 1291.4196
C14 | 0.04906 | 0.87546 | 2726.7905 | 1297.2661
C16 | 0.09741 | 0.99753 | 7637.923 | 1961.3383

## Slide 18: Effect of diluent chain length
Berthon, L., Martinet, L., Testard, F., Madic, C., & Zemb, Th. (2007). Solvent Penetration and Sterical Stabilization of Reverse Aggregates based on the DIAMEX Process Extracting Molecules : Consequences for the Third Phase Formation. Solvent Extraction and Ion Exchange, 25(5), 545‑576
[TOA] = 0.1 M
[1-octanol] = 0.063 M
Linear alcane
[U] = 10.5 M
[H2SO4] = 0.1 M
[(NH4)2SO4] = 1 M
Quand on s’approche de la troisème phase

## Slide 19: Quand on s’approche de la troisème phase
OCTANE
HEXANE
DECANE
DODECANE
HEXADECANE

## Slide 20: Caractérisation de la troisième phase
2M TOA 1pc oct light et heavy

## Slide 21: Résultats var TOA dans la light phase et dosage de la light phase
[TOA] = 1.8 M SAXS light phase Obs : remontée plus important quand y a octanol -> normalement octanol devrait empecher la remontée ?? Ou alors il permet que y ai des agregats quand meme mais qu’ils ne collapsent pas remontée pour tous les diluants même dans la phase legère
La TOA phase orga dans dodecane remonte droit, qu’est ce qu’on a dans la phase légère ?
[TOA] = 1.8 M SAXS 3rd phase Obs : remontée plus important quand y a octanol remontée pour tous les diluants même dans la phase legère
La TOA phase orga dans dodecane remonte droit, qu’est ce qu’on a dans la phase légère ?
TOA (mol/L) | 1.8 | 1.8 | 1.8 | 1.8
Diluent | hexane | dodecane | dodecane | hexadecane
% oct | 1 | 1 | 0 | 1
eau (mol/kg) | 3.40547778 | 4.00086296 | 5.38393333 | 3.97770556
% erreur | 0.02423805 | 0.09293236 | 0.09868908 | 0.02700362
TOA (mol/L) | 1.8 | 1.8 | 1.8 | 1.8
Diluent | hexane | dodecane | dodecane | hexadecane
% oct | 1 | 1 | 0 | 1
eau (mol/kg) | 0.41037222 | 0.25533333 | 0.04251111 | 0.22816944
% erreur | 0.01092235 | 0.0009271 | 0.00062854 | 0.00269093

## Slide 22
On double et triple la quantité d’extractant au dessus de la frontière 3rd phase
Dosage de l’eau 3rd phase
TOA (mol/L) | 0.6 | 1.2 | 1.8
% oct | 1 | 1 | 1
Diluent | hexadecane | hexadecane | hexadecane
eau (mol/kg) | 0.267475 | 0.23434722 | 0.22816944
% erreur | 0.00144171 | 0.00429371 | 0.00269093
TOA (mol/L) | 0.6 | 1.2 | 1.8
% oct | 1 | 1 | 1
Diluent | hexadecane | hexadecane | hexadecane
eau (mol/kg) | 3.68309167 | 4.00755 | 3.97770556
% erreur | 0.03084164 | 0.09409991 | 0.02700362

## Slide 23: Comparaison liquid ionique et 3ème phase

## Slide 24: Effect of diluent chain length
New mechanism of third phase formation controlled by:
        depletion forces
        diluent penetration
Notes: Modele de baxter
Mecanimse de foramtion de troisème phase

## Slide 25: Perspectives
Motokawa, R., Kobayashi, T., Endo, H., Mu, J., Williams, C. D., Masters, A. J., Antonio, M. R., Heller, W. T., & Nagao, M. (2019). A Telescoping View of Solute Architectures in a Complex Fluid System. ACS Central Science, 5(1), 85‑96.
Proposal submission for SANS measurement on JRR-3 in Japan in 2022 with Ruihey MOTOKAWA
2FDN funding
NEEDS project : FORMICA
JSPS fellowship application
Thank you for your attention
Notes: Cœur tout est petit donc dificile de fitter le saxs et du coup le modèle est pas toujours verifier car l’eau n’est peut etre pas en rond sére
Le sans fit otu l’agrégat et le contraste est plus fort
On peut s’amuser à deuterer une parrtie pour voir ou est l(‘octnaol par exemple

## Slide 26
Formulating new systems to optimize the AMEX process and to avoid 3rd phase problems:
    Effect of amines and diluent alkyl chains
    Applying quaternary ammonium ionic liquids
Objectives

## Slide 27: Ionic liquids
Trioctylammoniums ()
Ammonium-based Ionic Liquids
Methyltrioctylammoniums ()
Step 1: trialkylamine protonation
Step 2: uranyl extraction by anionic exchange
Replace organic phase
No dilution, no 3rd phase
Dodecane
1-octanol
DU = 0
DU = 100
viscous
[TOAH][NTf2]
[TOAH]2[SO4]
Notes: An ionic liquid (IL) is a salt in the liquid state. In some contexts, the term has been restricted to salts whose melting point is below some arbitrary temperature, such as 100 °C (212 °F). While ordinary liquids such as water and gasoline are predominantly made of electrically neutral molecules, ionic liquids are largely made of ions.

## Slide 28: Synergistic mixture of anions
Citer brevet
Mixtures with same anions and different cations
Mixtures with same cations and different anions
Organic phase
Mixtures of two ammoniums
Aqueous phase
0.1 M and 0.1 M + 250 ppm U(VI) and 250 ppm Fe(III)
A/O = 2
Objectives:
Comparisson of conventionnal and ionic liquid media for:
      Extraction capacity
      Extraction mechanism
      Explain the anionic synergy, not investigated in literature
Notes: The first chemical equilibrium is controlled by the solubility of IL cationic part in the aqueous
phase, which is highly dependent on the chemical structure of the cation and may vary
tremendously with the ILs nature. Given the fact that ILs are very hygroscopic, large amount
of water are dissolved in IL phase along with acids[5, 38, 39] and neutral salts,[40, 41, 42] after
equilibrium with aqueous phases.
Decrire le process de recherche
Ccl : synergie anionique sulfate ntf2 à comprendre

## Slide 29: Uranyl complexe caracterization
T. Sukhbaatar et. al., Chemical Communications, vol. 55, no. 53, pp. 7583–7586, 2019
3 in inner sphere of
H-bonds created bewteen and 3
Origin of synergy
Role of in complexation?
Role of ?
Role of ? ()
TOA + dodecane
What we know:
What we don’t know:
MD work in literature
Notes: A qui ont peut se raccrocher et comparer
Système de référence
Quest ce qu’on sait sur la TOA mais on doti le valider sur le liquide ionique
Comment l’uranium est complxé

## Slide 30: Uranyl complex in ILs mixture Role of SO42-
TOA in dodecane
*K. Servaes et. al., European Journal of Inorganic Chemistry, no. 32, pp. 5120–5126, 2007
Organic phase
[]/[] = 0.5, 0.75 and 1
or
0.1 M TOA in dodecane + 5% oct. loaded with 2500 ppm U(VI)
Similar trigonal symmetry*
3 in inner coordination sphere of uranyl in ILs system
= 0.5
= 0.75
= 1
UV-vis

## Slide 31: Uranyl complex in ILs mixture
EXAFS
U-Oyl
U-SSO4
U-OSO4
In first coordination sphere:
  3
  N and no
Run EXAFS
Synchrotron Soleil
Mars beamtime
2 days - April 2021
Synergy origin?
Notes: Pas de chgt avec synergie
((Même mode de complexation de l’U dans TOA et dodécane, contrairement au TBP + milieu nitrique ))
Ca se passe comme dans milieu conventionnel
Auncune différence entre les ratio ce qui veut dire pas de complxation synergique
Ntf2 ne rentre pas dans la premiere sphère de coordination?

## Slide 32: Role of water on synergistic extraction?
>
>
>
>
Different VA/VO ratio
Different concentration[(NH4)2SO4]
Reference:TOA + dodecane [H2O]org = 0.2 mol/L
32
Notes: Sulfates viennt complxer mieux l’eau que l’u et on perd de l’u
Interraction privilégiée
Mais quand y a trop d’eau extraite les sulfates viennent complexer l’eau et plus l’uranium et donc on perd de l’U
Viscosité augmente
Role de l’eau

## Slide 33: Conclusions / perspectives
No dilution, no third phase
Synergistic extraction of U
NTf2 not involved
Role of water?
Indentification of link with UO2 and link with H2O in FT-IR (DFT calculations)
Thank you for your attention