## Slide 1
Projet ARPENTONS
Comportement mécanique de l'argilite à travers les échelles :
effet de la température et de la non-saturation
Pierre Bésuelle , Edward Ando, Nicolas Zalamea, Stefano Dal Pont, Alice Di Donna, Jacques Desrues
Université Grenoble Alpes & CNRS
Laboratoire 3SR
Philippe Cosenza, Stephen Hédan, Dimitri Prêt
Université de Poitiers & CNRS
IC2MP
Laurent Brochard, Matthieu Vandamme
ENPC & CNRS & IFSTTAR
Institut Navier

## Slide 2
MOTIVATIONS
Roche argileuse, le dialogue entre les échelles et les couplages
Couplages multiphysiques :
Mécanique (déformation, endommagement)
Hydro (pression interstitielle, perméabilité, gonflement)
Température (endommagement, déformation, surpressurisation)
Hygro/Partiellement saturé (déformation, gonflement)
De quelles échelles parlent-on ?
Échelle macro
(ingénieur)
Échelle méso (inclusion)
Échelle micro (agrégat d’argile)
Échelle nano (moléculaire)

## Slide 3
Échelle macro
(ingénieur)
Échelle méso (inclusion)
Échelle micro (agrégat d’argile)
Échelle nano (moléculaire)
MOTIVATIONS
Roche argileuse, le dialogue entre les échelles et les couplages
Quelles approches ?
caractérisation
modélisation
Caractérisation de la déformation sous sollicitations T et HR
mesures de champs surfaciques en 3D
échantillons centimétriques
Caractérisation de la déformation sous sollicitations T
mesures de champs volumique (nano CT et DVC)
échantillons millimétriques
Modélisation double échelle (température)
Homogénéisation numérique (FEM2) (extérieur à NEEDS / EURAD HiTec)
Poromécanique
Modélisation moléculaire
(température et saturation partielle)
Modélisation du statut de l’eau confinée
  Mécanique moléculaire (nano)
  Mécanique granulaire (micro)
(Poitiers)
(Grenoble)
(Grenoble et Poitiers)
(Navier)

## Slide 4: 1. Nanoscale
Thin mineral layer (≈1 nm) with adsorbed/bound water
  Experimental measurement of deformation by XRD
  Theoretical prediction by molecular simulation
Sodium Wyoming montmorillonite
Na+
Al-> Mg
Si -> Al
Interlayer
(H2O + cations)
TOT mineral with substitutions
Navier

## Slide 5: Crystalline swelling
‘Crystalline’ because swelling stepwise with RH
Each plateau = discrete nb of H2O layers
0W = 0 layers, 1W = 2 layers etc…
XRD measurements – Na montmorillonite

## Slide 6: Molecular simulation of clay hydration
Historical perspective
  First all-atom simulations: Skipper et al. (1991), Delville (1991)
  Fixed water content: Boek et al. (1995), Smith (1998)
    xW layering
    Stepwise spacing
  Grand Canonical simulation to relate to RH: Karaboni et al. (1996)
    Usual GCMC too inefficient: need for improved algo
    Early works limited to 1 RH
﻿Skipper et al. (1991). JCP, 94(11), 7434
﻿Karaborni et al. (1996) Science, 271(5252), 1102
GC pressure isotherm
GC water content isotherm

## Slide 7: Molecular simulation of clay hydration
Historical perspective
  First swelling prediction: Hensen and Smit (2002)
    mPT ensemble : issue of large hysteresis
  Stable hydration transition: Shroll and Smith (1999), Tambach et al. (2004)
    mVT + thermodynamic analysis
﻿Hensen and Smit (2002) JPC B, 106(49), 12664
﻿Tambach et al. (2004). JPC B, 108(23), 7586

## Slide 8: Approach in this work
    mVT + thermo analysis
  Wide range of spacing and RH to provide complete hydration diagram (stability and metastability)
  Constitutive description of each hydration state
  Full stable swelling curve & confrontation with XRD
Molecular model:
  Wyoming Montmorillonite
  M0.75(Si7.75Al0.25)(Al3.5Mg0.5)O20(OH)4 + n H2O
Atomic potential:
  ClayFF + water SPCE
Algorithm:
  Configurational Bias Monte Carlo (inspired by Hensen et al., 2001)

## Slide 9: Pressure/density isotherms
Domains of decreasing pressure = xW states
Bulk liquid pressure/density recovered above cavitation (RH > 30%) for e > 19Å

## Slide 10: Thermodynamic stability analysis
Integration of the pressure isotherm provides the grand potential
A system under pressure control minimizes the swelling free energy
Stability analysis
  Unstable = non convex
  Stable states = convex envelop
  Metastable states = convex but not part of convex envelop
Unjacketed: Pext = Pvapor

## Slide 11: Free swelling : prediction vs. XRD

## Slide 12: Full hydration diagram
Plain lines = stable hydration transition
Dashed lines = metastable limit of the xW states

## Slide 13: On-going and perspectives
Other cations (K+, Ca2+), mixtures
Other temperatures (300K to 400K)
Open database

## Slide 14: 2. From nano to micro
Molecular mechanics
Granular mechanics
Continuum mechanics
Navier

## Slide 15: Sub-micron scale poorly known
Carrier (2013) PhD University Paris Est
< 0.1-1 µm almost inaccessible to direct imaging
>1-10 nm inaccessible to mol sim
In-between :
  Microstructure/behavior can only be inferred (small angle, adsorption, porosimetry, indentation)
  Only coarse-grained modeling possible

## Slide 16: Granular models of clays
Two types of contact law
  ‘diffuse double layer’ (continuum theory valid for large distances → clay suspension)
  ‘mean force potential’ from molecular simulation (valid for short distances → clay matrix)
Hydration transitions and layer flexibility not addressed
Source: Ebrahimi et al. (2014). The Journal of Chemical Physics, 140(15), 154309.

## Slide 17: Proposed bottom-up granular model (2D)
Clay layer = chain of particles
  Intra-layer harmonic interaction (bonds and angles)
  Calibration on bending and extension elasticity
  Inter-layer interaction : W potential
  Calibration on disjoining pressure and shear strength (1W and 2W states only)
Inter-layer potential
Calibration on 1W – 2W domain

## Slide 18: Microstructure generation
Simple procedure to control the degree of local order
  Start from suspension
  Brownian dynamics with constant compaction rate
  T small enough to avoid 2W-1W transition

## Slide 19: Mechanical behavior
Quasi-static isotropic compression
  Typical e-log(P) behavior
  At P < 1MPa, bending negligible and 2W hydration only
  At P ≈ 10 Mpa, 20% of 1W, elastic modulus controlled by bending (15% of energy)
CIGEO

## Slide 20: 2W-1W hydration transition

## Slide 21: De-hydration / re-hydration
2W-1W transition simply modeled by modulating one parameter (F0 ≈ Pcapillary)

## Slide 22: Critical role of consolidation state
Normally consolidated: current confining pressure is the maximum of the loading history
Over-consolidated: current confining pressure is not the maximum of the loading history
Irreversible compaction : NC >> OC
Consistent with drained heating exp

## Slide 23: Perspectives
Detailed characterization
  deviatoric behavior
  rheology / creep / fracture
  local fields / pore size distr.
  adsorption
Refined model
  combine mean force and double layer
  quantitative RH/T evolution
  3D

## Slide 24
3. Mesoscale deformation
Échelle macro
(ingénieur)
Échelle méso (inclusion)
Échelle micro (agrégat d’argile)
Échelle nano (moléculaire)
Caractérisations des mécanismes de déformation à l’échelle méso
Modèle de comportement double échelle méso ---> macro
3SR

## Slide 25
MESOSCALE DEFORMATION
Mechanisms of deformation
J.-C. Robinet, 2008
Evaluation des modes de déformations à l’échelle méso
BIB-SEM post-mortem
Nano-tomographie RX in operando
BIB-SEM
G. Desbois et al., 2017
10µm

## Slide 26
in situ test + η-X-ray CT + DIC
100µm
MESOSCALE DEFORMATION
Mechanisms of deformation
1 mm
Evaluation des modes de déformations à l’échelle méso
BIB-SEM post-mortem
Nano-tomographie RX in operando

## Slide 27
MESOSCALE DEFORMATION
Mechanisms of deformation
Evolution of a vertical slice during loading
3D+T microscale images

## Slide 28
MESOSCALE DEFORMATION
Mechanisms of deformation
Zoom in horizontal slice
Zoom in vertical slice
In a same specimen, several mechanisms
Decohesion of inclusions
Crushing of clay matrix
Some hard inclusion breakings
Faulting

## Slide 29
MESOSCALE DEFORMATION
Strain measurement
Combined DIC analysis
Mineralogies decomposition (quartz, carbonate, pyrite, other)
Discrete-DIC for inclusions
Continuous DIC for ‘other’
Merging

## Slide 30
MESOSCALE DEFORMATION
Mechanisms of deformation
Perspectives: different kind of loadings
Effect of mean stress level ongoing
Effect of RH evolution (driying, wetting) ongoing
Effect of thermal loading expected (ESRF proposal)

## Slide 31
Representative elementary volume (REV)
inclusion
clay matrix
interface inclusion/clay
potential cracks in clay
MODEL DOUBLE SCALE BETWEEN MESO & MACRO
Microstructure of the clay-rock

## Slide 32
Double scale FEM2 model
  Macro field equations
  Macro-to-micro
  Microscale model
  micro-to-Macro
4. Meso to Macro model
3SR

## Slide 33
MACRO to MICRO transition
Micro REV: boundary value problem (Macro --> micro)
Periodic boundary conditions:
w f + + w f - = 0 (flux)
Frey et al., 2012
Van den Eijnden, 2015

## Slide 34
MICROSCALE PROBLEM
Micro REV: mechanical model (constitutive laws)
Mechanics
Grains: linear elastic solid phases
Cohesive interfaces: damage laws
Normal
Tangential
Fluid flow
Cohesive interfaces (coupling M  H)
  Interface opening defines channel hydraulic conductivity (
Flow assumptions
  Laminar flow between smooth parallel platens
  Network of 1D channels between grains
  System of equations for flow in an element
Fluid forces (coupling H  M)
  Fluid pressure acting normally on solids boundaries

## Slide 35
Example of realistic microstructures
Numerical EV, 250 grains 18% quartz, 30% calcite, 2% pyrite, 50% clay
Grains elongation
(circumscribed ellipse)
Grains orientation
(circumscribed ellipse)
MODEL DOUBLE SCALE BETWEEN MESO & MACRO
Microstructure of the clay-rock
1%
ε22
2%
2.75%
3%
3.2%
1%
4.6%
2.4%
Shear strain
Shear strain
rate
Mimic of microstructure: density, elongation, orientation, etc…
Model calibration
Macroscale simulations

## Slide 36
Meso porosity
MODEL DOUBLE SCALE BETWEEN MESO & MACRO
THM coupling
Introduction of THM couplings
Thermal-deformation (solid, fluid)
Energy transport (conduction, convection, advection)
Menaceur et al, 2016
Improvement of porosity description (ongoing/EURAD)
Interface porosity
Meso porosity (new)
Nano porosity inside clay matrix (new)
Improvement of thermal effect in clay (perpective)
Braun et al, 2019

## Slide 37
Sample 5x5x5 cm3 submitted to thermal load (25°C to 90°C) and a constant relative humidity (RH=62%)
  Free surface in deformation
  Measurement of one face by Digital image Correlation of the cubic sample (called ‘DIC’ sample)
  Measurement of the mass of the second cubic sample (called ‘mass’ sample)
5. Macro Deformation (centimetric)
IC2MP

## Slide 38: 3. Centimetric scale
Sample 5x5x5 cm3 submitted to thermal load (25°C to 90°C) and a constant relative humidity (RH=62%)
  Free surface in deformation
  Measurement of one face by Digital image Correlation of the cubic sample (called ‘DIC’ sample)
  Measurement of the mass of the second cubic sample (called ‘mass’ sample)
Climatic chamber
Displacement fields

## Slide 39: Experimental setup
Climatic chamber
Time [days]
T [°C], RH [%]
period 1 (0.21 days)
period 2 (8.7 days)
RH, T -> each 30 seconds
‘Mass’ sample
Dm[g]
Water content (w)
Time [days]
w [%]

## Slide 40: DIC measurements
Images
H-DIC algorithm
displacement fields (u,v)
strain fields (exx,eyy,exy)
bulk strains (eS ROI)
surface strains (es)
jump fields (u’,v’)
crack kinematic fields (o,s)
crack area (CA)
direct crack porosity (fcrack-d)
enrichissment
Classical approach
5 cm
each 15 minutes

## Slide 41: DIC results
0
0.2
-0.28
0
0.067
0.14
-0.045
0.06
Horizontal displacement [mm]
Vertical displacement [mm]
Opening crack [mm]
shear crack [mm]
surface 1
surface 2
43.37 mm
Bedding plane
strain fields (exx,eyy,exy)
bulk strains (eS ROI)
surface strains (es)
One marker at each corner
finite differences
(grains, clay, interstitial water )
direct crack porosity (fcrack-d)
with
Distribution of local aperture and sliding
New surface generate by the aperture of the desiccation crack

## Slide 42: Results
1
1
fcrack-d [%]
eS ROI - es [%]
Time [days]
Time [days]
[%]
[%]
Bulk strain eS ROI
Crack porosity fcrack-d
Block strain es
T [°C]
RH [%]

## Slide 43: Observations/comments
w [%]
[%]
Bulk strain eS ROI
Crack porosity fcrack-d
surface strain es
es corresponding to the final thermal dilatation of grains, clay, water is close to 1 E-4
When w is lower than 2%, fcrack-d is dominant in the bulk strain eS ROI
When w is lower than 1%, the dilatation of solid phase (grains, clay, water) is constant es (≈1 E-4) and the dilatation of the sample (eS ROI ) is only due to the crack aperture fcrack-d
Close to w = 2,5% corresponding the change of temperature (25°C to 90°C in one hour) the bulk strain is only due to the dilatation of grains, clay, water
After we observe a diminution of es value to the suction
T

## Slide 44: Perspectives
At the centimetric scale
    Confirm these experimental results by a second test (25->90°C)
    Other thermal load (25->60->90°C)
    Numerical model (FEM (CodeAster©)
NOW
NOW
NOW
Pre-existing crack

## Slide 45: Perspectives
At the microscopic scale
  Developement of a new procedure to measure the deformation at the interfaces grain/grain or grain/clay matrix
NOW
MEBE, Wang et al. 2013
No results on grains and interface
Speckle by FIB patterning
PhD Mammadi Y. (2020)
Sample preparation (cutting, polishing)
FIB patterning
SEM images (secondary electrons)
Argillaceous rock
No results on grains and on interfaces
Not speckle on grains (Backseattered electrons)
PhD Fauchille AL (2015)
PhD Mammadi Y. (2020)

## Slide 46
CONCLUSIONS
Approches multiéchelles des couplages thermo-hygro/hydro-mécaniques
Echelle des feuillets d’argile (modèle moléculaire)
  Caractérisation complète de Na-, K- et Ca-Mnt en fonction de RH
  En bon accord avec le gonflement cristallin obtenu par DRX
Echelle des agrégats d’argile (modèle granulaire)
  Construction d’un modèle granulaire bottom-up valide pour les états denses
  Caractérisation comportement HM de l’échelle ‘matrice argileuse’
Echelle méso (modes de déformation)
  Essais in operando avec imagerie 3D+t haute résolution
  Mesure de la cinématique (DIC) par algorithme ad hoc
Passage méso-macro (modèle FEM2)
  Prise en compte d’une microstructure dans la modélisation macro
  Ajout des couplages THM + porosité réaliste à l’échelle méso
Echelle macro (mode de déformation)
  Quantification des processus de séchage et fissuration

## Slide 47
PERSPECTIVES
Approches multiéchelles des couplages thermo-hygro/hydro-mécaniques
Echelle des feuillets d’argile (modèle moléculaire)
  Caractérisation à d’autres températures (300K - 400K)
  Base de donnée publique
Echelle des agrégats d’argile (modèle granulaire)
  Poursuite caractérisation : fluage/rhéologie/fracture, porosité/microstructure
  Modèle raffiné : THM précis, DLVO, 3D
Echelle méso (modes de déformation)
  Extension aux effets de la température (endommagement thermique)
  Analyse comparative nano-tomographie et SEM (nano gravage)
Passage méso-macro (modèle FEM2)
  Prise en compte plus fine du comportement de la phase argileuse sous T
  Application à des calculs à grande échelle (benchmark)
Echelle macro (mode de déformation)
  Exploration des chemins de sollicitation RH et T