## Slide 1: Fast birefringence measurement and compensation using a pair of identical liquid crystals.
Shalika Singh, Marc Eisenmann, Matteo Leonardi

## Slide 2: KAGRA’s Test Mass
KAGRA cryogenic temperature
Thermal Noise when Temperature
KAGRA Sapphire
High Mechanical QF and thermal conductivity
But
  Birefringent sensitivity
23 kg
22 cm diameter
15 cm thickness

## Slide 3: Birefringence
  Polarization - oscillation of E
    k - Laser propagation
    S polarization - perpendicular
    P polarization - parallel
  Polarization Rotation
  Polarization Retardation
  Sapphire
Polarization Rotator
Polarization Retarder
Azimuth()
Ellipticity (Δn)
Sapphire
S
P
k
or
or
or
Same Phase
Phase delay

## Slide 4: Existing Measurement Methods in KAGRA
Polarimetry
Motorized HWP Variable polarization rotator
Rotation and Retardance At least two measurement
Credit: Correlation between Birefringence and absorption mapping in large size sapphire substrates for gravitational wave interferometry, Simon Zeidler et all 2023 (under review)
Pout = 0W
Pout ≠ 0W
Sample
Pin
Pout = Pin
Pout ≠ Pin
S pol
P pol
PBS
HWP

## Slide 5: Existing Measurement Methods in KAGRA
Soleil-Babinet Compensator (SBC)
Motorized HWP Variable polarization rotator
Translation SBC Variable polarization retarder
Direct Measurement
Credit: M Tokunari et al 2006 J. Phys.: Conf. Ser. 32 432
Sample
Pout = 0W
Pout ≠ 0W
P pol
HWP
Polarizer
Pin
Birefringent Crystal of varying thickness, R

## Slide 6: Disadvantages
  Mechanical control (step motor)
  4 Test Mass + spare (but more are tested)
Mass (kg) | Radius Increase | Birefringence measurement duration (polarimetry)
23 (present KAGRA) | 1 (Present 11 cm) | 1-2 weeks
40 | 1.2 | 1.4-2.8 weeks
200 | 2.1 | 4.4-8.8 weeks
Polarimetry | 6s per point
Compensation | 30s per point

## Slide 7: Liquid Crystal (LC)
Polarization retarder
Electronically controlled Fast (LCD have 60-360 Hz refresh rate)
Cheap
Requires low voltage (VMAX = 25 V)
0<VRMS<VMAX
Incident Laser
Glass Substrate
Transparent conductive layer
LC Alignment layer
LC cell spacer
LC Molecules
Polarization changed

## Slide 8: LC and Controlled Retardance
Polarization retarder Apply voltage
Polarization rotator rotate LC axis
Azimuth()
45 °
LC1
LC2
Rotation [rad]
LC1 Voltage [au]
LC1 Voltage [au]
LC2 Voltage [au]
LC2 Voltage [au]
Rotation [rad]
Rotation [rad]
Polarization state coverage
Retardation [rad]

## Slide 9: Setup
Electronically tunable fast measurement
Act on LC2 linear polarimeter
Act on both LC1 and LC2 Compensation
Measurement time will go down from weeks to hours (0.3s per point)
Sample
LC1
LC2
Polarizer
Pin
P pol
Pout ≠ 0W
Pout = 0W

## Slide 10: LC calibration setup
LASER-1064 nm
LC
FI
QWP & HWP
PD
Polarizer
LabVIEW
Voltage
Temperature
Ellipticity
Power Ppol
Azimuth
Main Power
PD
QWP & HWP
Switching speed= 95.8ms / 1.81ms @ 25.6°C
Op. Temperature = -20 °C to 45 °C

## Slide 11: Calibration
Measured retardation at 25 °C 987 nm to 14 nm
Estimated uncertainty : ~6E-9 like Polarimetry and SBC
Max Δn
Min Δn
Retardation [nm]
Voltage [V]

## Slide 12: Upcoming & Conclusion
What’s next?
  Finalize calibration
  Measure known birefringence sample
  Measure 2D polarization of KAGRA test mass
Conclusion
  Faster (0.3 s per point)
  Cheaper (compared to other electronically controlled optics)
  Similar uncertainty in retardance

## Slide 13: Birefringence in KAGRA

## Slide 14: Effect of temperature on sensitivity

## Slide 15: How do we get our calibration curve