## Slide 1: Test and Material Characterisation for superconducting magnets at CEA/Irfu Mechanical Laboratory
I.Fast – WP13
Workshop on Platforms for characterisation, treatments and test of materials
22/06/2023
PERRAUD Simon
Many thanks to C. Mayri, R. Vallcorba, G. Campagna, E. Fernandez-Mora, C. Genot, G. Lenoir, Y. Peron, H. Reymond, E. Rochepault, F. Stacchi and C. Wei
CEA Paris-Saclay/DRF/IRFU/DACM/LEAS

## Slide 2: Introduction : A lot of challenges for future accelerator magnets development
Strong magnetic field  High stress induced by Lorentz forces
Cryogenic environment  Different working temperature from 1.9 K to 77 K
Multi-scale composition  From filament to magnet
HTS tapes  Anisotropic behavior
Nb3Sn brittleness  Performance sensitive to stress
Magnet complexity  Composite with materials interactions
And more…
Necessity to investigate in detail all of those aspects…

## Slide 3: 10-stacks compression test
Goal : Characterize the mechanical behavior of a coil with representative samples made of 10 layers of Rutherford cables
Context : Upgraded setup in the framework of Nb3Sn CERN-CEA collaboration
Nb3Sn impregnated samples, compressed with loading cycles by a pushing bar under the 150 kN press at room temperature (RT), 77K and 4.2K.
Displacement measured by two extensometers at the extremity of the pushin bars
Exploded view of the setup
150 kN press configuration for compression tests at RT, 77 K and 4.2 K (with cryostat)
10stacks samples of FRESCA2 cables

## Slide 4: 10-stacks compression test
Results : Non-linear behavior characterized by stress-strain curve for differents temperatures
 Behavior law implementation in FEA models for correlation studies and better predictions for future magnet design
 Comparison with real magnet tests and measurements
Next steps : Mechanical characterization of R2D2 Nb3Sn cables, metallographic studies…
Example of stress-strain behavior on a Nb3Sn 10-stacks at RT and 77 K
Non-linear behavior law extracted from 10-stacks measurement and implemented in FEA model

## Slide 5: Tensile test on Nb3Sn strand
Goal : Characterize the mechanical behavior of a strand for correlation with multi-scale FEA model
Courtesy of G. Lenoir
σapplied
Extensometer
Context : Developpement in the framework of ANR Cocascope. Re-launched with Nb3Sn CERN-CEA collaboration
Break !
10 kN press configuration for tensile test at RT / 77 K / 4.2 K (with cryostat)
Extensometer installation on a strand
Nb3Sn strand tested in the 150kN press with the 10kN force cell, at RT and 77K
SCUTT method developped at CEA to limit transverse forces during a tensile test
Displacement measured by an extensometer glued to the strand

## Slide 6: Tensile test on Nb3Sn strand
Courtesy of G. Lenoir
Results : Non-linear behavior characterized at differents temperatures (RT and 77 K)
 Comparison with multi-scale FEA model from Cocascope project
Next steps : Test campaigns on differents strand geometries, tests at 4.2 K…
Experiment and FEA model comparison for a Nb3Sn strand under tensile test at RT
Example of Nb3Sn strand geometry generated with ANSYS
Exemple of stress-strain curve obtained for a Nb3Sn strand under tensile test at 77 K

## Slide 7: Behavior study of metal-resin interface
Goal : Study the behavior at the interface between metal parts and impregnated glass fiber under shear stress
Courtesy of G. Campagna
Context : G. Campagna thesis preparation in the framework of Nb3Sn CERN-CEA collaboration
Derivate form of « double lap shear test » with additional pressure applied lateraly on the sample
Stainless steel and titanium samples with differents surface roughness (smooth, after machining, after sandblast…) impregnated with fiberglass and CTD101K resin
Tests planned in 150kN press at RT and 77 K with strain gages, extensometers, temperature sensors and acoustic sensors
 Activities on-going with FEA model development and sample fabrication
Metal
Fiberglass impregnated
Tensile force
Sample compression during test
Drawing of principle

## Slide 8: Contact resistance under compression
Goal : Measure the contact resistance on HTS tapes under variable compressive load
Courtesy of C. Genot
Context : HTS developement at CEA by C. Genot during his PhD thesis
Stress applied up to 100MPa on a stack of HTS REBCO tapes with the 300kN press at 77K with samples immersed inside a box filled with liquid nitrogen
HTS tapes connected to a current supply, with resistance calculated through voltage taps measurement positionned all along the straight sections
CAD setup for the 300kN press configuration
Photo of the setup

## Slide 9: Contact resistance under compression
Courtesy of C. Genot
HTS
HTS
Stainless steel
Results : Comparison of contact resistance results for differents HTS tape manufacturer, insulations configurations…
 Implementation of contact resistance values inside quench models (Critical parameter to master, particularly in MI configuration
Next steps : New test campaigns on larger tapes, with different insulation configurations…
Example of contact resistance measurement evolution depending on the stress applied, for differents stacking configurations
Photo of an HTS sample, made with confocal microscopy
HTS sample representation

## Slide 10: Mechanical characterization of NbTi WiC
Goal : Study the mechanical behavior of a Wire-in-channel (WiC) NbTi coil representative sample under compression
Courtesy of H. Reymond
Context : Design of SuperFRS NbTi dipoles and future similar magnets for GSI
Samples made of WiC NbTi conductor extracted from unused coils and characterized in compression up to failure in the 300kN press, at RT and 77 K
 FEA model of the cable rebuild from a photo and compared to the experimental results achieved by an external DIC company
Next steps : New representative samples to test and correlate with FEA model, home-made DIC measurement…
Cooldown of the sample at 77 K in 300kN press
Setup of the compression test
Example of DIC results obtained
Example of sample compressed up to failure

## Slide 11: Tensile test on CICC copper jackets
Goal : Characterize the tensile yield strength of Cable-In-Conduit Conductor (CICC) copper jackets after differents cold work
Courtesy of F. Stacchi
Context : Design study of a NbTi dipole detector for Madmax project (Max Planck Institute)
Several copper jackets cold worked at different percentages, from 0 to 38%
Tensile test done in the 300 kN press with jaws and at RT. Displacement measured by one extensometer
 Tensile yield strength determine by standard ISO 6892 definition
Next steps : Characterization of other geometries and configurations for futures developements...
Setup of the experiment with the 300 kN press
Tensile yield strength results compared to NIST database
CICC copper jackets (left) and cable (top)

## Slide 12: Variable low temperature test bench
Courtesy of C. Mayri and S. Roux
Goal : Mechanical measurements at variable cryogenic temperature up to 4.2K
Context : Infrastructure investment from ANR PACIFICS
Specific interest from academies and industries for Nb3Sn and HTS developement with intermediate temperature characterization, like liquid hydrogen (20K).
Cryostat to be installed on the actual 300kN press, with a cooldown managed by cryocoolers
Designed for tensile and compression tests at stable temperature, from 4.2K to 150K or more (in discussion)
 Preliminary studies ongoing
CAO preliminary design
Drawing of principle

## Slide 13: Perspectives and conclusions
Larges spectrum of forces, dimensions and temperatures testable at the CEA/Irfu Mechanical Laboratory
Developement on more and more superconducting magnet projects, with specifities on each
Implementation of new tests capabilities and methods of measurement to respond to the need
Interest to share knowledges, experiences and capabilities between laboratories and industrials
Collaboration with a Paris-Saclay academic laboratory for a shared test facility able to characterize materials at high temperature with in-situ measurement systems

## Slide 14: Any questions ?