## Slide 1
ENHANCING CHARGE COLLECTION EFFICIENCY IN RADIATION-DAMAGED UNMETALLIZED 4H-SiC DETECTOR VIA LED ILLUMINATION
M. Rodríguez-Ramos, J. García-López, C. Torres-Muñoz, G. Pellegrini, P. Godignon, J.M. Rafi, G. Rius and M.C. Jiménez-Ramos
Centro Nacional de Aceleradores. Universidad de Sevilla

## Slide 2
ID-90
Slide 1/14
EuNPC2025
https://ccfe.ukaea.uk/wp-content/uploads/2019/09/MAST-plasma.gif
MAST Tokamak
SiC: AN EXCELLENT CANDIDATE FOR HOSTILE RADIATION ENVIRONMENTS
Emerging technologies require reliable devices for high radiation environments (fusion reactors, high-energy physics, outer space).
4H-SiC offers unique properties, making it a promising semiconductor for high-temperature and radiation-hard applications.

## Slide 3
Slide 1/14
SiC: AN EXCELLENT CANDIDATE FOR HOSTILE RADIATION ENVIRONMENTS
EuNPC2025
https://ccfe.ukaea.uk/wp-content/uploads/2019/09/MAST-plasma.gif
MAST Tokamak
ID-90
Emerging technologies require reliable devices for high radiation environments (fusion reactors, high-energy physics, outer space).
4H-SiC offers unique properties, making it a promising semiconductor for high-temperature and radiation-hard applications.
3.5 MeV He2+
4H-SiC detectors operate up to 450 ℃ with excellent energy resolution (≲2%) (J. Radiat. Phys. Chem. 2024, 214, 111283).

## Slide 4
Slide 1/14
SiC: AN EXCELLENT CANDIDATE FOR HOSTILE RADIATION ENVIRONMENTS
EuNPC2025
https://ccfe.ukaea.uk/wp-content/uploads/2019/09/MAST-plasma.gif
MAST Tokamak
4H-SiC detectors operate up to 450 ℃ with excellent energy resolution (≲2%) (J. Radiat. Phys. Chem. 2024, 214, 111283).
Detector radiation hardness was studied at room temperature up to fluences of 5×10¹¹ ions/cm², showing a significant decrease in charge collection with increasing fluence (J. Radiat. Phys. Chem 2020, 177, 190100)
ID-90
Emerging technologies require reliable devices for high radiation environments (fusion reactors, high-energy physics, outer space).
4H-SiC offers unique properties, making it a promising semiconductor for high-temperature and radiation-hard applications.
3.5 MeV He2+

## Slide 5
IMPROVING DETECTOR PERFORMANCE THROUGH DIFFERENT MECHANISMS
Slide 2/14
EuNPC2025
ID-90
Intrinsic or radiation-induced trapping centers (defects, impurities, …) in the lattice structure can capture free charge carriers, leading to signal degradation.
Lan Luo et al,. Phys. Status Solidi A,2025, 222: 2400840.

## Slide 6
Slide 2/14
EuNPC2025
ID-90
IMPROVING DETECTOR PERFORMANCE THROUGH DIFFERENT MECHANISMS
Dynamic annealing: defect recombination during irradiation at high temperature that mitigates damage accumulation.
Intrinsic or radiation-induced trapping centers (defects, impurities, …) in the lattice structure can capture free charge carriers, leading to signal degradation.
Lan Luo et al,. Phys. Status Solidi A,2025, 222: 2400840.

## Slide 7
Slide 2/14
EuNPC2025
ID-90
IMPROVING DETECTOR PERFORMANCE THROUGH DIFFERENT MECHANISMS
Dynamic annealing: defect recombination during irradiation at high temperature that mitigates damage accumulation.
Trap filling: Illumination fills active traps, reducing carrier trapping and improving charge collection.
Intrinsic or radiation-induced trapping centers (defects, impurities, …) in the lattice structure can capture free charge carriers, leading to signal degradation.
Lan Luo et al,. Phys. Status Solidi A,2025, 222: 2400840.

## Slide 8
Slide 2/14
EuNPC2025
Dynamic annealing: defect recombination during irradiation at high temperature that mitigates damage accumulation.
Trap filling: Illumination fills active traps, reducing carrier trapping and improving charge collection.
Photo-detrapping: Illumination with a light source can release trapped carriers by exciting them with photons.
ID-90
IMPROVING DETECTOR PERFORMANCE THROUGH DIFFERENT MECHANISMS
Intrinsic or radiation-induced trapping centers (defects, impurities, …) in the lattice structure can capture free charge carriers, leading to signal degradation.
Lan Luo et al,. Phys. Status Solidi A,2025, 222: 2400840.

## Slide 9
Slide 2/14
EuNPC2025
Dynamic annealing: defect recombination during irradiation at high temperature that mitigates damage accumulation.
Trap filling: Illumination fills active traps, reducing carrier trapping and improving charge collection.
Photo-detrapping: Illumination with a light source can release trapped carriers by exciting them with photons.
ID-90
IMPROVING DETECTOR PERFORMANCE THROUGH DIFFERENT MECHANISMS
Intrinsic or radiation-induced trapping centers (defects, impurities, …) in the lattice structure can capture free charge carriers, leading to signal degradation.
Goal: Investigate the use of optical excitation to partially restore CCE

## Slide 10
  Provided by the IMB-CNM-CSIC group
NEW TYPE OF UNMETALLIZED 4H-SiC SENSOR
n+ type 4H-SiC pn junction sensor manufactured at IMB-CNM and encapsulated in a commercial TO-257 package for high temperature applications.
Active area of 3x3 mm2 with ~50 mm active region.
Non-metalized surface, with only a guard ring structure.
Passivation:SiO2 (100 nm) + Si3N4 (500 nm).
Slide 3/14
EuNPC2025
ID-90

## Slide 11
  Provided by the IMB-CNM-CSIC group
Slide 3/14
EuNPC2025
SiC
NEW TYPE OF UNMETALLIZED 4H-SiC SENSOR
ID-90

## Slide 12
Slide 4/14
EuNPC2025
ID-90
CNA µ-PROBE: DAMAGE EXPERIMENTS AT VARIOUS TEMPERATURES
400ºC
Damaging ion beams: 3.5 MeV He2+ (relevant for fusion applications)
Nine different regions (100x100 mm2) were damaged at different doses (ranging from 1x1011 to 1x1013 ions/cm2) for each temperature.

## Slide 13
Slide 4/14
The irradition temperatures were settled at 30ºC, and 400ºC.
ID | Fluence (ions/cm2) | ID | Fluence (ions/cm2)
A | 1x1011 | F | 3x1012
B | 3x1011 | G | 5x1012
C | 5x1011 | H | 8x1012
D | 8x1011 | I | 1x1013
E | 1x1012 | J | Pristine
EuNPC2025
CNA µ-PROBE: DAMAGE EXPERIMENTS AT VARIOUS TEMPERATURES
ID-90
400ºC
Damaging ion beams: 3.5 MeV He2+ (relevant for fusion applications)
Nine different regions (100x100 mm2) were damaged at different doses (ranging from 1x1011 to 1x1013 ions/cm2) for each temperature.
Ceramic heater

## Slide 14
Charge sensitive
preamplifier
Amplifier
ADC
+
MCA
ION BEAM INDUCED CHARGE (IBIC)
Direction of electric field
IBIC technique is an analytical tool based on the creation of electrons/holes by ionizing radiation using single ions.
Vbias
Slide 5/14
Ions lose their energy dE/dx.
Creation of charge pairs e/h.
ID-90
EuNPC2025

## Slide 15
Vbias
Vout
Direction of electric field
IBIC technique is an analytical tool based on the creation of electrons/holes by ionizing radiation using single ions.
ION BEAM INDUCED CHARGE (IBIC)
Signal
Charge sensitive
preamplifier
Amplifier
ADC
+
MCA
Slide 5/14
Ions lose their energy dE/dx.
Creation of charge pairs e/h.
Charge transport.
Induced current at the electrodes (Shockley - Ramo theorem).
ID-90
EuNPC2025

## Slide 16
Vbias
Vout
Direction of electric field
IBIC technique is an analytical tool based on the creation of electrons/holes by ionizing radiation using single ions.
ION BEAM INDUCED CHARGE (IBIC)
Charge sensitive
preamplifier
Amplifier
ADC
+
MCA
Slide 5/14
Signal
N
100%
100%
Ions lose their energy dE/dx.
Creation of charge pairs e/h.
Charge transport.
Induced current at the electrodes (Shockley - Ramo theorem).
IBIC signal.
ID-90
EuNPC2025

## Slide 17
Vbias
Vout
Direction of electric field
ION BEAM INDUCED CHARGE (IBIC)
Charge sensitive
preamplifier
Amplifier
ADC
+
MCA
Slide 5/14
N
Signal
Presence of defects, impurities or recombination centers affect the collection of carriers and hence the current.
100%
<100%
100%
Ions lose their energy dE/dx.
Creation of charge pairs e/h.
Charge transport.
Induced current at the electrodes (Shockley - Ramo theorem).
IBIC signal.
Traps induced by radiation damage
ID-90
EuNPC2025

## Slide 18
Vbias
Vout
Direction of electric field
ION BEAM INDUCED CHARGE (IBIC)
Charge sensitive
preamplifier
Amplifier
ADC
+
MCA
Slide 5/14
Signal
Presence of defects, impurities or recombination centers affect the collection of carriers and hence the current.
Traps induced by radiation damage
Combining IBIC with a nuclear microprobe: Synchronous signal acquisition system with scanning (mappings).
ID-90
EuNPC2025

## Slide 19
Slide 6/14
EuNPC2025
ACCELERATORS FOR STUDYING RADIATION INDUCED DEFECTS IN DETECTORS
ID-90
CNA 3 MV tandem accelerator
The ion beam microprobe linked to a particle accelerator constitutes an powerful tool to characterize radiation detectors:
Small samples (3×3 mm²)
Controlled rate with micrometric slits to avoid additional damage during characterization

## Slide 20
The detector is exposed to the focused ion beam.
LED installed inside the ion beam nuclear microprobe.
Slide 6/14
EuNPC2025
ACCELERATORS FOR STUDYING RADIATION INDUCED DEFECTS IN DETECTORS
ID-90
CNA 3 MV tandem accelerator
The ion beam microprobe linked to a particle accelerator constitutes an powerful tool to characterize radiation detectors:
Small samples (3×3 mm²)
Controlled rate with micrometric slits to avoid additional damage during characterization

## Slide 21
Slide 6/14
EuNPC2025
ACCELERATORS FOR STUDYING RADIATION INDUCED DEFECTS IN DETECTORS
ID-90
The detector is exposed to the focused ion beam.
LED installed inside the ion beam nuclear microprobe.
CNA 3 MV tandem accelerator
The ion beam microprobe linked to a particle accelerator constitutes an powerful tool to characterize radiation detectors:
Small samples (3×3 mm²)
Controlled rate with micrometric slits to avoid additional damage during characterization

## Slide 22
Slide 6/14
EuNPC2025
ACCELERATORS FOR STUDYING RADIATION INDUCED DEFECTS IN DETECTORS
CNA 3 MV tandem accelerator
ID-90
The ion beam microprobe linked to a particle accelerator constitutes an powerful tool to characterize radiation detectors:
Small samples (3×3 mm²)
Controlled rate with micrometric slits to avoid additional damage during characterization
The detector is exposed to the focused ion beam.
LED installed inside the ion beam nuclear microprobe.

## Slide 23
Slide 7/14
Three commercial LEDs installed under identical conditions to illuminate the detector.
Spectral response measured offline using an optical spectrometer.
Illumination of the sensor did not result in photogeneration of electron-hole pairs.
• For the blue LED, the relative light output was measured with respect to the maximum operational voltage.
Absolute photon rate not available yet:
Work in progress…
LEDS PRESENT GOOD PERFORMANCE AS OPTICAL EXCITATION SOURCE
ID-90
EuNPC2025

## Slide 24
Slide 8/14
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
ID-90
EuNPC2025
LED OFF

## Slide 25
Slide 8/14
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
LED OFF

## Slide 26
Slide 8/14
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
LED OFF

## Slide 27
Slide 8/14
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
LED OFF

## Slide 28
Slide 8/14
Slight reduction in absolute CCE observed in regions with low damage levels.
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
LED OFF

## Slide 29
Slide 8/14
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
LED OFF

## Slide 30
Slide 8/14
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
LED OFF

## Slide 31
Slide 8/14
As fluence increases, a strong reduction in absolute CCE and peak broadening are observed.
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
LED OFF

## Slide 32
Slide 8/14
In our experimental setup, the detection limit is reached at 5×10¹² ions/cm², making higher fluences inaccessible for measurement.
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
LED OFF

## Slide 33
Slide 8/14
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
In our experimental setup, the detection limit is reached at 5×10¹² ions/cm², making higher fluences inaccessible for measurement.
LED OFF

## Slide 34
Slide 8/14
In our experimental setup, the detection limit is reached at 5×10¹² ions/cm², making higher fluences inaccessible for measurement.
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
LED OFF

## Slide 35
Slide 8/14
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE

## Slide 36
Slide 8/14
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
LED ON

## Slide 37
Slide 8/14
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
LED ON

## Slide 38
Slide 8/14
No significant effect of light on CCE observed in regions with low damage levels...
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
LED ON

## Slide 39
Slide 8/14
... But small CCE enhancements start to appear.
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
LED ON

## Slide 40
Slide 8/14
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
LED ON

## Slide 41
Slide 8/14
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
LED ON

## Slide 42
Slide 8/14
Significant recovery of the signal respect to the measurement without light.
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
LED ON

## Slide 43
Slide 8/14
The three previously inaccessible regions are now accessible due to strong CCE enhancements.
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
LED ON

## Slide 44
Slide 8/14
The three previously inaccessible regions are now accessible due to strong CCE enhancements.
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
LED ON

## Slide 45
Slide 8/14
The three previously inaccessible regions are now accessible due to strong CCE enhancements.
ID-90
EuNPC2025
IBIC USED TO ASSESS POST-IRRADIATION RESPONSE AT ROOM TEMPERATURE
LED ON

## Slide 46
Slide 9/14
ILLUMINATION HAS A SIGNIFICANT EFFECT IN THE MOST DAMAGED REGIONS
ID-90
EuNPC2025

## Slide 47
Slide 9/14
• CCE drops as fluence increases, making some damaged regions inaccessible.
ILLUMINATION HAS A SIGNIFICANT EFFECT IN THE MOST DAMAGED REGIONS
ID-90
EuNPC2025

## Slide 48
Slide 9/14
• CCE drops as fluence increases, making some damaged regions inaccessible.
• CCE is significantly better preserved at higher irradiation temperatures due to dynamic annealing.
ILLUMINATION HAS A SIGNIFICANT EFFECT IN THE MOST DAMAGED REGIONS
ID-90
EuNPC2025

## Slide 49
Slide 9/14
Light significantly affects CCE in the most damaged regions, enabling measurement of regions otherwise inaccessible.
ILLUMINATION HAS A SIGNIFICANT EFFECT IN THE MOST DAMAGED REGIONS
ID-90
EuNPC2025

## Slide 50
Slide 9/14
This effect is more pronounced in regions damaged at high temperature.
ILLUMINATION HAS A SIGNIFICANT EFFECT IN THE MOST DAMAGED REGIONS
ID-90
EuNPC2025

## Slide 51
Slide 10/14
STUDY OF THE EFFECT OF PHOTON RATE ON CCE
ID-90
EuNPC2025

## Slide 52
Slide 10/14
STUDY OF THE EFFECT OF PHOTON RATE ON CCE
• CCE drops as fluence increases, making some damaged regions inaccessible.
ID-90
EuNPC2025

## Slide 53
Slide 10/14
STUDY OF THE EFFECT OF PHOTON RATE ON CCE
• CCE improves with illumination, but at low photon rates not all damaged regions are accessible.
ID-90
EuNPC2025

## Slide 54
Slide 10/14
STUDY OF THE EFFECT OF PHOTON RATE ON CCE
CCE recovery improves further with increasing photon rate, but only in the most damaged regions.
ID-90
EuNPC2025

## Slide 55
Slide 10/14
STUDY OF THE EFFECT OF PHOTON RATE ON CCE
• CCE is enhanced and new regions become accessible, while light has no significant effect in low-damage regions.
ID-90
EuNPC2025

## Slide 56
Slide 11/14
STUDY OF THE LED WAVELENGTH ON CCE
• All three LEDs help recover CCE in the most damaged regions, with the blue LED apparently providing the largest improvement in detector performance.
ID-90
EuNPC2025

## Slide 57
Slide 11/14
However, comparison is tricky because the photon rates illuminating the detector differ; measurements should be done under the same illumination conditions.
ID-90
EuNPC2025
STUDY OF THE LED WAVELENGTH ON CCE

## Slide 58
Slide 12/14
THE UNDERLYING PROCESS IS NOT FULLY UNDERSTOOD…
ID-90
EuNPC2025

## Slide 59
Slide 12/14
THE UNDERLYING PROCESS IS NOT FULLY UNDERSTOOD…
ID-90
EuNPC2025
Effect in low-damage zones
Few traps exist, slightly more that the undamaged zone.
Most electrons and holes are already collected. Light releases only a small fraction of trapped electrons → negligible effect on CCE.
CCE is roughly the same with or without light, though slightly lower than the undamaged zone.

## Slide 60
Slide 12/14
THE UNDERLYING PROCESS IS NOT FULLY UNDERSTOOD…
ID-90
EuNPC2025
Effect in high-damage zones
Many active traps → many trapped electrons.
Light excites trapped electrons into conduction band → increases collected charge.
Time of detrapping is not instantaneous, but enough electrons reach contacts before recombination.
CCE increases with sub-gap light.
Effect in low-damage zones
Few traps exist, slightly more that the undamaged zone.
Most electrons and holes are already collected. Light releases only a small fraction of trapped electrons → negligible effect on CCE.
CCE is roughly the same with or without light, though slightly lower than the undamaged zone.

## Slide 61
Slide 13/14
THE UNDERLYING PROCESS IS NOT FULLY UNDERSTOOD…
ID-90
EuNPC2025
Other possible explanation is the presence of different types of electrically active traps, which depend on the damage regime.
Only one type of trap is light-sensitive, explaining why CCE improves mainly where this trap dominates.
Ivana Capan,. Phys. Crytals, 2025, 15(3), 255. https://doi.org/10.3390/cryst15030255
Common defects in 4H-SiC

## Slide 62
CONCLUSIONS
The potential use of commercial LEDs to improve the performance of a controlled-damaged 4H-SiC detector has been studied.
Illumination with LEDs can enhance the CCE of damaged regions.
The effect is most pronounced in regions with higher accumulated doses and depends of the photon rate.
Although the physical mechanism is not fully understood, these findings suggest a simple and effective way to mitigate radiation damage.
Future work: Study this phenomenon at high temperatures, potentially optimizing SiC-based detectors for harsh fusion environments.
Slide 14/14
ID-90
EuNPC2025

## Slide 63
CLEAR is a consortium of three installations: ATOMKI in Debrecen, CNA in Seville and IST in Lisbon, offering access to stable-ion and neutron beams in the framework of the EURO-LABS project.
Accelerator Complexes:
ATOMKI: 2 MV Tandem, 18 MeV Cyclotron, ECRIS.
CNA: 3 MV Tandem, 18 MeV Cyclotron, 1 MV Tandetron for Accelerator Mass Spectrometry (AMS).
IST: 2.5 MV Van de Graaff.
Transnational Access https://institucional.us.es/clear/
CLEAR: CLUSTER OF LOW ENERGY ACCELERATORS FOR RESEARCH
ID-90
EuNPC2025

## Slide 64
Actuación 1.1 Irradiación de detectores con aceleradores. (ASTRO21/1.1/1).
ACKNOWLEDGMENTS
Actividades del CNA para los "upgrades" de alta luminosidad de CMS y DRDs del ECFA (PID2023-148418NB-C44).
M.C. Jiménez-Ramos acknowledges the support to this work through a VI PPIT-US contract.
ID-90
EuNPC2025
Grant Award for EuNPC2025 Participation

## Slide 65
Thank you for
your attention

## Slide 66
BACKUP
ID-90
EuNPC2025

## Slide 67
Tunable penetration depth (0.1-6 MeV).
Good selection of ion species and ionization profiles.
Energy Loss
Detector
Beam current: nA to few pps (micrometric slits).
Scanning system: few mm2.
Synchronous signal acquisition system with scanning: mappings.
CNA m-probe
CCE OF SEMICONDUCTORS ANALYZED WITH FOCUSED MeV ION BEAMS
ID-90
EuNPC2025

## Slide 68
ELECTRICAL CHARACTERIZATION OF THE DEVICE
Pristine detector exhibits diode-like behavior, with a typical C-V response characteristic of a p-n junction.
A 3.5 MeV He2+ beam losses ≈306 keV in the passivation layers.
SRIM simulations confirm that all ions stop within the detector’s active volume for bias above 50V.
During real operation, the detector will be biased at 500 V.
ID-90
EuNPC2025

## Slide 69
PIXE AS AN EFFECTIVE METHOD TO MEASURE ACCUMULATED ION DOSE
ID-90
EuNPC2025
PIXE detects X-rays generated in the SiC detector during alpha particle exposure.
X-ray yield is proportional to ion fluence.
Enables real-time monitoring of delivered fluence.
The ceramic heater generates electronic noise, making direct measurement impossible.
An indirect system is used to determine the accumulated fluence during controlled high-temperature damage.

## Slide 70
ELECTRON TRAPPING DOMINATES CCE BEHAVIOR
Damaging ion beam: 3.5 MeV He++
Carriers traveling the farthest to the electrode experience the most trapping at the region of highest trap density.
Ionization profile: Energy loss is dominated by electronic stopping, peaking at the Bragg maximum near the end of the particle’s range.
Vacancy profile: As the particle slows down, nuclear stopping becomes dominant, producing a vacancy peak located to the right of the Bragg peak.
ID-90
EuNPC2025

## Slide 71
ION BEAM MICROPROBE UPGRADE ENABLES SAMPLE HEATING
ID-90
EuNPC2025

## Slide 72
3.5 MeV He2+ focused beam with spatial resolution ~2 mm.
IBIC map revealed high homogeneity in detector's CCE Values (red indicates 100% CCE).
CCE greater than 100%, identifies windows for potential electrical bondings.
HOMOGENEITY ENSURES NOT DEPENDENCE WITH THE IMPACT POINT
ID-90
EuNPC2025
CCE MAP