## Slide 1
Enhancing Target development at GANIL for nuclear research: Optimization of the deposition technique for lanthanide targets
Radia Rahali, Christelle Stodel, Georges Frémont, Marius Bourges, Franck Perocheau.
Grand Accélérateur National d’Ions Lourds (GANIL), CEA/DRF-CNRS/IN2P3

## Slide 2
GANIL/SPIRAL2 Facility
- Accelerators and targets.
2. GANIL target laboratory
3. Examples of target fabrication
4. Conclusion
Outline

## Slide 3
GANIL/SPIRAL2 Facility
Beams : 12C à U
Energy : from <1 MeV/nucleon up to 95MeV/nucleon
Up to 4 parallel experiments
Beams :
33 MeV protons
40 MeV deutons
He to U <14,5 MeV/nucleon ions lourds
nuclear physics
Astrophysics,
materials under irradiation and nanostructuring,
molecular collisions and the interstellar medium…
Radiobilogy

## Slide 4
No matter the type of experiment one wishes to perform, a good target is needed!
But… What the target looks like ?!
Gaseous, liquid or solid state
209 Bi ~ 150 µg/cm²
On carbone backing of 35 µg/cm²
Resistive heating
Enriched 208Pb target of 350 µg/cm² sandwiched between C 35 µg/cm² and C 5 µg/cm².
PVD
Sn ~ 150 µg/cm²
On carbone backing of 35 µg/cm²
Resistive heating
CD2 ~ 135 µg/cm²
Ni backing
polymerisation
60Ni
150 et 250 µg/cm²
Self supported
Electrodeposition
Au ~ 70 µg/cm²
Self supported
Al ~ 240 µg/cm²
Self supported
PVD (resistive heating)
70Zn ~ 480 µg/cm²
Self supported
PVD (resistive heating)
Bi ~ 250 µg/cm²
Self supported
PVD (resistive heating)
Notes: Zn 70 isotope
480 μg/cm²
Evaporation effet joule, dépôt sur du vinyl
Al naturel
240 μg/cm²
Effet joule, dépôt sur betaine
Bi naturel
250 μg/cm²
Effet joule, dépôt sur betaine

## Slide 5: GANIL Target Laboratory
How can we manufacture a target ?

## Slide 6
The target laboratory
  Multi-material Evaporator
Evaporator with resistive heating & Electron gun method
e-gun
Crucible/resistive heating
Crucible/resistive heating
10-100 µg/cm2
Carbon Evaporator
i
F = 3mm, length 75mm
Sublimation
evaporator with sputtering method for 238U and monoisotopic materials.
PALAIS Project Plateforme Cibles pour GANIL/SPIRAL2 A renew at our laboratory !
low melting point
high melting point
Heating system for backings
Rotating tray for 7 targets

## Slide 7
Mechanical Shaping: Tablet pressing, rolling
Chemical Techniques: Electrodeposition/Molecular Plating, Polymerization
The target laboratory
0.5 mg/cm2  g/cm2
Evaporator large dimension (diamètre 700 x1500)
Metallisation of thin foils for detectors
Rolling machines
Electro-deposition
Georges Fremont, et al, AIP Conf. Proc. 1962, 030002-1–030002-4; doi: 10.1063/1.5035519
Tablet pressing
~20 mg/cm²  g/cm²
Characterization system: X-ray fluorescence spectrometer for the chemical composition analysis of thin films
Weighing (balance)

## Slide 8: Overview of the targets fabricated and the techniques used

## Slide 9
Preparation of the nickel solution : Ni (Metal) + H2SO4 + H2O + NH4OH
180°C
Cathode : Cu foil
12 mA for 6 minutes
Target fabrication procedure
The current Electrodeposition rate ( µg/cm²/min)
the deposition time the thickness (surface density ( µg/cm²))
Chemical Technique  Electrodeposition
 thin self-supported Nickel targets
Several test shows:
dissolution
Ph ~ 6
Cathode
Notes: bain au sulfate de nickel : nickel métallique dissous dans de l’acide sulfurique
Ammonium hydroxide

## Slide 10
Target fabrication procedure
Chemical Technique  Electrodeposition  thin self-supported Nickel targets
 Deposition on Cu substrate (cathode)
 Recovery of the Ni foil with the selected target frame
Dissolution of Cu (trichloroacetic acid C2HCl3O2 + NH4OH ammonia + distilled water)
 Transfer to a bath (water) to rinse it from the Cu dissolution bath.
Transfer onto glass plate
Notes: faire flotter à la surface de la solution de dissolution ( acide trichloroacetic) 15mn

## Slide 11
Self supported natural and isotopic 60Ni  130-250 µg/cm²
 Homogenous and without comtaminatiton
Target fabrication procedure
L = 1.5 cm, l = 1.2 cm
60Ni 150 µg/cm²
Up to 4 target ( foils) with one solution of 7 mg Ni
The Ni foil is fished out and dried before being removed from the support frame.
Chemical Technique  Electrodeposition  thin self-supported Nickel targets

## Slide 12
Target fabrication procedure
Physical vapor deposition (PVD)  Resistive Heating (crucible)
 Thin self-supported Zinc targets
Evaporator for metals, isotopes low melting point (not higher then 1600 -1800 °C)
Cyclohexanone + vinyl powder
+ 100°C heating plate + vacuum heating 10-3 mbar
First step
Glass plate
5.10-4 mbar
The current is gradually increased
~ 40A
Second step
Preparation of the pellet: Zinc + tantalum
Third step

## Slide 13
Self supported 70Zn  250 to 500 µg/cm²
Target fabrication procedure
Physical vapor deposition (PVD)  Resistive Heating (crucible)  Thin self-supported Zinc targets
Final step
The deposit is circular and centred, the central area is cut out, the plate is immersed in distilled water to remove the foil.
Recover the foil on another plate and immerse it in cyclohexanone.
Recover the foil (target) on the frame.

## Slide 14
T < 1600° C
Crucible
Rotating wheel
Quartz
Physical vapor deposition (PVD)  Resistive Heating (crucible)
 thin Ytterbium/Carbon targets
Target fabrication procedure
Frame with carbon foils of ~ 35 µg/cm² rotating at 50 rpm
Yb2O3+ Hf or La (reductant agent)
Crucible : Tantalum
Distance = 7 - 9 cm
Control with quartz
Current ~ 60 – 85 A
High vacuum condition: 6.10−5 mbar
Carbon foil pre-mounted on the frame
Notes: Oxide form to metalic one ( Hf,La)
Dilemma : size ( surface area = 16 to 20)

## Slide 15
Target material
i
i
substrat
creuset
1 Frame with carbon foils of ~ 35 µg/cm² and a mask rotating at 50 rpm
Yb2O3+ Hf or La (reductant agent)
Crucible : Tantalum
Distance = 7 - 9 cm
Current ~ 60 – 85 A
High vacuum condition: 10−5 mbar
Nat Yb ~ 115 µg/cm²
Rotating wheel  Homogeneous distribution over a large surface
Yb/C  from 50 µg/cm² to 4 mg/cm²
Nat Yb ~ 4 mg/cm²
T < 1600° C
Target fabrication procedure

## Slide 16
Target material
i
i
substrat
creuset
1 Frame with carbon foils of ~ 35 µg/cm² and a mask rotating at 50 rpm
Yb2O3+ Hf or La (reductant agent)
Crucible : Tantalum
Distance = 7 - 9 cm
Current ~ 60 – 85 A
High vacuum condition: 10−5 mbar
Nat Yb ~ 115 µg/cm²
Rotating wheel  Homogeneous distribution over a large surface
Yb/C  from 50 µg/cm² to 4 mg/cm²
Nat Yb ~ 4 mg/cm²
T < 1600° C
Target fabrication procedure
Different results :
Variable deposition time
different distances (crucible- substrate)
Different type of crucible
Long deposition time → Possible contamination of the crucible
XRF device (courtesy of PLATIN)

## Slide 17
Conclusion
Target lab renovation almost completed - PALAIS project : stable + 238U
Wide range of fabrication techniques: PVD, electro-deposition, rolling, sputtering
Enriched target production ongoing: Zn, Ni, Yb, Gd on carbon, Al backing, self-supported foils…
Without rotation: uneven circular patterns, suitable for small target
With rotation: improved homogeneity and preserved crucible integrity ( both small and large target)
New characterization tools in place: ED-XRF acquired, alpha energy loss, advanced analysis via SEM, XPS, etc. performed through collaborations.
Process optimization across the full production chain: from material to quality control
Expand R&D to other lanthanides and actinides.
Continuous efforts to improve target quality and production reliability through monitoring at each stage: fabrication, beam behavior, and post-irradiation analysis.
🎯 Goal : support cutting-edge experiments with high-quality, reliable targets
Future actinide target lab under discussion – GRAND PALAIS (ATLAS) project  Open postdoctoral position in radiochemistry.
Talk: Christelle Stodel on Thursday, 25 Sept, Session P2: Accelerators and Instrumentation (6)

## Slide 18
Thank for your attention
ACKNOWLEDGMENTS
G. Fremont
M. Bourges
Ch. Stodel
F. Perocheau
F. Leroy (from the PLATIN platform)
Spectro-AMETEK staff

## Slide 19
Target fabrication procedure
Physical vapor deposition (PVD)  Resistive Heating of crucible
For thin Ytterbium/Carbon targets
Crucible
Glass plate
Quartz
1 glass plate with carbon foils of ~ 35 µg/cm²
Yb2O3+ Hf or La (reductant agent)
Crucible : Tantalum
Distance = ~ 5 cm
Control with quartz
Current ~ 60 – 85 A
High vacuum condition: 10−5 mbar

## Slide 20
Blue ~ 90 µg/cm²
Purple ~ 75 µg/cm²
Yellow ~ 52 µg/cm²
Target fabrication procedure

## Slide 21
Optimization of the procedure
Variable parameters :
Substrate (backing) : Carbon, Aluminium, Ta
Different currents ( step by step or not)
Different Evaporation boat (Crucibles) (Ta, Zr, Al2O3) – different forms/shapes, different diameters, different depths.
Amount of material used ( 20mg, to 200 mg )
Reducing agent (Zr, Hf, La)
Different distance crucible- substrat
With and without rotating the frame
The deposition time ( PVD, electrodeposition)
The type/amount of solution ( electrodeposition)
6
3mm

## Slide 22
Self supported natural and isotopic 60Ni  130-250 µg/cm²
 Homogenous and without comptaminatiton
Target fabrication procedure
L = 1.5 cm, l = 1.2 cm
60Ni 150 µg/cm²
Up to 4 target ( foils) with one solution of 7 mg Ni
Chemical Technique  Electrodeposition
cadre Exogam
La feuille de Ni est ensuite pêchée et séchée avant d’être démontée du cadre support

## Slide 23
Physical vapor deposition (PVD)  Resistive Heating of crucible
For thin Ytterbium/Carbon targets
Target fabrication procedure
Preparation du cadre avec le backing en carbone

## Slide 24
Sublimation
Step 1: High purity graphite from 3mm diameter rods are sublimed, and the C vapour is collected on betaine-sucrose-treated glass plates.
Step 2: The layers are carefully separated with cold distilled water, allowing them to float to the surface
With one evaporation we can have
  8 glass plates : (100*140) mm², 35 µg/cm² (150-200 nm)
  16 C strippers or 24 C backing.
  Thickness: 10 - 70 µg/cm²
  Surface : 20 X 20 cm
30 mm
110 mm
15 mm
P. Maier-Komor, NIM 102 (1972) 485-486
W. Thalheimer et al, Cryst. Res. Technol. 34 (1999) 175-179.
Fabrication Procedure
Step 3: The C thin film is picked up with target frames and used as strippers or backings for material deposition.
i
F = 3mm, length 75mm
Notes: Carbon evaporator,
Resistance heating, sublimed, collected on betain-saccharose treated glass plate
Floated off and recover using the target framework

## Slide 25
Target material
i
i
substrat
Crucible
110 mm
15 mm
30 mm
H.A.F. Muggleton, Vacuum 37 (1987) 785-817.
Frame
Bcking
Deposit
Fabrication Procedure
Rotating weel
Resistive Heating of crucible
Fixed deposition
Evaporator for metals, isotopes low melting point (not higher then 1600 -1800 C)
For metals, isotopes low melting point
Rotating multi-target plate: homogeneous deposition and several targets at times
Notes: Depending low or high meltingpoint
Either fixed position or by rotating the wheel
Cooled cooper plate
5 at once

## Slide 26
110 mm
15 mm
30 mm
Frame
Bcking
Deposit
Fabrication Procedure
Electrostatic focused electrons (EFe-)
Electron heating of crucible
i
Electronic bombardment of the crucible
Thickness ~100s nm
High melting point materials,
oxides  reduction for metallic deposit (with Zr, La..)
L. Westgaard et al, Nucl. Inst. Meth. 42 (1966) 77-81
A. Stolarz, Journal of Radioanalytical and Nuclear Chemistry vol. 299, pages 913–931 (2014)
electron gun
Electron heating of material
Electron
gun
Creuset refroidi
Evaporator with electron gun (3 kW or 6 kW)
Thickness > 1 µm
High melting point materials
Advantage : Prevent chemistry reaction with crucible according to temperature
G.E. Thomas et al., Nucl. Instr. and Meth. A 303 (1991) 162-164.
Notes: Electron gun

## Slide 27
Lanthanides targets
Crucible : Zirconium of 0.7 x 0.7 mm diameter
Deposition without rotation.
Deposition on aluminum foil attached to a copper plate cooled throughout the deposition.
Current 104 A
Yield ~ 1%
100 mg Gd2O3
200 Zr
120 mg Gd2O3
Zr 50mg
100 mg Gd2O3
100 Zr
Non-homogeneous distribution over the surface  Different thickness
Notes: Circular : thickness gradient

## Slide 28
Lanthanides targets
100 mg Gd2O3
100 Zr
1
2
Different thickness distribution over the surface
Crucible (Zr) destroyed but no comtamination!
Notes: Crucible destroyed
Fe : Device

## Slide 29
Technique used :
Evaporator with electrostatic focused electrons (EFe-)
oxides  reduction for metallic deposit (Zr)
i
Tantalum crucible
-Inner diameter: 3 mm
-Depth: 6 mm
Electronic bombardment/heating of the crucible
quartz (control of the start and end of the reaction)
Tantalum plate fixed 3 cm from the crucible
A current of 25 A passes through the W filament
The crucible is brought to 2.5 kV
Gadolinium target
First results of lanthanides targets

## Slide 30
Distance foil-crucible: 5 cm Deposition of 2.7 mg over 10 cm² (= 270 μg/cm²)
Distance foil - crucible: 3 cm Deposition of 260 μg over 4 cm² (= 65 μg/cm²)
Probable explanations:
Challenges in controlling the crucible temperature (dependent on I fil and U), which impacts the Gd/Zr mixture:
At T > 1700 °C: Gd reacts with Ta
At T < 1600 °C: incomplete reduction may occur.
Zr powder: issues with purity and particle size?
Initial test used irregular particles.
Subsequent test involved an aqueous solution, followed by vacuum drying and heating.
Gd₂O₃ powder: prone to moisture absorption and impurities?
Heated to temperatures ranging from 300 to 900 °C.
Mixing of Gd and Zr: uniformity concerns?
First results of lanthanides targets

## Slide 31: Fabrication Activities