## Slide 1
Application of the SILVACO program to the development of silicon detectors for the detection of high-energy particles
Li Long
llong@cismst.de
CiS research institute for Microsensor system
Konrad-Zuse-Str.14, 99099 Erfurt, Germany
22-24.Nov. 2023
SIMDET 2023 LPNHE-Paris

## Slide 2
CiS Research Institute for Microsensor system Location
Erfurt
Berlin
Hamburg
Munich
Frankfurt/Main

## Slide 3
Business Units
MEMS
MOEMS
Departments
Process Development
Microoptoelectronical Sensors
Micromechanical Sensors
Test & Analytics
Backend / Assembly
Wafer Processing
Simulation & Design
System
Technology
CiS Research Institute for Microsensor system Organisation
Silicon Detectors

## Slide 4
Simulation and design
Wafer technology
Device characterization and analysis
Assembly and packaging
Certified QM System DIN EN ISO 9001
Complete technology chain for R&D and production of high-performance micro-sensor systems
- Layout
FEM-Simulation
Process-Simulation
- Device-Simulation
- Circuit-Simulation

## Slide 5
Simulation and design
Layout and DRC: Layed, ICED, Tanner, Klayout
Electrical, mechanical and thermal simulation: ANSYS, COMSOL
Semiconductor simulation: Athena 5.26.1.R, ATLAS 5.34.0.R
Circuit simulation: HSPICE, free spices, and ORCAD

## Slide 6
Structuring by using
UV-Photolithography
<1um
- 4“ and 6” Wafer line, front and backside processing, - Spray-Coating for 3D-MEMS/MOEMS
RIE- and Plasma etch, Wet-Bench
High temperature processes
LP/PE-CVD, Magnetron sputtering
Si-direct bonding, anodic bonding
CiS Research Institute Wafer processing

## Slide 7
Radiation- and Particle-Detectors for HEP
  Micro-strip detectors
  Micro-pixel detectors
  X-Ray detectors
  Beta ray detectors
  Ion detectors
  Silicon photomultiplier
  DSSS
Radiation and particle detectors for high-energy physics

## Slide 8
© CiS Research Institute, 2023
Silicon detectors for HEP
Silicon detectors for particle detection
High granularity: high spatial resolution, microstrip, micropixel, single or double sided, AC or DC coupled
Big sensitive volume: full depletion
Low mass: thin substrate
Small dead area: edge region should be small
Low noise: low interstrip capacitance, high coupling capacitance for ac coupling
Good channel isolation
High operation voltage: sensitivity
Radiation hard: 1015cm-2 Fluence of 1MeV equivalent neutron
Good CCE, MIPS pulse height distribution
Specifications
Low and homogenous leakage current over all channels
Very few hot or defect channels, dielectric pin holes, defect poly resistors or metal lines
High breakdown voltage and no micro discharge
High dielectric breakdown voltage for ac coupling (double sided sensor)
Design rules and robust design
1. Patterning size limitation and mask alignment precision: Minimal structure size, minimal structure separation and overlap
2. Statistical deviation of film growth or deposition: Safety margin of process parameters
Notes: 8

## Slide 9
© CiS Research Institute, 2023
Process simulation
The fixed positive charge in the Si/SiO2 interface creates a conductive channel between adjacent strips or pixels, isolation is required.
Pspray or Pstop are used.
They have effects on interstrip
resistance, capacitance,
breakdown voltage and CCE.
Pstop profile
peak concentration 2.0E17, peak position 0.13um, depth 2.8um.
Deckbuild Optimizer
Notes: 9

## Slide 10
© CiS Research Institute, 2023
Process simulation
go athena
init infile=start_litef1.str
method fermi
deposit oxid thick=0.15 divisions=8
deposit photores thick=2 divisions=8
etch photores right p1.x=17
implant boron dose=2.0e15 energy=70 crystal
diffus time=60 temp=975 nitro press=1.00
diffus time=180 temp=975 nitro press=1.00
etch photores all
struct outfile=start_litef2.str
slope 5.42E14/cm2
flat 1.65E15/cm2
Ion implant on the KOH etched cavity
Deveidt structure
Athena
Notes: 10

## Slide 11
© CiS Research Institute, 2023
Device simulation, field plate
A field plate over the edge of an active zone can reduce the electric field strength and increase the breakdown voltage. The following simulation is performed to obtain the design rule.
Metal thickness: 1 µm, Scatter oxide thickness: 50 nm, Ground oxide thickness: 250 nm, Step in oxide (width of scatter oxide over active zone beside the contact opening): 10 µm.
Notes: 11

## Slide 12
© CiS Research Institute, 2023
Field plate, Electric field distribution @200V vs. overlap sizes
5.5µ
4.5µ
3.5µ
2.5µ
1.5µ
0.75µ
0µ
-0.75µ
-1.5µ
-2.5µ
Notes: 12

## Slide 13
© CiS Research Institute, 2023
Field plate, maximal electrical field strength @different bias vs. overlap
For three different biases, the maximum E-field strength is calculated for different metal overlaps.
With 2.5µ overlap you already get the smallest Emax.
Larger overlaps will increase the interstrip capacitance.
Notes: 13

## Slide 14
© CiS Research Institute, 2023
Field plate
The maximum electric field strength of the sensor is (in lateral direction) at the edge of the active zone.
The maximum electric field strength of the sensor is lower if the metal overlaps the substrate region.
Find the smallest possible metal overlaps that produce the smallest E-field peak.
Notes: 14

## Slide 15
© CiS Research Institute, 2023
Dicing edge
There are many deep defects at the dicing edge. When the space charge region touches the edge,
the leakage current will increase rapidly with bias. The effect of the dicing edge is simulated with this
modeling structure.
To compare the effect of a floating implant, we use a model with and without floating implants.
Dist is the distance to the dicing edge, sep=20um,strip=50um.
Notes: 15

## Slide 16
© CiS Research Institute, 2023
Dicing edge
The left plot is for a structure without floating implants, the right plot is for a structure with
floating implants.
dist are shown on legend.
An active zone too close to the dicing edge will result in greater leakage unless the edge is passivated.
Inserting a floating strip shortens the required distance to the edge.
Leakage current vs. biasing voltage for different distances
Notes: 16

## Slide 17
© CiS Research Institute, 2023
Dicing edge
Distance to dicing edge 100um Distance to dicing edge 400µm.
At a distance of 100µm, the space charge region touches the edge.
At a distance of 400µm, the leakage current remains small.
Electron concentration distribution for two distances
Notes: 17

## Slide 18
© CiS Research Institute, 2023
Multi guard ring
The multi guard ring structure is designed to relax the electric field at the strip edge
and to limit the space charge region.
This structure reforms the potential distribution
around the implant edge, so that the peak field strength
is reduced.
Two guard ring structures 10 rings and 15 rings
Notes: 86 15
18

## Slide 19
© CiS Research Institute, 2023
Multi guard ring
The electron concentration distribution for biases of 50, 100, 400, 1000V for the10-ring structure
Notes: 50 100 400 1000V
19

## Slide 20
© CiS Research Institute, 2023
Multi guard ring
The guard ring with 15 rings has a smaller peak in the electric field
Highly mesh dependent.
The electric field distribution of 1000V for 10 rings and 15 rings guard ring structures
Notes: 20

## Slide 21
© CiS Research Institute, 2023
The effect of border implant
We simulate structures of 200µ and 500µ thick with 4 guard rings plus different border implants
Structures
E-Field distributions
Notes: 21

## Slide 22
© CiS Research Institute, 2023
The effect of border implant
We simulate 200µ and 500µ thick structures with 4 guard rings, the boundary zone is 1035µ, plus different border implants starting from the chip edge.
Chart: E-Field peak @ 200V
| 9 | 50 | 100 | 985 | 1035
500µ | 283100 | 119400 | 83200 | 70700 | 70700
200µ | 233000 | 134800 | 132200 | 113100 | 113100
Chart: Darkcurrent density @200V
| 9 | 50 | 100 | 985 | 1035
500µ | 6.95e-08 | 7.05e-08 | 7.16e-08 | 7.4e-08 | 7.4e-08
200µ | 2.77e-08 | 2.84e-08 | 2.92e-08 | 3.03e-08 | 3.03e-08
For smaller distance the dark current is smaller but the maximum of electric field is higher.
Therefor a compromise must be found for the sensor design.
Notes: 22

## Slide 23
© CiS Research Institute, 2023
Inter strip capacitance
Above full depletion the inter-strip capacitance is the major contributor to amplifier noise.
A p-in-n microstrip sensor with AC coupled silicon detector, backside with pspray is simulated.
y axis the inter-strip capacitance [F/cm], x axis the metal overlap in [microns].
Notes: 23

## Slide 24
© CiS Research Institute, 2023
Inter strip capacitance
The interstrip capacitance is plotted as a function of various geometric parameters to provide
design information.
The interstrip capacitance of the ohmic side is much larger than that of the junction side.
Notes: 24

## Slide 25
© CiS Research Institute, 2023
Pspray
Pspray is used as channel isolation for n-in-n structures.
The field strength depends on the structure.
ovb=4um Emax320=198062 V/cm
ovb=0 Emax320=709930 V/cm
ovb=-2um Emax320=709930 V/cm
Notes: 25

## Slide 26
© CiS Research Institute, 2023
Signal formation
Double sided p-in-n strip detector, substrate n-silicon, strip 40um, gap 40um, the laser scans from 60um(A1 edge) to 80um (gap center). Ohmic side is n-in-n, with pspray. Junction side signals at electrodes A1 and A2 are shown by 5V bias for 10 laser scan positions.
curve | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9
position | 60 | 63 | 66 | 68 | 70 | 72 | 74 | 76 | 78 | 80
Notes: 26

## Slide 27
© CiS Research Institute, 2023
Charge sharing
Ohmic side signals at electrodes A1 and A2 are shown by 200V bias, with pspray
At 200V bias the signal is faster and the amplitude is larger. The signal becomes smaller when the laser is moved away from the A1 stripe, meanwhile the signal of the adjacent A2 stripe become larger.
Notes: 27

## Slide 28
© CiS Research Institute, 2023
Charge sharing
Signals on junction side at electrodes A1 and A2 by 200V biasing
The signal is faster and larger than that of the ohmic side.
Notes: 28

## Slide 29
Numerical simulation is useful for process and design and for possible failure analysis
SILVACO input deck script is for most case OK
Electrical simulations agree well with tests if lifetime is scaled
Process simulation and SIMS profile need fine tuning
We have produced high quality micropixel and microstrip sensor for ATLAS CMS CBM ...
Poly resistor and punch through basing
Single or double sided
Double metal possible
Pspray and pstop isolation for n-in-n structure
FZ-n or FZ-p silicon substrate
Detector on thin membrane
Conclusions

## Slide 30
CiS Forschungsinstitut für Mikrosensorik GmbH
Konrad-Zuse-Straße 14
99099 Erfurt
info@cismst.de
www.cismst.de
Managing director: Prof. Dr. Th. Ortlepp
Mr. Th. Brock hjfreitag@cismst.de
+49 361 663 1410
© CiS Research Institute, 2023
CiS Research Institute