## Slide 1: Introduction to Semiconductor Detectors with focus on applications at Hadron Colliders Michael Moll, CERN EP-DT, Geneva, Switzerland
SIMDET 2023, 22-24 November 2023, LPNHE Paris
https://indico.in2p3.fr/event/30704/

## Slide 2: OUTLINE
The Large Hadron Collider (LHC) at CERN
  Where are the silicon detectors?
Silicon Detectors for High Energy Physics Applications
  The basic concept of Semiconductor Detectors: A reverse biased pn-junction
  Strip and Pixel Detectors at the Large Hadron Collider (LHC) at CERN
  Recent developments in Silicon Detectors
Radiation Damage to Silicon Detectors
  Upgrade of the Large Hadron Collider (HL-LHC)
  Radiation damage mechanisms
    Microscopic defects and macroscopic damage
  Mitigation techniques: What can we do against radiation damage?
    Examples of radhard devices for the HL-LHC: p-type strip sensors and 3D sensors
Why do we need (TCAD) device simulations (introduction)?
Summary & Further reading
Details in following presentations: Marco Bomben; Arianna Morozzi; Matteo C.Vignali; Jairo Antonio Villegas Dominquez; Li Long; Alexander Bähr

## Slide 3: CERN & LHC - Large Hadron Collider
p
p
27 Km
CERN Large Hadron Collider (LHC) - 27 km accelerator ring
proton-proton beams of 6.8 TeV each collide in 4 experiments
Geneva
Alps
CERN
CERN (2023):
  23 member states
  ~13400 scientists (users)
  ~ 2660 personnel (staff) + 900 Fellows
  Budget ~1230 MCHF (France: 13.2%)
LHC: 27 km tunnel
   4600 MCHF + 1200 MCHF (accelerator + experiments)
  1232 dipoles B=8.3T (959
  Design: pp s = 14 TeV (Ldesign = 1034 cm-2 s-1)
  heavy ions (e.g. Pb-Pb; 5TeV)
Circulating beams:
  2008: first beam
  2009-13: Run 1 at 2 x 4 TeV
    2012: Higgs Boson “discovered”
  2015-18: Run 2 at 2 x 6.5 TeV (1034cm-2s-1 reached)
  2018-22: Long Shutdown 2 (LS2)
  2022-26: Run 3 at 2 x 6.8 TeV
  2026-28: Long Shutdown 3 (LS3)
  2028: HighLumi-LHC (Run 4, ….)
    collect 3000-4000 fb-1 until ~ 2042 (20 times more than today)
also a program with Pb beams at up to 5.36 TeV per nucleon
today
Notes: https://en.wikipedia.org/wiki/Large_Hadron_Collider

## Slide 4: The LHC Experiments
Geneva
LHCb
ATLAS
ALICE
CMS
Alps
CERN
Notes: 2023: LHC 6.8+6.8 TeV Large Hadron Collider, 27 km in circumference; 9 active experiments: ALICE, ATLAS, CMS, FASER, LHCb,
LHCf, MoEDAL-MAPP, SND and TOTEM

## Slide 5: Collisions in the LHC
event seen in 2011 Higgs  2 photons
CMS
every 25ns (40 MHz)
Silicon Tracker
Electromagnetic Calorimeter
Hadron Calorimeter
Muon chambers
Superconducting Solenoid
Iron return yoke
CMS DETECTOR
Weight: 14000 t
Diameter: 15.0 m
Length: 28.7m
Field: 3.8T

## Slide 6: Silicon Tracking Detector
LHC example: The CMS DETECTOR
CMS DETECTOR
Weight: 14000 t
Diameter: 15.0 m
Length: 28.7m
Field: 3.8T
5.4 m
2.4 m
Outer Barrel (TOB)
Inner Barrel (TIB)
End Cap (TEC)
Inner Disks (TID)
Inner Tracker
CMS – Inner Tracker & Pixel Detector
  Micro Strip:
  ~ 214 m2 of silicon strip sensors, 11.4 million strips
  Pixel:
  4 layers & 2 x 3 disks: silicon pixels (~ 1m2)
  124 million pixels (100x150mm2)
  Resolution: σ(rφ) ~ 10 mm, σ(z) ~ 25mm
104 cm
32 cm
Pixel Detector
scientist

## Slide 7: Present LHC Tracking Sensors
CMS Tracker insertion
December 2007

## Slide 8: Silicon Tracking Detectors
Silicon tracking detectors are used in almost all HEP experiments:
Different sensor technologies, designs, operating conditions,….
CMS Strip Tracker IB
ATLAS Pixel Detector
ALICE ITS Barrel New ITS for Run3:2022
CMS Pixel Detector
ATLAS SCT Barrel
LHCb VELO (New VELO for Run3:2022)
ALICE ITS Outer Barrel (Foto:Insertion Test 2021)
LHCb VELO (New VELO for Run3:2022)

## Slide 9: Silicon Sensors

## Slide 10: Solid State Detectors – Why Silicon?
Some characteristics of Silicon crystals
  Small band gap Eg = 1.12 eV  E(e-h pair) = 3.6 eV ( 30 eV for gas detectors)
  High specific density 2.33 g/cm3 ; dE/dx (M.I.P.)  3.8 MeV/cm  106 e-h/m (average)
  High carrier mobility e =1450 cm2/Vs, h = 450 cm2/Vs  fast charge collection (<10 ns)
  Very pure < 1ppm impurities and < 0.1ppb electrical active impurities
  Rigidity of silicon allows thin self supporting structures
  Detector production by microelectronic techniques  well known industrial technology, relatively low price, small structures easily possible
Alternative semiconductors
  Diamond
  Gallium arsenide (GaAs)
  Gallium nitride (GaN)
  Silicon Carbide (SiC)
  Germanium (Ge)

## Slide 11: How to obtain the signal?
In a pure intrinsic (undoped) semiconductor the electron density n and hole density p are equal.
For Silicon: ni  1.451010 cm-3
4.5 108 free charge carriers in this volume, but only 3.2 104 e-h pairs produced by a M.I.P.
 Reduce number of free charge carriers, i.e. deplete the detector
 Most detectors make use of reverse biased p-n junctions
E
f
E
valence band
conduction band
h
e

## Slide 12: Doping, resistivity and p-n junction
Doping: n-type silicon
  add elements from Vth group  donors (P, As,..)
  electrons are majority carriers
Doping: p-type silicon
  add elements from IIIrd group  acceptors (B,..)
  holes are majority carriers
Si
Si
Si
Si
Si
Si
Si
Si
P
e.g. Phosphorus
p-n junction There must be a single Fermi level!  band structure deformation  potential difference  depleted zone
 | detector grade | electronics grade
doping |  1012 cm-3 |  1017 cm-3
resistivity  |  5 k·cm | 1 ·cm
resistivity r
  carrier concentration n, p
  carrier mobility mn, mp

## Slide 13: Reverse biased p-n junction
Poisson’s equation
Electrical charge density
Electrical field strength
Electron potential energy
Positive space charge, Neff =[P] (ionized Phosphorus atoms)
neutral bulk (no electric field)
Full charge collection only for fully depleted detector (VB>Vdep)
Depleted zone growth with increasing voltage ( )
effective space charge density Neff
depletion voltage Vdep
detector thickness d

## Slide 14: Single Sided Strip Detector
Segmentation of the p+ layer into strips (Diode Strip Detector) and connection of strips to individual read-out channels gives spatial information
typical thickness: 300mm (150m-500m used)
pitch
using n-type silicon with a resistivity of  = 2 KWcm (ND ~2.2.1012cm-3) results in a depletion voltage ~ 150 V
Resolution  depends on the pitch p (distance from strip to strip) - e.g. detection of charge in binary way (threshold discrimination) and using center of strip as measured coordinate results in
typical pitch values are 20 mm– 150 mm  50 mm pitch results in 14.4 mm resolution

## Slide 15: Signal Formation in a strip sensor
TCAD simulation: minimum ionizing particle traversing the sensor
  with typical dimensions for presently operating large LHC trackers (p-in-n devices)
holes
electrons
TCAD
n-type bulk
p+ readout electrodes

## Slide 16: Signal Formation in a strip sensor
TCAD simulation: minimum ionizing particle traversing the sensor
  with typical dimensions for presently operating large LHC trackers (p-in-n devices)
holes
electrons
TCAD
n-type bulk
p+ readout electrodes

## Slide 17: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 1 ns
holes
electrons

## Slide 18: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 1.2 ns
holes
electrons

## Slide 19: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 1.4 ns
holes
electrons

## Slide 20: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 1.6 ns
holes
electrons

## Slide 21: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 1.8 ns
holes
electrons

## Slide 22: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 2.0 ns
holes
electrons

## Slide 23: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 3.0 ns
holes
electrons

## Slide 24: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 4.0 ns
holes
electrons

## Slide 25: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 5.0 ns
holes
electrons

## Slide 26: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 6.0 ns
holes
electrons

## Slide 27: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 7.0 ns
holes
electrons

## Slide 28: Signal formation in a strip sensor
Simulation:
  mip, 45 angle
Plot:
  Signals induced on electrodes
  Integration gives collected charge
Simulation: Thomas.Eichhorn@kit.edu
2,27e-15C
3,27e-15C
3,04e-15C
1,08e-15C
Strip 1
Strip 2
Strip 3
Strip 4
t = 2.0 ns
1 2 3 4
2ns
4ns
6ns
8ns

## Slide 29: Present LHC Tracking Sensors
CMS Tracker
M.Krammer, ICFA School, Bogota, 2013

## Slide 30: Present LHC Tracking Sensors
CMS Tracker
… 11.4 million strips
M.Krammer, ICFA School, Bogota, 2013

## Slide 31: Hybrid Pixel Detectors
HAPS – Hybrid Active Pixel Sensors
    segment silicon to diode matrix with high granularity ( true 2D, no reconstruction ambiguity)
    readout electronic with same geometry (every cell connected to its own processing electronics)
    connection by “bump bonding”
    requires sophisticated readout architecture
    Hybrid pixel detectors are used in LHC experiments: ATLAS, ALICE (from Run3 monolithic), CMS and LHCb (from Run 3)
Flip-chip technique
Solder Bump: Pb-Sn
(VTT/Finland)
~ 15mm

## Slide 32: Present LHC Tracking Sensors
CMS Pixel (Half disk forward pixel)
M.Krammer, ICFA School, Bogota, 2013

## Slide 33: Hybrid Pixels - Monolithic Pixels
Example: ALICE – Alpide Chip
  TowerJazz 0.18µm CMOS imaging process
Separately optimize sensor and FE-chip for very high radiation environment
Fine pitch bump bonding to connect sensor and readout chip
or
Charge generation volume integrated into the ASIC, but many different variants!
Thin monolithic CMOS sensor, on-chip digital readout architecture
N-well collection electrode in high resistivity epitaxial layer
State-of-art: based on quadruple well allows full CMOS
High resistivity (> 1kΩ cm) epi-layer (p-type, 20-40 μm thick) on p-substrate
Moderate reverse bias => increase depletion region around N-well collection diode to collect more charges by drift
s
Hybrid Pixel
Monolithic Pixel
s

## Slide 34: The future: Going full wafer monolithic!
ALICE ITS3 project (targeting installation in LS3 2026-2028)
  Use of 300mm wafer-scale MAPS chips in 65 nm CMOS !
    thinned down to  50 um making them flexible
    sensor length 266 mm x width 55 / 74 / 93 mm
    spatial resolution requirement 5 mm
  ITS3 detector comprised of 6 chips only!
  Mechanically held in place by carbon foam spacers
full scale chip (50 mm thick) bent to 19 mm radius
[Filip Krizek, VERTEX 2023]
Notes: 20-40um thick  0.02X to 0.04% X0

## Slide 35: The Charge Signal
Collected charge for a Minimum Ionizing Particle (MIP)
  Mean energy loss dE/dx (Si) = 3.88 MeV/cm  116 keV for 300m thickness
  Most probable energy loss ≈ 0.7 mean  81 keV
  3.6 eV to create an e-h pair  108 e-h / m (mean)  72 e-h / m (most probable)
  Most probable charge (300 m) ≈ 22500 e ≈ 3.6 fC
Mean charge
Most probable charge ≈ 0.7 mean
number of events
charge deposited [fC]

## Slide 36: The Charge Signal
Collected Charge for a Minimum Ionizing Particle (MIP)
Landau distribution has a low energy tail
  becomes even lower by noise broadening
  Noise sources: (ENC = Equivalent Noise Charge) - Capacitance - Leakage Current - Thermal Noise (bias resistor)
  Good hits selected by requiring NADC > noise tail If cut too high  efficiency loss If cut too low  noise occupancy
  Figure of Merit: Signal-to-Noise Ratio S/N
  Typical values >10-15, people get nervous below 10. Radiation damage severely degrades the S/N.
Signal
Cut (threshold)

## Slide 37: Summary: Silicon Sensors in HEP
Main sensor concepts:
Monolithic CMOS Pixel Detector
strip
pixel/pad
Hybrid Pixel Detector
(Mini) Strip Detector [AC coupled]
p-in-n
n-in-p
Need inter strip isolation!

## Slide 38: The LHC Upgrade

## Slide 39: LHC upgrade
[G.Calderini Vertex 2021]
today
[HL-LHC schedule – Feb.2022]
Example ATLAS:

## Slide 40: Phase 2 upgrades – High Lumi LHC
s
CMS Phase-2 upgrade
s
About 800 m2 of silicon sensors for the phase 2 upgrades of ATLAS & CMS (RUN 4 ≥ 2029)
..and all based on p-type silicon and no longer n-type silicon. Why? … let's see
Notes: 600m2 HGCAL
13m2 ATLAS Pixel
165m2 ATLAS Strip
200m2 CMS outer Tracker

## Slide 41: Radiation Damage
Damage to dielectric layers and interfaces (not covered)
Damage to the semiconductor bulk (introduction)
Radiation damage is just one of the many challenges in conceiving a High Energy Physics detector for hadron colliders.
Constraints like needs for high granularity, low mass, efficient cooling and low power consumption, low cost, high rate capability, precision timing capability, …. are adding up to the challenge of building a detector.

## Slide 42: Motivation and Challenge
Silicon detectors upgrades and operation - Radiation Hardness -
LHC operation
HL-LHC (High Luminosity LHC)
  detector developments for HL-LHC
    starting after LS3 (~2026-28);
    expect 4000 fb-1 (nominal LHC was 300 fb-1)
HL-LHC operation & upgrades
  operation of HL-LHC
    damage modelling, evaluation, mitigation
  ATLAS Pixel replacement, LHCb upgrade, …
FCC – Future Circular Collider
  ..also FCC-ee
Increasing radiation levels
  Semiconductor detectors will face >1016 neq/cm2 (HL-LHC) and >7x1017 neq/cm2 (FCC-hh)  detectors used at LHC cannot be operated after such irradiation
New requirement and new detector technologies
  New requirements or opportunities lead to new technologies (e.g. HV-CMOS, LGAD,…) which need to be evaluated and optimized in terms of radiation hardness and/or 4D tracking capabilities
[I. Dawson, P. S. Miyagawa, Sheffield University, Atlas]

## Slide 43: Displacement Damage
….. a wide range of point defects
example of point defect reactions:
V: V+O → VO; V+P →VP
I: I+CS → Ci → Ci + O →CiOi I+BS → Bi → Bi + O →BiOi … many more reactions!
particle
SiS
Vacancy + Interstitial
point defects and clusters of defects
EK>25 eV
V
I
EK>5 keV
“dopant removal”
s
[C.Besleaga et al. arXiv 2021]
Can we see the defects?
HRTEM on Si: n-irradiated 1019 neq/cm2
High Resolution Transmission Electron Microscopy
I
I
V
V
[van Lint 1980]

## Slide 44: Impact of Defects on Detector Properties
Shockley-Read-Hall statistics
trapping (e and h)  CCE shallow defects do not contribute at RT due to fast de-trapping
charged defects  Neff , Vdep e.g. donors in upper half, acceptors in lower half of the band gap
generation  leakage current levels close to midgap most effective
Impact on detector properties can be calculated if defect parameters are known:
n,p : cross sections E : ionization energy Nt : concentration
Defect spectroscopy
e.g. DLTS, TSC
allows to measure the defect properties (see backup)
Extracted parameters serve as input to TCAD simulations (see backup)
s

## Slide 45: Radiation Damage Summary
Macroscopic bulk effects:
Depletion Voltage (Neff) Leakage Current Charge Trapping
Cut (threshold)
noise
signal
Signal to Noise ratio is quantity to watch (material + geometry + electronics)

## Slide 46: Summary: Basics of Radiation Damage in Silicon Sensors
Two general types of radiation damage to the detector materials:
 Bulk (Crystal) damage due to Non Ionizing Energy Loss (NIEL) - displacement damage, built up of crystal defects –
  Change of effective doping concentration & acceptor/donor removal (higher depletion voltage, under- depletion)
  Increase of leakage current (increase of shot noise, thermal runaway)
  Increase of charge carrier trapping (loss of charge)
 Surface damage due to Ionizing Energy Loss (IEL) - accumulation of positive in the oxide (SiO2) and the Si/SiO2 interface – affects: interstrip capacitance (noise factor), breakdown behavior, …
Impact on detector performance and Charge Collection Efficiency (depending on detector type and geometry and readout electronics!) Signal/noise ratio is the quantity to watch
 Sensors can fail from radiation damage !
Same for all tested Silicon materials!
Influenced by impurities in Si – Defect Engineering is possible!
Can be optimized!
Notes: 46
46
efficacité de collection de charge influencé par deux mécanisme
piégeage – porteurs de charge sont pièges par les défaut profond
déficit de collection de charge augmente en fonction de la fluence

## Slide 47: Radiation Hard Detectors

## Slide 48: RD50 Collaboration (2002-2023)
RD50 (Nov.2023): 65 institutes and 440 members
51 European institutes Austria (HEPHY), Belarus (Minsk), Czech Republic (Prague (3x)), Finland (Helsinki, Lappeenranta ), France (Marseille, Paris, Orsay), Germany (Bonn, Dortmund, Freiburg, Göttingen, Hamburg (Uni & DESY), Karlsruhe, Munich (MPI & MPG HLL)), Greece (Demokritos), Italy (Bari, Perugia, Pisa, Trento, Torino), Croatia (Zagreb), Lithuania (Vilnius), Montenegro (Montenegro), Netherlands (NIKHEF), Poland (Krakow), Romania (Bucharest), Russia (Moscow, St.Petersburg), Slovenia (Ljubljana), Spain (Barcelona(2x), Santander, Sevilla (2x), Valencia), Switzerland (CERN, PSI, Zurich), United Kingdom (Birmingham, Glasgow, Lancaster, Liverpool, Oxford, Manchester, RAL)
8 North-American institutes Canada (Ottawa), USA (BNL, Brown Uni, Fermilab, LBNL, New Mexico, Santa Cruz, Syracuse) 7 Asian institutes China (Beijing-IHEP, Dalian, Hefei, Jilin, Shanghai), India (Delhi), Israel (Tel Aviv)
Full member list: www.cern.ch/rd50
LPHNE, UPMC; Université Paris-Diderot; CNRS/IN2P3, Paris Marco Bomben, Giovanni Calderini, J.Chauveau, F.Crescioli, Giovanni Marchiori
IJCLab - Laboratoire de Physique des 2 Infinis, Irène Joliot-Curie L.Iconomidou-Fayard, Abdenour Lounis, C.Nellist
CPPM Marseille; Marlon Barbero, P.Barrillon, P.Breugnon, A.Habib, P.Pangaud, M.Zhao
Last RD50 Workshop: 28.11.-1.2.2023
..followed by a new collaboration called DRD3

## Slide 49: Device engineering example: n-in-p sensors
Why will we use p-type strip/pixel sensors (n-in-p) for the LHC upgrade in ATLAS and CMS instead of p-in-n sensors?
Why are segmented sensors(*) build on p-type silicon sensors radiation harder than n-type sensors?
p-in-n
n-in-p
Need inter strip isolation!
(*) 300 mm

## Slide 50: Sensor Signal: Pad vs. Strip/Pixel
Signal = Induced charge on read-out electrode
  Described by Shockley-Ramo Theorem
  Charged induced on electrode by moving charge can be calculated from the weighting potential (field)
Pad
Strip
  Total collected charge in both cases 100% (Q = q) when charges have reached the electrodes, however
    Diode: 50% from (+q); 50% from (-q)
    Strip: 87% from (+q); 13% from (-q)
  In a p-in-n strip sensor the holes give a higher contribution to the (m.i.p.) signal than the electrons!

## Slide 51: Device engineering: p-in-n vs. n-in-p (or n-in-n)
p-in-n silicon, under-depleted:
Charge spread – degraded resolution
Charge loss – reduced CCE
p+in-n
n-in-p silicon, under-depleted:
Limited loss in CCE
Less degradation with under-depletion
Collect electrons (3 x faster than holes)
n+in-p
n-type silicon after high fluences: (type inverted)
p-type silicon after high fluences: (still p-type)
Comments: - Instead of n-in-p also n-in-n devices could be used - Reality is much more complex: Usually double junctions form leading to fields at front and back! (next slide)

## Slide 52: E-Field after irradiation: “double junctions”
n-in-p sensor still “p-type” (i.e. highest field at front electrode) after high level of radiation
Investigation by measurement
Dominant junction close to n+ readout strip for FZ n-in-p
[G.Kramberger et al, 2014 JINST 9 P10016]
…to add more complexity
different particle irradiation on identical sensors
neutron irradiated 7×1015 neq/cm2
proton irradiated 7×1015 neq/cm2
[S.Pape, 43rd RD50 Workshop, 29. November 2023]

## Slide 53: Double Junction
Double Junction = Polarization Effect
[V.Eremin et al., NIMA 476 (2002) 556-564]
Double junction in TCAD (see e.g. M.Bomben, SIMDET 2020 in Nov. 2021)

## Slide 54: Device engineering example: n-in-p sensors
p-in-n
n-in-p
Need inter strip isolation!
Sensors in LHC trackers today HL-LHC trackers tomorrow (2028) (ATLAS/CMS) (… in production now)

## Slide 55: ATLAS Phase II
Strips & Pixel
all n-in-p
F.Hartmann, Last RD50 Workshop, Nov.2023

## Slide 56: CMS Phase II
Outer Tracker modules in final configuration – n-in-p
Pixel Tracker module – n-in-p
High Granularity Calorimeter – n-in-p
F.Hartmann, Last RD50 Workshop, Nov.2023

## Slide 57: Device engineering example: 3D Hybrid Pixel Detectors
Array of narrow electrode columns (~ 5-10mm) passing through the silicon thickness (micromaching):
Depletion voltage prop. spacing2
Collection time prop. spacing
Reduced charge sharing
 More suited to high radiation environment
Connected to standard pixel ASIC – hybrid pixel detector
Installed 2014 in ATLAS IBL (Inner b-layer)
& inner pixel layers for LHC phase II (2028)

## Slide 58: TCAD simulations

## Slide 59: TCAD simulations
Why do we need TCAD simulations for understanding (irradiated) sensors ?
  Complexity of the problem: Coupled differential equations (semiconductor equations)
  Complex device geometry and complex signal formation in segmented devices ….
  Evaluation of new an innovative design approaches
  Impact of defects depending on local charge densities, field-strength, … (“feedback loop”)
  Interplay of surface and bulk damage..
Electric field distribution in 3D detector (Al & oxide layer transparent for clarity)
n+
n+
Column depth =
bulk thickness
Np,n = 5e18 cm-3
Nbulk = 1.7e12 cm-3
Doping profiles
3D sensor: T.Peltola (HIP, Helsinki): CMS & RD50
p+
V=0
n+
Vbias
Vbias
Vbias
Vbias
3D detector
Details in the following presentations

## Slide 60: Device simulation: TCAD & signal simulators
Status of TCAD device simulations
  Required by complexity of the problem:
    solve semiconductor equations with physics properties, complex geometry and radiation damage
    mainly commercial tools used (Silvaco and Synopsis)
  Excellent tools for sensor optimization
Radiation damage TCAD: enormous progress over recent years
  getting predictive power but need further optimization!
  “effective” defect levels (2 to 5 levels) are used
Signal simulators
  TCAD simulations for signal formation are complex (time consuming, TCAD is not a fitting tool!)
  Custom build signal simulators (open code) developed: sensor optimization, parameter fitting
    ..using E-Field and other parameters (e.g. charge trapping) from TCAD as input
needs more work !
Measured defects TCAD input
PixelAV, KdetSim, Garfield++, Weightfield2, TRACS,
(unpublished codes), ...

## Slide 61: Summary
Silicon Sensors are based on reverse biased pn-junctions (silicon sensors are reverse biased diodes)
Silicon Detectors at the LHC and upgrade of LHC
  Inner tracking at LHC and HL-LHC done by silicon detectors
  Hybrid-pixel (planar and 3D) and strip sensors implemented in LHC experiments (ALICE upgraded to monolithic sensors)
  Radiation Hard Monolithic sensors under development (competing beyond LS3 for HL-LHC upgrades)
Radiation Damage in Silicon Sensors
  Damage: displacement damage that is evidenced as defect levels in the band gap of the semiconductor (+ some impact of surface damage in segmented sensors)
  Modification of internal electric field (space charge distribution, depletion voltage, “type inversion”, reverse annealing, loss of active volume, …), defect engineering possible!
  Increase of Leakage Current and Charge Trapping (same for all silicon materials)
  Signal to Noise ratio is quantity to watch (material + geometry + electronics)
Radiation tolerant silicon sensors
  Several examples of successful Material and Device Engineering (mitigation strategies) oxygenation, 3D sensors, p-type (n-readout) sensors
“Hot topics” in R&D on radiation hard silicon sensors
  Sensors for timing (i.e. LGAD with intrinsic gain, acceptor removal); monolithic sensors; CMOS; re-evaluation of SiC and Diamond sensors
  Reliability of TCAD simulations with defects; characterization of damage beyond 1016 cm-2

## Slide 62: Acknowledgements & References
Most references to particular works given on the slides
  RD50 workshop presentations: http://www.cern.ch/rd50/
  Conferences: VERTEX, PIXEL, RESMDD, …
Instrumentation Schools
  ICFA, EDIT, ESI, CERN & DESY Summer Student Lectures
Books about silicon tracking detectors (and radiation damage)
  Helmuth Spieler, “Semiconductor Detector Systems”, Oxford University Press 2005
  C.Leroy, P-G.Rancoita, “Silicon Solid State Devices and Radiation Detection”, World Scientific 2012
  Frank Hartmann, “Evolution of silicon sensor technology in particle physics”, Springer 2009 & 2017 (2023: writing on new edition)
  L.Rossi, P.Fischer, T.Rohe, N.Wermes “Pixel Detectors”, Springer, 2006
  Gerhard Lutz, “Semiconductor radiation detectors”, Springer 1999
  Hermann Kolanoski and Norbert Wermes, “Particle Detectors – Fundamentals and Appilcations”, Oxford University Press 2020
Review Articles
  2018: Garcia-Sciveres and Wermes, A review of advances in pixel detectors for experiments with high rate and radiation, https://doi.org/10.1088/1361-6633/aab064
  2018: M.Moll, Displacement Damage in Silicon Detectors for High Energy Physics https://doi.org/10.1109/TNS.2018.2819506
  2021: Radiation Effects in the LHC-Experiments, 154 pages, CERN Yellow Report https://cds.cern.ch/record/2764325
Research collaborations and web sites
  CERN RD50 collaboration (http://www.cern.ch/rd50 ) - Radiation Tolerant Silicon Sensors
  CERN RD42 collaboration – Diamond detectors
  Inter-Experiment Working Group on Radiation Damage in Silicon Detectors (CERN) – CERN Yellow Report
  ATLAS IBL, ATLAS and CMS upgrade groups

## Slide 63: Backup Slides

## Slide 64: Collisions in the LHC
2012 – Discovery of the Higgs Boson

## Slide 65: Microscopic Damage Formation of Defects and Impact on Detectors

## Slide 66: Radiation Damage – Microscopic effects
Spatial distribution of vacancies created by a 50 keV Si-ion in silicon. (typical recoil energy for 1 MeV neutrons)
I
I
V
V
van Lint 1980
M.Huhtinen 2001
particle
SiS
Vacancy + Interstitial
point defects (V-O, C-O, .. )
point defects and clusters of defects
EK>25 eV
EK > 5 keV
V
I

## Slide 67: NIEL – Non Ionizing Energy Loss
Displacement Damage Function
  Normalization of radiation fields to 1 MeV neutron equivalent damage (neq)
NIEL Hypothesis:
  Assumption: NIEL scaling of damage parameters
  Applied to predict damage of radiation fields in HEP
  NIEL violation observed:
    Material dependence
    Proton vs. neutron damage
    …
    Acceptor removal ?
[Data: A.Vasilescu and G.Lindstroem]
1
1 MeV
0.62 (23 GeV protons)
1.85 (26 MeV protons)
2.20 (23 MeV protons)
1.14 (192 MeV pions)
0.92 (TRIGA reactor neutrons)
[M.Huhtinen, NIMA 491(2002), 194]
10 MeV protons 23 GeV protons 1 MeV neutrons
Simulation: Vacancies in (1m)3 after 1014 particles/cm2
Notes: Allport 2019

## Slide 68: Radiation induced defects with impact on device performance
RD50 map of most relevant defects for device performance near room temperature:
BiOi (acceptor removal)
Phosphorus: shallow dopant (positive charge)
BD: positive charge higher introduction after proton than after neutron irradiation, oxygen dependent
E30: positive charge higher introduction after proton irradiation than after neutron irradiation
Leakage current: V3
Reverse annealing (negative charge)
Boron: shallow dopant (negative charge)
leakage current & neg. charge current after  irrad, V2O (?)
  Trapping: Indications that E205a and H152K are important (further work needed)
  Converging on consistent set of defects observed after p, p, n, g and e irradiation.
  Defect introduction rates are depending on particle type and energy, and some on material!

## Slide 69: Some TCAD models from literature
Several models available (non exhaustive list):
Table: M.Moll, Displacement Damage in Silicon Detectors, doi.org/10.1109/TNS.2018.2819506

## Slide 70: Macroscopic Damage Degradation of Detector Performance

## Slide 71: Summary: Basics of Radiation Damage in Silicon Sensors
Two general types of radiation damage to the detector materials:
 Bulk (Crystal) damage due to Non Ionizing Energy Loss (NIEL) - displacement damage, built up of crystal defects –
  Change of effective doping concentration & acceptor/donor removal (higher depletion voltage, under- depletion)
  Increase of leakage current (increase of shot noise, thermal runaway)
  Increase of charge carrier trapping (loss of charge)
 Surface damage due to Ionizing Energy Loss (IEL) - accumulation of positive in the oxide (SiO2) and the Si/SiO2 interface – affects: interstrip capacitance (noise factor), breakdown behavior, …
Impact on detector performance and Charge Collection Efficiency (depending on detector type and geometry and readout electronics!) Signal/noise ratio is the quantity to watch
 Sensors can fail from radiation damage !
Same for all tested Silicon materials!
Influenced by impurities in Si – Defect Engineering is possible!
Can be optimized!
Notes: 71
71
efficacité de collection de charge influencé par deux mécanisme
piégeage – porteurs de charge sont pièges par les défaut profond
déficit de collection de charge augmente en fonction de la fluence

## Slide 72: Radiation Damage in the LHC Experiments (Silicon Detectors)

## Slide 73: Radiation Effects in LHC Experiments
5 workshops on “Radiation Effects at LHC Experiments and Impact on Operation and Performance” organized (2011 - 2019)
  Common Workshop: (ALICE), ATLAS, CMS, LHCb, RD50
    Sensor Measurements
    Electronics/Optoelectronics
    Radiation Simulation and Monitoring
    Sensor Simulation
Outcome and follow-up:
  Generally good agreement between RD50 damage prediction models (e.g.“Hamburg model”) and radiation damage observed by the LHC experiments.
  More coherent approach in data analyses agreed and documented.
  Modelling will have to be refined in some areas for run 3 !
CERN Yellow Report written and edited by a team from RD50 & all LHC experiments has been published (154 pages, Radiation effects in the LHC experiments https://cds.cern.ch/record/2764325) summarizing observations, comparing results from different experiments against each other, listing open questions and outlining further work towards Run 3.
  [https://indico.cern.ch/event/769192]
  [https://cds.cern.ch/record/2764325 ]

## Slide 74: Radiation Effects in LHC Experiments
Review of radiation effects in the LHC Experiments in several workshops [INDICO]
  Common working group: RD50 & LHC experiments  Publication of a summary report in April 2021 [CERN Yellow Report link]
ATLAS B-layer data vs. MC&NIEL strong z-dependence; unexpected
Plots: Radiation Effects Workshop Feb.2019 K.Mochizuki(ATLAS SCT) J.L.Agram (CMS Tracker), Aiden Grummer (ATLAS Pixel) , G.Sarpis (LHCb Velo) , F.Feindt (ATLAS Pixel)
Leakage currents in ATLAS SCT and CMS tracker and model predictions
LHCb Velo depletion voltage reduced by annealing; according to model
CMS pixel layers; deviation of Vdep from modelling at high fluences

## Slide 75: How to increase the radiation hardness?

## Slide 76: Approaches to develop radiation harder solid state tracking detectors
Defect Engineering of Silicon Deliberate incorporation of impurities or defects into the silicon bulk to improve radiation tolerance of detectors
  Needs: Profound understanding of radiation damage
    microscopic defects, macroscopic parameters
    dependence on particle type and energy
    defect formation kinetics and annealing
  Examples:
    Oxygen rich Silicon (DOFZ, Cz, MCZ, EPI)
    Oxygen dimer & hydrogen enriched Si
    Pre-irradiated Si
    Influence of processing technology
New Materials
  Silicon Carbide (SiC), Gallium Nitride (GaN)
  Diamond (CERN RD42 Collaboration)
  Amorphous silicon, Gallium Arsenide
Device Engineering (New Detector Designs)
  p-type silicon detectors (n-in-p)
  thin detectors, epitaxial detectors
  3D detectors and LGAD - Low Gain Avalanche
  Cost effective detectors
  Monolithic devices – HV-CMOS
Scientific strategies:
Material engineering
Device engineering
Change of detector operational conditions
CERN-RD39 (closed, now part of RD50) “Cryogenic Tracking Detectors” operation at 100-200K to reduce charge loss