## Slide 1: Detector Development at the MPG - HLL
Alexander Bähr on behalf of the MPG-HLL

## Slide 2: Semiconductor laboratory of the Max-Planck Society
Central facility of the Max Planck Society with 40 employees: scientists, engineers and technicians + guest scientists, engineers and students
At present @ Siemens Campus Neuperlach Munich
1000m2 of clean room area
330m2 of ISO3 area
Full 6 inch silicon process line
IPP Campus Garching
1500m2 of clean room area
600m2 of ISO3 & ISO4 area
8 inch silicon process line
HLL will be part of Munich Quantum Valley
New building in autumn 2023 – move started

## Slide 3: HLL in a nutshell
Idea for a scientific experiment
within the research institutes
Ideas, simulations,
development
Fabrication, operational parameter extraction quality control
Testing, system development, qualification
Scientific experiment
performed by the institute
Assembly , integration, test, verification
MPG HLL
MPG HLL R&D
Optimal sensor for the given science case

## Slide 4: (some) HLL Sensor examples
electron (7GeV)
positron (4GeV)
Vertex Detector
2 layers DEPFET + 4 layers DSSD
DePFETs at KEK - Japan
DePFET particle tracking
WFI aboard Athena
DePFET - X-ray imaging spectroscopy
curtesy ESA
We also produce
-SDD (silicon drift detectors)
-Diodes
-Avalanche Diodes
-etc.
XMM-Newton
  pnCCD
  X-ray imaging spectroscopy
  curtesy ESA
DePFET -planetary science
curtesy ESA
MIXS abouard BepiColombo

## Slide 5: The DePFET
  MOSFET on n-substrate
  deep-n implant below gate
    positive potential
    „internal gate“ (IG)
    conductivity modulated by electrons
  reset via clear and clear gate
  good signal to noise
  unobstructed backside contact
  typical charge gain values ~420 pA/e-
  Applications:
    Belle II, BepiColombo, Athena, EDET, etc.
drain
source
Q(t)
signal(t)
clear gate
gate

## Slide 6: Device Simulations
3D device simulation - study complex geometries
charge collection, clear, etc
source
gate
drain
clear gate
clear
internal gate
source
gate
drain
2D device simulation – DePFET transistor properties
charge gain, noise, impact ionization, etc

## Slide 7: 2d simulation flow
Process
Simulation
Electrical
Simulation
Signal Response
Impact Ionization
Noise
I-V characteristics
operation point
charge gain (current readout)
gain (source follower)
at the moment only white noise
source
gate
drain
cause additional electrons in
the internal gate

## Slide 8: Comparing Measurements and Simulations – 2D
 | Tn-1 | Tn-2 | Tn-3 | Tn-4 | Tk-1 | Tk-2 | Tk-3 | LG1 | LG2 | LG3 | LG4
Source | [2] | [2] | [2] | [2] | [2] | [2] | [2] | [3] | [3] | [3] | [3]
Technology | Thin Halo | Thin | Thin | Thin Plasma | Thick | Thick | Thick Plasma | Thick | Thick | Thick | Thick
W/L | 20/5 | 20/5 | 20/5 | 24/5 | 20/5 | 20/5 | 24/5 | 20/5 | 24/4 | 24/4.5 | 24/5
Measured |  |  |  |  |  |  |  |  |  |  | 
[µS] | 64.6 | 64.94 | 64.45 | 70.18 | 48.75 | 48.74 | 49.47 | 50.3 | 66.5 | 60.3 | 57.5
Gain [µV/e] | 6.2 | 5.95 | 5.66 | 4.86 | 8.06 | 8.28 | 6.75 | 8.19 | 8.98 | 7.69 | 6.88
@ current [µA] | 100 | 100 | 100 | 100 | 177 | 199 | 188 | 133 | 221 | 188 | 155
ENC | 2.2 | 2.44 | 2.38 | 2.69 | 1.95 | 2.04 | 2.18 | 1.95 | 1.95 | 2.09 | 2.22
2D Simulation |  |  |  |  |  |  |  |  |  |  | 
[µS] | 69.39 | 65.89 | 65.89 | 69.51 | 53.98 | 53.98 | 53.46 | 53.98 | 63.78 | 61.26 | 59.38
Gain [µV/e] | 5.75 | 5.42 | 5.42 | 4.47 | 8.04 | 7.94 | 7.38 | 8.18 | 8.47 | 7.60 | 6.94
 | Tn-1 | Tn-2 | Tn-3 | Tn-4 | Tk-1 | Tk-2 | Tk-3 | LG1 | LG2 | LG3 | LG4
Source | [2] | [2] | [2] | [2] | [2] | [2] | [2] | [3] | [3] | [3] | [3]
Technology | Thin Halo | Thin | Thin | Thin Plasma | Thick | Thick | Thick Plasma | Thick | Thick | Thick | Thick
W/L | 20/5 | 20/5 | 20/5 | 24/5 | 20/5 | 20/5 | 24/5 | 20/5 | 24/4 | 24/4.5 | 24/5
Measured |  |  |  |  |  |  |  |  |  |  | 
 | 64.6 | 64.94 | 64.45 | 70.18 | 48.75 | 48.74 | 49.47 | 50.3 | 66.5 | 60.3 | 57.5
Gain [µV/e] | 6.2 | 5.95 | 5.66 | 4.86 | 8.06 | 8.28 | 6.75 | 8.19 | 8.98 | 7.69 | 6.88
@ current [µA] | 100 | 100 | 100 | 100 | 177 | 199 | 188 | 133 | 221 | 188 | 155
ENC | 2.2 | 2.44 | 2.38 | 2.69 | 1.95 | 2.04 | 2.18 | 1.95 | 1.95 | 2.09 | 2.22
2D Simulation |  |  |  |  |  |  |  |  |  |  | 
 | 69.39 | 65.89 | 65.89 | 69.51 | 53.98 | 53.98 | 53.46 | 53.98 | 63.78 | 61.26 | 59.38
Gain [µV/e] | 5.75 | 5.42 | 5.42 | 4.47 | 8.04 | 7.94 | 7.38 | 8.18 | 8.47 | 7.60 | 6.94
% | 7.41 | 1.46 | 2.23 | -0.95 | 10.72 | 10.75 | 8.06 | 7.32 | -4.09 | 1.59 | 3.27
 | 7.41 | 1.46 | 2.23 | -0.95 | 10.72 | 10.75 | 8.06 | 7.32 | -4.09 | 1.59 | 3.27
% | -7.26 | -8.91 | -4.24 | -8.02 | 1.49 | -1.21 | 9.33 | -0.12 | -5.68 | -1.17 | 0.87
 | -7.26 | -8.91 | -4.24 | -8.02 | 1.49 | -1.21 | 9.33 | -0.12 | -5.68 | -1.17 | 0.87
W. Treberspurg et. al, “Measurement results of different
options for spectroscopic X-ray DEPFET sensors”, JINST 13, P09014, 2018
W. Treberspurg et. al “Layout options of spectroscopic X-ray DePFETs”, JINST 14, 2019
Measurements on Athena prototype DeFPETs
different technology, different geometry

## Slide 9: Comparing Measurements and Simulations – 2D - Noise
 | LG2 | LG1 | Tk-1 | Tk-2 | LG3 | Tk-3 | Tn-1 | LG4 | Tn-3 | Tn-2 | Tn-4
Source | [3] | [3] | [2] | [2] | [3] | [2] | [2] | [3] | [2] | [2] | [2]
Technology | Thick | Thick | Thick | Thick | Thick | Thick Plasma | Thin Halo | Thick | Thin | Thin | Thin Plasma
W/L | 24/4 | 20/5 | 20/5 | 20/5 | 24/4.5 | 24/5 | 20/5 | 24/5 | 20/5 | 20/5 | 24/5
Measured |  |  |  |  |  |  |  |  |  |  | 
ENC | 1.95 | 1.95 | 1.95 | 2.04 | 2.09 | 2.18 | 2.2 | 2.22 | 2.38 | 2.44 | 2.69
increasing measured noise
with one exception
increasing simulated white noise
W. Treberspurg et. al, “Measurement results of different
options for spectroscopic X-ray DEPFET sensors”, JINST 13, P09014, 2018
W. Treberspurg et. al “Layout options of spectroscopic X-ray DePFETs”, JINST 14, 2019
Measurements on Athena prototype DeFPETs
different technology, different geometry
at the moment only white noise
1/f noise is not included
2D Simulation |  |  |  |  |  |  |  |  |  |  | 
[pA/e] | 1019 | 741 | 758 | 763 | 849 | 626 | 551 | 709 | 505 | 505 | 434
[pA²/Hz] | 1.98 | 1.11 | 1.27 | 1.34 | 1.62 | 0.99 | 1.13 | 1.33 | 1.08 | 1.08 | 1.13
 | 1,38 | 1,42 | 1,49 | 1,52 | 1,50 | 1,59 | 1,93 | 1,62 | 2,06 | 2,06 | 2,45
2D Simulation |  |  |  |  |  |  |  |  |  |  | 
 | 1019 | 741 | 758 | 763 | 849 | 626 | 551 | 709 | 505 | 505 | 434
 | 1.98 | 1.11 | 1.27 | 1.34 | 1.62 | 0.99 | 1.13 | 1.33 | 1.08 | 1.08 | 1.13
 | 1,38 | 1,42 | 1,49 | 1,52 | 1,50 | 1,59 | 1,93 | 1,62 | 2,06 | 2,06 | 2,45

## Slide 10: Comparing Measurements and Simulations – 2D - Impact Ionization
measured

## Slide 11: Comparing Measurements and Simulations – 2D - Impact Ionization
Drain
Source
Gate
Potential Distribution
Electric Field
Impact Ionization
Drain
Source
Gate
Drain
Source
Gate

## Slide 12: Comparing Measurements and Simulations – 2D - Impact Ionization
good qualitative agreement of onset
measured
simulated

## Slide 13: Verification of Simulations
Measured gm and gain met within ±10%
Measured noise correlates with simulated white noise
qualitative agreement of impact ionization between simulations and measurements
overall good agreement between simulations and measurements
utilize simulations for study of DePFET improvements

## Slide 14: Improving the DePFET - Scaling
source
gate
drain
source
gate
drain
reduce gate length to minimize the internal gate and increase charge gain

## Slide 15: Improving the DePFET - Scaling
gate width of 20µm
readout time of 5 µs
gate width of 20µm
readout time of 5 µs

## Slide 16: Improving the DePFET - Super gq
source
gate
drain
internal gate
source
gate
drain
additional n-implant

## Slide 17: Improving the DePFET - Super gq
gate width of 20µm
readout time of 5 µs

## Slide 18: 2D simulations - recap
we verified our simulations against measurements
  overall good agreement
we studied the effects of scaling on the DePFET
  overall improvement but limits due to impact ionization
we developed a new DePFET technology
  decoupling internal and external gate size
  improving gq
  reducing impact ionization

## Slide 19: One example of 3d Simulations - Quadorpix
Quadropix: combination of 4 DePFETs into a Superpixel structure
Designed for the use in fast optical polarimetry
Layout scetch
functional principle
device simulation

## Slide 20: Quadropix - Asymmetrie of charge collection
3x3 Array
A
B
C
D
A
B
C
D
1 Superpixel
(4 DePFETs)
charge spreading

## Slide 21: Quadropix - Improvements
charge spreading

## Slide 22: DePFET test production
Production finished recently
Test of new DePFET technologies
reference (2)
reference + HE (2)
optimized (4)
super gq (2)
DePFET Layouts | 
Belle DePFET | fast readout
Athena DePFET | spectroscopy
Small DePFET | 15 – 30 µm test devices
Infinipix | 2 storage nodes per pixel
Quadropix | 4 storage nodes per pixel
RNDR DePFET | low noise (subelectron)
Production started October 2022

## Slide 23
Summary
Simulations are a useful tool to gain „insight“ into devices
Simulations can be a tool to predict the behaviour of devices
for well tested and known regions, quantitative agreement within 10% is possible
for less well known regions at least qualitative agreement is possible
Simulations are a crucial part of sensor development
Outlook
Lab is currently moving into a new building
reassembly and qualification until mid to end of 2024
Test of prototyping run start of 2024
cross check between measurements and simulations
-> next SimDet

## Slide 24: Thanks for your attention
Alexander Bähr on behalf of the MPG-HLL

## Slide 25: DePFET layouts
Standard
Belle Type
55 x 50 µm²
fast readout
Athena Type
130 x 130 µm²
imaging spectroscopy
Small Pixels
15 x 15 µm² to 30 x 30 µm²
“limit” test
drift 2
S
D
G
S
D
G
CG
CG
CL
CL
CL
D
D
S
G
G
CL
D
S
G
S
drift
drift
drift 1

## Slide 26: DePFET layouts
Multiple storages
Infinipix
2 storage nodes
selectable charge collection
suppress rolling shutter effects
Quadropix
4 storage nodes
selectable charge collection
suited for high precision polarimetry
RNDR DePFETs
repetitive non destructive readout (RNDR)
subelectron noise
single electron resolution
S
D
G1
G2
TG
CG
S
S
G1
G2
G1
G2
D1
D2
D1
D2
D4
D3
CG
CL
CG
CL
CL