## Slide 1: Development of a decontamination process for radioactive effluents
Mathurin Robin, TOMO SUZUKI, Abdesselam abdelouas, Marcel mokili

## Slide 2: Summary
3
4
5
2
1
Introduction
Synthetic Samples
Active
Samples
Surrogate Samples
Perspectives
PREDIS
Context
Objectives
Optimisation
Characterisation
Oxalic acid
Precipitant
Elements
Decontamination factor
2

## Slide 3
WP4
WP5
WP6
WP7
PREDIS Project
3
3
3
Belgoprocess, Belgium
SURAO, Czech Republic
SERAW, Bulgaria
NIRAS/ONDRAF, Belgium
ENGIE SA, Belgium
PURAM, Hungary
Campoverde srl, Italy
Fortum, Finland
SVAFO, Sweden
Studsvik, Sweden
SKB, Sweden
ARAO, Slovenia
COVRA, Netherlands
Vattenfall, Sweden
LLW Repository Ltd, United Kingdom
Chornobyl NPP, Ukraine
Nagra, Switzerland
ITER, France
Andra, France
TVO, Finland
Copyright © Free Vector Maps.com
https://freevectormaps.com/world-maps/europe/WRLD-EU-01-0002?ref=atr
Idaho National Laboratory, United States
URENCO Ltd, United Kingdom
1. Introduction
2. Synthetic samples
3. Surrogate samples
4. Active sample
5. Perspectives
3

## Slide 4
Characterisation
Characterisation
Encapsulation
Task 4.5
Task 4.6
Minimize the amount of Radioactive Metallic Waste (RMW)
Develop a new reference for the storage and final disposal of RMW
Estimate the potential opportunity for optimizing European RMW management
Decontamination & Treatment
Encapsulation
Task 4.4
Task 4.5
Task 4.6
Objectives of WP4
1. Introduction
2. Synthetic samples
3. Surrogate samples
4. Active sample
5. Perspectives
4

## Slide 5
Context
Deposition of radionuclides from primary circuit
Non-contaminated metal
Non-contaminated metal
+
Radioactive effluent
Decontamination
Surface contamination
Deep contamination
CORD process :
Decontamination by chemical oxidation-reduction
Use of KMnO4 and H2C2O4
Dissolution of most metals on the surface
1. Introduction
2. Synthetic samples
3. Surrogate samples
4. Active sample
5. Perspectives
5

## Slide 6
Objectives
1. Introduction
2. Synthetic samples
3. Surrogate samples
4. Active sample
5. Perspectives
Reduction of secondary effluent volume by concentrating radionuclides in solid form
+
Optimisation of chromatographic separation of residual radionuclides
The protocol needs to be cheap, fast and adaptable at large scale.
Radioactive effluent
Solid waste
!
Reduce the amount of resin required as much as possible
+
Cationic resin
Decontaminated effluent
6

## Slide 7
Experimental protocol
Oxide
Hydroxide
Sulphide
Phosphate
Chloride
Fluoride
Several types of precipitates are possible :
Oxide
Hydroxide
Sulphide
Phosphate
Chloride
Fluoride
Cheap reagent, fine for WAC, safe and fast
Low density sludge, pH dependant
Filtration
ICP-MS
Supernatant
Precipitate
Precipitate
Synthetic sample
pH ≈ 1.5 – 2
Fe / Ni / Cr / Co / Zn / Mn / Ce
Precipitation with NaOH 1M
pH 8,5
Fe / Cr / Co / Zn / Ce
Precipitation with NaOH 1M
pH 12
Ni / Co / Zn / Mn
Supernatant
1. Introduction
2. Synthetic samples
3. Surrogate samples
4. Active sample
5. Perspectives
7

## Slide 8
Optimisation
Precipitation pH:
Modelling with PHREEQC software
Study of solubility of metal hydroxides as a function of pH
Precipitation with NaOH
Results :
Two optimum precipitation pH values to precipitate all metals in solution
pH 8.5 (Fe, Cr, Zn, Ce)
pH 12 (Co, Mn, Ni, Ag)
1. Introduction
2. Synthetic samples
3. Surrogate samples
4. Active sample
5. Perspectives
8

## Slide 9
Test on synthetic sample
Elements | % precipitated pH 8.5 | % precipitated pH 12
52Cr | 100.0 | 100.0
55Mn | 48.4 | 100.0
56Fe | 100.0 | 100.0
59Co | 76.8 | 100.0
60Ni | 84.3 | 100.0
66Zn | 99.2 | 99.9
121Sb | 100.0 | 99.9
140Ce | 100.0 | 100.0
Total : | 77.0 | 100.0
1. Introduction
2. Synthetic samples
3. Surrogate samples
4. Active sample
5. Perspectives
9

## Slide 10
Characterisation
1. Introduction
2. Synthetic samples
3. Surrogate samples
4. Active sample
5. Perspectives
First precipitate :
Fe(OH)3·nH2O
FeO(OH)·nH2O
Second precipitate :
Mn3O4
MnO.Mn2O3
10
Fourier-transform infrared spectroscopy (FTIR) :
Metal-Oxygene bonds (M-O)
Hydrogen bonds
Unbound water molecules
Thermogravimetric analysis (TGA) :
Crystallisation pics (hydroxide → oxide)
Changes in the crystalline structure of iron oxide
X-rays diffraction (XRD) :
Amorphous or nano-crystalised solid below 200°C
Iron oxide at high temperature
Manganese oxide at room temperature
Fourier-transform infrared spectroscopy (FTIR) :
Metal-Oxygene bonds (M-O)
Hydrogen bonds
Unbound water molecules
Thermogravimetric analysis (TGA) :
Crystallisation pics (hydroxide → oxide)
Changes in the crystalline structure of iron oxide
X-rays diffraction (XRD) :
Amorphous or nano-crystalised solid below 200°C
Iron oxide at high temperature
Manganese oxide at room temperature

## Slide 11
Tests on surrogate sample
+
CORD process
Precipitation
KMnO4
H2C2O4
pH 8.5
pH 12
Elements | % precipitated
52Cr | 45.43
55Mn | 100.00
56Fe | 99.97
60Ni | 99.93
Total : | 99.29
Competition between chromium hydroxide and oxalate1 ?
1E. Remoundaki (2007)
1. Introduction
2. Synthetic samples
3. Surrogate samples
4. Active sample
5. Perspectives
11

## Slide 12
Oxalic acid destruction
Master 2 internship (Cavit Percin) :
Development and optimisation of an oxalic acid destruction protocol
H2O2 concentrations: 0.1 / 0.5 / 1 M
Heating time: 1 to 48h
UV light
Temperature : 65 and 80°C
Test on simulated samples to observe the influence of the protocol on chromium precipitation
1. Introduction
2. Synthetic samples
3. Surrogate samples
4. Active sample
5. Perspectives
12

## Slide 13
Precipitant
NaOH
KOH
Na2S
Na3PO4
1. Introduction
2. Synthetic samples
3. Surrogate samples
4. Active sample
5. Perspectives
13

## Slide 14
Complex sample
Sample contaminated with a multi-element acid solution (spent fuel simulation)
1. Introduction
2. Synthetic samples
3. Surrogate samples
4. Active sample
5. Perspectives
14

## Slide 15
1. Introduction
2. Synthetic samples
3. Surrogate samples
4. Active sample
5. Perspectives
Complex sample
First precipitation (KOH – pH 8.5)
  Hydroxide form -> ex : Fe(OH)3
  High efficiency (> 96%)
Second precipitation (KOH – pH 12)
  Main component is Mn3O4
  Really important to remove Mn (0.4 g/L initially)
Second precipitation (Na2S – pH 12)
  Main component is Mn3O4 and S8
  Efficient only for chromium
Not precipitated
  Requires use of resins
Not measured
15

## Slide 16
Active sample
SEM
Radionuclide | Energy | Intensity | Average Activity | 
 | keV | % | (Bq/g) | error
Mn-54 | 834.85 | 99.98 | 112.21 | 22.65
Co-57 | 122.06 | 85.51 | 13.59 | 6.94
Co-60 | 1173.23 | 99.85 | 24442.50 | 1391.60
 | 1332.49 | 99.98 |  | 
Sb-125 | 427.87 | 29.55 | 116.87 | 31.28
 | 463.36 | 10.48 |  | 
 | 600.6 | 17.76 |  | 
Total (Bq/g) |  |  | 24559.37 | 1391.95
Total (Bq) |  |  | 12002.16 | 680.25
Analysis using HPGe Gamma detector
  Count time of 15 minutes
Sample weighing 0.48g
  Total activity of 24559 ± 1392 Bq/g
  99.5% coming from Co-60.
1. Introduction
2. Synthetic samples
3. Surrogate samples
4. Active sample
5. Perspectives
16

## Slide 17
1. Introduction
2. Synthetic samples
3. Surrogate samples
4. Active sample
5. Perspectives
Active sample
Decontamination factors measured with
  Gamma spectrometry (HPGe detector)
  Dose rate (Gamma and X-ray detectors)
  Liquid scintillation (0 – 2000 keV)
First precipitation (KOH – pH 8.5)
  % ≈ 29 ± 9
  DF ≈ 1.2
Second precipitation (KOH – pH 12)
  % ≈ 103 ± 3
  DF ≈ 3330
  The main contribution in terms of activity is 60Co
  Cobalt precipitates between pH 10 and 12
17

## Slide 18: Perspectives
Optimisation of oxalic acid destruction
    Reduce the impact on the environment (LCA)
    Ratio H2O2 concentration / heating time
Hydroxide precipitation by electrocoagulation
    Avoid the use of precipitants
    Improved efficiency
Optimization of cationic resins in collaboration with Triskem International
    Removal of traces of remaining radionuclides
    Removal of non-precipitated elements
Articles under formulation
    Oxalic acid destruction, in collaboration with NNL
    Contaminated SG samples
1. Introduction
2. Synthetic samples
3. Surrogate samples
4. Active sample
5. Perspectives
18

## Slide 19
Contact information
robin@subatech.in2p3.fr
SUBATECH (IMT Atlantique, CNRS/IN2P3, Université de Nantes), BP 20722, 44307 Nantes Cedex 3, France
19

## Slide 20
Characterisation (FTIR)
Chart: Wavenumber (cm-1)
Chart: Wavenumber (cm-1)
First precipitate at pH 8.5
Second precipitate at pH 12
ν = 3000 – 3500 cm-1/ OH bonds and hydrogen bonds1,2
ν = 1650 cm-1/ Corresponds to unbound water molecules1,2
ν = 1350 – 1400 cm-1/ Metal-oxygen bonding
1 S. Nasrazadani (1997)
²M. S. Seehra (2004)

## Slide 21
Characterisation (TGA)
First precipitate at pH 8.5
Second precipitate at pH 12
Hypothesis1 :
Crystallisation from hydroxide to oxide form at around 160, 220°C
Change in crystalline structure at 520°C (γ-Fe2O3 -> α-Fe2O3)
No crystallisation or change in structure
Endothermic peak at 500°C with no loss of mass
1C. Vichery (2012)

## Slide 22
Characterisation (XRD)
1er précipité (pH 8.5)
2nd précipité (pH 12)
Mn3O4
α - Fe2O3
α - Fe2O3
γ - Fe2O3
α
γ
α
α
α