## Slide 1
GRAiNITA test bench updates: 3 May 2024
The preliminary results for CaWO4 grains (dry and with water) in TROLL-3 under
excitation with the cosmic muons:
Mean ~1060
Mean ~1240

## Slide 2
GRAiNITA test bench updates: 3 May 2024
The “yield” for CaWO4 grains is about 1.6 times higher in comparison with ZnWO4 grains
With adding of water we gain about 17-20% of light (both for CaWO4 and ZnWO4)
Condition | Counting gate, mks | Dark current, Nphe
ZnWO4 grains (TROLL-2, O-2(300) WLS fibers) | 25 | 46
CaWO4 grains (TROLL-3, Y-11 WLS fibers) | 12.5 | 35
Condition | Estimated number of phe | 
 | ZnWO4 grains (TROLL-2, O-2(300) WLS fibers) | CaWO4 grains (TROLL-3, Y-11 WLS fibers)
Dry | 660-650 | 1060
With water | 780-800 | 1240
! No dark current correction

## Slide 3
Brief summary
Using of CaWO4 grains for GRAiNITA
Advantages 
More light in comparison with ZnWO4
Two times shorter counting time (and lower dark current level)
Custom Y-11 WLS fibers (less self-absorption compare to O-2 WLS fibers)
Disadvantages 
Lower density (77.5% of ZnWO4) -> increase of the detector size…
Possible solution: partial substitution of Ca2+ ions to Pb2+ ions, i.e. scintillation grains
of Ca1-xPbxWO4 (“cook and look” approach)