## Slide 1: Design and optimisation of radiation resistant AC- and DC-coupled resistive LGADs
A. Fondacci, T. Croci, D. Passeri, R. Arcidiacono, N. Cartiglia, M. Boscardin, M. Centis Vignali, G. Paternoster, O. Hammad Ali, L. Lanteri, L. Menzio, F. Siviero, M. Ferrero, V. Sola, A. Morozzi, F. Moscatelli

## Slide 2: An impossible challenge?
Spatial resolution
Temporal resolution
Very low material budget
Very low power consumption
Each pixel requires a lot of power
Plenty of power
Bulky cooling infrastructure
The signal in thin sensors is very small
pixels/cm2
Is there a way to fulfil the four specifications simultaneously?
alessandro.fondacci@pg.infn.it

## Slide 3: An intriguing candidate for future colliders
alessandro.fondacci@pg.infn.it

## Slide 4: FBK RSD2 performance summary
pixels/cm2
Layout
Device made and bonded
alessandro.fondacci@pg.infn.it

## Slide 5: RSD LGAD: AC or DC coupled electrodes?
pixels/cm2
alessandro.fondacci@pg.infn.it

## Slide 6: Simulation approach (SPICE & TCAD)
pixels/cm2
SPICE: Quick estimation of the optimal sheet resistance (2 kΩ/sq)
Full 3D TCAD: Evaluation of various geometrical layouts (pad and pixel shapes and dimensions) and technological options (resistive strips and silicon oxide trenches) on signal-sharing properties.
2 kΩ/sq
alessandro.fondacci@pg.infn.it

## Slide 7: Playing with pad shape
MIP
MIP
Thickness = 20 µm;
Pitch = 20 µm;
Cross length = 16 µm ;
Cross width = 1 µm.
MIP
MIP
Thickness = 20 µm;
Pitch = 20 µm;
Pad radius = 2 µm.
alessandro.fondacci@pg.infn.it

## Slide 8: Silicon oxide trenches
MIP
MIP
MIP
MIP
alessandro.fondacci@pg.infn.it

## Slide 9: Watch out for contact resistance
MIP
MIP
alessandro.fondacci@pg.infn.it

## Slide 10: Radiation damage modelling @ PG
pixels/cm2
alessandro.fondacci@pg.infn.it

## Slide 11: After irradiation performances
8.0×1014 1 MeV neq/cm2
1.5×1015 1 MeV neq/cm2
As the fluence increases, the total collected charge decreases due to charge trapping.
However, the total collected charge is always divided in the same way by the resistive plane.
24.82
0.08
0.08
0.02
24.70
0.14
0.14
0.02
alessandro.fondacci@pg.infn.it
MIP
MIP
MIP
MIP

## Slide 12: Conclusions
DC-RSDs are promising candidates for future colliders (e.g. FCC);
Their first production was guided by comprehensive 3D TCAD simulations:
  The pads should be small to avoid introducing significant distortion into the impact point reconstruction;
  Pad-to-pad trenching effectively confines the signal when utilising small circular pads.
The wafers left the clean room a fortnight ago, and the first experimental measurements were carried out.
alessandro.fondacci@pg.infn.it

## Slide 13: Backup
pixels/cm2

## Slide 14: Heavy Ion Model
pixels/cm2
A MIP can be modelled through the Heavy Ion Model, whose generation rate is given by the following expression:
is a function describing the temporal variation of the generation rate;
  In particular, it’s a Gaussian function whose mean value represents the moment of the heavy ion penetration.
is a function describing the spatial variation of the generation rate;
  It too is a Gaussian and represents its standard deviation.
represents the linear energy transfer generation density, expressed in e/h pairs per cm3 by default .
How many e/h pairs are generated by the MIP for each µm crossed?
S. Meroli et al., Energy loss measurement for charged particles in very thin silicon layers, Journal of Instrumentation, vol. 06, P06013, Jun. 2011

## Slide 15: Charge imbalance algorithm
pixels/cm2

## Slide 16: Crosses of various sizes
pixels/cm2

## Slide 17: Crosses 🤼‍♂️ bars
pixels/cm2

## Slide 18: Resistive strips
pixels/cm2

## Slide 19: Silicon oxide trenches
pixels/cm2

## Slide 20: Different pad arrangements
pixels/cm2
Matrices of squares
Matrices of hexagons

## Slide 21: Different pad arrangements
pixels/cm2
Matrices of squares
Matrices of hexagons
Percentages by event type:
1-electrode: 30%
2-electrode: 40%
3-electrode: 14%
4-electrode: 16%
Percentages by event type:
1-electrode: 38%
2-electrode: 25%
3-electrode: 37%

## Slide 22: Different pad arrangements
pixels/cm2
Matrices of squares
Matrices of hexagons
Percentages by event type:
1-electrode: 30%
2-electrode: 40%
3-electrode: 14%
4-electrode: 16%
Percentages by event type:
1-electrode: 38%
2-electrode: 25%
3-electrode: 37%
By adding silicon oxide trenches
25%
33%
12%
30%
28%
12%
60%