## Slide 1: Status of MIMOSIS
M. Deveaux, for the CBM-MVD collaboration
(05P19RFFC1)
Supported by
Measurements leading to these results have been performed at the Test Beam Facility at DESY Hamburg (Germany), a member of the Helmholtz Association (HGF)
A. Altingun², Julio Andary1, Benedict Arnoldi-Meadows1, Ole Artz1, Jérôme Baudot2, Grégory Bertolone2, Auguste Besson2, Norbert Bialas1, Roma Bugiel2, Gilles Claus2, Claude Colledani2, Hasan Darwish1,2,3, Michael Deveaux1,3,6, Andrei Dorokhov2, Guy Dozière2, Ziad El Bitar2, Ingo Fröhlich1,3, Mathieu Goffe2, Benedikt Gutsche1, Fabian Hebermehl1, Abdelkader Himmi2, Christine Hu-Guo2, Kimmo Jaaskelainen2, Oliver Michael Keller6, Michal Koziel1, Franz Matejcek1, Jan Michel1, Frédéric Morel2, Christian Müntz1, Hung Pham2, Christian Joachim Schmidt3, Stefan Schreiber1, Matthieu Specht2, Dennis Spicker1, Joachim Stroth1,3,4, Isabelle Valin2, Roland Weirich1, Marc Winter5and Yue Zhao2 1Goethe-Universität Frankfurt, Germany 2Université de Strasbourg, CNRS, IPHC UMR 7178, Strasbourg, France 3GSI Helmholtzzentrum für Schwerionenforschung GmbH, Germany 4Helmholtz Forschungsakademie Hessen für FAIR, Germany 5IJCLab, UMR9012 – CNRS / Université Paris-Saclay / Université de Paris, France 6Facility for Antiproton and Ion Research in Europe GmbH,Germany

## Slide 2
Compressed Baryonic Matter (CBM) experiment @ FAIR
Aim of the CBM Micro Vertex Detector (MVD):
Open charm reconstruction
Low momentum tracking
…
=> and <0.5% X0/layer.
at 100 kHz ~10 AGeV Au+Au collisions.
10 MHz ~30 GeV p+Au collisions.
CAD: F. Matejcek
MVD
Beam

## Slide 3
Requirements on the sensor
 | Requirements
Spatial, time resolution | ~5 µm, 5 µs
Sensor thickness | ~ 50 µm
Power dissipation (in vacuum) | <100 mW/cm²
Radiation doses | 7 × 10¹³ neq/cm² ~ 5 MRad
Radiation gradient over sensor | ~ 100%
Heavy ion tolerance | 1 kHz/cm²
Rate (average/ 35 µs peak) | 20 / 80 MHz/cm²
Size of MIMOSIS-1
~10 x ALPIDE
~20 x ALPIDE
(internal)
Need to design customized sensor for CBM: MIMOSIS
(Minimum Ionizing MOs active pixel sensor for experiments at and beyond the SchwerIonen Synchrotron)
Derive from ALPIDE (priority encoder readout) in TJ180nm.
Add fully depleted sensing node.
Re-design digital front- and back end (higher bandwidth, elastic buffer…)

## Slide 4: MIMOSIS R&D plan
MIMOSIS-0 (2018)
Demonstrate pixel concept.
Demonstrate zero suppression.
Demonstrate readout concept.
MIMOSIS-1 (2020)
Full dimension sensor
Add buffer structure.
SEE hardening 1/2
MIMOSIS-2 (Q2/2023)
On-chip pixel grouping.
Final pixels.
SEE hardening 2/2
MIMOSIS-3
Final sensor for mass production
In synergy with:
Add features
Fix issues
Add features
Fix issues
Design optimization
Design optimization
Fix issues
Final design choice
MIMOSIS-2.1 (Q2/2024)
Fix issues
We are here

## Slide 5: MIMOSIS, the sensor for the MVD (inspired by ALPIDE)
Size: 504 x 1024 pixels (27x30µm²), 5µs time binning
Full integrated: 20 MHz/cm² (80 MHz/cm² for 35µs), ~70mW/cm²
Fully depleted: >20V top bias
MIMOSIS-1, 60µm thick
p-stop
standard
Standard
Rad. hard, candidate 1
First proposed by W. Snoeys et al.
H. Pernegger et al., 2017 JINST 12 P06008
>20V HV top bias
Capacitor blocks HV
Epitaxial layer thickness: 25µm, 50µm (new => reported today).
Inject test signal into pixel
Known from ALICE/ALPIDE
+ Radiation hardness
- Spat. Resolution

## Slide 6
MIMOSIS-1/2.1 beam test setup
MIMOSIS - beam telescope:
6 MIMOSIS-1 or 2.1 sensors
4 reference sensors (standard epi-layer)
2 device under test
Reference Track Uncertainty:
  2.5 µm + 1.5 µm Mult. Scattering (DESY only)
Irradiation:
1 MeV reactor neutrons (TRIGA, Ljubjana).
Few 10 keV X-rays (KIT)
Storage at room temperature.
Beam test:
5 GeV e- Beam @ DESY
120 GeV Pion Beam @SPS-CERN
~ 1 GeV d – beam @ COSY
Stabilized room temperature

## Slide 7
MIMOSIS-1 performance: New and after 5 MRad + 1014neq/cm²
Best performing pixel: AC P-stop
Efficiency >99% (end of life-time).
Spatial resolution: ~6 µm
Dark rate:
  Marginal before irradiation.
  <10-6 after irradiation.
Short dimension
of 27x30µm² pixel.
Conclusion on sensor performance:
All pixels work excellent before irradiation.
Standard pixels show best spatial resolution.
P-stop AC pixel most radiation hard, matches requirements of CBM.
CBM

## Slide 8
Sensor performance: MIMOSIS-1 vs. MIMOSIS 2.1
Design goal
noise
Det. limit
noise
Preliminary, 10. Sept. 24
Observations:
MIMOSIS-2.1 reaches lower threshold than MIMOSIS-1.
MIMOSIS-2.1 reaches even(!) higher efficiency than MiSIS-1.
Best performance: Novel 50µm epitaxial layer with p-stop.
Dark occupancy marginal for all sensors (noisy pixels NOT masked).
p-stop, vbb=-1V, HV=10V, no masking
H. Darwish, A. Altingun
Default working range

## Slide 9
MIMOSIS 2.1: Cluster multiplicity
Frequency [1]
Fired pixel/hit [1]
Observation:
MIMOSIS-2.1 p-stop 50µm combines high cluster multiplicity with rad. tolerant structure.
Might yield best combination of spatial resolution and radiation tolerance.
Radiation soft, good resolution
Radiation hard, reduced resolution
Radiation hard (?), good resolution

## Slide 10
Spatial resolution, MIMOSIS-1 vs. MIMOSIS 2.1
Design goal (open charm)
~500 nm align-
ment uncertainty?
Preliminary, 10. Sept. 24
H. Darwish, A. Altingun
Observations:
MIMOSIS-2.1 and MIMOSIS-1 show mostly same resolution for 25 µm (expected, discrepancy to be studied).
MIMOSIS-2.1 50 µm reaches better resolution (as hoped).
+ ~0.5 µm for longer pixel dimension
p-stop, vbb=-1V, HV=10V, no masking
Preliminary conclusion:
Novel 50 µm p-stop appears most promising.
Need to confirm radiation tolerance before concluding => t.b.d. Q1/2025.
Default working range

## Slide 11
Latch-up studies (MIMOSIS-2 with ~4 AMeV Au-ions)
Requirement for MVD:
  Must withstand 1kHz/cm² ions with
    LET< 35 MeV cm²/mg.
    (H. Darwish, PhD under preparation)
Preliminary test results (Bit flips):
  Frequent single bit errors seen.
  Correction in status registers works…
    … but may be overwhelmed by simultaneous to 2-bit flips (at unrealistically high ion fluxes).
  Data registers not protected.
Preliminary test results (Latch-up):
  No LU for LET≲50 MeV cm²/mg.
  Some LU seen above.
Beam impact test: few 100 MHz/cm² for few ms - OK.
Preliminary conclusion: Sensor matches requirements – no LU protection system needed.
T.b.d: Bit flip tolerance of data chain.
CBM requirement
Required
> 1 LU/lifetime
< 1 LU/lifetime
Preliminary
10. Sept 2024
MIMOSIS-2
Safety margin
B. Arnoldie-Meadows,
PhD under preparation

## Slide 12
Summary and conclusion
MIMOSIS-1/2.1 form the full-size prototypes of the MIMOSIS sensor for the CBM-MVD.
    5 µs / ~5 µm time/spatial resolution.
    80 MHz/cm² peak rate.
MIMOSIS-1: irradiated with up to 3x1014 neq/cm² were tested in laboratory and in beam.
    >> 99% detection efficiency after 1014 neq/cm², 5 MRad and a combination of both
    <10-6 fake hit rate (after 1014 neq/cm², <0.05% of all pixels masked)
    ~6 µm spatial resolution before and after irradiation => Satisfactory w.r.t requirement.
MIMOSIS-2.1:
    Further improved detection efficiency and spat. resolution with 50 µm p-stop sensing node.
    Tolerates HI with up to LET ~50 MeV cm² / mg without observed latch-up.
    Tolerates and corrects bit-flips in steering registers.
MIMOSIS-2.1 matches the requirements of the CBM-MVD…
… and forms a mile-stone toward a sensor for higgs-factories.
Submission of final sensor foreseen mid 2025. Open for collaboration on further applications.
Open issues (still t.b.d): SEE tolerance of data path, Rad. tolerance of p-stop 50µm sensing node.

## Slide 13
Backup

## Slide 14
MIMOSIS block diagram