## Slide 1
The “green” use of fluorocarbons in Cherenkov detectors
and silicon tracker cooling systems: challenges and opportunities
https://link.springer.com/article/10.1140/epjp/s13360-023-04703-w
See also: https://indico.cern.ch/event/1263731/contributions/5398511/attachments/2648319/4584649/G_Hallewell_DRD4%20Rad%20Gas%20GWP%20with%20annexes%20May%2016%202023.pdf
https://indico.cern.ch/event/1371158/contributions/5773321/attachments/2788215/4861759/G_Hallewell_ATLAS_sustainability_forum_Jan_26_2024_v2.pptx
ICHEP2024 (July 2024): https://indico.cern.ch/event/1291157/contributions/5900402/
“From the Speed of Sound to the Speed of Light: and beyond!”
G. D. Hallewell
Aix Marseille Université, CNRS/IN2P3, CPPM, Marseille, France
1
.
G. Hallewell: Seminaire CPPM: 16 sep 2024
With thanks to many people for information, as detailed on a later slide.
Notes: 1

## Slide 2
Abstract (see https://indico.in2p3.fr/event/33405)
Saturated fluorocarbons (SFCs: of chemical form CnF(2n+2)) are chosen for their optical properties (refractive index and UV transparency) for use as Cherenkov radiators, with C4F10 and CF4 used in the COMPASS and LHCb RICH1&2 ring imaging Cherenkov detectors to provide m±/p±/K±/p± particle identification over a wide momentum range. Non-conductivity, non-flammability and radiation resistance also make SFCs ideal coolants, with C6F14 liquid used in all LHC experiments, while C3F8 evaporatively cools the ATLAS silicon tracker.
These fluids however have high GWPs (>5000*CO2), and represented around 36%of CERN’s CO2-equivalent emissions in 2018. There is thus an impetus to reduce their use, losses in purification and wastage through leaks, via improved monitoring and closed circulation system design.
While not yet industrialised over the full CnF2nO range, spur-oxygenated fluoro-ketones can offer similar performance at very low, or zero GWP. The radiation tolerance and thermal performance of 3M 'NOVEC 649' (C6F12O) was sufficiently promising for it to be chosen by CERN to replace C6F14. Subject to optical testing, 3M 'NOVEC 5110' (C5F10O) - blended with nitrogen and monitored in real time by sound velocity gas analysis - might replace C4F10 and CF4 in RICH detectors.
Ultrasonic gas mixture analysis is very sensitive to concentration changes of a heavy vapour in a light carrier, and is used for real-time monitoring of C3F8 coolant leaks from the ATLAS pixel and SCT silicon trackers into their nitrogen-flushed environmental volumes, where typical C3F8 sensitivity of better than 10-5 is achieved. Advanced new ultrasonic algorithms allow measurement of the concentrations of a pair of gases of particular interest on top of a varying known baseline of other gases. The technique could be used to blend fluoro-ketones with nitrogen or argon to reduce the GWP “load” of large volume Cherenkov radiators. The technique is also of interest in xenon-based anaesthesia, which has a similar problematic.
Light fluoro-ketone molecules (e.g. C2F4O, with similar thermodynamics to C2F6) – might allow lower temperature, 0GWP operation than evaporative CO2 in Si trackers operated at high luminosity.
This seminar outlines an approach to GWP reduction with fluoro-ketone fluids and the blending of heritage SFCs or fluoro-ketones with lighter gases using ultrasonic monitoring and control. Possible avenues for the use of fluoro-ketones in liquid phase and evaporative cooling of silicon trackers are discussed.
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 3
“Green” fluorocarbons for Cherenkov detectors & silicon tracker cooling systems: challenges and opportunities
Saturated fluorocarbons (PFCs, SFCs: CnF(2n+2)) chosen for optical properties as Cherenkov radiators: C4F10 & CF4 in COMPASS & LHCb RICH1&2.
Non-conductivity, non-flammability, non-toxicity & radiation resistance
 ideal coolants
- C6F14 used in all LHC experiments,
- C3F8 evaporatively cools ATLAS silicon tracker, TOTEM;
These fluids however have high GWPs (GWP20 > 5000*CO2);
Fluoro-ketones (CnF2nO), while not industrialised over a wide CnF2nO range,
can offer similar performance at very low, or 0 GWP however F-gas restrictions;
Gas blending using ultrasonic monitoring will be needed: promising advances
Radiation tolerance & thermal performance of linear-C6F12O (3M NOVEC 649 ®) sufficiently promising to be considered by CERN to replace C6F14 for
cooling, but acid production & materials compatibility to resolve;
We will see that fluoro-ketone molecular shape and O atom placement
affects GWP, chemi-activity, toxicity, and might limit future options
GEOMETRY IS EVERYTHING!!!!
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 4
RICH2
RICH1
Two RICH detectors identify m±/p±/K±/p±: momentum 1 - 100 GeV/c
RICH1: C4F10 (4 m3 gas at 1 bar) + aerogel: RICH2: CF4 (100 m3 gas at 1 bar)
LHCb Detector (CERN-LHC)
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 5
L’effet Tcherenkov: mécanisme
Quand une particule chargée passe dans un milieu
diélectrique les molécules polaires sont déplacées
par son passage: pôles – (+) attirées par une
particule chargée + (-).
Après le passage de la particule, cette énergie est
émise par les molécules  « de-excitation »
comme une onde électromagnétique (E-M)
Chaque molécule absorbe une très faible quantité
d’énergie en faisant une rotation
Si la vitesse de la particule est inférieure à celle
de la lumière dans le milieu, la « de-excitation »
collective donne une émission E-M de forme isotrope
Hallewell/ Conférence Université de temps libre, La Ciotat 02.04.2017

## Slide 6
L’effet Tcherenkov: mécanisme
Quand une particule chargée passe dans un milieu
diélectrique, les molécules polaires sont déplacées
par son passage: pôles – (+) attirées par une
particule chargée + (-).
Après le passage de la particule, cette énergie est émise
par les molécules  « de-excitation »
comme une onde électromagnétique
Chaque molécule absorbe une très faible quantité
d’énergie en faisant une rotation
Si la vitesse, v, de la particule dépasse celle de la
lumière dans le milieu, la « de-excitation » collective
donne une émission cohérente de forme conique
Hallewell/ Conférence Université de temps libre, La Ciotat 02.04.2017

## Slide 7
Similarité entre l’onde de choc sonique du Concorde, F18… et l’onde lumineuse Tcherenkov
Ondes de Choc
v < Mach 1.0
Ondes de Choc
v = Mach 1.0
Enveloppe des Ondes de Choc
v > Mach 1.0
Trajectoire particule
Vpart = 1.4 * Vlum (milieu)
Trajectoire particule
Trajectoire particule
Vpart = 1.2 * Vlum (milieu)
Vpart = 0.8 * Vlum (milieu)
Emission du Rayonnement Tcherenkov
Angle d’émission, q, de
l’onde de choc cohérente p.r. à la trajectoire de la particule:
q = cos-1 (vlum(milieu) /vpart)
Ondes
v < Mach 1.0
Ondes de Choc
v = Mach 1.0
Enveloppe des Ondes de Choc
v > Mach 1.0
Seuil pour l’émission d’une
onde de choc cohérente:
b = vpart > vlum(milieu)
Hallewell/ Conférence Université de temps libre, La Ciotat 02.04.2017

## Slide 8
Même si le rendement en photons est très faible, avec des millions de particules chargées baladant simultanément on voit un effet impressionnant…
Lumière Tcherenkov produite par des électrons rapides en modérateur D2O;
réacteur nucléaire “LIDO” de type ‘piscine’: Harwell, GB (1950’s)
Source: electrons sortant des désintégrations de noyeaux uranium
Hallewell/ Conférence Université de temps libre, La Ciotat 02.04.2017

## Slide 9
Capteurs de radiation Tcherenkov:
Mode: mesure de la masse et l’énergie de la particule par le rayon d’anneau de lumière
“RICH detectors” = Ring Imaging Cherenkov
Multi
Capteur de lumière
resolution ~mm2 et de surface ~m2
Qc = cos-1 (1/bn)
Dans un gaz:
r = f tanqc
f
of Refractive index n
r
Hallewell/ Conférence Université de temps libre, La Ciotat 02.04.2017

## Slide 10
Faisceau
Particule secondaire à identifier
Premier grand détecteur RICH: au spectromètre
“OMEGA” supraconducteur, CERN, 1982-88
Collaboration WA69: Bonn, Lancaster, Manchester, Rutherford & Sheffield
OMEGA RICHdetektor
Paschal Coyle missed
out on this photo
Hallewell/ Conférence Université de temps libre, La Ciotat 02.04.2017

## Slide 11
RICH 1: C4F10 radiator:
lower momentum PID
RICH 2: CF4 (+CO2) radiator:
higher momentum PID
COMBINED RICH PEFORMANCE & PARTICLE SPECIES IDENTIFCATION RANGE
G. Hallewell: Seminaire CPPM: 16 sep 2024
Qc = cos-1 (1/bn)
Saturation angle (b  c)
Qc = cos-1 (1/n)

## Slide 12: https://link.springer.com/article/10.1140/epjp/s13360-023-04703-w
G. Hallewell: Seminaire CPPM: 16 sep 2024
OK, back to the farm….

## Slide 13
G. D. Hallewell
Aix Marseille Université, CNRS/IN2P3, CPPM, Marseille, France
13
.
G. Hallewell: Green FCs for Cherenkov detectors and Si tracker cooling: Sustainability session ICHEP2024 Praque 18-24 July 2024
Green use of fluorocarbons in Cherenkov detectors and silicon tracker cooling systems: challenges & opportunities. https://indico.cern.ch/event/1291157/contributions/5900402/
Notes: 13

## Slide 14: Molecular shapes and GWP (1)
Upper: molecular shapes of SFCs, including common gaseous Cherenkov radiators
Lower: shapes of some non-cyclic CnF2nO analogues
(20-year GWPs noted where known – refs: https://link.springer.com/article/10.1140/epjp/s13360-023-04703-w)
SATURATED FLUOROCARBONS (CnF(2n+2)) with current uses at CERN
FLUOROKETONES (CnF2nO)
COOLING (Liq.)
InH. Toxicity
H331,
reactive
Inh. Toxicity H330,
Reactive
RICH
(Gas?)
RICH
(Gas (blend))
Probable
Uses
(if/when
available)
COOLING (Liq.)
Si COOLING (Evap.)
RICH (Gas)
RICH (Gas)
Current
uses
at CERN
Ex-DELPHI
RICH (Gas)
C2F4O
G. Hallewell: Seminaire CPPM: 16 sep 2024
Inh. Toxicity
H331,
reactive

## Slide 15
Cyclic, non-cyclic & non-cyclic double carbon-bonded C4F8O isomers: refs at end.
Placement of oxygen atom can also determine chemi-potential, flammability & toxicity­
Molecular shapes and GWP (2)
High GWP!!
?
ALICE VHMPID,
BTeV studies:
Refractive index,
UV transparancy OK
(similar to C4F10), but…

?
?
G. Hallewell: Seminaire CPPM: 16 sep 2024
CAS: 67641-44-5
H332, H335, H336
CAS:10493-43-3
H332, H335, H336
CAS 773-14-8
Unlisted
CAS: 677-84-9
H335
CAS 335-42-2
H331, H335
CAS: 337-20-2
H335

## Slide 16: Classification Criteria for Inhalation Toxicity
G. Hallewell: Seminaire CPPM: 16 sep 2024
H330 | Fatal if inhaled
H331 | Toxic if inhaled
H332 | Harmful if inhaled
H333 | May be harmful if inhaled
H334 | May cause allergy or asthma symptoms or breathing difficulties if inhaled
H335 | May cause respiratory irritation
H336 | May cause drowsiness or dizziness
H310 | Fatal in contact with skin
H311 | Toxic in contact with skin
H312 | Harmful in contact with skin
H313 | May be harmful in contact with skin
H314 | Causes severe skin burns and eye damage
H315 | Causes skin irritation

## Slide 17: So why are some of these spurred fluoro-ketones CnF2nO potential low GWP substitutes for saturated fluorocarbons? CnF(2n+2)
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 18: Q: What gives a spurred-Oxygen fluoro-ketone molecule (like 3M NOVEC 649/1230®) its low GWP?
A: Structure!: a double-bonded oxygen atom on a peripheral spur of the molecule
This fluoro-ketone configuration is:
CF3CF2C(O)CF(CF3)2
18
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 19: Q: What gives NOVEC 649/1230 its low GWP?
Scission by UV photons of l around 300 nm
In the atmosphere (low pressure, high UV): the fragments do not reassociate* into saturated fluorocarbons of the type CnF(2n+2) (which would have high GWP)
*The Environmental Impact of CFC Replacements HFCs and HCFCs
T. WALLINGTON et al Environ.Sci.Technol.1994(28)7 320A https://doi.org/10.1021/es00056a714
https://www.nist.gov/system/files/documents/el/fire_research/R0301570.pdf
19
[15]
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 20
This latest CERN environmental report https://doi.org/10.25325/CERN-Environment-2023-003
G. Hallewell: Seminaire CPPM: 16 sep 2024
R449: (CFH blend) GWP=1397
R1234 (HFO): GWP = 7
NOVEC 649 (C6F12O): GWP=0
CF4 LHCb RICH2: GWP20 = ¬ 4880_CO2* [16]
C2F6 ATLAS evap cooling (potential use): GWP20 = ¬ 8210_CO2* [16]
C3F8 F2 Chemicals , Astor, ATLAS evap cooling: GWP20 = ¬ 6640_CO2*[16]
C4F10 LHCb RICH1, COMPASS RICH: GWP20 = ¬ 6870_CO2* [16]
C5F12 PP50: GWP20 = ¬ 6350_CO2* [16] (ex-DELPHI, no longer used at CERN)
C6F14 PP1, F2 Chemicals: Liquid cooling, many expts:
GWP20 = ¬ 5890_CO2*[16]
For some perspective: SF6 GWP ~ 23000 * CO2
See also:
https://www.ghgprotocol.org/sites/default/files/ghgp/Global-Warming-Potential-Values%20%28Feb%2016%202016%29_1.pdf
For 100 yr (average of 2nd, 4th & 5th assessment reports; AR2,4,5)
Collective loss of SFCs only around 10 tonnes (whole of LHC + expts)
(compare that to mass-loss at a ‘grande surface’ supermarket!)

## Slide 21
EU strategy to reduce Fluronated (PFAS) compound production and use
(includes also fluorinated plastics not shown here: see back-up material)
ICHEP2024
Projected Usage
Dynamic price hiking :
like imposing demand-dependent customs duty…?
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 22
But no mention at all of the ATLAS ultrasonic fluorocarbon leak monitor system !
https://doi.org/10.25325/CERN-Environment-2023-003
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 23: Ultrasonic gas analysis in ATLAS: the only fluorocarbon leak detection of its type at CERN.
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 24: Unpeeling the ATLAS Onion
ATLAS Inner detector:
Includes silicon microstrips
(‘SCT’ tracker) & pixel detectors
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 25: Unpeeling the ATLAS Onion: the evaporators ‘Semi-Conductor Tracker’ (SCT) silicon microstrip tracker surrounding pixel detector
SCT + pixels: 204 C3F8 evaporative cooling circuits
60kW total power to evacuate (1.2 kgs-1 C3F8)
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 26: Unpeeling the ATLAS Onion: Outer Silicon Pixel Detector Structure
~50 Horizontal evaporative C3F8 cooling channels (l ~ 1,60m)
18 “radial” channels: disk sectors
(Another (innermost layer) is cooled by evaporating CO2)
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 27
Chart: CO2 concentration (ppm)
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 28: Ultrasonic gas analysis in a process environment with multiple background gases
G. Hallewell: Seminaire CPPM: 16 sep 2024
https://www.mdpi.com/2410-390X/5/1/6
Gas aspirated through
150m tubes from
silicon tracker
N2 environmental
volumes to
‘sonar’ devices
to look for C3F8
leak rates
(C3F8 in N2 )

## Slide 29: Ultrasonic gas analysis in a process environment with multiple background gases
29
https://www.mdpi.com/2410-390X/5/1/6
Precision: 10-5 C3F8 into N2 at 1 bar
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 30
Polaroid Capacitative transducer components
Capacitative 350V activation/ bias  rapid response
37mm diameter determines 50 kHz dominant frequency: can operate over wide pressure range (50mbar >35 bar…)
30
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 31
31
G. Hallewell: Seminaire CPPM: 16 sep 2024
Ultrasonic algorithm to find component molar concentrations wi=1,2… of a pair of gases of primary interest in multi-gas blends

## Slide 32
(1) Calculate data base of individual CVi..n CPi..n
over expected T, P. range:
Example here: C4F10: (mol. wt.) = 238 in N2 (mol. wt. = 28)
32
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 33
(2) Calculate c‘theo’ as a function of concentration from component
Cp, Cv’s over the expected sonar temperature, pressure range to
make database of c‘theo’ vs. conc. fit equations to store in ‘cans’
Example here 0- 1% C3F8 (m.w.= 188) in N2 (m.w.= 28): only one pressure shown here for clarity)
33
G. Hallewell: Seminaire CPPM: 16 sep 2024
Polynomial
Fit
Parameters

## Slide 34
(3) CAN UTILITY: Store these c‘theo’ vs. molar conc. polyfit coeffs covering expected temperature & pressure range in “cans” at P,T grid intersections
T 
P 
Tmin
Tmax
Pmax
Pmin
Tstep
Pstep
Tmeas
Pmeas
(4) Calculate component concentrations wi from measured sound velocity cmeas & stored fit coeffs. interpolated to correspond to the measured T, P
!! This grid can become 3-D or higher-D with known contaminant gas(es) 
34
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 35: Aah…what if 3 gases are present? Acoustic Ambiguity ? 2 combinations of 3 gases  same c… so must find w3 from a different (non-acoustic) technology source… Examples inc. clinical…): CO2 from ND infra-red, H2O from hygrometry, O2 from EC cell… etc.
35
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 36: Example: Look-up tables of SoS. vs. composition for C3F8/N2 (+ CO2) (ATLAS silicon tracker cooling leak analysis)
36
CAN UTILITY DB expanded
from 2-D to 3-D:
C3F8/N2 fit coeffs
stored @{T, P, CO2} grid
Extra interpolation step,
starting from grid cub(oid) of uncertainty
to Tmeas, Pmeas,CO2 meas
Calculate sound vel vs. conc. eqns from
C3F8 & N2 AND KNOWN CONTAMINANT GAS
Cp & Cv over expected T,P, %CO2 range.
Demonstration:
1st acoustic measurement of concentrations of binary gas pair
of interest (C3F8/N2)
in known varying conc. of 3rd gas (CO2) :
(4 envelopes cycling every 4 hours)
Algorithm: industrial & anaesthesia applications
https://www.mdpi.com/2410-390X/5/1/6
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 37
37
LHCb RICH 2 change in refractivity with varying CO2 radiator addition
Acoustic ‘pair’ would be CF4 & N2 : O2 by e-chemical cell, CO2 from NDIR)
G. Hallewell: GasRad GWP: ECFA TF-4 Meeting May16-17th 2023
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 38
T
P
CO2
P
T
P
P
P
P
P
P
T
T
T
T
T
T
CO2
CO2
CO2
CO2
CO2
CO2
H2O
Example with a second known contaminant gas: here H2O but could be another measurable gas like O2 : 4-D {T,P, CO2, H2O} Process dataspace example ‘Cans’ of c vs. conc1,2 fit coefficients now at corners of tesseract. (Here in Coxeter B4 projection)
8 cube faces:
2 x {T,P,CO2} exc. H2O
2 x {T,P, H2O} exc. CO2
2 x {T, CO2, H2O} exc. P
2 x {P, CO2, H2O} exc. T
Opposite cubic faces explored in the following slides
H2O
H2O
H2O
H2O
H2O
H2O
H2O
38
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 39
Tessar-Can-Action
Canterpolation (Extractio-reduction)
https://www.mdpi.com/2410-390X/5/1/6
39
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 40
Short digression:
Anesthésie et Ventilation: oxygène avec xénon
Anesthésie
Ventilation:
Neuro-protecteur contre blessures hypoxique/
Ischémique du cerveau
suite aux manques d’oxygène
Présente dans l’air (8.7.10-8)
Masse moléculaire: 131
Séparation en séquence de liquéfaction/ distillation progressive
d’air pour LN2, LO2, Ar etc…
Potentiel comme gaz anesthésique connu depuis les 1950’s
Le seul gaz noble anesthésique @ la pression normale
Anesthétique idéale : rapide, effets indésirables minimaux
Très cher: (Xe médical @ € 30/n.t.p. litre)  peu utilise
Systèmes de circulation fermée nécessaires:
Consommation Xe ciblée < 16 litres/anesthésie typique de 4h
Récupération de Xe Post-opératoire:
(système + dégazage partiel de patient)
40
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 41
Contrôle de mélanges Xénon – Oxygène (aujourd’hui)
Technologie actuel “split”: (Instrum. Russe)
Sonde électrochimique pour O2,
Sonde conductibilité thermique pour Xe: (analyseur INSOVT GKM-03):
41
Retro-adaptation de débitmètre ultrasonique (« FDA-approved »: Drager Spirocell) ajout de logiciel pour l’analyse simultanée des mélanges Xe-O2 : preuve de principe
Inc. GH (CPPM), J. Dingley & D. Williams: Dept. Anaesthetics, Swansea Uni., GB
G. Hallewell: Seminaire CPPM: 16 sep 2024
Soda-lime
CO2 adsorber

## Slide 42
Analyseur a ultrasons de mélanges de gaz Xe-O2
Pour mesurer la concentration de Xe avec une
précision de 0.1% il faut mesurer la vitesse de son
avec une précision de 0.2 m/s
(instrument @ CERN: typ. 0.05 m/s)
In practice, work in the 100%RH regime:
 H2O molar concentration given by svp:
Xe/O2 anesthetic gas mixture can contain CO2 if soda-lime absorber cannister ineffective.
implement Xe/O2 gas concentration measurement algorithm in T, P, CO2 space
Maybe go to 4D (tessaract) if need to monitor on top of varying H2O conc..
G. Hallewell: Seminaire CPPM: 16 sep 2024
Masse moléculaire Xe: 131
Masse moléculaire di-oxygène: 32
Polyfit parms
in « cans »

## Slide 43
SoS CALC: Of course, CP & CV for all gases (primary & background)
must be calculated for all T, P points on the n-D grid;
CAN FILLING: Calculate & fit c in gas pair of primary interest from CP & CV over their conc. range AND @T, P, known background gas conc. Grid points.
Database size (3-D example)
DB size = No. primary fit coeffs * **…
RoI_n = range of interest_n: d_n = stepsize_n  Database explosion ?!?
Increasing stepsize ( longer interpolation distance) can reduce No. of cans (“cubes” become “cuboids”)…
Some dimensions can be suppressed altogether using physical law (rather than empirical changes):
example for temperature dimension:
Database growth control
(important in instruments using embedded m-controllers)
43
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 44: Cherenkovicity…
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 45
COMBINED RICH PEFORMANCE & PARTICLE SPECIES IDENTIFCATION RANGE
G. Hallewell: Seminaire CPPM: 16 sep 2024
RICH 1: C4F10 radiator:
lower momentum PID
RICH 2: CF4 (+CO2) radiator:
higher momentum PID

## Slide 46
Refractive index & GWP ’load’ in a Cherenkov Gas Radiator
3 large RICH detectors currently in operation at CERN:
using saturated fluorocarbon gas volumes:
C4F10 (COMPASS: 100m3, LHCb RICH 1: 4m3): GWP20 = 4880,
CF4 (LHCb RICH 2: 100m3): GWP20 = 6870
A Cherenkov radiator vessel of volume V(m3) filled with
a blend of gases of densities ri (kgm-3),
fractional concentrations wi and individual GWPi (tonnes CO2 eq.)
has a GWP environmental “load” (& release potential) L given by:
) (tonnes CO2 eq.) [Eq. (1)]
The corresponding radiator gas mixture refractivity is given by :
) [Eq. (2)]
For just two gases we can blend small conc. wx of (heavier) SFC or Fluoro-Ketone
vapour of high refractivity (n-1)x with wy of light transparent gas, refractivity (n-1)y
to replicate refractivity (n-1)z of a lighter SFC at high conc. – for a lower GWP load.
wx = [Eq. (3)]
V,r
With j contaminant gases of known molar concentrations wj present we can still
add a small concentration wx of (heavier) SFC or Lin-FK vapour of high refractivity
(n-1)x with wy of light transparent gas to substitute the refractivity (n-1)z(target)
of a lighter SFC at high concentration – to achieve a lower overall GWP load.
+
[Eq. (2) Eq. (2b)]
wx = [Eq. (3)  Eq. (3b)]
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 47: An interesting fluoroketone: C5F10O MW = 266: GWP <1 (e.g. 3M Novec 5110®)
Blend with N2 to match C4F10 or CF4 - refractivity?
47
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 48
Use real-time speed of sound to get component molar concentrations,wi
(SoS traditionally also called “c” by acousticians to confuse things)
Then use standard refractivity formula to get from calculated w1,2
to refractive index of the radiator gas in real-time, along with standard relativistic expressions to get from n to Cherenkov g thresholds for different particle species and b = 1 angle
Real-time measurement of speed of sound c takes us via the relative concentrations of the components to the speed of light b and beyond!! in the radiator gas
48
Eyes on the prize…(focus here on LHCb RICH2 (n-1)…)
(488.10-6)CF4 = (~1750.10-6)C5F10O*0.12+(300.10-6)N2*0.88
)
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 49
Historical: The SLD barrel CRID gas radiators (SLAC: 1990s)
87% C5F12/13%N2
gas radiator
Sonar transducer
6 transducer pairs
@ 3 different heights
(hydrostatics)
49
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 50
Maintaining C5F12/N2 refractive index
through sonar-based active mixture control
(In this paper submitted to IEEE TNS)
Flowmeter
analyzer in supply line
to tune the blend by
hardwired 4-20mA
links to mass flow controllers
50
G. Hallewell: Seminaire CPPM: 16 sep 2024
Undergrads: Queen Elizabeth College
+ Notting Hill
Spokesperson:
DUNE
Spokesperson:
KM3NeT

## Slide 51
Chart: C5F12-N2 40 ⁰C
| 361.57150866452997 | 256.66370132773199 | 207.76041110631601 | 177.74100163378299 | 156.771959339836 | 140.96541864529999 | 128.432486611158 | 118.12923971441801 | 109.42497216462201 | 101.912772216321 | 95.316482075286103
e thresh | 0.20021 | 0.16566 | 0.14445 | 0.12974 | 0.11878 | 0.11019 | 0.10324 | 0.09746 | 0.092555 | 0.088324 | 0.084626
mu thresh | 4.2043 | 3.4788 | 3.0335 | 2.7246 | 2.4943 | 2.3141 | 2.1681 | 2.0467 | 1.9436 | 1.8548 | 1.7772
pi thresh | 5.4857 | 4.5391 | 3.9579 | 3.555 | 3.2545 | 3.0193 | 2.8288 | 2.6704 | 2.536 | 2.4201 | 2.3188
kthresh | 19.9006 | 16.4666 | 14.3584 | 12.8965 | 11.8065 | 10.9534 | 10.2622 | 9.6876 | 9.1999 | 8.7794 | 8.4119
pthresh | 37.4788 | 31.0115 | 27.0412 | 24.288 | 22.2351 | 20.6285 | 19.3269 | 18.2446 | 17.3262 | 16.5342 | 15.842
% C5F12 | 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
SLD-CRID: Cherenkov threshold in C5F12/N2 mixtures vs. measured speed of sound in radiator gas mixture (1)
Typical mix 87%C5F12,13%N2
C5F12 concentration (%)
51
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 52
Chart: C5F12-N2 40 ⁰C: (N2-C5F10O should be very similar
| 361.57150866452997 | 256.66370132773199 | 207.76041110631601 | 177.74100163378299 | 156.771959339836 | 140.96541864529999 | 128.432486611158 | 118.12923971441801 | 109.42497216462201 | 101.912772216321 | 95.316482075286103
e thresh | 0.20021 | 0.16566 | 0.14445 | 0.12974 | 0.11878 | 0.11019 | 0.10324 | 0.09746 | 0.092555 | 0.088324 | 0.084626
mu thresh | 4.2043 | 3.4788 | 3.0335 | 2.7246 | 2.4943 | 2.3141 | 2.1681 | 2.0467 | 1.9436 | 1.8548 | 1.7772
pi thresh | 5.4857 | 4.5391 | 3.9579 | 3.555 | 3.2545 | 3.0193 | 2.8288 | 2.6704 | 2.536 | 2.4201 | 2.3188
kthresh | 19.9006 | 16.4666 | 14.3584 | 12.8965 | 11.8065 | 10.9534 | 10.2622 | 9.6876 | 9.1999 | 8.7794 | 8.4119
pthresh | 37.4788 | 31.0115 | 27.0412 | 24.288 | 22.2351 | 20.6285 | 19.3269 | 18.2446 | 17.3262 | 16.5342 | 15.842
Thresh/c | 0.99969 | 0.99954 | 0.9994 | 0.99926 | 0.99911 | 0.99897 | 0.99883 | 0.99868 | 0.99854 | 0.9984 | 0.99825
SLD-CRID: Cherenkov threshold in C5F12/N2 mixtures
vs. measured speed of sound in radiator gas mixture (2)
Cherenkov Threshold (GeV/c)
b = 1/n
Measured Sound Velocity (m/s)
So.. from (“acoustic”) c to b…
52
G. Hallewell: DRD4 WG 2 Low GWP FC radiator gases: June 19 2024

## Slide 53
Chart: 
| 361.57150866452997 | 256.66370132773199 | 207.76041110631601 | 177.74100163378299 | 156.771959339836 | 140.96541864529999 | 128.432486611158 | 118.12923971441801 | 109.42497216462201 | 101.912772216321 | 95.316482075286103
e thresh | 0.20021 | 0.16566 | 0.14445 | 0.12974 | 0.11878 | 0.11019 | 0.10324 | 0.09746 | 0.092555 | 0.088324 | 0.084626
mu thresh | 4.2043 | 3.4788 | 3.0335 | 2.7246 | 2.4943 | 2.3141 | 2.1681 | 2.0467 | 1.9436 | 1.8548 | 1.7772
pi thresh | 5.4857 | 4.5391 | 3.9579 | 3.555 | 3.2545 | 3.0193 | 2.8288 | 2.6704 | 2.536 | 2.4201 | 2.3188
kthresh | 19.9006 | 16.4666 | 14.3584 | 12.8965 | 11.8065 | 10.9534 | 10.2622 | 9.6876 | 9.1999 | 8.7794 | 8.4119
pthresh | 37.4788 | 31.0115 | 27.0412 | 24.288 | 22.2351 | 20.6285 | 19.3269 | 18.2446 | 17.3262 | 16.5342 | 15.842
% C5F12 | 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
C5F12 or C5F10O concentration (%)
LHCb RICH 2 with C5F10O/N2
GWP load = (0.13 molar*1*V.r)
LHCb RICH 2: CF4 thresholds
GWP load = (0.95 molar*4880*V.r)
Cherenkov threshold: C5F10O/N2 & (heritage) C5F12/N2 blend and GWP load comparison for LHCb RICH2 (100m3 CF4)
C5F12 SFC/N2 and NOVEC5110 (C5F10O) /N2 will be very similar (MW 266 vs. 288)
~ 14% molar C5F10O
gives a GWP load reduction of 1737 tonnes:
Even substituting CF4 with ~ 13% molar heritage stock C5F12 reduces GWP load by ~800 tonnes
53
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 54
Base fluid | Base fluid density (1bar,25˚C) kgm-3 | Base fluid GWP (20-yr) | Component (n-1) (*106) (@ nm) | % Blend with N2 to match (n-1) CF4 | GWP load (t.CO2) | % Blend with N2 to match (n-1) C4F10 | GWP load (t.CO2)
CF4 LHCb RICH2 (100m3) | 3.56 [18] | 4880 [16] | 488 (180-310 nm) [19] | 100 | 1737 | not applicable | n/a
CF2O | - |  |  | ~100 | 1 | n/a | n/a
C2F6 | 5.63 [18] | 8210 [16] | 793 (180-310 nm) [19] | 38.1 | 1762 | not applicable | n/a
Lin-C2F4O | - |  |  | - |  | n/a | n/a
C3F8 | 7.75 [18] | 6640 [16] | 1180 (250 nm) [16] | 21.4 | 1099 | not applicable | n/a
Lin-C3F6O | - |  |  | - |  | n/a | n/a
C4F10 LHCb RICH1 (4m3): COMPASS (100m3) | 9.97 [18] | 6870 [16] | 1450 (250 nm) [16] | 16.3 | 1119 | 100 | 6849
Lin-C4F8O (Non-cyclic C4F8O)* | 9.5 (est.) | Probably < 1 (NOVEC 5110 Analogy) | 1380 @ 400nm (based on 3M PFG-3480 c-C4F8O [7]: linear C4F8O not yet measured but assumed similar) | 18.4 | 0.18 | 112.7* (>100% would imply necessity of operating C4F8O at slight overpressure) | 1.07
C5F12 | 11.63 [18] (BP 30 ˚C at 1 bar) | 6350 [16] | 1750 (180-310nm)[19] (40 ˚C, undiluted) | 13.0 | 957 | 79.3 | 5857
NOVEC 5110 C5F10O | 10.7 [13] (BP 27 ˚C at 1 bar) | <1 [13] | Not yet measured: probably around 1650 by analogy with C4F10 and C4F8O ratio | 13.9 | 0.149 | 85.2 | 0.91
Table 1: GWP loads of various SFCs and NOVEC 5110 blended with N2 ((n-1) = 310.10-6) to match refractivity of CF4 and C4F10
assumed radiator volume: 100 m3
Positions of presently unavailable-in-bulk CnF2nO fluids are shown in italics. Refractivities to match (CF4 and C4F10) shown in bold.
GWP loads and refractivities calculated using eqs. (1)-(3): assumed radiator volume: 100 m3
*Made in research quantities by Synquest Inc. as isomers Heptafluorobutyryl fluoride PN: 2116-2-07 CAS: 335-42-2
Octafluoro-2-butanone PN: 2117-2-10 CAS: 337-20-2 & Heptafluoroisobutyryl fluoride PN: 2116-2-0A CAS: 677-84-9
https://link.springer.com/article/10.1140/epjp/s13360-023-04703-w
GWP load reduction through CF4 index matching (LHCb RICH2)
Hypothetical (not industralised)
G. Hallewell: Seminaire CPPM: 16 sep 2024
Note: Xe ((n-1) around 750.10-6), GWP=0, another possibility for CF4 substitution:
Higher concentration (more m3) of a very expensive gas however

## Slide 55: Radiator volume GWP load: 100 m3 gas radiator with different mw gases blended with nitrogen to replace CF4 (note: blends with Ar very similar: need refractivity data for linear fluoro-ketones, probably similar to SFCs) blends with CO2 not consdered: high CO2 triple point temp (-56 C)  thermodynamic recirculation difficulty)
Chart: Molecular weight of heavy component in N2
| 88 | 288 | 238 | 131 | 84 | 138 | 188
Required Heavy component molar conc (%) in N2 vs molecular weight | 100 | 12.9655 | 17.0909 | 40.4301 | 132.3944 | 37.6 | 18.8
GWP load 100m3 (tonnes CO2) | 1737.28 | 957.5099 | 1170.623 | 0 | 0 | 1737.9585 | 967.448 | 0
CF4 (pure) 1737 tonnes
Krypton: (>100% indicates need
for slight pressuisation)
Xe
CF4
C2F6
C3F8
C4F10
C5F12
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 56
C4F10 radiator (COMPASS): volume 100m3, 1 bar
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 57
Chart: e.g.: COMPASS RICH (100m3), LHCb RICH 1 (4m3), : C4F10-N2 @ 25 ⁰C: animation for N2 depassivation
| 352.80554329709202 | 263.393983949394 | 217.54894792942801 | 188.28848822732601 | 167.42098121844799 | 151.49471355246499 | 138.76788802501201 | 128.253185480963 | 119.34320896725301 | 111.640770856572 | 104.873532673703
e thresh | 0.20021 | 0.1704 | 0.15087 | 0.13682 | 0.12609 | 0.11754 | 0.11053 | 0.10464 | 0.099602 | 0.095231 | 0.09139
mu thresh | 4.2043 | 3.5783 | 3.1683 | 2.8733 | 2.6478 | 2.4683 | 2.3211 | 2.1974 | 2.0916 | 1.9998 | 1.9192
pi thresh | 5.4857 | 4.6688 | 4.1339 | 3.7489 | 3.4548 | 3.2206 | 3.0284 | 2.8671 | 2.7291 | 2.6093 | 2.5041
kthresh | 19.9006 | 16.9373 | 14.9967 | 13.6001 | 12.533 | 11.6835 | 10.9864 | 10.401 | 9.9004 | 9.4659 | 9.0841
pthresh | 37.4788 | 31.898 | 28.2434 | 25.613 | 23.6034 | 22.0035 | 20.6907 | 19.5883 | 18.6455 | 17.8272 | 17.1082
% C4F10 | 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
Situation for RICH radiators using C4F10 with N2 passivant
Cherenkov Threshold (GeV/c)
C4F10 concentration in radiator gas (%)
Measured Sound Velocity (m/s)
57
Can make the same C5F10O comparison
as previously done for a CF4 radiator (see preceeding table)
Of course… low GWP non-cyclic C4F8O
would be easier to circulate, if available.
G. Hallewell: DRD4 WG 2 Low GWP FC radiator gases: June 19 2024

## Slide 58
Chart: 
| 361.57150866452997 | 256.66370132773199 | 207.76041110631601 | 177.74100163378299 | 156.771959339836 | 140.96541864529999 | 128.432486611158 | 118.12923971441801 | 109.42497216462201 | 101.912772216321 | 95.316482075286103
e thresh | 0.20021 | 0.16566 | 0.14445 | 0.12974 | 0.11878 | 0.11019 | 0.10324 | 0.09746 | 0.092555 | 0.088324 | 0.084626
mu thresh | 4.2043 | 3.4788 | 3.0335 | 2.7246 | 2.4943 | 2.3141 | 2.1681 | 2.0467 | 1.9436 | 1.8548 | 1.7772
pi thresh | 5.4857 | 4.5391 | 3.9579 | 3.555 | 3.2545 | 3.0193 | 2.8288 | 2.6704 | 2.536 | 2.4201 | 2.3188
kthresh | 19.9006 | 16.4666 | 14.3584 | 12.8965 | 11.8065 | 10.9534 | 10.2622 | 9.6876 | 9.1999 | 8.7794 | 8.4119
pthresh | 37.4788 | 31.0115 | 27.0412 | 24.288 | 22.2351 | 20.6285 | 19.3269 | 18.2446 | 17.3262 | 16.5342 | 15.842
% C5F12 | 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
C5F10O concentration (%)
COMPASS (& LHCb RICH 1): C4F10 thresholds
COMPASS RICH GWP load = (6849 tonnes)
Cherenkov threshold in C5F10O/N2 mixtures and GWP load comparison with COMPASS RICH (100m3)
N2-NOVEC5110 (C5F10O) very similar to C5F12 (MW 266 vs. 288)
85% Novec 5110 gives a huge GWP load reduction of 6849 tonnes
58
G. Hallewell: DRD4 WG 2 Low GWP FC radiator gases: June 19 2024

## Slide 59
Base fluid | Base fluid density (1bar,25˚C) kgm-3 | Base fluid GWP (20-yr) | Component (n-1) (*106) (@ nm) | % Blend with N2 to match (n-1) CF4 | GWP load (t.CO2) | % Blend with N2 to match (n-1) C4F10 | GWP load (t.CO2)
CF4 LHCb RICH2 (100m3) | 3.56 [18] | 4880 [16] | 488 (180-310 nm) [19] | 100 | 1737 | not applicable | n/a
CF2O | - |  |  | ~100 | 0 | n/a | n/a
C2F6 | 5.63 [18] | 8210 [16] | 793 (180-310 nm) [19] | 38.1 | 1762 | not applicable | n/a
Lin-C2F4O | - |  |  | - |  | n/a | n/a
C3F8 | 7.75 [18] | 6640 [16] | 1180 (250 nm) [16] | 21.4 | 1099 | not applicable | n/a
Lin-C3F6O | - |  |  | - |  | n/a | n/a
C4F10 LHCb RICH1 (4m3): COMPASS (100m3) | 9.97 [18] | 6870 [16] | 1450 (250 nm) [16] | 16.3 | 1119 | 100 | 6849
Lin-C4F8O (Non-cyclic C4F8O)* | 9.5 (est.) | Probably < 1 (NOVEC 5110 Analogy) | 1380 @ 400nm (based on 3M PFG-3480 c-C4F8O [7]: linear C4F8O not yet measured but assumed similar) | 18.4 | 0.18 | 112.7* (>100% would imply necessity of operating C4F8O at slight overpressure) | 1.07
C5F12 | 11.63 [18] (BP 30 ˚C at 1 bar) | 6350 [16] | 1750 (180-310nm)[19] (40 ˚C, undiluted) | 13.0 | 957 | 79.3 | 5857
NOVEC 5110 C5F10O | 10.7 [13] (BP 27 ˚C at 1 bar) | <1 [13] | Not yet measured: probably around 1650 by analogy with C4F10 and C4F8O ratio | 13.9 | 0.149 | 85.2 | 0.91
Table 1: GWP loads of various SFCs and NOVEC 5110 blended with N2 ((n-1) = 310.10-6) to match refractivity of CF4 and C4F10
assumed radiator volume: 100 m3
Even bigger GWP load reduction through C4F10 index matching
(eg here: COMPASS RICH)
Lin-C4F10O: Almost Nirvana if industrialised,
Might need slight over-pressure
or slightly-modified Cherenkov thresholds
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 60: CnF2nO fluid selection search criteria
Start(ed)
Non-toxic
(MSDS)
?
N
Y
Non-
Flammable
(MSDS)
?
N
Y
Non-
Oxone-
depleting
?
N
Y
Next CnF2nO fluid
(order & isomer)
to evaluate
Materials/
purifier
Compatible
?
N
Y
N
Y
Rad.
Tolerant
(more for
cooling)
?
N
Y
Dielectric
?
Acid
formation
with H2O
?
N
Y
N
Y
N
Recirc.
Thermo-
dynamics
OK
?
Y
Y
Y
UV-Vis
transparency
OK
?
(n-1) &
Chrom. Disp.
OK
?
N
N
Accept
fluid
Optotests
Materials tests
Bibliographic
Low GWP!
?
N
Y
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 61: Some molecular shapes to study (or eliminate) for UVT, GWP, radiation stability & materials compatibility: example: C4F8O isomers,
Octafluorotetrahydrofuran
CAS: 773-14-8
Octafluoro-3-methoxyprop-1-ene
CAS: 67641-44-5
H332, 335, 336
Inhalation toxicity Cat. 4
BTeV, ALICE VHMPID evaluated; good properties but high GWP
Pentafluoroethyl trifluorovinyl ether CAS: 10493-43-3
Flammable,
H332, 335, 336
Inhalation toxicity Cat 4
Octafluoro-2-butanone
CAS: 337-20-2
Inhalation toxicity H335:
may cause resp. irritation
2,2,3,3,4,4,4-Heptafluorobutanoyl
Fluoride CAS: 335-42-2
H331, 335 Inhalation toxicity Cat. 3
Heptafluoroisobutyryl
Fluoride CAS: 677-84-9
H335 Inhalation toxicity Cat. 3
Source: https://www.synquestlabs.com
Most promising candidate?
analogy with NOVEC 5110,
649 structures…
G. Hallewell: Seminaire CPPM: 16 sep 2024
Shape is everything:
The more shielded the O atom,
the less toxicity, more chemical stability
and probably bigger GWP:
Need expert Chemist input

## Slide 62: Classification Criteria for Inhalation Toxicity
G. Hallewell: Seminaire CPPM: 16 sep 2024
H330 | Fatal if inhaled
H331 | Toxic if inhaled
H332 | Harmful if inhaled
H333 | May be harmful if inhaled
H334 | May cause allergy or asthma symptoms or breathing difficulties if inhaled
H335 | May cause respiratory irritation
H336 | May cause drowsiness or dizziness
H310 | Fatal in contact with skin
H311 | Toxic in contact with skin
H312 | Harmful in contact with skin
H313 | May be harmful in contact with skin
H314 | Causes severe skin burns and eye damage
H315 | Causes skin irritation

## Slide 63: Detector cooling (liquid)
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 64
64
CERN has tested
3M NOVEC 649 C6F12O, (GWP = 0) &
NOVEC 7110 C4F9OCH3 (GWP=249)
Equivalent radiation stability
to C6F14 used as a liquid coolant
in all LHC experiments;
(C6F12O) needs dessicants to prevent acid formation, but standard molecular sieves, activated-C OK: chosen MAPMT coolant; LHCb RICH detector (T ~15°C)
G. Hallewell: Seminaire CPPM: 16 sep 2024
NOVEC 7110
C4F9OCH3
(GWP20=249)

## Slide 65
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 66
G. Hallewell: Seminaire CPPM: 16 sep 2024
Low temp. (-40°C) cooling operation more of a problem
with NOVEC 649:
Undissolved residual water can cause acid formation;
Unresolved issue

## Slide 67
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 68: The Silicon tracker cooling aspect See also https://link.springer.com/article/10.1140/epjp/s13360-023-04703-w
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 69: Examples from cooling particle physics Si trackers (ATLAS, CMS, LHCb)
Two distinct types of detector cooling geometry at HL-LHC:
Tube and block ‘DNA’
ATLAS barrel SCT (present) ATLAS ITK Barrel longerons and Si module
block attachment (future HL-LHC)
Disadvantages: long(er) heat conduction path (more interfaces) Si cold(er) coolant: lower Thermal figures of merit
(2) Micro-channel cooling
LHCb VELO upgrade
Advantages: shortest heat conduction path to coolant: coolant can be warmer:
Disadvantages: fraglity issues: channels etched in silicon and cover plate attached
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 70
Micro-channel cooling: the LHCb VELO upgrade
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 71
Micro-channel cooling: more on the LHCb VELO upgrade
Recent mastery of evaporative CO2 cooling in microchannels
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 72
CO2 problems:
High evaporation pressure at room temperature (60-70 bar):
(test pressure 150 bar)
the detector has to ‘surf ‘ down the saturated liquid line to the operating evaporation temperature of -30  -40 °C (pressure around 12 - 18 bars):
fatigue cycling an issue in
microchannels..?
(2) High triple point temperature of -56 °C
limits the lowest temperature attainable in the tubes of a tube & block cooling system: may not be cold enough for operation of Si detectors after years of irradiation in the LHC High Luminosity program (2029-41)
G. Hallewell: Seminaire CPPM: 16 sep 2024
ATLAS plans to change its inner pixel detector half way through…
A very complicated alternative trans-critical krypton evaporative cycle has been proposed …

## Slide 73: The Silicon Tracker Perspective in the HL-LHC era
https://lhc-commissioning.web.cern.ch/schedule/LHC-long-term.htm
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 74
Cold Krypton system for the Phase III Upgrade of the LHC
Luca Contiero, Krzysztof Banasiak (NTNU), Armin Hafner (NTNU), Bart Verlaat (CERN), Paolo Petagna (CERN)
[46] L. Contiero et al; Cold Krypton system for the Phase III Upgrade of the LHC,
Forum on Tracking Detector Mechanics 2023, Tuebingen Germany May 31-June 2 2023
People are clearly worried about poor performance of CO2 particularly for ‘tube & block’ tracker cooling geometries
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 75
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 76: Presentation outlines
Necessity to go colder with the future upgrade of the LHC (HL-LHC plan)
Issues: temperatures unattainable by current CO2 cooling technology
Definition of a new cooling cycle using Krypton
Definition of the different transient modes encountered during gradual cooldown
Design principles to base future design
Dynamic modelling and control logic
Prototype to test cooling concept
[46] L. Contiero et al; Cold Krypton system for the Phase III Upgrade of the LHC,
Forum on Tracking Detector Mechanics 2023, Tuebingen Germany May 31-June 2 2023
HL-LHC operation
2029-2041 (at least)
!!!!
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 77: Xenon demonstrator for the Krypton cycle
Use of Krypton problematic due to very cold temperatures (Tcrit ≈ -64°C)
Xenon proposed thanks to its warmer critical temperature (≈ 17degC)
Required to precondition the unit to start in supercritical phase
Xenon
Krypton
[46] L. Contiero et al; Cold Krypton system for the Phase III Upgrade of the LHC,
Forum on Tracking Detector Mechanics 2023, Tuebingen Germany May 31-June 2 2023
Gymnastodynamics
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 78
Low GWP Alternatives to CO2:
Noble gases like Xenon and Krypton
Both very expensive and in very short supply, particularly since the war in Ukraine.
Complex transcritical circulation for Krypton (outside the scope of this unit);
Xenon probably just squeaks in (~50 bar @ 15 C) but still has relatively high pressure evaporation at room temp, but no triple point problem (-112 ˚C)
(2) Fluoroketone (CnF2nO) replacements for SFCs
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 79
Fluid thermophysical property | NOVEC 649: C2F5C(O)CF(CF3)2 Perfluoro-2-methyl-3-pentanone (C6F12O fluoro-ketone) | C6F14 (Perfluorohexane, Saturated fluorocarbon)
Boiling temp @ 1 atm (˚C) | 49 | 56
Critical Temp (˚C) | 169 | 178
Critical Pressure (MPa) | 1.87 | 1.89
Freezing temperatre (˚C) | < -100 | < -100
Specific heat (J.kg-1K-1) | 1103 | 1050
Density (kg.m-3) | 1610 | 1680
Kinematic viscosity (cSt) | 0.42 | 0.4
Latent Heat (J.kg-1) | 88 | 88
Vapour Pressure @ 25 ˚C (kPa) | 40.4 | 30.9
Vapour Pressure @ 100 ˚C (kPa) | 441 | 350
Water solubility (ppmw) | 21 | 10
Thermophysical Properties of NOVEC 649 (C6F12O) & C6F14
(at 25°C except where noted)
Analogy: a Fluoroketone (CnF2nO) replacement
for a saturated fluorocarbon (CnF(2n+2))
No reason why thermo parameters
of other SFCs and same
order FK analogs shouldn’t be
similarly similar
(though placement of the O atom affects chemi-activity and toxicity, not just GWP…)
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 80
Some Thermodynamic comparisons two convenient SFCs, CO2, Xe
(F-K thermodynamics should be similar to same carbon order SFCs)
C3F8 probably
won’t go cold
enough for
HL-LHC operation, particularly in tube & block trackers
A C2F4O isomer would be the ideal fluid: much cheaper than Xe (depends on toxicity considerations & studies)
https://link.springer.com/article/10.1140/epjp/s13360-023-04703-w
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 81
Strengths CO2 Non-flammable, non-toxic, electrical insulator, non-ozone-depleting, radiation resistant, GWP=1 | Weaknesses CO2 High pressure circulation (60 bar) at ambient temp before cooldown to operating temp High triple point ( -56°C)
Threats CO2 High triple point may make Si tracker operation problematic: less thermal ‘headroom’ after heavy irradiaton (‘thermal runaway’ phenomenon) | Opportunities CO2 Extensive R&D program at CERN Evaporative coolant of choice for ATLAS, CMS for start of HL-LHC program
Strengths C2F6 Non-flammable, non-toxic, electrical insulator, non-ozone-depleting, radiation resistant | Weaknesses C2F6 Very high GWP (around 6000 x CO2)
Threats C2F6 Production will be phased out unless a strong motivation from semiconductor manufacture industry | Opportunities C2F6 Proved to decrease the operating temp of an ATLAS SCT thermal model in blend with 75% C3F8
Strengths xenon Non-flammable, non-toxic, electrical insulator, non-ozone-depleting, radiation resistant, GWP=0 | Weaknesses xenon High pressure circulation (50 bar) at ambient temp before cooldown to operating temp (amost transcritical) Extremely expensive
Threats xenon Very difficult future procurement (war in Ukraine) (10-8 atmospheric content.) | Opportunities xenon Could find expertise In particle physics community for fabrication of circulators: already used in dark matter experiments
Strengths CnF2nO Non-flammable, electrical insulator, non-ozone-depleting, radiation resistant, GWP=0 | Weaknesses CnF2nO
Threats CnF2nO (CAS 354-34-7) Large scale industrial production may depend on the phasing-out of SFCs, needs of semiconductor manufacture industry: Material compatibility needs further study. Toxicity studies needed | Opportunities CnF2nO Expertise in particle physics community for 3M NOVEC 649 (C6F12O)
SWOT analysis of cooling fluids HL-LHC
G. Hallewell: Seminaire CPPM: 16 sep 2024
Trifluoroacetyl fluoride
CAS-354-34-7
H311, H331
Tetrafluorooxirane
CAS: 694-17-7
Unlisted

## Slide 82
The uncertain ECHA (European Chemicals Agency) route to fluorocarbon (PFC, PFAS…) prohibition
(A path paved with impracticalities..?)
Au revoir 3M… need to clarify manufacturers’ attitudes (Dehon Co. (Fr), Synquest (USA), F2 (UK), various companies in China)…
on future lin-fluoroketone (CnF2nO) production
Electronics industry is the driver: we just ride the coat-tails!
[51] ECHA/NR/23/04;
https://echa.europa.eu/-/echa-publishes-pfas-restriction-proposal]
[52] ECHA Candidate List of substances of very high concern for Authorisation;
https://echa.europa.eu/candidate-list-table
[53] Annex to the Annex XV restriction report proposal for restriction: Per- & polyfluoroalkyl substances (PFASs); ECHA; 22/03/2023
https://echa.europa.eu/documents/10162/d2f7fce1-b089-c4fd-1101-2601f53a07d1
[54] Per- and polyfluoroalkyl substances (PFAS); ECHA
https://echa.europa.eu/hot-topics/perfluoroalkyl-chemicals-pfas
[references from https://link.springer.com/article/10.1140/epjp/s13360-023-04703-w
: see back –up material
On the turning away…
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 83: Massive use of fluorocarbons in electronics industry for semiconductor manufacture and soldering complex computer mother boards with SMD components
83
Vapour phase (non-contact) soldering of components on PCBs
(particularly surface mount) in high T fluorocarbon atmosphere !!!
The demand for vapour phase soldering is hardly going to “evaporate”.
New, lower GWP, transfer vapours will be needed (e.g. NOVEC)
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 84
Conclusion
High GWP Saturated fluorocarbons (SFCs: CnF(2n+2)) have ideal optical properties as Cherenkov radiators: C4F10 and CF4 used in COMPASS & LHCb RICH1&2;
Non-conductivity, non-flammability & radiation resistance  ideal coolants: C6F14 used in all LHC experiments; C3F8 evaporatively cools ATLAS silicon tracker;
While not industrialised over a wide CnF2nO range fluoro-ketones could offer similar performance at very low, or 0 GWP;
Radiation tolerance & thermal performance of 3M NOVEC 649 (lin-C6F12O) & NOVEC 7110 (C4F9OCH3) sufficiently promising for consideration to replace C6F14 @ CERN or cooling; issues with lin-C6F12O with acid formation via residual water to be resolved
Cherenkov detectors: subject to optical testing, lin-C4F8O could replace C4F10 while lin-C4F8O or lin-C5F10O (or even heritage C5F12) blended with N2 and monitored in real time by sound velocity gas analysis - could replace CF4 in RICH radiators;
SI tracker COOLING: Lighter molecules (e.g. C2F4O, with similar thermodynamics to C2F6) - would allow lower temperature, 0GWP operation than evaporative CO2 in Si trackers operated at high luminosity: low order CnF2nO toxicity vs molecular shape needs study
Future PFAS Availability issues to understand, but total PFAS bans unrealistic due to demands of the electronics industry which we can profit from.
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 85: https://link.springer.com/article/10.1140/epjp/s13360-023-04703-w Thanks to…
Helen McNamee and Andy Penman (F2 Chemicals, Preston, UK);
Cristophe Frei and Antonello di Mauro (CERN) for discussions on the current availability of fluorocarbons for use as Cherenkov gas radiators;
Jaroslav Vavra (SLAC) for recollections of the SLD CRID commissioning;
Paola Tropea and Erik Butz (CERN) and Nick Lumb (CPPM) for thermal operation details of the CMS silicon tracker;
Martin Doubek (CERN), Koichi Nagai (Oxford University) and Alexandre Rozanov (CPPM) for similar data on the TOTEM and the ATLAS IBL, SCT and pixel detectors
Eric Vigeolas (CPPM) and Joleen Pater (Manchester University) for information on the expected thermal performance of elements of the upgraded ATLAS ITk silicon tracker under HL-LHC conditions.
Paula Collins and Wiktor Byczynski (CERN) for extensive information on the LHCb VELO;
Mathieu Perrin-Terrin (CPPM) for information on the NA62 Gigatracker;
Sune Jacobsen (CERN) for information concerning the cooling of the LHCb Scintillating fibre tracker.
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 86: References and back-up material
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 87
References (1 of 3) https://link.springer.com/article/10.1140/epjp/s13360-023-04703-w
[1] CERN Environment Report 2017–2018 https://doi.org/10.25325/CERN-Environment-2020-001
[2] B. Mandelli; Eco-gas mixtures and mitigation procedures for Green-house Gases (GHGs);
ECFA Detector R&D Road-map Symposium: T.F. 1 Gaseous Detectors, 29/4/2021
https://indico.cern.ch/event/999799/contributions/4204191/attachments/2236047/3789965/BMandelli_ECFA.pdf,
[3] B. Mandelli; R&D for the optimization of the use of greenhouse gases in particle detector systems;
Mini workshop on gas transport parameters for present and future generation of experiments: CERN April 22, 2021
https://indico.cern.ch/event/1022051/contributions/4325947/
[4] G. Rigoletti; Studies to reduce greenhouse gas emissions from detectors at the LHC; EP-DT Seminar May 4, 2022.pdf (cern.ch)
[5] S. Dalla Torre et al; Long term experience with C4F10 in COMPASS RICH-1; Presentation 11th Intl. Workshop on Ring Imaging Cherenkov detectors, Edinburgh, Scotland, Sept 12-16 2022. https://indico.cern.ch/event/1094055/contributions/4932286/attachments/2508724/4311387/RICH2022_C4F10_dallatorre.pdf
[6] 3M PFG-3480: c-octofluorotetrahydrofuran (C4F8O). Note: fluid out of production : product reference now used for a non-fluidic product. For historic product data sheet mentioning its high GWP see (for example): http://static6.arrow.com/aropdfconversion/a7116f41dfdd5b79d2eb7b40afd687f8af23d8ef/mediawebserver(563).pdf
[7] M. Artuso et al; Nucl. Instr & Meth. A Volume 558, (2006), 373-387
[8] Product #2H07-2-08 Synonyms: 2,2,3,3,4,4,5,5-octafluorotetrahydrofuran, Perfluorotetrahydrofuran; CAS No: 773-14-8, MDL No. MFCD00465561: SynQuest Labs Inc., 13201 Rachael Boulevard, Alachua, FL 32615, USA https://www.synquestlabs.com/Home/ProductDetail?SearchText=Octafluorotetrahydrofuran
[9] T. Acconcia et al ; Nucl. Instr & Meth A 767 (2014) 50–60
[10] M. Vollmer et al; Abundances, emissions, and loss processes of the long-lived and potent greenhouse gas octafluorooxolane (octafluorotetrahydrofuran, c-C4F8O) in the atmosphere; Atmos. Chem. Phys., 19, 3481–3492, 2019
[11] 3M Novec® range of fluorinated fluids; https://www.3m.com/3M/en_US/p/c/b/novec/?Ntt=novec
[12] 3M Novec 649/1230 fluid (C6F12O); https://multimedia.3m.com/mws/media/569865O/3m-novec-engineered-fluid-649.pdf,
https://multimedia.3m.com/mws/media/124688O/3m-novec-1230-fire-protection-fluid.pdf]
[13] 3M Novec 5110 fluid (C5F10O); https://multimedia.3m.com/mws/media/1132123O/3m-novec-5110-insulating-gas.pdf
[14] CERN report EN-CV 22/12/2017, EDMS 1751219 2017-334 rev 1.0: Technical Note NOVEC Fluids Qualification Report: Report on the study executed for the qualification of the NOVEC Fluid for Detector Cooling applications.
[15] J. Owens, Understanding the stability and environmental characteristics of a sustainable Halon alternative.
3M Performance Materials 3M Center, St. Paul, MN 55144
[16] CERN Mini-workshop on gas transport parameters for present and future generation of experiments 20/04/2021;
S. Easo; LHCb-RICH detectors and their gas radiators
https://indico.cern.ch/event/1022051/contributions/4333562/attachments/2231064/3780374/LHCb-RICH-Current-GasRadiators-April-2021.pdf,
Options for alternate radiators in LHCb-RICH system (including calculations by O. Ullaland); S. Easo,
https://indico.cern.ch/event/1022051/contributions/4319538/attachments/2231436/3781060/LHCb-RICH-Future-Radiators.pdf
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 88
References (2 of 3) https://link.springer.com/article/10.1140/epjp/s13360-023-04703-w
[17] S.Easo; Nucl.Inst.& Meth. A 876 (2017) 168-173
[18] E. Lemmon, M. Huber, & M. McLinden; REFPROP Standard reference database 23, version 9.0 (2010)
U.S. National Institute of Standards & Technology.
[19] E. Nappi and J. Seguinot Rivista del Nuovo Cimento Vol. 28, N. 8-9 2005 DOI 10.1393/ncr/i2006-10004-6
[20] K. Abe et al. ; IEEE Trans. Nucl. Sci. 45 (1998) 648 SLAC-PUB-7705 DOI: 10.1109/23.6826
[21] G. Hallewell et al; Nucl. Instr. & Meth A264 (1988) 219-234
[22] G. Hallewell; Nucl. Instr & Meth A 876, (2017) 50-53
[23] G. Hallewell et al; MDPI Instruments (2021) 5(1), 6;
[24] P. Stassi et al; Ultrasonic Gas mixture analysis system in the Forward RICH of DELPHI,
DELPHI Internal Note 95-124 RICH73, 25 July 1995
[25] M.Sannino; Nucl. Instr. and Methods in Physics Research A 595 (2008) 208–211
[26] C. D'Ambrosio et al; Monitoring, Alignment and Control of the RICH Detectors; LHCb-Memo-2000-80 RICH 6 September 2000.
[27] P. Fauland, PhD thesis; (COMPASS experiment) University of Bielefeld March 2004.
[28] Now marketed as SensComp model 600 transducer, http://www.senscomp.com/ultrasonic-sensors/
[29] T. Blake et al; Nucl. Instr. Meth A791 (2015) 27-31
[30] A. Papanestis; Nucl. Instr. Meth. A766 (2014) 14–18
[31] R. Calabrese et al; 2022 JINST 17 P07013
[32] J. Vavra (SLAC National Laboratory); private communication.
[33] P. Tropea; The CMS tracker fluorocarbon cooling system,
Engineering Forum: experiences from cooling systems for LHC detectors Oct 30 2008
P. Tropea, E. Butz (CERN); private communications.
[34] G. Aglieri Rinella et al, 2019 JINST 14 P07010
M. Perrin-Terrin (CPPM); private communication.
[35] G. Anelli et al ; 2008 JINST 3 S08007
M. Doubek (CERN); private communication.
[36] D. Attree et al, 2008 JINST 3 P07003
K. Nagai (Oxford), A. Rozanov (CPPM); private communications.
[37] W. Adam et al ; 2021JINST16P02027
CMS Technical Design Report for the Pixel Detector Upgrade CMS-TDR-011, CERN-LHCC-2012-016 07/09/2012
[38] ATLAS Insertable B-Layer Technical Design Report; CERN-LHCC-2010-013 ATLAS TDR 19 15/09/2010
A. Rozanov (CPPM); private communication.
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 89
References (3 of 3) https://link.springer.com/article/10.1140/epjp/s13360-023-04703-w
[39] O. de Aguiar Francisco et al; Nucl. Instr. Meth A. 1039 (2022) 166874
https://www.sciencedirect.com/science/article/pii/S0168900222003394
P. Collins & W. Byczynski (CERN); private communications.
[40] Fluoroketone C2F5C(O)CF(CF3)2 as a Heat Transfer Fluid for Passive and Pumped 2-Phase Applications; P. Tuma, 3M Co., 3M Center, 236-2B-01St. Paul, MN 55144, USA, Proc. 2008 IEEE 24th IEEE Semiconductor Thermal
Measurement and Management Symposium, San Jose CA, March 16-20 DOI: 10.1109/STHERM.2008.4509386
also accessible via: https://twiki.cern.ch/twiki/pub/LHCb/SciFiDemoCooling/F.Tuma_c6K_as.....pdf
[41] L. Gruber et al; Nucl. Instr. & Meth. 958 (2020) 162025 https://www.sciencedirect.com/science/article/abs/pii/S016890021930422X?via%3Dihub
[42] ”Building the future of LHCb”; C. Frei, S. Gambetta, B. Leverington; CERN Courier, September 2021 (2 September 2021)
https://cerncourier.com/a/building-the-future-of-lhcb
[43] M. Battistin et al; Int. J. Chemical Reactor Engineering 2015; 13(4): 511–521
[44] R. Bates et al; 2015 JINST 10 P03027
[45] https://lhc-commissioning.web.cern.ch/schedule/LHC-long-term.htm
[46] L. Contiero et al; Cold Krypton system for the Phase III Upgrade of the LHC,
Forum on Tracking Detector Mechanics 2023, Tuebingen Germany May 31-June 2 2023
[47] L. Contiero et al; Krypton, applied as refrigerant for cooling of silicon detector trackers;
GL 2022: 15th IIR-Gustav Lorentzen Conference on Natural Refrigerants, Trondheim, Norway, June 13-15 2023
[48] D. Alvarez et al: Thermo-Mechanical Performance of the Local Supports for the ATLAS ITk Pixel Outer Barrel:
Experimental and FEA Studies; Forum on Tracking Detector Mechanics 2023, Tuebingen Germany May 31-June 2 2023
E. Vigeolas (CPPM), J. Pater (Manchester University); private communications
[49] B. Verlaat; CO2 cooling experiences in the LHCb Velo Thermal Control System
Engineering Forum: experiences from cooling systems for LHC detectors Oct 30 2008
[50] R. Bates et al; 2013 JINST 8 P02006
[51] ECHA/NR/23/04; https://echa.europa.eu/-/echa-publishes-pfas-restriction-proposal]
[52] ECHA Candidate List of substances of very high concern for Authorisation;
https://echa.europa.eu/candidate-list-table
[53] Annex to the Annex XV restriction report proposal for restriction: Per- & polyfluoroalkyl substances (PFASs);
ECHA; 22/03/2023 https://echa.europa.eu/documents/10162/d2f7fce1-b089-c4fd-1101-2601f53a07d1
[54] Per- and polyfluoroalkyl substances (PFAS); ECHA
https://echa.europa.eu/hot-topics/perfluoroalkyl-chemicals-pfas
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 90
NOVEC 649: C6F12O: GWP <1
NOVEC 7100: C5F9H3O: GWP = 297
NOVEC 649 cools MAPMTs in LHCb!
90
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 91
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 92
The uncertain ECHA path to prohibition
(a path paved with impracticalities?)
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 93
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 94
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 95
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 96
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 97: Some Conclusions at this stage : drawing on https://link.springer.com/article/10.1140/epjp/s13360-023-04703-w
Is the banning of fluorocarbons…a realistic aim? … probably not…
Attractive alternatives to saturated fluorocarbons (CnF(2n+2)) currently exist (!!):
Fluoro-ketone (CnF(2n)O): & NOVEC® molecules with side-spurred O atoms;
3M seem to have lost enthusiasm to produce fluorinated fluids after 2025, but companies like F2 Chemicals (Preston, UK), Astor (Ru), Synquest (FL), Techspray (GA) continue (probably many others: e.g.China): groups at CERN looking into alternative suppliers (stated Jan 26 2024)
We are a small-scale users who will always ride on the back of the semiconductor industry.
We should nonetheless enter discussions with other manufacturers! CERN is already doing this!
But discussion should concentrate on CnF2nO molecules over the full carbon spectrum with GWP = 0.
Points relevant to ATLAS cooling: “Although these fluids do not yet exist in large quantities over the full CnF2n “matrix” the radiation tolerance and thermal performance of NOVEC 649 (C6F12O) is sufficiently promising for it be chosen by LHCb as a C6F14 replacement for the cooling silicon photomultipliers of the new scintillating fibre tracker. Since the NA62 Gigatracker [34] successfully used C6F14 liquid cooling, NOVEC649 may also turn out to be a good substitute for the liquid cooling of future silicon microchannel vertex detectors built in technologies (and/or with inter-module connectivity) unable to resist the high maximum test pressures (160 bars) typical of CO2 evaporative cooling systems. Such vertex detector cooling systems would contain a relatively small volume of liquid coolant.
A new C2F4O – structured evaporative coolant could be a thermodynamic substitute for C2F6 or xenon to achieve silicon temperatures of -40 ˚C or lower in “block and tube” tracker configurations operated at high luminosity below the practical temperature limit for CO2 evaporative cooling systems.”
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 98
https://indico.cern.ch/event/1155238/attachments/2436920/4173752/EP-DT%20Seminar%20May%202022.pdf
https://indico.cern.ch/event/1155238/attachments/2436920/4173752/EP-DT%20Seminar%20May%202022.pdf
98
CPPM ATLAS physics meeting Feb 23 2024

## Slide 99
Approaches to low-GWP fluorocarbon RICH radiator gases
.
See also:
https://link.springer.com/article/10.1140/epjp/s13360-023-04703-w (paper: EuroPhysics J. Plus, Dec 2023)
https://indico.cern.ch/event/1263731/contributions/5398511/attachments/2648319/4584649
/G_Hallewell_DRD4%20Rad%20Gas%20GWP%20with%20annexes%20May%2016%202023.pdf
https://indico.cern.ch/event/1410802/ (DRD4 WG2 meeting 17 May 2024)
https://indico.cern.ch/event/1420840/ (DRD4 WP_3.1 meeting 28 May 2024)
“From the Speed of Sound to the Speed of Light: and beyond!”
99
Notes: 99

## Slide 100
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 101
UV transparency, refractivity, cmhemical stability & compatibility studies needed
for different CnF2nO molecular shapes. RICH detector community very competent & equipped for detailed UVT & (n-1) - much ex-DELPHI RICH diagnostic equipment at CERN for example
Minuteman Model 302 VM.
Most probable PC spectral range
in new build gas RICH detectors
A
ALICE VHMPID: transparancy
measurements in c-C4F8O
Octafluorotetrahydrofuran
CAS: 773-14-8
Synquest Inc. FL, USA
G. Hallewell: Seminaire CPPM: 16 sep 2024

## Slide 102: Q: What gives NOVEC 649/1230 its low GWP?
Scission by UV photons of l around 300 nm
In the atmosphere (low pressure, high UV): the fragments do not reassociate* into saturated fluorocarbons of the type CnF(2n+2) (which would have high GWP)
*The Environmental Impact of CFC Replacements HFCs and HCFCs
T. WALLINGTON et al Environ.Sci.Technol.1994(28)7 320A https://doi.org/10.1021/es00056a714
https://www.nist.gov/system/files/documents/el/fire_research/R0301570.pdf
102
[15]
G. Hallewell: Seminaire CPPM: 16 sep 2024