## Slide 1
Valerio Calvelli
On Behalf of EIC Detector Magnet team
EIC France 2024
IJC Lab Orsay, Oct 9-11, 2024
The MARCO Magnet

## Slide 2: The MARCO Magnet
Parameter | Value
Coil length | 3.51 m
Warm bore diameter | 2.84 m
Cryostat length | 3.84 m
Cryostat outer diameter | 3.54 m
Current | 3924 A
Central Field B0 | 2.0 T
Energy | 45.7 MJ
Field Uniformity | 12.5 % ± 100 cm around center 80 cm radius
Projectivity in RICH Area | < 0.1 (mrad@30GeV/c) < 10 T/A/mm² From Z = 180 cm to 280 cm
Thickness/Nuclear interaction length | 0.468
Detailed Design Phase Concluded
Final TDR Review in Oct 5/6, 2023 :
No remarks on the technical design.
DOE Review Nov 17, 2023 (CD3A) :
Project approved

## Slide 3: Why MARCO?
ECCE
Reuse of BaBar @ 1.5 T in the ECCE yoke
25y operative life + 30y of operation forecast
Sensors problems
New solenoidal magnet @ 1.5 T for replacement as contingency plan – DOE Request
ePIC
New solenoidal magnet @ 1.5 T (minimum), possibly 2.0 T Same dimensions as BaBar
August 2022, from 1.5 T to 2.0 T
MAgnet with Renewed COils
ePIC  Same Barrel Calorimeter structure as sPHENIX

## Slide 4: What is different?
ePIC
Ferromagnetic Yoke in ePIC is different respect to ECCE
Magnet is shifted of 10 cm respect to the IP
BaBar in ePIC with
I = 5 kA (existing lines)
Tmargin = 2.7 K (@4.5K)
provides only 1.15 T at IP
Goal is 2 T, possibly using existing lines and with
Tmargin = 2.5 K (@Tmax in the coil)

## Slide 5: MARCO at a glance
Phase Separator
Chimney
Mandrel
(3 Modules)
Vapor Cooled Lead
Conductor Splices
Primary/Spare Thermosiphon
Radial Tie-Rods
(4 each end)
Axial Tie-Rods
(3 each end)
Outer Vacuum Vessel / Thermal Shield removed for clarity

## Slide 6: MARCO: a technological revolution
Conclusions from Workshop on Superconducting Detector Magnets @ CERN, 12/14 Sept 2022
Detector magnets  Aluminum stabilizer conductors because Aluminum is 3x more transparent to the passage of particles
No existing extrusion line in the world
2022: this technology is not available anymore
2024: CERN and ENEA work together to rediscover this technology again  no industrial partner
CHINA works on it too

## Slide 7: MARCO: a technological revolution
Material | Transparency | 
 | BaBAR 1.15 T* (Al conductor) | Marco 2T (Cu conductor)
Al | 0.382 | 0.113
Cu | 0.011 | 0.166
SS/Brass | 0.000 | 0.181
NbTi | 0.007 | 0.008
G10 | NA | 0.028
Total | 0.400 | 0.468
 | Copper
 | NbTi/Cu
 | Brass
 | G10
 | Fiber-glass
External mandrel
1506.5 mm
3492 mm
6 layers
1668 turns
Internal winding method
RIC conductor for the Iseult 11.7T MRI
  Design developed by CEA/Alstom
  Cable production by Luvata
  The insertion line still exists!
RIC: Rutherford cable In Copper Channel
On-going contract with Luvata
It is possible to use copper stabilizer conductors for detectors magnets
33.6 mm
30 mm
*in ePIC yoke. In sPHENIX, B = 1.4 T

## Slide 8: MARCO: Cold Mass Design
z
IP
3850
100
offset
MOD 1
MOD 2
MOD 3
Hadron
cryostat
1668 turns
93 turns per layer
6 layers
3 modules
350
Lepton

## Slide 9: MARCO: Conductor Design
 | Parameters | Values | Units
Strand | Strand diameter | 0.7 | mm
 | Cu/NbTi | 1.3 | 
 | Ic @ 2.7T & 4.7K | > 680 | A
 | Filament diameter | < 30 | µm
 | RRR Cu | > 80 | 
Cable | NbTi strands | 20 | 
 | Transposition pitch | 50 | mm
Channel | RRR Cu | > 100 | 
 | Copper section (Final) | 43.7 | mm²
Conductor | Nominal current | 3924 | A
 | RRR conductor | > 100 | 
 | Temp. margin @ 2.6T & 4.7K | 2.5 | K
 | LL Margin @ 2.6T & 4.7K | 46.8 | %
 | σ0.2% @ 293K | > 165 | MPa
 | Unit length | 1.05 | km
 | Total length | 18.9 | km
Dimensions are in mm
6.78
4.6
1.26
11.4
Rutherford cable:
20×Ø=0.7 Nb-Ti strands
R~0.3
(2.31)
Solder
0.26
Copper
Fiber Glass Insulation
4.9 mm
Iseult RICC conductor | Ic degradation
Cabling process | <5%
Soldering process | <5%
Ic degradation: 15%
9.2 mm
Qualification tests on samples are ongoing at Twente University

## Slide 10: MARCO: Conductor Margins
B0 | 1.5 T | 1.7 T | 2.0 T | Units
Current | 2900 | 3296 | 3924 | A
Bpeak | 2.00 | 2.27 | 2.67 | T
Temp. margin | 3.1 | 2.9 | 2.5 | K
Enthalpy margin |  |  | 7.4 | kJ/m3
Load line margin | 60.6 | 55.3 | 46.8 | %
I / Ic(Tm,Bpeak) | 17.3 | 21.3 | 28.8 | %
Chart: Bpeak [T]
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
Jc @ 4.7K | 7360.1711 | 4905.6453 | 3646.4254 | 2796.8281 | 2147.8738 | 1614.8926 | 1154.8952 | 741.714 | 354.2996 | 0
Load line | 0 | 870.1062 | 2206.6058 | 6328.0451
B0 = 2T | 1175
B0 = 1.7T | 987
B0 = 1.5T | 870
T helium = 4.55 K
T cable @ Bpeak ≤ 4.7 K
DT = 0.15 K
Bpeak

## Slide 11: MARCO: Magnetic Performances
Parameter | 1.5 T | 1.7 T | 2.0 T | Units
Current | 2942 | 3335 | 3924 | A
# turns | 1668 |  |  | 
B0 | 1.505 | 1.706 | 2.000 | T
Bpeak | 2.003 | 2.271 | 2.672 | T
Energy | 25.440 | 32.689 | 45.008 | MJ
Inductance | 5.847 | 5.847 | 5.846 | H
Fz tot | -23.8 | -29.2 | -32.2 | kN
Parameter | 2.0 T | Requirement | Units | Validation
B0 | 2.000 | 2.0 | T | OK
Field uniformity | 12.5 | 12.5 | % | OK
Projectivity | 3.28 | < 10 | T/A/mm² | OK
Transparency | 0.468 | <0.5 |  | OK
B5300 | 15.4 | <10 | G | Local solution to be studied
B7200 | 10.9 | <10 | G | 
B3400 | 2.4 | <10 | 2.4 | OK
Projectivity region
Uniformity region

## Slide 12: MARCO: Mechanical Design

## Slide 13: MARCO: Mechanical Performances #1

## Slide 14: MARCO: Mechanical Performances #2

## Slide 15: MARCO: Cryogenics Design
Phase separator
13 W
Current leads
12 W – 0.65 g/s
Tie-rods
4 W
Joints
0.3 W
Thermal radiation
21 W
Cable hysteresis
2.8 W@ 1A/s
Mandrel eddy currents
3.2 W@ 1A/s
Heat loads:
Thermal shield (45K – 65K) = 600 W
Cold mass = 31.3 W
Safety devices dimensioned according to
NORM EN21013-3 (stricter than ASME BPVC VIII Div.1)
Cool-down the magnet should take around 10 days

## Slide 16: MARCO: The role of the mandrel for safety
Parameter | Value | Units
Current | 3924 | A
B0 | 2.000 | T
Inductance | 5.846 | H
Ramp | 1 | A/s
Power | 3.642 | W
Eddy current | -1015.32 | A
R mandrel (P/I²) | 3.516 | μΩ
M mandrel | 3.570 | mH
L mandrel | 2.346 | μH
k | 0.964 | 
Chart: Fast Discharge
The strong electromagnetic coupling between the mandrel and the coils will induce a quench-back

## Slide 17: MARCO: Quench
T (K)
MOD1
MOD2
MOD3

## Slide 18: Conclusions
MARCO Detailed Design is achieved:
One in a kind magnet
RIC conductor in copper jacket based on Iseult design
Confortable margins at nominal case
Robust mechanical design
No issue on transparency (even with copper)
Magnet design is full of redundancies to make it work for more than 30 years
MARCO passed the CD3a and it is ready for the procurement phase
Conductor sample in production and test
Technical design report available in the next weeks (there you will find the instrumentation, fault scenarios, drawings etc etc etc…)