## Slide 1: Study and development of new radon adsorbents The IRENE project
GDR DUPhy
Lyon 9 october 2024
José Busto
CPPM / Univ. Aix-Marseille

## Slide 2
Natural, Radioactive, Noble gas
from the U and Th chains
Easy to transport, complicated to capture
Short half-life, high intrinsic activity
Radioactive Background

## Slide 3
Natural, Radioactive, Noble gas
from the U and Th chains
Easy to transport, complicated to capture
Short half-life, high intrinsic activity
Emanation
Radioactive Background

## Slide 4
Natural, Radioactive, Noble gas
from the U and Th chains
Easy to transport, complicated to capture
Short half-life, high intrinsic activity
Emanation
Adsorption
Radioactive Background

## Slide 5
Natural, Radioactive, Noble gas
from the U and Th chains
Easy to transport, complicated to capture
Short half-life, high intrinsic activity
Emanation
Adsorption
Radioactive Background

## Slide 6
Rn Noble gas
Radon Capture
--> no chemistry => physical process : physical adsorption
--> porous materials
Physical adsorption : Surface capture by Van der Waals forces
But not all pores are equally effective
Need to optimise porosity

## Slide 7
Porosity
Activated Charcoal : universal adsorbent (very big surface area (2000 m2/g),
big stability, not toxic, low cost , …)
Activated charcoal : very popular for radon capture
: dozens of papers are published

## Slide 8
2015 : Capture of Rn in over 60 commercial or research materials by dynamic adsorption (SuperNEMO)
- Activated charcoals
- Carbon molecular sieves
- Carbon aerogels (Granada)
- Molecular cages - CC3 (Liverpool)
- MOF
Zeolites (Al, Si) (Marseille, Mulhouse)
Dedritic polymers (Marseille )
On the road to IRENE - Act 1
Pressure = 1 bar
Temperature = +20°C à – 80°C
Gas : N2, He
Rn retention time in the column
Rn reduction factor of the column
Adsorption factor

## Slide 9
2015 : Capture of Rn in over 60 commercial or research materials by dynamic adsorption (SuperNEMO)
- Activated charcoals
- Carbon molecular sieves
- Carbon aerogels (Granada)
- Molecular cages - CC3 (Liverpool)
- MOF
Zeolites (Al, Si) (Marseille, Mulhouse)
Dedritic polymers (Marseille )
Pressure = 1 bar
Temperature = +20°C à – 80°C
Gas : N2, He
Rn retention time in the column
Rn reduction factor of the column
Adsorption factor
On the road to IRENE - Act 1

## Slide 10
Chart: Correlation Factor Adsoption v.s. porosite
| 0 | V<0.5 nm | V0.5-0.7 nm | V0.7-0.9 nm | V0.9-1.2 nm | V1.2-1.6 nm | V1.6-2 nm | V<2 nm
K +20 C | 0 | 0.52071 | 0.63441 | 0.62329 | -0.65135 | -0.4839 | -0.48051 | -0.32304
K 0 C | 0 | 0.14103 | 0.59143 | 0.042759 | -0.33842 | -0.50215 | -0.30707 | -0.11592
K-30 C | 0 | 0.4085 | 0.49058 | 0.011248 | -0.28666 | -0.45601 | -0.29274 | -0.18133
K-50 C | 0 | 0.10848 | 0.6918 | 0.16748 | -0.62133 | -0.5599 | -0.56217 | -0.12336
K_0 Arrhen | 0 | 0.61024 | 0.095637 | -0.2612 | 0.095442 | -0.47321 | 0.034297 | -0.43514
- Optimal porosity :
0.5 - 0.7 nm (Rn 0.4 nm)
- Small effect on the chemical
composition (sulphur)
Some results
Adsorption @ – 50°C and -30°C in AC, CMS, Aerogels
AC CMS Aerogel
Microporosity from 0.5 to 2 nm : IJL
Chemical compostion : CINaM
- 30°C
- 50°C

## Slide 11
2018 : Study of Xe / Rn adsorption with Crytophane supramolecular cages
Very efficient for molecular encapsulation .
Already used for Xe capture
Adjustable cage dimensions
Three cages were studied on two different supports
Silica MCM-41
diamètre de 2,6 nm 6,5 nm.
Silica SBA-14
1000 m2/g
500 m2/g
cages
supports
On the road to IRENE - Act 2

## Slide 12
Rn adsorption in N2 (CPPM)
Xe adsorption (MADIREL)
Activated charcoal Silcarbon K48 180 ± 25
Rn(K48)/Xe(YC125) « selectivity » = 7.8
Very preliminary results.
- Possibility of improving the performance
(type and size of cage, chemical composition, support).
1,68
13.12

## Slide 13
2020 : Study of radon capture on commercial silver zeolites by dynamical adsorption
On the road to IRENE - Act 3

## Slide 14
Adsorption on silver zeolites
(2020 -2023)
- Closed circuit: very high adsorption (very long measurement time)
Breakthrough curbe @-30°C in
0.2 g ETS-10-Ag, 60 l/h N2

## Slide 15
Some results
[m3/kg]
Active Charcoal
Ag Zeolite
1 Reference charcoal (CarboAct®)
3 Commercial Ag zeolites
Ag-ZSM-5
Ag-13X
Ag-ETS-10

## Slide 16
Some results
[m3/kg]
Active Charcoal
Ag Zeolite
1 Reference charcoal (CarboAct®)
3 Commercial Ag zeolites
Ag-ZSM-5
Ag-13X
Ag-ETS-10
~ 100

## Slide 17
[m3/kg]
Active Charcoal
Ag Zeolite
Zeolite NO Ag
1 Reference charcoal (CarboAct®)
3 Commertial Ag zeolites
Ag-ZSM-5
Ag-13X
Ag-ETS-10
2 NO Ag zeolite
13X
ETS-10
Some results
Huge impact of silver on adsorption

## Slide 18
Adsorption fonction T
ETS-10-Ag
ZSM-5-Ag
13X-Ag
Zeolites Ag + AC, CMS, Aerogel
Some results

## Slide 19
High concentration of 226Ra
=> high emanation
Some results
High sensibility to the water
=> Very dry gas
Evolution of the g line at 609 keV of 214Bi in AC and ETS-10
with a flow of dry air + Rn
Rn reach equilibrium
Rn is empty by water

## Slide 20
Potential improvement
Cu and Ni seem to be better candidates than Ag, and are less expensive !

## Slide 21
Innovative mateRials for Extreme radoN capturE
4-year funding project (ANR)
5 labs consortium
Particle physicist + Chemist and Physico-chemist
Experimentalist + theoreticians
The IRENE project

## Slide 22
The IRENE project
Project submitted to the ANR in 2022
Project start in February 2024
-Feedback between the 5 laboratories
-Modelling as a guide
-Three families of adsorbents (Zeolites, Cages, Carbon-based) -Xenon as a reference gas -Radon capture in N2, He, and Xe
Project philosophy

## Slide 23
XRD, SEM/EDX analysis of ETS-10 and ZSM-5 zeolites
The samples used (ETS-10, ZSM-5) could be improved by eliminating non-adsorbent phases (quartz, alumina, etc.).
The contribution of silver to the capture of radon needs to be better understood (Ag+, nanoparticles )
Some preliminary results from simulation
Quartz
ETS-10
Imagerie par électrons secondaires
BSE

## Slide 24
Some preliminary results from simulation
Monte Carlo simulation of adsorption of Rn & Xe in zeolites
Simulated Rn adsorption isotherms @ 298K & isosteric heats of adsorption

## Slide 25
Some preliminary results from simulation
How chemical composition of zeolite influences Rn & Xe adsorption

## Slide 26
Conclusion
Low-energy and low-counting rate experiments require materials with extreme purity and ultra-low radon
concentration.
Traditionally, activated carbons has been used to capture radon with a good efficiency. However the
purification levels reached are not always sufficient.
Materials with adsorption capacities more than 100 times higher than the best active carbons are now
commercially available but they do not have the necessary purity levels and their performance are not well
understood.
-Possible improvements in radon capture can be reached by choosing the right chemical composition and
good porous structure.
-The objective of the IRENE project is to tackle the problem of radon capture in microporous materials
in a scientific and coherent way, thanks to a unique consortium of physical chemists and particle physicists

## Slide 27
IRENE
Thank you for your attention

## Slide 28
Natural, Radioactive, Noble gas
from the U and Th chains
Easy to transport, complicated to capture
Short half-life, high intrinsic activity
Emanation
Adsorption
Radioactive Background

## Slide 29
Emanation : Rn range (10 to 100 nm)
: 226Ra
Transport : temperature
density
intergrain composition (gas, liquid, …)
tortuosity
adsorption
Exhalation = Emanation + Transport
Transport
Range Rn dans N2 ~ 2.5 Range Rn dans Xe.

## Slide 30
Emanation chamber few cm3 (F)
MPK - Heidelberg
Emanation chamber IP2I-Bx 700 L (N2)
Exhalation in gases
Emanation chamber Univ. Zurich
few liters (N2, He)

## Slide 31
What about liquids?
Very few data
Difficult to extract Rn
Extraction with Rn permeable membrane
Extraction by spraying
Extraction by bubbling
Outgasing in vacuum
Outgasing with microwaves
But this concern only water !

## Slide 32
What about the emanation in detection liquids ?
-> Water, Liquid Scitillator, LAr, LXe
Water : few data ( JUNO)
LS : nothing ??
LAr : few ? -> PNNL
LXe : few ? -> CREF projet (UK)
At low temperature the diffusion term is suppressed
In liquids the recoil term is enhanced
What are the rates in cryogenic liquids ?

## Slide 33
What about the detection liquids ?
-> Water, Liquid Scitillator, LAr, LXe
Water : few
LS : nothing ??
LAr : few ?
LXe : few ? -> CREF projet
PNNL LAr
Cold Radon Emanation Facility (UK)

## Slide 34
SNO 1994
Back to water
Increased emanation in the presence of water ?!

## Slide 35
Few results on the field from Marseille
Radon in water (JUNO)
300 cm3 H2O
Air H2O
Radon transport in HEP enhanced by water

## Slide 36
700 L radon emanation chamber (20 PMT)  4 ± 0.3 mBq / PMT In N2 @ LP2i much higher than glass bulbs
10 L radon emanation chamber (2 PMT)  5.6 ± 1.1 mBq /PMT In N2 @ CPPM
Few results on the field from Marseille
Emanation 3’’ PM (JUNO) in N2 v.s. water
In N2
Emanation chamber 10 L, 2 PM, Dt = 30 days
 8 ± 1.5 mBq / PMT
Main uncertainty from Rn extraction in water

## Slide 37
Emanation LXe
Xenon phase diagram
Emanation in liquid phase Xe ~ 1. 4 x Emanation in gas phase
To be confirmed

## Slide 38
Conclusion
Great lack of information on emanation in liquids
A number of effects to be confirmed suggest that the emanation data measured in standard gases are not reliable.
The study of radon emanation in detection liquids is very important for future experiments.
France needs innovative technical projects in the field of very low activity.
Potentially interesting topic for a technical ANR application in future years.