## Slide 1: PSD Data Analysis
ZnWO4 plate
ZnWO4 grains
CaWO4 grains
ZnWO4
Acquisition in a short time range (2.5us)
Acquisition in a long time range (100us)
+ for ZnWO4
for CaWO4

## Slide 2
1. Offset correction (Voffset ~ 25-27 mV)

## Slide 3
2. Shift correction (toffset ~ 5.3us for the long range WF acquisition and 0.23us for the short range WF)
3. Exponential fit

## Slide 4
4. Mix the two waveforms
5. Exponential fit

## Slide 5
ZnWO4 plate
1.9% (instead of 2%)
11.6% (instead of 9%)
86.5% (instead of 89%)

## Slide 6
1.7%
8.8%
89.6%
ZnWO4 plate

## Slide 7
ZnWO4 plate
Tau | %
0.239 | 0.5
2.323 | 6.1
23.8 | 93.4

## Slide 8
ZnWO4 grains
2.2% (instead of 2%)
13.1 % (instead of 9%)
84.7% (instead of 89%)
Cherenkov peak.

## Slide 9
ZnWO4 grains
1.3% (instead of 2%)
7.5% (instead of 9%)
91.2% (instead of 89%)
Cherenkov peak.

## Slide 10
ZnWO4 grains
Tau | %
0.264 | 0.6
2.17 | 5.6
23.98 | 93.8

## Slide 11
ZnWO4 plates vs grains
 | ZnWO4 plate (Voff -27.7, t off -5.3) | 
PLATE | tau | %
1 | 0,7 | 1,88
2 | 7,5 | 11,59
3 | 25,9 | 86,52
 | ZnWO4 plate (Voff -27.7, t off -5.3) | 
PLATE | tau | %
1 | 0,785 | 1,66
2 | 5,524 | 8,77
3 | 25,77 | 89,57
 | ZnWO4 grain (Voff -27.9, t off -5.3 ) | 
GRAIN | tau | %
1 | 0,7 | 2,23
2 | 7,5 | 13,08
3 | 25,9 | 84,69
 | ZnWO4 grain (Voff -27.9, t off -5.3 ) | 
GRAIN | tau | %
1 | 0,56 | 1,33
2 | 3,76 | 7,50
3 | 24,45 | 91,18

## Slide 12
CaWO4 grains
7.3%
92,7%

## Slide 13
CaWO4 grains
8.1%
91,9%