## Slide 1: Few words about test with fine BGO crystal
Friday 29 th November 2024
Magne Magali

## Slide 2: Test setup
PMT
Fine BGO crystal
1.8cm *1.8 cm *1mm
Pmt Hamamastsu R7877
+ divider bridge
HV - 800 V
Oscilloscope Tektronix
BW 350MHz
Input : 50 ohms
Output file: .csv
Signal sheet read and analysed by Labview software
Trigger:
Signal < 5mV during minimum 15 ns
(to supress single photons / dark noise)
Cosmics flux

## Slide 3: acquisition of 1day
It’s takes time to find the right trigger
With coincidence of PMT top and botom low rate and only few signal on BGO
Finaly only trig on pmt signal with more constraint in trigger selection and post selection before analysing .
With this trigger in one arround 1 day we have :
1500 signal capture by the oscilloscope
We reduce to 1106 of significant signal to be availaible for analyse

## Slide 4: Simple Analyse
Mean signaux of the avalaible signal
Zoom of the begin of the mean signal
Fall time = ~ 4 ns
1st peak ~6 ns (20/ 80%)
Rise time ~400ns

## Slide 5: test in progress
Bgo15
Bgo crystal perpendicular to pmt
Bgo16 in progress
Bgo crystal perpendicular to pmt with alpha souce in front of the bgo
Pmt 1
Pmt 2
Next week with pmt coincidence