## Slide 1: Aperiodic gratings for slitless spectroscopy
Constraints
  Easily switch imager / spectro.
  Unbent spectrograph
  Converging beam
Usual gratings:
  Strong defocus due to optical path variations with the diffraction angle
  Distorsion when used with a converging beam
Auxtel solution: Holographic grating
  forced focus on the focal plane at all wavelengths: 0th and 1rst order at same focus
  No distorsion by design of hologram

## Slide 2: Holographic Optical Element (HOE): concept
Record the hologram: record interference pattern of coherent point-sources in A and B at the requested wavelength (l = 639nm)
Read the hologram, the optical function: when illuminated by a beam converging in A, produces an image at B for l = 639nm, and an image along the AB line for other l.
In theory (infinite and perfect linear hologram): only 0, +1 and -1 orders

## Slide 3
Holographic plate
Prismatic mirror
Point source A (reference wave)
Point source B (object wave)

## Slide 4: HOE performances: focus, resolution
Profile width of the dispersed first order light, as a function of the wavelength (Gunn-z passband)
-> Commensurable with the expectations from simulations (ZEMAX)
-> Low performance of the photopolymer hologram due to the extra glass layer (no anti-reflective)
Spectrum profile of CALSPEC standard star
Phase hologram
O2
Ronchi 400 l/mm
Estimates of spectral finesse R=l/Dl @Ha
Gratings
- Ronchi 400 l/mm: R ~ 70
- Blazed 300 l/mm: R ~ 125
Holograms
- Photopolymer : R ~ 130
- Phase argentic : R ~ 280
- Amplitude Ag : R ~ 390

## Slide 5: Réseau synthétique pour StarDice
Objectif: graver un réseau apériodique à profil en dent de scie (asymétrique) non réalisable en holographie
Pourquoi dent de scie?
  100% de la lumière part dans l’ordre 1 (à une longueur d’onde choisie)
Pourquoi apériodique?
  Equivalent holographique: fonction de focalisation à l’ordre 1 au point souhaité
  On peut même avoir une focalisation différente entre l’ordre 0 et l’ordre 1
Dmax=450nm
Hauteur motif = 900nm

## Slide 6: Schéma de principe

## Slide 7: Vérification image générée pour gravure
Détail du profil central
zoom
bas-gauche
zoom
bas-droite
Image de 1cm2 (résolution 0.2m, 8 bits, 175Mo) produite par combinaison de
- figure d’interférences à 2 sources ponctuelles
- profil du motif (lentement variable) en dents de scie

## Slide 9: R&D fabrication motif en relief
Contacts préliminaires pour synthèse additive
Fournir une carte 3D
  Jean-Eric a fabriqué une image combinant le motif élémentaire et le dessin généraldes lignes du réseau.
Fabrication d’un élément 1cm2
  > Relancer

## Slide 10: COMPLEMENTS

## Slide 13: PNG356.9+04.4

## Slide 14: Hologramme