## Slide 1: Optimising the yield of optically stimulated luminescence in BaF2
1/14

## Slide 2: Main result
2/14

## Slide 3: Luminescence via self-trapped excitons
3/14

## Slide 4: Luminescence via self-trapped excitons
4/14

## Slide 5: Luminescence process in baf2
Ionizing radiation excites an electron from a fluor ion
Neighbouring fluors bind together as a hole in the form of a molecule
Reorientation of the molecule self-traps the hole and creates a vacancy to trap the electron
The trapped electron and hole form a self-trapped exciton (STE)
Non-radiative decay of the STE leads to spatially separated defects
J.C. Warming et al., Nature Photonics (in review)
5/14

## Slide 6: Optical absorption
6/14

## Slide 7: Optical absorption – transient
Two main bands dominate
Charges are trapped immediately
A fast component couples the bands
6/14

## Slide 8: Optical absorption – stable
The two main bands persist over a long time.
Spectral separation and difference in shapes indicates distinct traps.
Optical bleaching suggests these to be responsible for OSL.
7/14

## Slide 9: Lattice configurations
Spectral separation of traps
  Allows for selective liberation
Hole liberation
  F center + H center (scintillation STE)
Electron liberation
  Free electron + H center
8/14

## Slide 10: Yield increase
Electron stimulation increases the OSL yield for the following measurement
Hole liberation/bleaching seems to reset the effect
9/14

## Slide 11: Emission spectra
OSL emission spectrum is very similar to scintillation
  Possibly due to STE configurations
Scintillation can be induced by two-photon absorption (2PA)
  Not limited to ionizing radiation
200
250
300
350
400
450
10/14

## Slide 12: optical excitation and osl
Decay times are similar between scintillation and OSL, although OSL rise is slow
OSL from ionizing radiation and optical excitation decay equivalently
Scintillation
OSL
11/14

## Slide 13: Spatial readout
Imaging of OSL after ”irradiation” from 2PA with fs-laser pulses (~50 µJ)
Moving the irradiation position creates spatially separated signals
Solid spatial resolution (~500µm) limited by readout beam width.
12/14

## Slide 14: Conclusion and outlook
Charge trapping in BaF2 results from non-radiative STE decay
The OSL yield can be increased by selective liberation of electrons
Scintillation and OSL are both independent of excitation source
Can we homogeneously increase the OSL yield?
How do we determine the optimal stimulation wavelength?
Can the spatial readout be used to gain information about non-linear processes?
13/14

## Slide 15: Thank you for your attention
Questions?
Contact: jcwarming@phys.au.dk
Supervision: Rosana M. Turtos & Peter Balling
14/14
Funding: