## Slide 1
CaxPb1-xWO4 grains (first attempt of production)
Ca0.7Pb0.3WO4
Ca0.5Pb0.5WO4
Mixed CaxPb1-xWO4 grains were produced by the flux method
(as well as ZnWO4 and CaWO4 grains before):
CaCO3+PbO+WO3 (in stoichiometric proportions)+Na2WO4 (flux)
The yield of the grains is very low at the moment, they are "sticked"
in the flux volume.
According to XRD powder analysis the grains have the crystal lattice
of sheelite (CaWO4) type.
Real stoichiometric composition of the grains (chemical analysis):
Nominal composition | Real composition
Ca0.7Pb0.3WO4 | Ca0.75Pb0.25WO4 (ensemble of grains)
Ca0.5Pb0.5WO4 | Ca0.75Pb0.25WO4 (small grain)
 | Ca0.92Pb0.08WO4 (medium grain)
 | Ca0.91Pb0.09WO4 (big grain)

## Slide 2
Wavelength, nm
Intensity, abs.un.
CaWO4 grains
ZnWO4 grains
Ca0.5Pb0.5WO4 grains
X-ray excited luminescence
Photo-excited luminescence
Excitation
λem=440 nm
Emission
λex=300 nm
Decay curves under photo-excitation
λex=266 nm, λem=430 nm
τ~5 µs
λex=266 nm,
λem=410 nm
Luminescent properties*
*All luminescent measurements were done using the ensemble of the grains

## Slide 3
Brief summary
At the moment, the desired Ca0.5Pb0.5WO4 composition is not achieved, the highest content of Pb in the grains is 0.25. Is it due to the physical-chemical limits for the solubility? If yes, is Ca0.75Pb0.25WO4 composition is “acceptable” for GRAiNITA?
What is the bulk density of the mixed grains? For experimental study a sufficient amount (~30-50 cm3) is required.
The real chemical composition changes from one grain to another. How this fact will affect on the uniformity of the scintillation performance? If we have some small amount of the grains in the next future, we can check the light yield for each grain using Am241 source as we have done before for ZnWO4 grains.
The technology for the mixed grains production should and can be  improved to increase the yield, optimize the chemical composition uniformity, etc.