## Slide 1
Study of point-like absorbing defects in large mirrors for gravitational wave detectors
Maxime LE JEAN
Supervisor : Jérôme DEGALLAIX
Laboratoire des Matériaux Avancés
(LMA)

## Slide 2
Increasing the circulating power
Direct way to decrease shot noise
Comes with drawback :
  Wavefront distortion
  Radiation pressure
We have possibilities to counterbalance the drawback
- Quantum Squeezing
- Thermal compensation systems
Virgo Attempts
Still problematic until now Increase of power attempts at O4
not completely succesfull

## Slide 3
Point absorbers (PA)
A punctual site of excess absorption
Wide range of diameters [10 – 500] µm
Wide range of local absorption expected
There can be several PA’s per mirrors
  (2018 : LHO ITMY  « Constellation of PAs »)
Generally of metallic nature (Al)
The more power is in the ITF, the more problematic the PAs become -> limits improvements of the detectors
Critical for arm cavity mirrors

## Slide 4
Detecting them at LMA
Originate from deposition process
- Embedded in the coating
- Small particules from mounts, walls, protective sheets
Detecting them before their installation in the ITF. (Corrective treatments, preparing compensations …)
Virgo cannot detect PAs before mirror installation
A joint study LIGO/LMA has already allowed to reduce the population of PA’s
Benefitial for other projects high optical power experiments

## Slide 5
Construction of caracterization bench
CW laser at 1064 nm (200 W)
Will be able to holds 62 cm diameter and > 300kg test masses
Same power density than in AdV ~3kW/cm²
Shack-Hartman wavefront sensitivity
 (λ/100)
Expanding the Caltech bench (TM-HPAD) Test mass Hartman PA Diagnostic
Bonus :
Scattering measurement with CCD camera

## Slide 6
Principle scheme of measurement
P
t [s]
T
t [s]
t0
t1
tf
(near PA)
t0
t1

## Slide 7
Numerical simulations
Finite element simulation (FEM)
 Simulation of an AdV test mass in the ITF configuration
Discretization of the geometry and linearization of equations
Finds approximate solutions for fields ( T, u, , … )
Compute for stationary solution or transient evolution
Point absorbers are simulated by declaring nodes as heat sources

## Slide 8
Absorption Uniforme
Silica cylinder φ = 35cm
Parameters from Suprasil material
Incident Power 100kW (AdV+)
Uniform Absorption 0.2ppm
Below Shack-Hartman sensitivity
Stationnary solution
Results on uniform absorption are convincing enough to
use COMSOL model to simulate point absorbers

## Slide 9
Point absorbers
Conditions of our setup
P = 200W , = 2,5mm
Few comparable ressources for point absorption
PA properties :
Radius : 10 m, Abs = 1 mW

## Slide 10
Transient evolution
We observe a convergence of the transient evolution to the stationary value
For point absorbers we expect to have more than 70% of the effects after 20s of pump time duration
The cooling dynamics could also be used to improve the detection accuracy

## Slide 11
Theoretical capabilities of our setup
A size limit we could choose is one dictated by the dark field microscope
Even in defavorable cases we’ll be able to detects Pas of larger size
May be improved by a deeper analysis of the wavefront or the dynamical evolutions
Similar to Caltech’s bench sensitivity

## Slide 12
Status of the setup
( Installed in the cleanroom )

## Slide 13
Upcoming work
Automatise callibrations / data acquisition / logs and error handling/…
Enhancing the sensivity by reducing vibrations, optimizing optical alignment
Design of the large mount and adaptations
Collecting datas over test samples
(relatively long scan time, provide feedback for coating R&D processes)
Develop an analysis pipeline for theses datas
Testing Virgo test masses ?
Remote-Controlled Elements :
- Laser 200W - Power-meter
- 2x Piezo-mounts - Wavefront sensor
- 4x Linear Stages

## Slide 14
Experimental study of point-like absorbing defects in large mirrors for gravitational wave detectors
Maxime LE JEAN
Supervisor : Jérôme DEGALLAIX
Laboratoire des Matériaux Avancés
(LMA)

## Slide 15
Thermo-elastic effects
Thermo-optical effects
Elasto-optic effects
Computation details

## Slide 16
Small mounts
The large mount takes time to design and manufacture so I ordered a solution to scan smaller mirrors
100 diameter samples : 30 min scan time duration

## Slide 17
SHWFS HASO 4

## Slide 18
Resume of PA in LIGO test masses