## Slide 1: Ultra-thin Diamond Detectors for On-line Monitoring of Ion Microbeams
Claire Léonhart
JUIN 2025 – Assemblée Générale du GDR DI2I
Mission pour les Initiatives Transverses et Interdisciplinaires
80|PRIME

## Slide 2: Table of contents
  Context
      Microbeam and their monitoring
      Diamond detectors
  Diamond etching
      Why an ultra-thin diamond ?
      Etching technique and parameters
      Defects and consequences
      Optimization of etching recipe
  Membrane detector fabrication
      Etching masks and steps of process
      In lab characterization of membrane
  Conclusion

## Slide 3: Contexte: Ion microbeam and monitoring
01

## Slide 4: Microbeam’s interest in radiobiology
Global irradiation
Each cell receives a mean number of particle
Irradiation by microbeam
Targeted irradiation
-> select the irradiated cells
-> select the part of each cell
Irradiated nucleus
Irradiated cytoplasm

## Slide 5: Two microbeam line with few differences
MIRCOM
Solid and gaseous ion sources
AIFIRA
Gaseous ion sources
Singeltron 3,5 MV accelerator
3 MeV Proton 3 MeV Alpha
TandetronTM 2 MV accelerator
4 MeV Proton 6 MeV Alpha 8 MeV C3+, O3+

## Slide 6: Presentation of microbeam lines

## Slide 7: Microbeam monitoring
secondary electrons
ions
air
PIPS detector
Si3N4 extraction window
vacuum
Activ Diamond window
    Chaneltron detector
Efficient detection of carbon and oxygen ions
Efficient detection of alpha particle but need to adapt the extraction window
Not efficient for protons
(Lalanne, 2023, PhD thesis)
×
The detector must be able to:
- efficiently detect protons as well as heavier ions
- count ions at very low (single ion) and high beam intensities (104 particle.s-1)
Sample holder - Produced by the Detector, Instrumentation and Electronics Departments at LPSC

## Slide 8: The diamond as a solid-state ionization chamber
Incident particle
+
+
+
E
Read out electronics
Diamond as a detector:
Very low leakage current
Low noise
Good radiation hardness
Very fast
Work at room temperature
+
+
+
+
-
-
-
-
-
-
-
Diamond = Wide band-gap semiconductor

## Slide 9: Ultra-thin diamonds and their problematics
Why ultra-thin?
To have a minimum quantity of material before the biological environment,
And to limit disturbances: loss of energy and spatial deviation.
Window Ø 500 µm, few micrometers thin
Metallized electrodes for diamond biased and signal read-out
50 µm
scCVD diamond
Electronical or optical grade
How to obtain this kind of thinness ?
  Etching of diamond
  Polycrystalline diamond mask
  Objectives :
  - good thickness homogeneity
  - sufficiently low surface roughness to limit leakage currents
1 mm
Polycrystalline diamond masks with laser cut square and round patterns

## Slide 10: Diamond etching
02

## Slide 11: Plasma etching of diamond
Reactive Ion Etching : use of a mix of chemical reactant and chemically inert species ; physical and chemical process
Can be of two types :
  CCP = Capacity Coupled Plasma : only one RF parameter
          Need a highly chemical specy (like O2) for good kinetic.
  ICP = Inductively Coupled Plasma : two RF powers permitting to separate plasma density and its acceleration
          More suitable for deep etching because plasma can be denser.
plasma
~
~
plasma
~
Sample

## Slide 12: Important characteristics to evaluate an etching
Etching rate (nm/min) measured with profilometers
Final rugosity of sample (nm RMS) measured with profilometers
  to be compared with initial rugosity
Thickness homogeneity (%) depends on initial planarity of sample
Etching defects : etch pit / microtrenching
        Etch pits : preferential etching of dislocation by oxygen resulting in pits
        Microtrenching : overetching on the side of the pattern, due to the important thickness of both mask and deep etching

## Slide 13: Etching defect : etch pits
SEM picture
!!! Each black dot on the surface is a hole about 1 µm deep !!!
250 µm
RIE-CCP : 280 W Platen
CF4 7 sccm + O2 40 sccm
77 mTorr
19,2 µm etched (80 nm/min)
Resolved by eliminating O2 in the process

## Slide 14: Etching defect : microtrenching
RIE-ICP : 400 W Platen + 1600 W ICP
CF4 25 sccm + Ar 25 sccm
10 mTorr
27,1 µm etched (113 nm/min)
Microtrenching : 800 nm (3 % of etched depth)

## Slide 15: Comparing etching recipes
Recipe | RIE-CCP : 280 W 50 sccm O2 + 7 sccm CF4 77 mTorr | RIE-CCP : 280 W Only CF4 77 mTorr | RIE-ICP : 400 W + 1600 W Only CF4 10 mTorr | RIE-ICP : 400 W + 1600 W 50 % CF4 + 50 % Ar 10 mTorr | RIE-ICP : 400 W + 1600 W 40 % CF4 + 60 % Ar 10 mTorr
Kinetic | 80 nm/min | 31 nm/min | 133 nm/min | 114 nm/min | 83 nm/min
Optical characterization |  |  |  |  | 
Profilometry (microtrenching) | No | No | 10 % ( ~800 nm for 8,5 µm) | 3 % (~800 nm for 27,1 µm) | 1 % (~100 nm for 10 µm)
Promising but needed to be confirmed in longer etching

## Slide 16: FABRICATION OF Membrane detector
03

## Slide 17: Etching process with two masks
Concentric patterns
Diameters difference of 100 µm
Expected profile:
Apparition of microtrenching on long etching.
Smooth edge on the small diameter after 2nd short etch.

## Slide 18: Etching process with two masks : optical and profilometer characterization
37,8 µm etched in 6h.
One of the window broke during cleaning steps using ultrasound.
No microtrenching measured by profilometer.
Imperfect alignment of the two masks resulted in an offset in patterns.
42,4 µm etched in total, membrane is less than 8 µm thick.
First deep etching
Second deep etching
With Ø 600 µm mask
With Ø 500 µm mask
Profil ligne

## Slide 19: Etching process with two masks : MEB characterization
Microtrench spread out on ~10 µm but limited in depth.
Etched surface is smooth and defect free.
42,4 µm

## Slide 20: Conclusion & Perspectives
Thinning of diamond for membrane detector is a real challenge:
Etching defects are a problem for detection and could rupture the window. Oxygen in etching recipes is responsible for revealing etch pits. High kinetic recipe produce also microtrenching.
Adjustments on etching recipe permit a sufficient kinetic with good surface quality for detector purpose but do not eliminate microtrenching problematic, only reduce it.
A 8 µm-thick membrane was fabricated, with limited microtrenching and low surface defects concentration.
Test on detector capability are planned in July at AIFIRA.
Ultimate thinning of the membrane without any mask is considered.

## Slide 21
Mission pour les Initiatives Transverses et Interdisciplinaires
80|PRIME
M-L. Gallin-Martel
D. Dauvergne
A. Bes
J-F. Muraz
M. Reynaud
E. Gheeraert
J-F. Motte
F. Donatini
J. Pernot
P. Barberet
J. Jouve
F. Vianna-Legros
M. Cardot-Martin
K. Lalanne
C. Léonhart

## Slide 22: Back-up slides

## Slide 23: Contact deposition for bias and signal collection
400 W Platen + 1600 W ICP
CF4 25 sccm + Ar 25 sccm
10 mTorr
27,1 µm on a test sample (etching rate = 113 nm/min)
Next step = aluminum deposition
To ensure electric continuity between the bottom of the pit and the non-etch surface of the diamond
Deepest etching yet with this surface quality
Ω
Measured resistance of a few ohms only
The technique of deposition is suitable for contact even with steep angles.

## Slide 24: Evolution of the etching recipe: oxygen-free = etch pits-free
Etching rate = 31 nm/min
Really slow, but without any etch pit.
1h20 etching
2,4 µm
280 W
CF4 50 sccm
77 mTorr
O2
CF4
250 µm
Dislocation
125 µm

## Slide 25: Change of etching device: RIE ICP (oxford @ CEA)
125 µm
Circle 500 µm
400 W Platen + 1600 W ICP
CF4 50 sccm
10 mTorr
1h etching
8,5 µm
Rugosity: 14 nm RMS
for 9 nm initially
ICP: Inductively Coupled Plasma, Decoupling plasma density and acceleration with two distinct RF power
Etching rate = 142 nm/min
Compatible with detection device manufacturing requirements