## Slide 1
New X-ray analysis techniques for performance characterization of semiconductors for electronics
Pierre Everaere
Presented by : Robin Molle

## Slide 2: ESRF - European Synchrotron Radiation Facility and BM05 Beamline
BM05 beamline:
60 m far from source
Parallel beam to cm size
Focused beam to µm size
White beam Energy:3 to 160keV
Monochromatic Energy: 4 to 60 keV
From 2020, ESRF-Extreme Brilliant Source, the first of a new generation of high-energy synchrotron sources, opens up new opportunities in X-ray science.
Grenoble, France
BM05

## Slide 3: Experiment on BM05 beamline
Defects characterization techniques at BM05 by:
  Bragg Diffraction Imaging
  X-Ray Beam induced Current (XBIC)
  Time of Flight XBIC (ToF-XBIC)
Context
Semiconductor industry often requires high quality crystalline thin layers and substrates to create their devices otherwise it generates defects.

## Slide 4: Experiment on BM05 beamline
Context
Semiconductor industry often requires high quality crystalline thin layers and substrates to create their devices otherwise it generates defects.
Linear dislocation
« Punctual »
Precipitate / Inclusion
Other defects: twins, stacking faults, growth striations, subgrain boundaries, ….
Defects characterization techniques at BM05 by:
  Bragg Diffraction Imaging
  X-Ray Beam induced Current (XBIC)
  Time of Flight XBIC (ToF-XBIC)

## Slide 5: Experiment on BM05 beamline
Context
Semiconductor industry often requires high quality crystalline thin layers and substrates to create their devices otherwise it generates defects.
Defects characterization techniques at BM05 by:
  Bragg Diffraction Imaging
  X-Ray Beam induced Current (XBIC)
  Time of Flight XBIC (ToF-XBIC)

## Slide 6: x RAY DIFFRACTION Imaging
Based on the X-ray diffraction on crystal planes
      Here Si monocrystal
Bragg’s law:
      with X-ray wavelength ↔ X-ray energy (Planck-Einstein law)
      interplanar distance, linked to the material
      Bragg’s angle, between the material plane and the X-ray beam
      (and we use )
In this configuration, a part of the X-ray beam is diffracted with the same angle , instead of passing straight through the material.
A disturbance in the crystalline stack, which can affect the material properties (damage, deformation, curvature, defects…), affects also the diffraction

## Slide 7: Characterization techniques : Bragg diffraction Imaging (monocrystal)
Rocking Curve Imaging
Bragg’s law : λ = 2d sin(ϴ).
The sample is tilted (steps of at the Bragg angle ϴ and a 2D X-ray detector at 2 ϴ. => Rocking curve
Parameter extraction (FWHM, integral and peak position)
2D map
Density of defects
Orientation of defects
No Sample preparation
Notes: The EPN science campus is an international science hub hosting three major European institutes along with joint partnerships. It hosts a staff of 1500, including 500 scientists or postgraduate students, and welcomes more than 8000 guest researchers every year, resulting in more than 2500 publications annually in peer-reviewed journals.
Grenoble, in the heart of the French Alps, is famous for science and innovation. In a world where technological progress depends more than ever on fundamental research, the European Photon and Neutron Science Campus (EPN) offers not only the world’s most powerful neutron source, the ILL, but also the world’s premier source of protons, the ESRF.
As service institutes, the ILL and the ESRF provide facilities for scientists from their 19 member countries and others from all over the world. The EMBL has its Grenoble laboratories on the campus and runs a scientific programme strongly related to the neighbouring neutron and photon facilities and amplified through numerous collaborative projects.
Scientific instrumentation of this quality has made the campus a unique location for experiments breaking new ground in modern research, in fields as diverse as structural biology, fundamental physics, or the science of materials.
To maintain this momentum the institutes seek synergies and scientific partnerships at every level. As science advances and research needs develop, new support facilities are provided such as the Partnership for Structural Biology (PSB), with its highly specialised laboratory for the deuteration of biological samples (D-Lab), and its materials science support laboratory. At the ESRF, eleven Collaborating Research Groups complement the offer of beamlines to the European scientific community.

## Slide 8: Experiment on BM05 beamline
Defects characterization techniques at BM05 by:
  Bragg Diffraction Imaging
  X-Ray Beam induced Current (XBIC)
  Time of Flight XBIC (ToF-XBIC)
Crystal and semiconductor as GaN, SiC, Diamonds, solar panel, aluminium nitride, etc…
Context
Semiconductor industry often requires high quality crystalline thin layers and substrates to create their devices otherwise it generates defects.

## Slide 9: Characterization techniques : X Beam Induced Current
XBIC
SemiC.
+
+
+
+
+
+
—
—
—
—
—
—
+
—
X-ray
Electrode
Electrode
X-ray interaction with semiconductor:
  Photoelectric effect
  Compton effect
  Pair creation

## Slide 10: Characterization techniques : X Beam Induced Current
XBIC
SemiC.
+
+
+
+
+
+
—
—
—
—
—
—
+
—
X-ray
Electrode
Electrode
A
Pico-ammeter
X-ray interaction with semiconductor:
  Photoelectric effect
  Compton effect
  Pair creation
Electric field apply
=> Induced current inside the semiconductor

## Slide 11: Characterization techniques : X Beam Induced Current
XBIC
SemiC.
+
+
+
+
+
+
—
—
—
—
—
—
+
—
X-ray
Electrode
Electrode
A
Pico-ammeter

## Slide 12: Characterization techniques : X Beam Induced Current
XBIC
SemiC.
+
+
+
+
+
+
—
—
—
—
—
—
+
—
X-ray
Electrode
Electrode
A
Pico-ammeter
Induced
Current
Monochromatic beam (Energy around 10 keV) (Diameter around 20 µm)
Monitoring by pin diode and ionization chamber
Scan with beam => 2D current map
Measure the impact of defects and impurities in the material on the transport of the charge carrier
Parameters : Beam energy, beam flux and beam size

## Slide 13: XBIC maps of various diamonds substrates
The electronic response of diamond substrates strongly depends on the type of growth and orientation.
It can be very heterogeneous even with crystals with low structural defects density
and the XBIC technique is particularly adequate to measure precisely this property.
Diamond grown on iridium
HPHT IIa diamond
110-oriented CVD diamond
CVD diamond
100-oriented CVD diamond
HPHT Ib diamond
“Electronic grade”
“Optical grade”
“HPHT”
Notes: The EPN science campus is an international science hub hosting three major European institutes along with joint partnerships. It hosts a staff of 1500, including 500 scientists or postgraduate students, and welcomes more than 8000 guest researchers every year, resulting in more than 2500 publications annually in peer-reviewed journals.
Grenoble, in the heart of the French Alps, is famous for science and innovation. In a world where technological progress depends more than ever on fundamental research, the European Photon and Neutron Science Campus (EPN) offers not only the world’s most powerful neutron source, the ILL, but also the world’s premier source of protons, the ESRF.
As service institutes, the ILL and the ESRF provide facilities for scientists from their 19 member countries and others from all over the world. The EMBL has its Grenoble laboratories on the campus and runs a scientific programme strongly related to the neighbouring neutron and photon facilities and amplified through numerous collaborative projects.
Scientific instrumentation of this quality has made the campus a unique location for experiments breaking new ground in modern research, in fields as diverse as structural biology, fundamental physics, or the science of materials.
To maintain this momentum the institutes seek synergies and scientific partnerships at every level. As science advances and research needs develop, new support facilities are provided such as the Partnership for Structural Biology (PSB), with its highly specialised laboratory for the deuteration of biological samples (D-Lab), and its materials science support laboratory. At the ESRF, eleven Collaborating Research Groups complement the offer of beamlines to the European scientific community.

## Slide 14: Example of Characterization : scvd diamond as alpha beam monitor
Diamond
Notes: The EPN science campus is an international science hub hosting three major European institutes along with joint partnerships. It hosts a staff of 1500, including 500 scientists or postgraduate students, and welcomes more than 8000 guest researchers every year, resulting in more than 2500 publications annually in peer-reviewed journals.
Grenoble, in the heart of the French Alps, is famous for science and innovation. In a world where technological progress depends more than ever on fundamental research, the European Photon and Neutron Science Campus (EPN) offers not only the world’s most powerful neutron source, the ILL, but also the world’s premier source of protons, the ESRF.
As service institutes, the ILL and the ESRF provide facilities for scientists from their 19 member countries and others from all over the world. The EMBL has its Grenoble laboratories on the campus and runs a scientific programme strongly related to the neighbouring neutron and photon facilities and amplified through numerous collaborative projects.
Scientific instrumentation of this quality has made the campus a unique location for experiments breaking new ground in modern research, in fields as diverse as structural biology, fundamental physics, or the science of materials.
To maintain this momentum the institutes seek synergies and scientific partnerships at every level. As science advances and research needs develop, new support facilities are provided such as the Partnership for Structural Biology (PSB), with its highly specialised laboratory for the deuteration of biological samples (D-Lab), and its materials science support laboratory. At the ESRF, eleven Collaborating Research Groups complement the offer of beamlines to the European scientific community.

## Slide 15: Example of Characterization : scvd diamond as alpha beam monitor
Diamond
Used as beam monitor for charged particle
  Quantify the impact of irradiation
Creation of mono-vacancies Altered Metallization
Irradiated
The diamond was irradiated on several points :
Same fluence
Different flux
F. Lafont, 2023
https://doi.org/10.1016/j.diamond.2023.110454
Notes: The EPN science campus is an international science hub hosting three major European institutes along with joint partnerships. It hosts a staff of 1500, including 500 scientists or postgraduate students, and welcomes more than 8000 guest researchers every year, resulting in more than 2500 publications annually in peer-reviewed journals.
Grenoble, in the heart of the French Alps, is famous for science and innovation. In a world where technological progress depends more than ever on fundamental research, the European Photon and Neutron Science Campus (EPN) offers not only the world’s most powerful neutron source, the ILL, but also the world’s premier source of protons, the ESRF.
As service institutes, the ILL and the ESRF provide facilities for scientists from their 19 member countries and others from all over the world. The EMBL has its Grenoble laboratories on the campus and runs a scientific programme strongly related to the neighbouring neutron and photon facilities and amplified through numerous collaborative projects.
Scientific instrumentation of this quality has made the campus a unique location for experiments breaking new ground in modern research, in fields as diverse as structural biology, fundamental physics, or the science of materials.
To maintain this momentum the institutes seek synergies and scientific partnerships at every level. As science advances and research needs develop, new support facilities are provided such as the Partnership for Structural Biology (PSB), with its highly specialised laboratory for the deuteration of biological samples (D-Lab), and its materials science support laboratory. At the ESRF, eleven Collaborating Research Groups complement the offer of beamlines to the European scientific community.

## Slide 16: Example of Characterization : scvd diamond as alpha beam monitor
Diamond
Used as beam monitor for charged particle
  Quantify the impact of irradiation
Creation of mono-vacancies Altered Metallization
Irradiated
The diamond was irradiated on several points :
Same fluence
Different flux
Annealing at 1000 °C (6h)
Regain efficiency in irradiated and non-irradiated areas
F. Lafont, 2023
https://doi.org/10.1016/j.diamond.2023.110454
Notes: The EPN science campus is an international science hub hosting three major European institutes along with joint partnerships. It hosts a staff of 1500, including 500 scientists or postgraduate students, and welcomes more than 8000 guest researchers every year, resulting in more than 2500 publications annually in peer-reviewed journals.
Grenoble, in the heart of the French Alps, is famous for science and innovation. In a world where technological progress depends more than ever on fundamental research, the European Photon and Neutron Science Campus (EPN) offers not only the world’s most powerful neutron source, the ILL, but also the world’s premier source of protons, the ESRF.
As service institutes, the ILL and the ESRF provide facilities for scientists from their 19 member countries and others from all over the world. The EMBL has its Grenoble laboratories on the campus and runs a scientific programme strongly related to the neighbouring neutron and photon facilities and amplified through numerous collaborative projects.
Scientific instrumentation of this quality has made the campus a unique location for experiments breaking new ground in modern research, in fields as diverse as structural biology, fundamental physics, or the science of materials.
To maintain this momentum the institutes seek synergies and scientific partnerships at every level. As science advances and research needs develop, new support facilities are provided such as the Partnership for Structural Biology (PSB), with its highly specialised laboratory for the deuteration of biological samples (D-Lab), and its materials science support laboratory. At the ESRF, eleven Collaborating Research Groups complement the offer of beamlines to the European scientific community.

## Slide 17: Characterization techniques comparison
a) XBIC map for a 500 µm thick high quality diamond
b) FWHM X-ray RCI map of the same sample as in a). The red arrow shows a bunch of dislocations and the black arrows growth sector boundaries
c) XBIC map for a 150-um diamond from the same batch but irradiated with 68 MeV protons
d) FWHM X-ray RCI map of the same sample as in c)

## Slide 18: Experiment on BM05 beamline
Defects characterization techniques at BM05 by:
  Bragg Diffraction Imaging
  X-Ray Beam induced Current (XBIC)
  Time of Flight XBIC (ToF-XBIC)
Crystal and semiconductor as GaN, SiC, Diamonds, solar panel, aluminium nitride, etc…
Context
Semiconductor industry often requires high quality crystalline thin layers and substrates to create their devices otherwise it generates defects.

## Slide 19: Characterization techniques : Time of flight-XBIC
XBIC
SemiC.
+
+
+
+
+
+
—
—
—
—
—
—
+
—
X-ray
Electrode
Electrode
Preamp
SAMPLING
&
DAQ
A
Pico-ammeter
For timing studies
C. Hoarau, 2021
https://doi.org/10.1088/1748-0221/16/04/T04005
Notes: The EPN science campus is an international science hub hosting three major European institutes along with joint partnerships. It hosts a staff of 1500, including 500 scientists or postgraduate students, and welcomes more than 8000 guest researchers every year, resulting in more than 2500 publications annually in peer-reviewed journals.
Grenoble, in the heart of the French Alps, is famous for science and innovation. In a world where technological progress depends more than ever on fundamental research, the European Photon and Neutron Science Campus (EPN) offers not only the world’s most powerful neutron source, the ILL, but also the world’s premier source of protons, the ESRF.
As service institutes, the ILL and the ESRF provide facilities for scientists from their 19 member countries and others from all over the world. The EMBL has its Grenoble laboratories on the campus and runs a scientific programme strongly related to the neighbouring neutron and photon facilities and amplified through numerous collaborative projects.
Scientific instrumentation of this quality has made the campus a unique location for experiments breaking new ground in modern research, in fields as diverse as structural biology, fundamental physics, or the science of materials.
To maintain this momentum the institutes seek synergies and scientific partnerships at every level. As science advances and research needs develop, new support facilities are provided such as the Partnership for Structural Biology (PSB), with its highly specialised laboratory for the deuteration of biological samples (D-Lab), and its materials science support laboratory. At the ESRF, eleven Collaborating Research Groups complement the offer of beamlines to the European scientific community.

## Slide 20: Characterization techniques : Time of flight-XBIC
XBIC
SemiC.
+
+
+
+
+
+
—
—
—
—
—
—
+
—
X-ray
Electrode
Electrode
Preamp
SAMPLING
&
DAQ
A
Pico-ammeter
For timing studies
50%
Time difference
FWHM
Time resolution
Both sides of the sample
Notes: The EPN science campus is an international science hub hosting three major European institutes along with joint partnerships. It hosts a staff of 1500, including 500 scientists or postgraduate students, and welcomes more than 8000 guest researchers every year, resulting in more than 2500 publications annually in peer-reviewed journals.
Grenoble, in the heart of the French Alps, is famous for science and innovation. In a world where technological progress depends more than ever on fundamental research, the European Photon and Neutron Science Campus (EPN) offers not only the world’s most powerful neutron source, the ILL, but also the world’s premier source of protons, the ESRF.
As service institutes, the ILL and the ESRF provide facilities for scientists from their 19 member countries and others from all over the world. The EMBL has its Grenoble laboratories on the campus and runs a scientific programme strongly related to the neighbouring neutron and photon facilities and amplified through numerous collaborative projects.
Scientific instrumentation of this quality has made the campus a unique location for experiments breaking new ground in modern research, in fields as diverse as structural biology, fundamental physics, or the science of materials.
To maintain this momentum the institutes seek synergies and scientific partnerships at every level. As science advances and research needs develop, new support facilities are provided such as the Partnership for Structural Biology (PSB), with its highly specialised laboratory for the deuteration of biological samples (D-Lab), and its materials science support laboratory. At the ESRF, eleven Collaborating Research Groups complement the offer of beamlines to the European scientific community.

## Slide 21: Characterization techniques : Time of flight-XBIC
Time resolution
XBIC
SemiC.
+
+
+
+
+
+
—
—
—
—
—
—
+
—
X-ray
Electrode
Electrode
Preamp
SAMPLING
&
DAQ
A
Pico-ammeter
For timing studies
Monochromatic beam (Energy around 10 keV) (Diameter around 100 µm)
Monitoring by pin diode and ionization chamber
Scan with beam => 2D Time resolution map
Measure the impact of defects and impurities in the material on the transport of the charge carrier
Parameters : Beam energy, beam flux and beam size

## Slide 22: Characterization techniques : Time of flight-XBIC
XBIC
SemiC.
+
+
+
+
+
+
—
—
—
—
—
—
+
—
X-ray
Electrode
Electrode
Preamp
SAMPLING
&
DAQ
A
Pico-ammeter
For timing studies
sCVD
pCVD
Notes: The EPN science campus is an international science hub hosting three major European institutes along with joint partnerships. It hosts a staff of 1500, including 500 scientists or postgraduate students, and welcomes more than 8000 guest researchers every year, resulting in more than 2500 publications annually in peer-reviewed journals.
Grenoble, in the heart of the French Alps, is famous for science and innovation. In a world where technological progress depends more than ever on fundamental research, the European Photon and Neutron Science Campus (EPN) offers not only the world’s most powerful neutron source, the ILL, but also the world’s premier source of protons, the ESRF.
As service institutes, the ILL and the ESRF provide facilities for scientists from their 19 member countries and others from all over the world. The EMBL has its Grenoble laboratories on the campus and runs a scientific programme strongly related to the neighbouring neutron and photon facilities and amplified through numerous collaborative projects.
Scientific instrumentation of this quality has made the campus a unique location for experiments breaking new ground in modern research, in fields as diverse as structural biology, fundamental physics, or the science of materials.
To maintain this momentum the institutes seek synergies and scientific partnerships at every level. As science advances and research needs develop, new support facilities are provided such as the Partnership for Structural Biology (PSB), with its highly specialised laboratory for the deuteration of biological samples (D-Lab), and its materials science support laboratory. At the ESRF, eleven Collaborating Research Groups complement the offer of beamlines to the European scientific community.

## Slide 23: Example of Characterization : scvd diamond as proton beam monitor
XBIC
TOF-XBIC

## Slide 24: Example of Characterization : scvd diamond as proton beam monitor
XBIC
TOF-XBIC
Correlation between the XBIC and ToF-XBIC map
More diffused protons
The diamond was irradiated on several points :
Same flux
Different fluence

## Slide 25: Conclusion
Unique setup available at BM05-ESRF to characterize both structural (X-ray diffraction) and electronic (XBIC and ToF-XBIC) properties of a semiconductor as diamond
Adaptable setup in function of the sample (size, thickness, kind of crystal or semiconductor)
Open to collaboration and industrial access possible
P. Everaere : pierre.everaere@esrf.fr

## Slide 26
THANK YOU FOR YOUR ATTENTION
PIONEERING SYNCHROTRON SCIENCE
BM05 Team:
P. Everaere
J. Baruchel
S. Benichou
R. Dowek
T.N. Tran Caliste

## Slide 28
Precedent experiment

## Slide 29: LPSC 0V
Beam off
Refill
Time (s)
Diamond Current (A)
Lot of instability (20%) is still observe during a long time
XBIC mapping not possible at 0V

## Slide 30: LPSC 25 V
Beam off
Refill
Time (s)
Diamond Current (A)
High difference between beam on and beam off due to the high photons flux provide by ML
Previous experiment
Beam off

## Slide 31: LPSC 25 V
Refill
Time (s)
Diamond Current (A)
Still 10 % variation on the current measured (static beam)
XBIC Mapping not possible, this variation will be superposed to the map and not removable