## Slide 1: Introduction to Semiconductor Detectors with focus on applications at Hadron Colliders Michael Moll, CERN EP-DT, Geneva, Switzerland
SIMDET 2025, 1-3 October 2025, LPNHE Paris
https://indico.in2p3.fr/event/36667/

## Slide 2: OUTLINE
The Large Hadron Collider (LHC) at CERN
  Where are the silicon detectors?
Silicon Detectors for High Energy Physics Applications
  The basic concept of Semiconductor Detectors: A reverse biased pn-junction
  Strip and Pixel Detectors at the Large Hadron Collider (LHC) at CERN
  Upgrade of the Large Hadron Collider (HL-LHC)
  Beyond the LHC: Recent developments in Silicon Detectors and the R&D landscape
Radiation Damage to Silicon Detectors
  Radiation damage mechanisms
    Microscopic defects and macroscopic damage
  Mitigation techniques: What can we do against radiation damage?
    Examples of radiation hard devices for the HL-LHC: p-type strip sensors and 3D sensors
Why do we need (TCAD) device simulations (introduction)?
Summary & Further reading
Details in following presentations: Marco Bomben; Arianna Morozzi; Jairo Villegas; Ashish Bisht, Alexander Bähr; Giulio Borghello

## Slide 3: CERN & LHC - Large Hadron Collider
p
p
27 Km
CERN Large Hadron Collider (LHC) - 27 km accelerator ring
proton-proton beams of 6.8 TeV each collide in 4 experiments
Geneva
Alps
CERN
CERN (2023):
  23 member states (25 member states in 2025)
  ~13400 scientists (users)
  ~ 2660 personnel (staff) + 900 Fellows
  Budget ~1230 MCHF (France: 13.2%)
LHC: 27 km tunnel
   4600 MCHF + 1200 MCHF (accelerator + experiments)
  1232 dipoles B=8.3T
  Design: pp s = 14 TeV (Ldesign = 1034 cm-2 s-1)
  heavy ions (e.g. Pb-Pb; 5TeV)
Circulating beams:
  2008: first beam
  2009-13: Run 1 at 2 x 4 TeV
    2012: Higgs Boson “discovered”
  2015-18: Run 2 at 2 x 6.5 TeV (1034cm-2s-1 reached)
  2018-22: Long Shutdown 2 (LS2)
  2022-26: Run 3 at 2 x 6.8 TeV
  2026-30: Long Shutdown 3 (LS3)
  2030: HighLumi-LHC (Run 4, ….)
    collect 3000-4000 fb-1 until ~ 2042 (20 times more than today)
also a program with Pb beams at up to 5.36 TeV per nucleon
today 13.6 TeV
Notes: https://en.wikipedia.org/wiki/Large_Hadron_Collider
Estonia joined in 2024 and Slovenia in 2025

## Slide 4: The LHC Experiments
Geneva
LHCb
ATLAS
ALICE
CMS
Alps
CERN
Notes: 2023: LHC 6.8+6.8 TeV Large Hadron Collider, 27 km in circumference; 9 active experiments: ALICE, ATLAS, CMS, FASER, LHCb,
LHCf, MoEDAL-MAPP, SND and TOTEM

## Slide 5: Collisions in the LHC
event seen in 2011 Higgs  2 photons
CMS
every 25ns (40 MHz)
Silicon Tracker
Electromagnetic Calorimeter
Hadron Calorimeter
Muon chambers
Superconducting Solenoid
Iron return yoke
CMS DETECTOR
Weight: 14000 t
Diameter: 15.0 m
Length: 28.7m
Field: 3.8T
Notes: Eiffel Tower – 10.000 tons

## Slide 6: Silicon Tracking Detector
LHC example: The CMS DETECTOR
CMS DETECTOR
Weight: 14000 t
Diameter: 15.0 m
Length: 28.7m
Field: 3.8T
5.4 m
2.4 m
Outer Barrel (TOB)
Inner Barrel (TIB)
End Cap (TEC)
Inner Disks (TID)
Inner Tracker
CMS – Inner Tracker & Pixel Detector
  Micro Strip:
  ~ 214 m2 of silicon strip sensors, 11.4 million strips
  Pixel:
  4 layers & 2 x 3 disks: silicon pixels (~ 1m2)
  124 million pixels (100x150mm2)
  Resolution: σ(rφ) ~ 10 mm, σ(z) ~ 25mm
104 cm
32 cm
Pixel Detector
scientist

## Slide 7: Present LHC Tracking Sensors
CMS Tracker insertion
December 2007

## Slide 8: Silicon Tracking Detectors
Silicon tracking detectors are used in almost all HEP experiments:
Different sensor technologies, designs, operating conditions,….
CMS Strip Tracker IB
ATLAS Pixel Detector
ALICE ITS Barrel New ITS for Run3:2022
CMS Pixel Detector
ATLAS SCT Barrel
LHCb VELO (New VELO for Run3:2022)
ALICE ITS Outer Barrel (Foto:Insertion Test 2021)
LHCb VELO (New VELO for Run3:2022)

## Slide 9: Silicon Sensors

## Slide 10: Solid State Detectors – Why Silicon?
Some characteristics of Silicon crystals
  Small band gap Eg = 1.12 eV  E(e-h pair) = 3.6 eV ( 30 eV for gas detectors)
  High specific density 2.33 g/cm3 ; dE/dx (M.I.P.)  3.8 MeV/cm  106 e-h/m (average)
  High carrier mobility e =1450 cm2/Vs, h = 450 cm2/Vs  fast charge collection (<10 ns)
  Very pure < 1ppm impurities and < 0.1ppb electrical active impurities
  Rigidity of silicon allows thin self supporting structures
  Detector production by microelectronic techniques  well known industrial technology, relatively low price, small structures easily possible
Alternative semiconductors
  Diamond
  Gallium arsenide (GaAs)
  Gallium nitride (GaN)
  Silicon Carbide (SiC)
  Germanium (Ge)

## Slide 11: How to obtain the signal?
In a pure intrinsic (undoped) semiconductor the electron density n and hole density p are equal.
For Silicon: ni  1.451010 cm-3
4.5 108 free charge carriers in this volume, but only 3.2 104 e-h pairs produced by a M.I.P.
 Reduce number of free charge carriers, i.e. deplete the detector
 Most detectors make use of reverse biased p-n junctions
E
f
E
valence band
conduction band
h
e

## Slide 12: Doping, resistivity and p-n junction
Doping: n-type silicon
  add elements from Vth group  donors (P, As,..)
  electrons are majority carriers
Doping: p-type silicon
  add elements from IIIrd group  acceptors (B,..)
  holes are majority carriers
Si
Si
Si
Si
Si
Si
Si
Si
P
e.g. Phosphorus
p-n junction There must be a single Fermi level!  band structure deformation  potential difference  depleted zone
 | detector grade | electronics grade
doping |  1012 cm-3 |  1017 cm-3
resistivity  |  5 k·cm | 1 ·cm
resistivity r
  carrier concentration n, p
  carrier mobility mn, mp

## Slide 13: Reverse biased p-n junction
Poisson’s equation
Electrical charge density
Electrical field strength
Electron potential energy
Positive space charge, Neff =[P] (ionized Phosphorus atoms)
neutral bulk (no electric field)
Full charge collection only for fully depleted detector (VB>Vdep)
Depleted zone growth with increasing voltage ( )
effective space charge density Neff
depletion voltage Vdep
detector thickness d

## Slide 14: Single Sided Strip Detector
Segmentation of the p+ layer into strips (Diode Strip Detector) and connection of strips to individual read-out channels gives spatial information
typical thickness: 300mm (150m-500m used)
pitch
using n-type silicon with a resistivity of  = 2 KWcm (ND ~2.2.1012cm-3) results in a depletion voltage ~ 150 V
Resolution  depends on the pitch p (distance from strip to strip) - e.g. detection of charge in binary way (threshold discrimination) and using center of strip as measured coordinate results in
typical pitch values are 20 mm– 150 mm  50 mm pitch results in 14.4 mm resolution

## Slide 15: Signal Formation in a strip sensor
TCAD simulation: minimum ionizing particle traversing the sensor
  with typical dimensions for presently operating large LHC trackers (p-in-n devices)
holes
electrons
TCAD
n-type bulk
p+ readout electrodes

## Slide 16: Signal Formation in a strip sensor
TCAD simulation: minimum ionizing particle traversing the sensor
  with typical dimensions for presently operating large LHC trackers (p-in-n devices)
holes
electrons
TCAD
n-type bulk
p+ readout electrodes

## Slide 17: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 1 ns
holes
electrons

## Slide 18: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 1.2 ns
holes
electrons

## Slide 19: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 1.4 ns
holes
electrons

## Slide 20: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 1.6 ns
holes
electrons

## Slide 21: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 1.8 ns
holes
electrons

## Slide 22: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 2.0 ns
holes
electrons

## Slide 23: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 3.0 ns
holes
electrons

## Slide 24: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 4.0 ns
holes
electrons

## Slide 25: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 5.0 ns
holes
electrons

## Slide 26: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 6.0 ns
holes
electrons

## Slide 27: Signal formation in a strip sensor
Simulation:
  Current density
  mip, 45 angle
Simulation: Thomas.Eichhorn@kit.edu
t = 7.0 ns
holes
electrons

## Slide 28: Signal formation in a strip sensor
Simulation:
  mip, 45 angle
Plot:
  Signals induced on electrodes
  Integration gives collected charge
Simulation: Thomas.Eichhorn@kit.edu
2,27e-15C
3,27e-15C
3,04e-15C
1,08e-15C
Strip 1
Strip 2
Strip 3
Strip 4
t = 2.0 ns
1 2 3 4
2ns
4ns
6ns
8ns

## Slide 29: Present LHC Tracking Sensors
CMS Tracker
M.Krammer, ICFA School, Bogota, 2013

## Slide 30: Present LHC Tracking Sensors
CMS Tracker
… 11.4 million strips
M.Krammer, ICFA School, Bogota, 2013

## Slide 31: Hybrid Pixel Detectors
HAPS – Hybrid Active Pixel Sensors
    segment silicon to diode matrix with high granularity ( true 2D, no reconstruction ambiguity)
    readout electronic with same geometry (every cell connected to its own processing electronics)
    connection by “bump bonding”
    requires sophisticated readout architecture
    Hybrid pixel detectors are used in LHC experiments: ATLAS, ALICE (from Run3 monolithic), CMS and LHCb (from Run 3)
Flip-chip technique
Solder Bump: Pb-Sn
(VTT/Finland)
~ 15mm

## Slide 32: Present LHC Tracking Sensors
CMS Pixel (Half disk forward pixel)
M.Krammer, ICFA School, Bogota, 2013

## Slide 33: Hybrid Pixels - Monolithic Pixels
Example: ALICE – Alpide Chip
  TowerJazz 0.18µm CMOS imaging process
Separately optimize sensor and FE-chip for very high radiation environment
Fine pitch bump bonding to connect sensor and readout chip
or
Charge generation volume integrated into the ASIC, but many different variants!
Thin monolithic CMOS sensor, on-chip digital readout architecture
N-well collection electrode in high resistivity epitaxial layer
State-of-art: based on quadruple well allows full CMOS
High resistivity (> 1kΩ cm) epi-layer (p-type, 20-40 μm thick) on p-substrate
Moderate reverse bias => increase depletion region around N-well collection diode to collect more charges by drift
s
Hybrid Pixel
Monolithic Pixel
Foto: ITS2 inner 3 layers (1st layer at 24 mm)
Installed in LS2
In operation since 2021
Notes: 5 um resolution
28um x 28um pixel pitch; 1.5 x 3 cm2 chip
10m2; 24120 pixel sensors with 12.5 Gpixel

## Slide 34: The future: Going full wafer monolithic!
ALICE ITS3 project (targeting installation in LS3 2026-2030)
  Use of 300mm wafer-scale MAPS chips in 65 nm CMOS !
    thinned down to  50 um making them flexible
    sensor length 266 mm x width 55 / 74 / 93 mm (stitching)
    spatial resolution requirement 5 mm
  ITS3 detector with 3 layers comprised of 6 chips only!
    ..meanwhile (2025) some more 
  Mechanically held in place by carbon foam spacers
full scale chip (50 mm thick) bent to 19 mm radius
[Filip Krizek, VERTEX 2023]
ITS2
ITS3
Notes: 20-40um thick  0.02X to 0.04% X0

## Slide 35: ALICE ITS3 project - prototypes
[ALICE – Sept.2025]
300mm wafer
ITS3 installation in LS3 (2026-2030)
air cooling
MOSS chip – MOnolithic Stiched Sensor (14x259mm2)
1 segment with 10 RSU (Repeated Sensor Units)
MOST – MOnolithic Stiched Sensor with Timing next (final):
MOSAIC - MOnolithic Stitched Active pIXel
up to 5 x segments combined (layer 2)
[VERTEX 2025 – L.Terlizzi & J.Lalic – August 2025]

## Slide 36: The Charge Signal
Collected charge for a Minimum Ionizing Particle (MIP)
  Mean energy loss dE/dx (Si) = 3.88 MeV/cm  116 keV for 300m thickness
  Most probable energy loss ≈ 0.7 mean  81 keV
  3.6 eV to create an e-h pair  108 e-h / m (mean)  72 e-h / m (most probable)
  Most probable charge (300 m) ≈ 22500 e ≈ 3.6 fC
Mean charge
Most probable charge ≈ 0.7 mean
number of events
charge deposited [fC]

## Slide 37: The Charge Signal
Collected Charge for a Minimum Ionizing Particle (MIP)
Landau distribution has a low energy tail
  becomes even lower by noise broadening
  Noise sources: (ENC = Equivalent Noise Charge) - Capacitance - Leakage Current - Thermal Noise (bias resistor)
  Good hits selected by requiring NADC > noise tail If cut too high  efficiency loss If cut too low  noise occupancy
  Figure of Merit: Signal-to-Noise Ratio S/N
  Typical values >10-15, people get nervous below 10. Radiation damage severely degrades the S/N.
Signal
Cut (threshold)

## Slide 38: Summary: Silicon Sensors in HEP
Main sensor concepts:
Monolithic CMOS Pixel Detector
strip
pixel/pad
Hybrid Pixel Detector
(Mini) Strip Detector [AC coupled]
p-in-n
n-in-p
Need inter strip isolation!
See backup slide “DRD3: Paths of present silicon detector R&D“ for a more detailed “map” on sensor types under development

## Slide 39: The LHC Upgrade …and beyond

## Slide 40: LHC and HL-LHC
today
[HL-LHC schedule – Sept.2025]
Example ATLAS:

## Slide 41: Phase 2 upgrades - High Lumi (HL)-LHC
s
CMS Phase-2 upgrade
s
About 800 m2 of silicon sensors for the phase 2 upgrades of ATLAS & CMS (RUN 4 from 2030)
..and all based on p-type silicon and no longer n-type silicon. Why? … let's see last part of this talk
Installation in LS3 (2026-2030)
Notes: 600m2 HGCAL
13m2 ATLAS Pixel
165m2 ATLAS Strip
200m2 CMS outer Tracker

## Slide 42: HL-LHC upgrades: ALICE & LHCb
HL-LHC: further proposed upgrades of ALICE (ALICE 3) and LHCb (Upgrade II) in LS4
From F.Gianotti – June 2025
Goal is to operate at L = 1 x 1034 cm-2 s-1(2 x 1033 today) and record 300 fb-1 by end of HL-LHC (cfr 50 fb-1 before LS4).
Full replacement of tracking detectors (high-granularity, radiation-hard detectors with fast timing capability), new readout for ECAL and RICH.
Significant improvements in precision, world-best sensitivity to most key flavour physics observables, broad programme beyond flavour
s
Goal is to record ~ 35 nb-1 in Run 5 (cfr 13 nb-1 before LS4)
Fully new detector, CMOS silicon tracker, monolithic time-of-flight sensors, RICH, and new superconducting magnet with 1-2 T.
Significant improvement in pointing precision and acceptance. Unprecedented studies of quark-gluon plasma using in particular heavy flavour hadrons and di-electron mass spectra
s
2034-35

## Slide 43: Future Large Experiments ??
Community discussing on future options
  ESPP 2026 update in progress
    European Strategy for Particle Physics
  CERN performed feasibility study on FCC
    Future Circular Collider (FCC-ee then FCC-hh)
  ..many other proposals on how to proceed
For any choice of project: more advanced detectors will be needed!
  Need to keep detector development running (preserve know-how & community) while next large project is being decided
[LHC schedule – Sept.25]
(HL-) LHC timeline
today
ALICE & LHCb
upgrades ?
?
?
?

## Slide 44: R&D on Solid-state Detector Technologies for High Energy Physics applications
since 2024
RD42
Long and very successful history on global R&D collaborations anchored at CERN is presently continued in form of DRDs born out of the 2021 ECFA detector roadmap
RD48
https://drd3.web.cern.ch/
145 Institutes with > 700 scientists
RD39
History of this R&D: Michael Moll et al., CERN: A Global Hub for Materials Science, Chapter in book: Between Science and Industry: Institutions in the History of Materials Research; May 2024;; Part of Encyclopedia of the Development and History of Materials Science
https://doi.org/10.1142/13625
previous R&D
All academic speakers at SIMDET are DRD3 members: LPNHE Paris (Giovanni), APC (Marco), Aix-Marseille Uni, CEA-Irfu, CPPM Marseille, IJCLAB Orsay (Anna), IHC, IP2I Lyon, LPSC; CERN (Michael), Uni.Perugia (Arianna), CNM/CNA (Jairo), FBK(Ashish), HLL Munich (Alexander),… and further 130 institutes

## Slide 45: The DRD Collaborations
DRD3 - Solid-State Detectors: part of the overall Detector R&D (DRD) program

## Slide 46: Silicon Detector Challenges beyond LHC
Past: remarkable challenges were over come in the last decade for the LHC upgrade!
  Radiation hardness at levels not imagined decades ago (few 1016 n cm-2, tens of MGy) - 25x100, 50x50 mm2 cells, device and defect engineered sensors
  Not only the position but precise timing (~30 ps) resolution should be measured for the particle collisions Endcap Timing detectors for ATLAS and CMS (4D tracking)
  Superb resolution at low mass (ALICE ITS)
New Major Challenges for the future:
  FCC-ee/CEPC:
    Vertex detectors with low mass, high resolution Target per layer spatial resolution of ≤ 3 µm and X/X0≤ 0.05%
  FCC-hh/SppC:
    low power and high radiation hardness up to 8·1017 neqcm-2
    Resolving many pp hits in a bunch by ultra-fast timing in O(10-100ps)
  Full integration with electronics, mechanics, services
  Large area sensors at low cost for calorimetry
s
s
European Commission for Future Accelerators (ECFA)
2021 road map document on sensors [CERN CDS]
Targeted by the DRD3 collaboration
(see Annex for present work program)
RD50 collaboration
and many others

## Slide 47: Radiation Damage
Damage to dielectric layers and interfaces (not covered)
Damage to the semiconductor bulk (introduction)
Radiation damage is just one of the many challenges in conceiving a High Energy Physics detector for hadron colliders.
Constraints like needs for high granularity, low mass, efficient cooling and low power consumption, low cost, high-rate capability, precision timing capability, …. are adding up to the challenge of building a detector.

## Slide 48: Motivation and Challenge
Silicon detectors upgrades and operation - Radiation Hardness -
LHC operation
HL-LHC (High Luminosity LHC)
  detector developments for HL-LHC
    starting after LS3 (~2026-28);
    expect 4000 fb-1 (nominal LHC was 300 fb-1)
HL-LHC operation & upgrades
  operation of HL-LHC
    damage modelling, evaluation, mitigation
  ATLAS Pixel replacement, LHCb upgrade, …
FCC – Future Circular Collider
  ..also FCC-ee
Increasing radiation levels
  Semiconductor detectors will face >1016 neq/cm2 (HL-LHC) and >7x1017 neq/cm2 (FCC-hh)  detectors used at LHC cannot be operated after such irradiation
New requirement and new detector technologies
  New requirements or opportunities lead to new technologies (e.g. HV-CMOS, LGAD,…) which need to be evaluated and optimized in terms of radiation hardness and/or 4D tracking capabilities
[I. Dawson, P. S. Miyagawa, Sheffield University, Atlas]

## Slide 49: Displacement Damage
….. a wide range of point defects
example of point defect reactions:
V: V+O → VO; V+P →VP
I: I+CS → Ci → Ci + O →CiOi I+BS → Bi → Bi + O →BiOi … many more reactions!
particle
SiS
Vacancy + Interstitial
point defects and clusters of defects
EK>25 eV
V
I
EK>5 keV
“dopant removal”
s
[C.Besleaga et al. arXiv 2021]
Can we see the defects?
HRTEM on Si: n-irradiated 1019 neq/cm2
High Resolution Transmission Electron Microscopy
I
I
V
V
[van Lint 1980]

## Slide 50: Impact of Defects on Detector Properties
Shockley-Read-Hall statistics
trapping (e and h)  CCE shallow defects do not contribute at RT due to fast de-trapping
charged defects  Neff , Vdep e.g. donors in upper half, acceptors in lower half of the band gap
generation  leakage current levels close to midgap most effective
Impact on detector properties can be calculated if defect parameters are known:
n,p : cross sections E : ionization energy Nt : concentration
Defect spectroscopy
e.g. DLTS, TSC
allows to measure the defect properties (see backup)
Extracted parameters serve as input to TCAD simulations (see backup and following talks)
s

## Slide 51: Radiation Damage Summary
Macroscopic bulk effects:
Depletion Voltage (Neff) Leakage Current Charge Trapping
Cut (threshold)
noise
signal
Signal to Noise ratio is quantity to watch (material + geometry + electronics)

## Slide 52: Device engineering example: n-in-p sensors
Why will we use p-type strip/pixel sensors (n-in-p) for the LHC upgrade in ATLAS and CMS instead of p-in-n sensors?
Why are segmented sensors(*) build on p-type silicon sensors radiation harder than n-type sensors?
p-in-n
n-in-p
Need inter strip isolation!
(*) 300 mm

## Slide 53: Sensor Signal: Pad vs. Strip/Pixel
Signal = Induced charge on read-out electrode
  Described by Shockley-Ramo Theorem
  Charged induced on electrode by moving charge can be calculated from the weighting potential (field)
Pad
Strip
  Total collected charge in both cases 100% (Q = q) when charges have reached the electrodes, however
    Diode: 50% from (+q); 50% from (-q)
    Strip: 87% from (+q); 13% from (-q)
  In a p-in-n strip sensor the holes give a higher contribution to the (m.i.p.) signal than the electrons!

## Slide 54: Device engineering: p-in-n vs. n-in-p (or n-in-n)
p-in-n silicon, under-depleted:
Charge spread – degraded resolution
Charge loss – reduced CCE
p+in-n
n-in-p silicon, under-depleted:
Limited loss in CCE
Less degradation with under-depletion
Collect electrons (3 x faster than holes)
n+in-p
n-type silicon after high fluences: (type inverted)
p-type silicon after high fluences: (still p-type)
Comments: - Instead of n-in-p also n-in-n devices could be used - Reality is much more complex: Usually double junctions form leading to fields at front and back! (next slide)

## Slide 55: E-Field after irradiation: “double junctions”
n-in-p sensor still “p-type” (i.e. highest field at front electrode) after high level of radiation
Investigation by measurement
Dominant junction close to n+ readout strip for FZ n-in-p
[G.Kramberger et al, 2014 JINST 9 P10016]
…to add more complexity
different particle irradiation on identical sensors
neutron irradiated 7×1015 neq/cm2
proton irradiated 7×1015 neq/cm2
[S.Pape, 43rd RD50 Workshop, 29. November 2023]

## Slide 56: Double Junction
Double Junction = Polarization Effect
[V.Eremin et al., NIMA 476 (2002) 556-564]
Double junction in TCAD (see e.g. M.Bomben, SIMDET 2023)

## Slide 57: Device engineering example: n-in-p sensors
p-in-n
n-in-p
Need inter strip isolation!
Sensors in LHC trackers today HL-LHC trackers tomorrow (2028) (ATLAS/CMS) (… in production now)

## Slide 58: ATLAS Phase II
Strips & Pixel
all n-in-p
F.Hartmann, Last RD50 Workshop, Nov.2023

## Slide 59: CMS Phase II
Outer Tracker modules in final configuration – n-in-p
Pixel Tracker module – n-in-p
High Granularity Calorimeter – n-in-p
F.Hartmann, Last RD50 Workshop, Nov.2023

## Slide 60: Device engineering example: 3D Hybrid Pixel Detectors
Array of narrow electrode columns (~ 5-10mm) passing through the silicon thickness (micromaching):
Depletion voltage prop. spacing2
Collection time prop. spacing
Reduced charge sharing
 More suited to high radiation environment
Connected to standard pixel ASIC – hybrid pixel detector
Installed 2014 in ATLAS IBL (Inner b-layer)
& inner pixel layers for LHC phase II (2030)

## Slide 61: TCAD simulations

## Slide 62: TCAD simulations
Why do we need TCAD simulations for understanding (irradiated) sensors ?
  Complexity of the problem: Coupled differential equations (semiconductor equations)
  Complex device geometry and complex signal formation in segmented devices ….
  Evaluation of new an innovative design approaches
  Impact of defects depending on local charge densities, field-strength, … (“feedback loop”)
  Interplay of surface and bulk damage..
Electric field distribution in 3D detector (Al & oxide layer transparent for clarity)
n+
n+
Column depth =
bulk thickness
Np,n = 5e18 cm-3
Nbulk = 1.7e12 cm-3
Doping profiles
3D sensor: T.Peltola (HIP, Helsinki): CMS & RD50
p+
V=0
n+
Vbias
Vbias
Vbias
Vbias
3D detector
Details in the following presentations

## Slide 63: Device simulation: TCAD & signal simulators
Status of TCAD device simulations
  Required by complexity of the problem:
    solve semiconductor equations with physics properties, complex geometry and radiation damage
    mainly commercial tools used (Silvaco and Synopsis)
  Excellent tools for sensor optimization
Radiation damage TCAD: enormous progress over recent years
  getting predictive power but need further optimization!
  “effective” defect levels (2 to 5 levels) are used
Signal simulators
  TCAD simulations for signal formation are complex (time consuming, TCAD is not a fitting tool!)
  Custom build signal simulators (open code) developed: sensor optimization, parameter fitting
    ..using E-Field and other parameters (e.g. charge trapping) from TCAD as input
needs more work !
Measured defects TCAD input
Allpix2, KdetSim, Garfield++, Weightfield2, TRACS,
(unpublished codes), ...

## Slide 64: Summary
Silicon Sensors are based on reverse biased pn-junctions (silicon sensors are reverse biased diodes)
Silicon Detectors at the LHC and upgrade of LHC
  Inner tracking at LHC and HL-LHC done by silicon detectors
  Hybrid-pixel (planar and 3D) and strip sensors implemented in LHC experiments (ALICE upgraded to monolithic sensors)
  Radiation Hard Monolithic sensors under development (competing beyond LS3 for HL-LHC upgrades)
Radiation Damage in Silicon Sensors
  Damage: displacement damage that is evidenced as defect levels in the band gap of the semiconductor (+ some impact of surface damage in segmented sensors)
  Modification of internal electric field (space charge distribution, depletion voltage, “type inversion”, reverse annealing, loss of active volume, …), defect engineering possible!
  Increase of Leakage Current and Charge Trapping (same for all silicon materials)
  Signal to Noise ratio is quantity to watch (material + geometry + electronics)
Radiation tolerant silicon sensors
  Several examples of successful Material and Device Engineering (mitigation strategies) oxygenation, carbonation, 3D sensors, p-type (n-readout) sensors
“Hot topics” in silicon sensor R&D
  Sensors for timing (i.e. LGAD with intrinsic gain, acceptor removal,3D,4D); monolithic sensors; SiC and Diamond sensors, large area low cost
  Radiation resistance to extreme particle fluences (longterm: FCC-hh)
    Reliability of TCAD simulations with defects; characterization of damage beyond 1016 cm-2

## Slide 65: Acknowledgements & References
Most references to particular works given on the slides
  RD50 workshop presentations: http://www.cern.ch/rd50/ ; DRD3 workshop presentations: https://drd3.web.cern.ch/
  Conferences: VERTEX, PIXEL, RESMDD, …
Instrumentation Schools
  ICFA, EDIT, CERN & DESY Summer Student Lectures
Books about silicon tracking detectors (and radiation damage)
  Helmuth Spieler, “Semiconductor Detector Systems”, Oxford University Press 2005
  C.Leroy, P-G.Rancoita, “Silicon Solid State Devices and Radiation Detection”, World Scientific 2012
  Frank Hartmann, “Evolution of silicon sensor technology in particle physics”, Springer 2024: third edition
  L.Rossi, P.Fischer, T.Rohe, N.Wermes “Pixel Detectors”, Springer, 2006
  Gerhard Lutz, “Semiconductor radiation detectors”, Springer 1999
  Hermann Kolanoski and Norbert Wermes, “Particle Detectors – Fundamentals and Appilcations”, Oxford University Press 2020
Review Articles
  2018: Garcia-Sciveres and Wermes, A review of advances in pixel detectors for experiments with high rate and radiation, https://doi.org/10.1088/1361-6633/aab064
  2018: M.Moll, Displacement Damage in Silicon Detectors for High Energy Physics https://doi.org/10.1109/TNS.2018.2819506
  2021: Radiation Effects in the LHC-Experiments, 154 pages, CERN Yellow Report https://cds.cern.ch/record/2764325
Research collaborations and web sites
  CERN RD50 collaboration (http://www.cern.ch/rd50 ) - Radiation Tolerant Silicon Sensors
  DRD3 collaboration (https://drd3.web.cern.ch/) – R&D on Solid State Detectors
  Inter-Experiment Working Group on Radiation Damage in Silicon Detectors (CERN) – CERN Yellow Report
  ATLAS and CMS upgrade groups, LHCb and ALICE upgrades

## Slide 66: Backup Slides

## Slide 67: EDIT - Instrumentation School 2026
EDIT (Excellence in Detector and Instrumentation Technologies)
  aimed at young researchers, including graduate students and early-career postdocs, who seek to deepen their knowledge of detector technologies and instrumentation for particle physics
CERN, 3-13 March 2026 (15 years since its first edition)
Deadline was 1.10.2025 … but all lectures will be broadcasted!
Website: https://indico.cern.ch/e/edit2026
EDIT 2026
  10 days with lectures, key-note talks and hands-on sessions
  48 students – split into groups of two to six students for hands-on
  Local organizers: F.Brunbauer, D.Dannheim, M.Moll, E.Oliveri (DRD1,DRD3, CERN EP-DT)
Past EDIT schools:
2024 at FNAL, Link
2023 at BNL, Link
2020 at DESY, Link
2018 at FNAL, Link
2015 at Frascati, Link
2013 at KEK, Link
2012 at FNAL, Link
2011 at CERN, Link
Core Lectures:
Particle Interactions with Matter
Silicon Detectors
Gaseous Detectors
Photon Detectors
Noble Liquid Detectors
Signal Processing & Front-End Electronics
Modelling and Simulation
Key-note talks:
Avenues for the Physics to Come
Particle Accelerators
Collider Physics and Beyond
Future Detectors for Tracking, Calorimetry, and Timing
Quantum Sensors
Applications Outside HEP
Lab sessions:
Silicon Detectors
Gaseous Detectors
Photon Detectors
Signal Processing & Front-End Electronics
Modelling and Simulation
DAQ and Trigger
Beam Instrumentation/Radiation Monitoring and Instrumentation

## Slide 68: Collisions in the LHC
2012 – Discovery of the Higgs Boson

## Slide 69: Timing Detectors

## Slide 70: Timing Detectors: Motivation
“sorting the mess”
  [F.Hartmann, CMS, Feb.2025]

## Slide 71: Timing Detectors: Motivation
“sorting the mess”
  [F.Hartmann, CMS, Feb.2025]

## Slide 72: Timing Detectors: Motivation
“sorting the mess”
  [F.Hartmann, CMS, Feb.2025]

## Slide 73: Timing Detectors: Motivation
“sorting the mess”
  [F.Hartmann, CMS, Feb.2025]

## Slide 74: Timing Detectors: Motivation
“sorting the mess”
  [F.Hartmann, CMS, Feb.2025]

## Slide 75: Timing Detectors: Motivation
“sorting the mess”
  [F.Hartmann, CMS, Feb.2025]

## Slide 76: Timing: Time of arrival measurement
Low Gain Avalanche Diode (LGAD)
Internal charge multiplication by impact ionization in the p+ gain layer
Gain
3D sensor
Short drift path, independent of thickness
Radiation hard
Time of arrival measurements will be critical for pileup suppression at HL-LHC (pileup 200)
  Targeted time resolution per sensor < 50 ps
  ATLAS High Granularity Timing Detector and CMS Endcap Timing Layer
We want to measure the time of arrival with respect to a reference time
  Reference at LHC the 25 ns clock (bunch crossing time)
  In lab a reference signal (from reference detector or laser trigger pulse)
    At least two channels are recorded
    Time of Arrival: time when signal crosses a selected threshold
  Time resolution defined as RMS of the time difference ;
Radiation hard sensor technologies for timing:
[B.Hiti – 2nd TCT school – Sept.2025]

## Slide 77: Timing: Contributions to time resolution
Jitter contribution minimized by high signal-to-noise ratio, fast signal rise time
Pulse shape contribution:
Time walk (signal size) – correctable (constant fraction discriminator)
LGAD: nonhomogenous MIP charge deposition (Landau fluctuations) – uncorrectable – not present in laser measurements
3D: Weighting field distortion (weighting field not constant within a cell) – focused laser good tool to probe this
[B.Hiti – 2nd TCT school – Sept.2025]

## Slide 78: R&D on Solid-State Detectors DRD3 collaboration

## Slide 79: DRD3 Organizational Structure
Michael
Giovanni
A working group dedicated to simulations!

## Slide 80: DRD3: Paths of present silicon detector R&D
[G.Kramberger, Sept.2025]

## Slide 81: DRD3: WG1/WP1 Monolithic silicon sensors
[G.Kramberger, Sept.2025]

## Slide 82: DRD3 WG2/WP2: Hybrid silicon technologies and 4D tracking
[G.Kramberger, Sept.2025]

## Slide 83: DRD3: WG2/WP2: LGADs
[G.Kramberger, Sept.2025]

## Slide 84: DRD3: WG2/WP2: LGAD flavours

## Slide 85: DRD3 WG2/WP2: 3D detectors
[G.Kramberger, Sept.2025]

## Slide 86: DRD3: WG3/WP3: Radiation damage characterization and sensor operation at extreme fluence

## Slide 87: DRD3 WG6/WP3: Other materials – non silicon
[G.Kramberger, Sept.2025]

## Slide 88: DRD3: WG4 Simulations

## Slide 89: DRD3 WG7/WP4: In house bonding and wafer-wafer
[G.Kramberger, Sept.2025]

## Slide 90: Microscopic Damage Formation of Defects and Impact on Detectors

## Slide 91: Radiation Damage – Microscopic effects
Spatial distribution of vacancies created by a 50 keV Si-ion in silicon. (typical recoil energy for 1 MeV neutrons)
I
I
V
V
van Lint 1980
M.Huhtinen 2001
particle
SiS
Vacancy + Interstitial
point defects (V-O, C-O, .. )
point defects and clusters of defects
EK>25 eV
EK > 5 keV
V
I

## Slide 92: NIEL – Non Ionizing Energy Loss
Displacement Damage Function
  Normalization of radiation fields to 1 MeV neutron equivalent damage (neq)
NIEL Hypothesis:
  Assumption: NIEL scaling of damage parameters
  Applied to predict damage of radiation fields in HEP
  NIEL violation observed:
    Material dependence
    Proton vs. neutron damage
    …
    Acceptor removal ?
[Data: A.Vasilescu and G.Lindstroem]
1
1 MeV
0.62 (23 GeV protons)
1.85 (26 MeV protons)
2.20 (23 MeV protons)
1.14 (192 MeV pions)
0.92 (TRIGA reactor neutrons)
[M.Huhtinen, NIMA 491(2002), 194]
10 MeV protons 23 GeV protons 1 MeV neutrons
Simulation: Vacancies in (1m)3 after 1014 particles/cm2
Notes: Allport 2019

## Slide 93: Radiation induced defects with impact on device performance
RD50 map of most relevant defects for device performance near room temperature:
BiOi (acceptor removal)
Phosphorus: shallow dopant (positive charge)
BD: positive charge higher introduction after proton than after neutron irradiation, oxygen dependent
E30: positive charge higher introduction after proton irradiation than after neutron irradiation
Leakage current: V3
Reverse annealing (negative charge)
Boron: shallow dopant (negative charge)
leakage current & neg. charge current after  irrad, V2O (?)
  Trapping: Indications that E205a and H152K are important (further work needed)
  Converging on consistent set of defects observed after p, p, n, g and e irradiation.
  Defect introduction rates are depending on particle type and energy, and some on material!

## Slide 94: Some TCAD models from literature
Several models available (non exhaustive list):
Table: M.Moll, Displacement Damage in Silicon Detectors, doi.org/10.1109/TNS.2018.2819506

## Slide 95: Macroscopic Damage Degradation of Detector Performance

## Slide 96: Summary: Basics of Radiation Damage in Silicon Sensors
Two general types of radiation damage to the detector materials:
 Bulk (Crystal) damage due to Non Ionizing Energy Loss (NIEL) - displacement damage, built up of crystal defects –
  Change of effective doping concentration & acceptor/donor removal (higher depletion voltage, under- depletion)
  Increase of leakage current (increase of shot noise, thermal runaway)
  Increase of charge carrier trapping (loss of charge)
 Surface damage due to Ionizing Energy Loss (IEL) - accumulation of positive in the oxide (SiO2) and the Si/SiO2 interface – affects: interstrip capacitance (noise factor), breakdown behavior, …
Impact on detector performance and Charge Collection Efficiency (depending on detector type and geometry and readout electronics!) Signal/noise ratio is the quantity to watch
 Sensors can fail from radiation damage !
Same for all tested Silicon materials!
Influenced by impurities in Si – Defect Engineering is possible!
Can be optimized!
Notes: 96
96
efficacité de collection de charge influencé par deux mécanisme
piégeage – porteurs de charge sont pièges par les défaut profond
déficit de collection de charge augmente en fonction de la fluence

## Slide 97: Radiation Damage in the LHC Experiments (Silicon Detectors)

## Slide 98: Radiation Effects in LHC Experiments
5 workshops on “Radiation Effects at LHC Experiments and Impact on Operation and Performance” organized (2011 - 2019)
  Common Workshop: (ALICE), ATLAS, CMS, LHCb, RD50
    Sensor Measurements
    Electronics/Optoelectronics
    Radiation Simulation and Monitoring
    Sensor Simulation
Outcome and follow-up:
  Generally good agreement between RD50 damage prediction models (e.g.“Hamburg model”) and radiation damage observed by the LHC experiments.
  More coherent approach in data analyses agreed and documented.
  Modelling will have to be refined in some areas for run 3 !
CERN Yellow Report written and edited by a team from RD50 & all LHC experiments has been published (154 pages, Radiation effects in the LHC experiments https://cds.cern.ch/record/2764325) summarizing observations, comparing results from different experiments against each other, listing open questions and outlining further work towards Run 3.
  [https://indico.cern.ch/event/769192]
  [https://cds.cern.ch/record/2764325 ]

## Slide 99: Radiation Effects in LHC Experiments
Review of radiation effects in the LHC Experiments in several workshops [INDICO]
  Common working group: RD50 & LHC experiments  Publication of a summary report in April 2021 [CERN Yellow Report link]
ATLAS B-layer data vs. MC&NIEL strong z-dependence; unexpected
Plots: Radiation Effects Workshop Feb.2019 K.Mochizuki(ATLAS SCT) J.L.Agram (CMS Tracker), Aiden Grummer (ATLAS Pixel) , G.Sarpis (LHCb Velo) , F.Feindt (ATLAS Pixel)
Leakage currents in ATLAS SCT and CMS tracker and model predictions
LHCb Velo depletion voltage reduced by annealing; according to model
CMS pixel layers; deviation of Vdep from modelling at high fluences

## Slide 100: How to increase the radiation hardness?

## Slide 101: Approaches to develop radiation harder solid state tracking detectors
Defect Engineering of Silicon Deliberate incorporation of impurities or defects into the silicon bulk to improve radiation tolerance of detectors
  Needs: Profound understanding of radiation damage
    microscopic defects, macroscopic parameters
    dependence on particle type and energy
    defect formation kinetics and annealing
  Examples:
    Oxygen rich Silicon (DOFZ, Cz, MCZ, EPI)
    Carbon enriched LGAD gain layers
    Oxygen dimer & hydrogen enriched Si
    Pre-irradiated Si
    Influence of processing technology
New Materials
  Silicon Carbide (SiC), Gallium Nitride (GaN)
  Diamond , Amorphous silicon, Gallium Arsenide
Device Engineering (New Detector Designs)
  p-type silicon detectors (n-in-p)
  thin detectors, epitaxial detectors
  3D detectors and LGAD - Low Gain Avalanche
  Cost effective detectors
  Monolithic devices – HV-CMOS
Scientific strategies:
Material engineering
Device engineering
Change of detector operational conditions
Regular exchange of detectors
“Cryogenic Tracking Detectors” operation at 100-200K to reduce charge loss (not followed up in the moment)