## Slide 1
Luminescence of
Chiral Lanthanide Complexes
Annika Sickinger
DSA, SynPA team
Journée scientifique et technique IPHC

## Slide 2
Synthèse pour l’Analyse (SynPA) Team
Coordination complexes for medical imaging
Mn-based MRI
contrast agents
PET radiotracors
Nanocarriers for drug delivery
Hybrid Lanthanide-Nanoparticles for bioanalytical applications
Microscoy
PET and MRI imaging
Bioassays
Luminescent lanthanide (Ln) complexes
Upconversion
1
Notes: Coordination complexes, assemblies and nanoparticles (NPs)

## Slide 3
2
Ln(III) Complexes
- Long Excited State Lifetime
- Ladder-like Energy Diagram
- Narrow Emission Lines
- Pronounced MD Nature
Properties of Ln(III) f-f transitions
Upconversion Emission
Lanthanide Complexes
Radial probability distribution
4f
5d
6s
6p
Emission spectra
Eur. J. Inorg. Chem. 2005, 1425. Chem. Rev. 2010, 110, 2729. Los Alamos Sci. 2000, 26. Eur. J. Inorg. Chem. 2009, 4357-4371.
Notes: Application: - Magnetic molecular materials
- Particular NMR applications
- MRI contrast agent
- Laser materials
- Visualization/Illumination devices
- Bioimaging & Biosensing

## Slide 4
3
Ln(III) Complexes
- Long Excited State Lifetime
- Ladder-like Energy Diagram
- Narrow Emission Lines
- Pronounced MD Nature
Properties of Ln(III) f-f transitions
Upconversion Emission
Lanthanide Complexes
Radial probability distribution
4f
5d
6s
6p
E0
E1
E2
E1‘
hνlum
UC Emission
hνUC
Excitation hνexc
hνUC > hνexc
Upconversion Emission
Exemple of ESA mechanism.
Circularly Polarized Luminescence
Emission
CPL
Emission spectra
Eur. J. Inorg. Chem. 2005, 1425. Chem. Rev. 2010, 110, 2729. Los Alamos Sci. 2000, 26. Eur. J. Inorg. Chem. 2009, 4357-4371.
Notes: Application: - Magnetic molecular materials
- Particular NMR applications
- MRI contrast agent
- Laser materials
- Visualization/Illumination devices
- Bioimaging & Biosensing

## Slide 5
Circularly Polarized Luminescence (CPL)
4
→ Ability of chiral systems to rotate the plane of polarized light
→ Intensity difference of right- and left-handed circ. pol. light: ΔI = IL - IR
→ Quantification by dimensionless disymmetry factor (max. ± 2 )
Nat. Commun. 2023, 14, 1065. Chem. Rev. 1986, 86, 1. Space Sci. Rev. 2008, 135, 187. Front. Chem. 2020, 8, 1-27.
Established ligand systems for chiral complexes:

## Slide 6
→ Alternative description of glum
for transition i → j
→ CPL amplitude of transition i → j is governed by rotary strength
→ Normalization by global emission, ruled by overall transition oscillator strength
Circularly Polarized Luminescence (CPL)
4
→ Ability of chiral systems to rotate the plane of polarized light
→ Intensity difference of right- and left-handed circ. pol. light: ΔI = IL - IR
→ Quantification by dimensionless disymmetry factor (max. ± 2 )
Nat. Commun. 2023, 14, 1065. Chem. Rev. 1986, 86, 1. Space Sci. Rev. 2008, 135, 187. Front. Chem. 2020, 8, 1-27.
And why Ln3+ ??
glum =
4 Rij
│Dij│
Rij = │µij│·│mij│cos θ
electric transition dipole moment (ED)
magnetic transition dipole moment (MD)
angle between vectors
Dij = │µij│2·│mij│2
Notes: glum is constant for a given transition ij
Rij probability of emitting/absorbing a CP photon

## Slide 7
→ Alternative description of glum
for transition i → j
→ CPL amplitude of transition i → j is governed by rotary strength
→ Normalization by global emission, ruled by overall transition oscillator strength
Circularly Polarized Luminescence (CPL)
4
→ Ability of chiral systems to rotate the plane of polarized light
→ Intensity difference of right- and left-handed circ. pol. light: ΔI = IL - IR
→ Quantification by dimensionless disymmetry factor (max. ± 2 )
And why Ln3+ ??
Rij = │µij│·│mij│cos θ
Dij = │µij│2·│mij│2
glum = =
4 Rij
│Dij│
4 │µij│·│mij│cos θ
│µij│2 + │mij│2
mostly:│µij│>>│mij│

Ideal for high glum: │µij│≈│mij│
Nat. Commun. 2023, 14, 1065. Chem. Rev. 1986, 86, 1. Space Sci. Rev. 2008, 135, 187. Front. Chem. 2020, 8, 1-27.
Notes: glum is constant for a given transition ij
Rij probability of emitting/absorbing a CP photon
Negligible for organic chromophores, due to │µij│>>│mij│, involving parity-allowed ED- and MD-forbidden transitions

## Slide 8
CPL of Eu3+ Complexes
Methods Appl. Fluoresc. 2014, 2, 012001. Front. Chem. 2020, 8, 1-27.
Energy diagram of Ln ions with spectroscopic levels.
Eu3+: 5D0 → 7FJ
5

## Slide 9
Eu3+: 5D0 → 7FJ (J =0-6)
6
Emission
J =1
J = 2
J = 3
J = 4
9-Coordinate dipicolinate complexes
Excitation of Antenna, Sensitization of Ln(III)
Ln(III) emission
CPL of Eu3+ Complexes
Inorg. Chem. Front., 2021, 8, 914.

## Slide 10
Eu3+: 5D0 → 7FJ (J =0-6)
6
CPL
Emission
J =1
J = 2
J = 3
J = 4
glum (J =1) ≈ 0.2
glum (J =2) ≈ 0.1
f-f transitions
ED transitions forbidden by Laporte’s rule → low │µij│
MD transitions allowed for ΔJ= 0, +/-1 (except 0-0)
Spectra acquired at rt in MeOH.
CPL of Eu3+ Complexes
glum =
4 │µij│·│mij│cos θ
│µij│2 + │mij│2
Inorg. Chem. Front., 2021, 8, 914.

## Slide 11
Energy diagram of Ln ions with spectroscopic levels.
Yb3+: 5F5/2 → 2F7/2
7
CPL of Yb3+ Complexes
Methods Appl. Fluoresc. 2014, 2, 012001. Front. Chem. 2020, 8, 1-27.

## Slide 12
8
Crystal field splitting
In ligand field, spherical symmetry of electronic structure and genereracy of spectroscopic levels is lifted (mj sub-levels)
Emission
Yb3+: 5F5/2 → 2F7/2
2’
1’
0’
3
2
1
0
CFS
Spectra acquired at 4K in PDMS.
CPL of Yb3+ Complexes
Phys. Chem. Chem. Phys. 2024, 26, 15776–15783.
Spectroscopic states
CFS states

## Slide 13
8
2’
1’
0’
3
2
1
0
CPL
→ Mirror-type spectra for two enantiomers
→ Improved discrimination of individual transitions
→ Each CFS transition has its own CPL response (intensity + sign)
Emission
Spectra acquired at 4K in PDMS.
Yb3+: 5F5/2 → 2F7/2
CFS
0’→ 0
0’→ 2
0’→ 1
0’→ 3
CPL of Yb3+ Complexes
Phys. Chem. Chem. Phys. 2024, 26, 15776–15783.
Spectroscopic states
CFS states

## Slide 14
9
Lanthanide-CPL
Applications
Anti-counterfeit devices / security inks
Display technologies
Molecular / Biological sensing
(induction/change of CPL in presence of chiral peptides)
Fundamental insight in Lanthanide photophysics
Chem. Commun., 2008, 4261-4263.
Commun. Chem., 2020, 3, 119.
!
CPL response (and glum) is not constant for one emission band/wavelength

## Slide 15
10
Yb3+-CPL at variable temperature
CPL activity / glum values vary with :
Wavelength
Temperature (population of hot bands !)
Experimental bandwidth
Phys. Chem. Chem. Phys. 2024, 26, 15776–15783. J. Mater. Chem. C, 2024, 12, 4253-4260.
Er3+-CPL at variable bandwidth
Fundamental insight in Lanthanide photophysics
Lanthanide-CPL

## Slide 16
10
Yb3+-CPL at variable temperature
CPL activity / glum values vary with :
Wavelength
Temperature (population of hot bands !)
Experimental bandwidth
Phys. Chem. Chem. Phys. 2024, 26, 15776–15783. J. Mater. Chem. C, 2024, 12, 4253-4260.
Er3+-CPL at variable bandwidth
!
Precise documentation of measurement conditions required for reproducibility
Fundamental insight in Lanthanide photophysics
Lanthanide-CPL

## Slide 17
11
Upconversion Emission
Lanthanide Complexes
E0
E1
E2
E1‘
hνlum
UC Emission
hνUC
Excitation hνexc
hνUC > hνexc
Upconversion Emission
Exemple of ESA mechanism.
Circularly Polarized Luminescence
Emission
CPL
E0
E1
E2
E1‘
Envisaged Project
Insight into chiral activity of higher excited states
→ Fundamental knowledge in Ln3+
photophysics
→ Novel materials with unprecedented
properties
Combination of Upconversion Emission (UC) and Circularly Polarized Luminescence (CPL) in one molecular complex
Notes: parity forbidden, and in many cases spin forbidden, nature of the 4f 씮 4f transitions and the fact that the 4f electrons, being effectively shielded by 5p and 6s electrons, are not involved in chemical bonding.
Application: - Magnetic molecular materials
- Particular NMR applications
- MRI contrast agent
- Laser materials
- Visualization/Illumination devices
- Bioimaging & Biosensing

## Slide 18
12
E0
E1
E2
E1‘
Envisaged Project
UC
CPL
Ln3+ Complex
Ln3+
Excitation of
chromophore
ET to Ln3+ Center (Antenna effect)
Emission of UC- CPL
Requirements on Complex Design
i) Induction of chirality
ii) Efficient sensitization
(antenna with high absorption cross-section)
iii) Maximum decrease of non-emissive deactivation
pathways (CN = 9, deuteration,…)
Ln3+ = Er3+
Insight into chiral activity of higher excited states
Notes: parity forbidden, and in many cases spin forbidden, nature of the 4f 씮 4f transitions and the fact that the 4f electrons, being effectively shielded by 5p and 6s electrons, are not involved in chemical bonding.
Application: - Magnetic molecular materials
- Particular NMR applications
- MRI contrast agent
- Laser materials
- Visualization/Illumination devices
- Bioimaging & Biosensing

## Slide 19
your kind attention !
Acknowledgements
Dr. Aline NONAT
Dr. Loïc CHARBONNIERE
Dr. Clémence CHEIGNON
Dr. Câline CHRISTINE
Dr. Cyrille CHARPENTIER
Alexandre LECOINTRE
Dr. Mainak BANERJEE
Samuel SANCHEZ
Dr. Brigino RALAHY
Dr. Charlotte HEINRITZ
Abiram SELVARATNAM
Pol CASTILLO-TORRES
Manon COURSEYRE
ANR-25-CE07-6425
Annika Sickinger
sickinger@unistra.fr
Thanks for
Soutien ITI QMat
Financial support

## Slide 20
Er3+
UC-CPL Emission
Antenna, attached to tridentate ligand
Chiral ligands
Energy Transfer
Excitation
4I15/2
0
4I13/2
4I9/2
4S3/2
6500
12250
18450
2H11/2
19150
Er(III)
Excitation
hν ≈ 800 nm
ΔE [cm-1]
UC-CPL
hν ≈ 540/520 nm
NIR-Emission + CPL
hν ≈ 1500 nm

## Slide 21
Sample
Excitation
lense
lenses
λ/4
waveplate
polarizer beam splitter
mono-chromator
CCD camera
CPL setup
‘hot band’ emissive levels