## Slide 1: Prospects for 39Ca beam production with TULIP at SPIRAL1
ACCLAIM MORA kickoff meeting

## Slide 2: Production history
05/2019 : 40Ca20+ 95 AMeV at 700W (38mK experiment)
  In-target production 39Ca : 1.3e6 pps/W ≈ 1e9 pps (SigmaSIRA EPAXV2)
  Observed : none
04/2023 : 50Cr23+ 72 AMeV at 19W (48Cr study)
  In-target production 39Ca : 5.5e5 pps (SigmaSIRA EPAXV2)
  Observed : none
Problem with production/release/detection ?
Anode
Cathode
Target
Cavity
Window
Primary beam
Radioactive beam
Standard FEBIAD Target Ion-Source System (TISS)

## Slide 3: Decay & detection
EffGe(511KeV) ≈ 1% at the closest in IBE
Should we have seen 39Ca if 1% atom-to-ion efficiency ?
1E7pps -> 2E5 cps in faster
Impossible to miss
5E3pps -> 100 cps in faster
Difficult to miss
Not a detection problem

## Slide 4: Diffusion (graphite)
Sr in graphite. No data for Ca in C. As Sr has a larger radius than Ca, diffusion of Ca in C is expected to be larger than diffusion of Sr.
Diffusion of Ca in Ti.
Tfus (Ti)
Targets: TRIUMF ISAC : (Ta) and TiC. CERN ISOLDE: Ti rods & foils, Ta foils
Extracted from A. Ribet database
T1/2,diff = 1 to 100 s in 20µm Ti
T1/2,diff = 7E-3 to 3 s in 0.5mm graphite
To be calculated in Nb, Ta for sustainability at high temperature
Kirchner, NIMB 1992
Probably not a diffusion problem in graphite

## Slide 5: Diffusion (metals)
Ta, Nb, Ti have similar lattice parameter and atomic radius
We can assume that:
DCa-in-Ta ≈ DCa-in-Nb ≈ DCa-in-Ti << DCa-in-gr
Also :
DCa-in-Mo << DCa-in-Nb<< DCa-in-Zr
Source : Handbook of Self-diffusion and impurity diffusion in pure metals. G. Neumann and Cornelis Tuijn, Elsevier
Diffusion could be a problem in refractory metals
?
?

## Slide 6: Effusion (graphite)
Test production stable Ca ions
Max 230nA of 40Ca observed for a ≈ 6E19 atoms sample. Very low, can be explained by :
  Very low efficiency (No apparent reason)
  Issue with experiment (target at 1240°C before the starting source)
  Very slow release (T1/2 = 2 months!)
    Target and cavity not hot enough (target at 1240-1750 °C during test)
    Ca too sticky. Ca output doubled with CF4 injection at 1500 °C
    Ca oxidized before starting the vacuum (CaO melting point 2570°C) or carbonized next to the target (CaC2 melting point 2300°C) -> to be investigated with HSC
Effusion is quite possibly the limiting factor in graphite but to needs to be investigated

## Slide 7: Effusion (metals)
Sticking time on refractory metals
Calculation at 2073 K
Values from
B. Eichler and H. Robbach, Adsorption von Metallen auf metallische oberflächen und Möglichkeiten ihrer Nutzung in der Kernchemie, vol. 527, 1984
 Low sticking time(<10-4 s) of Ca on refractory metals (typically 10000 contacts in a standard graphite cavity, and could also be reduced)
y
z
x
Ca
Effusion should not be limiting in a metal cavity

## Slide 8: TULIP
20Ne Primary beam
Mo-Ni-Mo target
(fusion-evaporation)
graphite window
Graphite catcher
Radioactive ion beam
60 mm
TULIP cavity
On-line test in 2023: production of 74-78Rb+ ions (≈10%)
Recent on-line test (09/2025)
At least 100pps of 74Rb (65ms)
Release time in the ms range
July 2023
TULIP FEBIAD
Tested offline in 2024-2025
Calibrated Ar leak : EffAr > 6% (stable) and up to 17%
Ag, In, Sn tracers : Eff = 9-15%
For Ca, FEBIAD > SIS, but thick target required

## Slide 9: Implantation
Optimum 12C target thickness to maximize 39Ca fragment out of target:
For a graphite cavity closed with the target
774 mg/cm2 = 3.44 mm at « normal » 2.253 g/cm3 graphite density
4.36 mm at graphite density of usual targets (1.775 g/cm3)
For a Ta cavity closed with a 7 µm Ta window
758 mg/cm2 = 3.36 mm at « normal » 2.253 g/cm3 graphite density
4.27 mm at graphite density of usual targets (1.775 g/cm3)
Small range (and production) difference

## Slide 10: Implantation
Stopped in graphite
Stopped in Ta

## Slide 11: TISS concept

## Slide 12: TISS concept
TARGET
Cavity
Catcher
entrance window

## Slide 13: Conclusion
Ca beams are limited by release in current TISS -> new design
A full graphite system could be effusion limited
A full metal system could be diffusion limited
Limiting the implantation depth and cavity volume/surface is possible -> same as for TULIP
We received first applications for the master/PhD thesis