## Slide 1: Looking beyond 28nm CMOS
XIII FRONT-END ELECTRONICS
For Particle Physics, Photon Science and Related Applications
18 - 22 May 2026 Paris, France
Kostas Kloukinas (CERN)

## Slide 2: Outline
Technology Landscape
HEP considerations
Outlook & sweet-spot question

## Slide 3: Semiconductor Market
Will reach $1 trillion by 2026
AI ignites record growth
  Logic scaling
    FinFET, nanosheet, GAA, CFET..
  SRAM scaling
    ~100× bit cell area reduction from 130nm to 3nm
  Compute architectures
    From CPUs & GPUs to NPUs
  Data rates
    Silicon photonics, co-packaged optics
  Power reduction
    Also assisted by 3D interconnects
Source: https://www.techi.com/semiconductor-industry-1-trillion-chip-boom-ai-demand/ https://bits-chips.com/article/chip-market-on-track-for-1-trillion-in-2026/

## Slide 4: Scaling is Failing
Moore’s Law
  Number of transistors doubles approximately every two years.
  Physics, costs and material constraints are slowing down the law
Dennard’s Law
  As transistors shrink, their power density remains constant — delivering more speed and density at no thermal cost
  ~2005 onward (~65nm) Vt and Isub leakage do not scale with size
  Clock frequencies stopped scaling (the "frequency wall") and the industry pivoted to multicore processors
Amdahl’s Law
  The speedup of a system is fundamentally limited by its irreducible serial fraction, no matter how much parallelism is added
  Multicore scaling is power limited
Extending Moore’s Law
Power Wall
Notes: If 90% of your program parallelises perfectly, the best you can ever do is 10× speedup — the remaining 10% serial portion always takes the same time regardless of how many cores you add.

## Slide 5: Migrating to Fully-Depleted finFET
Subthreshold Swing (SS)
  Planar MOSFETs: gate shares channel control with the bulk substrate → imperfect electrostatics, SS well above 60 mV/decade
  FinFET gate wraps around three sides of the fin → near-perfect gate control → SS approaches the 60 mV/decade ideal
  Steeper slope means the transistor switches off more abruptly → for the same I_off, threshold voltage V_T can be set lower
DIBL (Drain-Induced Barrier Lowering)
  Planar MOSFET: drain field penetrates deeply into the channel, lowering the source-channel barrier without gate action → large DIBL, premature conduction, poor V_T stability
  FinFET geometry screens the channel from the drain field on three sides → DIBL reduced by 2–5× compared to planar at the same node
  Lower DIBL → V_T stable across operating conditions → predictable leakage and better I_off control
Combined effect — enabling V_DD reduction
  Together they allow V_DD to scale from ~0.9 V (28nm planar) to ~0.75 V (7nm FinFET) ~17% reduction in V_DD
  Dynamic power scales as P ∝ CV²f → ~31% reduction in dynamic power
  Static leakage power ~5–10× lower driven by improved SS and lower V_DD
Loke et al., Analog/Mixed-Signal Design in FinFET Technologies

## Slide 6: Extending Moore’s Law
Lithography evolution
  CD = k₁ × λ / NA
  UV (λ = 436 nm) -> DUV (λ = 193 nm)
  Immersion -> Double Patterning
  EUV (λ = 13.5 nm at 0.33 NA) single exposure
  High-NA EUV (0.75 NA) -> Research
Device Architecture evolution
  Triple gate finFET
  Gate-All-Around (GAA)
    NSFET: Nanosheet FET
      Enhanced electrostatic control of gate
    FSFET: Forksheet FET
      Minimizing gap between devices
    CFET: Complementary FET
      2x the logic density
      Monolithic or Sequential (bonded wafers)
      The last device architecture (?)
a) finFET -> b) NSFET -> c) FSFET -> d) CFET
Source: IEEE ELECTRON DEVICES MAGAZINE, DECEMBER 2025
Possible roadmap

## Slide 7: Logic & Interconnect Scaling
Notable feature: the "metal pitch scaling slows/plateaus" annotation between 7nm and A6, reflecting the imec statement that metal pitch scaling ends at ~12–16nm around 2030.
Notes: The key message
The slope of both curves tells a story of two distinct eras. Before ~2005 the curves fall steeply and together — pure Dennard scaling, geometry driving everything. After ~2005 the metal pitch curve flattens significantly (each node buys less pitch reduction than before), and the gate length essentially stops scaling around 10–12nm and becomes nearly flat. The transistor architecture innovations — FinFET, nanosheet, CFET — are the industry's response to this flattening: when you can no longer simply shrink the device, you have to reinvent its geometry entirely to keep extracting density and performance gains.
The projected open symbols on the right side of the chart carry genuine uncertainty — they represent the industry's ambition, not a guarantee, and depend on High-NA EUV delivering on its promise and CFET reaching manufacturability.

## Slide 8: Logic Scaling Potential Roadmap
Scaling Metrics
  Device feature size
  CPP: Contact Poly Pitch
  Metal Pitch
  Metals Tracks
Source: IEEE ELECTRON DEVICES MAGAZINE, DECEMBER 2025

## Slide 9: Back Side Interconnects
Example of a standard cell layout (a) and a corresponding cross-section cut (b) to illustrate the BSPDN’s scheme wherein each of the cell’s transistors (e.g., NSFETs) is connected from the wafer’s backside through a BS contact landing directly on the device’s source (BSC-S). This enables more compact NSFET-based cells, as a simplified 3D schematics also shows in (c)
Source: IEEE ELECTRON DEVICES MAGAZINE, DECEMBER 2025 https://www.imec-int.com/en/articles/how-power-chips-backside
BSPDN Back Side Power Delivery Network
Buried Power Rail
  Extreme wafer thinning (100nm)
  Expect to reduce IR drop by 7x
Global Clock & Global signals network
  Nano TSVs to contact NSFET devices
  Alignment precision ~10nm
https://www.imec-int.com/en/press/imec-launches-first-design-pathfinding-process-design-kit-n2-node

## Slide 10: Industry’s adoption of BSPDN
Samsung uses BSPDN technology for 2nm chips, improving performance by 44% and efficiency by 30%
TSMC Outlines 2nm Plans: N2P Brings Backside Power Delivery in 2026, N2X Added To Roadmap
TSMC A16TM @ TSMC TechSymposium, USA, April 2024

## Slide 11: Chiplets: Reversing Integration
Chiplets are the response to the end of monolithic scaling economics
  Decompose the SoC into smaller, functionally-specialized dies ("chiplets")
  Manufacture each chiplet in its optimal process node
  Integrate them in a package via a high-bandwidth die-to-die interconnect
  2.5D interposer-based
    Silicon interposer: passive Si with dense RDL, bump pitch ~45–55 µm,
    Organic interposer: cheaper, lower density
  3D die stacking
    Hybrid bonding: Cu-Cu thermocompression, pitch down to 1–3 µm, eliminates bumps entirely, bandwidth density ~10–100× over flip-chip
    Face-to-face or face-to-back configurations depending on power delivery constraints
UCIe Chiplet Interconnect protocol
Notes: Instead of integrating everything on one large die in an advanced node, you decompose the SoC into smaller, functionally-specialized dies ("chiplets") manufactured in their optimal process nodes, then integrate them in a package using a high-bandwidth die-to-die interconnect.

## Slide 12: Chiplets at HEP
Disaggregate the analog front-end (noise-optimized) from the digital hit-processing fabric and the high-speed serializer PHY
Structural reconfigurability:
  analog die is fixed and qualified
  the digital processing chiplet is retargeted per experiment and application
Alternative (non-chiplet approach):
  Parameter-programmable not structurally reconfigurable
  Configurable modes (ToT/ToA modes, per-pixel threshold trim, multiple readout modes. Still a fixed architecture underneath)
  Analog front-end parameterization has limits

## Slide 13: 2.5 - 3D Interconnects
CoWoS: Chip-on-Wafer-on-Substrate
SoW: System-on-Wafer
InFO: Integrated Fan-Out

## Slide 14: 3D Interconnects
Hybrid bonding: Wafer to Wafer hybrid bonding delivers unprecedented interlayer connectivity
Tight 3D integration => shorter wires => Low Power Energy/op ~ (CFET + LWIRE • CWIRE) • V2
Low Noise for “sensor wafer” – ”readout ASIC wafer” bonding
Wafer-to-wafer hybrid bonding process flow. Source: EV Group

## Slide 15: Interconnects & Photonics

## Slide 16: 2.5 - 3D Interconnects
Standardized ecosystem
Available on “high-end” nodes
  Minimum engagement volumes are calibrated to commercial customers, not HEP runs of a few hundred modules.
Use of specialized EDA tools for electrothermal and mechanical analysis and optimization

## Slide 17: Interconnects R&D at CERN using Timepix4 (65nm)
Experience with several vendors for TSV Last processing
Very promising results from a non-European vendor
  For the first time we were able to process 300mm wafers
  Just 0.1% dead pixels after processing. 5 wafers (73 chips / wafer) available @CERN. More on the way
  Vendor announced EOL of TSV-last processing !!!
Notes: solution décroissante

## Slide 18: Logic Scaling
TSMC foundry process technologies: https://www.tsmc.com/english/dedicatedFoundry/technology/logic
28nm | half-node, planar CMOS
22nm | half-node, Ultra Low Leakage
20nm | Double patterning
16/12nm | FinFET, immersion litho
7nm | FinFET, EUV lithography
2nm | nanoSheet
A16-A14 | Angstrom scale
PERFORMANCE COMPARED TO 65 NM:
  x 4-5 GATE DENSITY INCREASE
  > x2 FASTER
  ➢ x50 LEAKAGE INCREASE – CAN BE REDUCED EXPLOITING MULTI-VT and MULTI-GL DESIGNS

## Slide 19: Exploiting performance at 28nm
tcbn28hpcbwp35p140
30 nm
35 nm
40 nm
Gate length
7, 9, 12
SVT, LVT, HVT,
UHVT, ULVHT
Tracks
Voltage threshold
Poly pitch
140nm
I
Z
140nm
Faster
Less Power
HPC+ 30P | Raw Gate Density Kgates/mm2 | Speed GHz | Active Power nW/MHz | Static Power nW/MHz
7T | 4,289 | 0.742 | 0.601 | 0.485
9T | 3,961 | 0.886 | 0.781 | 0.714
12T | 2,971 | 1 | 1 | 1
HPC+ 12T | Raw Gate Density Kgates/mm2 | Speed GHz | Active Power nW/MHz | Static Power nW/MHz
30nm | 2,971 | 1 | 1 | 1
35nm | 2,971 | 0.9 | 0.992 | 0.446
40nm | 2,971 | 0.806 | 1.003 | 0.232
HPC+ 12T 30P | Raw Gate Density Kgates/mm2 | Speed GHz | Active Power nW/MHz | Static Power nW/MHz
LVT | 2,971 | 1.351 | 1.235 | 5.305
SVT | 2,971 | 1 | 1 | 1
HVT | 2,971 | 0.654 | 0.911 | 0.127
EHVT | 2,971 | 0.229 | 0.903 | 0.019
  120 different digital library sets
  Optimized implementation for Performance and Power

## Slide 20: Jumping to 22nm ULL & ULP
22 ULP: Ultra Low Power
  uLVT, LVT, SVT, HVT, UHVT
22 ULL: Ultra Low Leakage
  uLVT, LVT, SVT, HVT, UHVT, eHVT (+Thick Gate)
  SRAM ULL
  Low Vdd solution, down to 0.6V
  Foundry Low-Vdd libraries
  MRAM/RRAM offering on MPWs
TID response ?

## Slide 21: 22nm RRAM
Advanced RRAM Integration
  Resistive RAM is embedded into TSMC 22nm ULL manufacturing process, combining advanced non-volatile memory with cutting-edge planar semiconductor technology
Low Power and Fast Access
  RRAM technology is fully logic compatible with low process complexity. It is an excellent replacement for eFlash with comparable write speed, endurance and retention

## Slide 22: FinFET Design Challenges
⚙ DEVICE & PROCESS
Quantized Fin Geometry Width is discrete (N fins), not continuous. Complicates analog sizing, current matching, and W-stepping that planar CMOS handles freely.
Layout-Dependent Effects (LDE) Vth shifts 10s of mV from neighbour fins, STI stress, and MEOL contacts. Geometry-aware SPICE models mandatory.
Self-Heating Narrow Si body surrounded by low-κ isolation traps heat. Thermal-aware electrothermal co-simulation required, especially for RF/high-current blocks.
Gate Length Variability RDF suppressed but LER/LWR dominates at 7/5nm. Pelgrom law holds with different physical roots — process control is critical.
〜 ANALOG & MIXED-SIGNAL
Constrained Analog Sizing — FinFET electrostatics preserve output resistance (ro) well at moderate L. The real analog burden is discrete W quantization: fin count replaces continuous W/L trade-offs, forcing coarser gm and bias point control than planar designers are accustomed to.
Reduced Supply Headroom VDD = 0.7–0.8 V at 7nm squeezes dynamic range (DR ∝ VDD²/noise) and limits cascode stacking depth.
Discrete-Width Mismatch Classical Pelgrom matching (σ_ΔVth ∝ 1/√WL) restricted to discrete W options. Common-centroid layouts need identical fin-neighbour environments.
ESD Protection Thick-oxide I/O devices harder to implement; fin geometry elevates snapback current density and limits ballasting strategies.

## Slide 23: FinFET Design Challenges
▦ DIGITAL DESIGN
Std-Cell Library Complexity Fin quantization + multi-patterning-aware routing rules produce tight track heights (e.g. 6T at 5nm). PnR must respect coloring constraints throughout.
Multi-Patterning (SADP/SAQP) Below 16nm, no single exposure covers critical layers. LELE/SADP introduce overlay errors and forbidden pitches. EUV from ~7nm alleviates this but is not universal.
Clock & Power Grid Tight pitch raises metal resistance; PDN IR drop and EM limits tighten. Power/clock gating must be co-optimised with physical implementation from day one.
Timing Closure & OCV LDE/stress/proximity grow OCV budgets. Flat SPEF-based timing insufficient; AOCV/POCV (path-based) models required for reliable signoff.
☢ RADIATION HARDNESS
Single Event Upset (SEU) Mixed behavior
Smaller sensitive volume → less charge collection
Lower node capacitance → less charge needed to flip a bit
Net result: SEU cross-section ≈ similar to 28 nm
Single Event Transient (SET) Still a major issue
Fast transients due to high drive current and fast edges
Can propagate further in deep pipelines
Single Event Latchup (SEL) Major improvement
FinFETs are typically: Latchup-immune
No continuous bulk substrate path
No classical parasitic SCR structure
Much better TID tolerance than planar CMOS
Reasons:
No thick field oxide near channel
Reduced charge trapping impact
Better electrostatic control.

## Slide 24: Analog Design in finFETs
Problem
  Arbitrary transistor sizing → complex, non-uniform hand-drawn layouts
  Increased layout dependent effects (LDE): fin profile variation, stress, well proximity — all harder to model accurately
  Growing simulation-to-silicon gap at advanced nodes
Analog block Approach
  Few selected W/L options with track-based, pre-drawn cell heights
  Brick-like abutment enables structured, uniform array placement
  Guard ring cells share the same layout structure as active cells, enabling seamless abutment between arrays
  This co-design eliminates the area overhead of conventional guard ring utilities.
Source: 978-4-86348-815-1 ©2025 JSAP 2025 Symposium on VLSI Technology and Circuits Digest of Technical Papers

## Slide 25: High Energy Physics Motivation
Why Advanced Nodes Help
Hit Rate & Pixel Pitch
Smaller technology nodes enable much higher logic and memory density per mm²
Allows integration of Larger pixel matrices without increasing chip area and More complex per-pixel logic (zero suppression, buffering, clustering)
Enables finer pixel pitch by reducing routing congestion and area per channel
Critical for high-luminosity environments where occupancy is extreme
Data Bandwidth
Hit rates in the tens of MHz per pixel require on-pixel zero-suppression, time-stamping, and buffering — tasks that demand dense digital logic only achievable in advanced nodes
High-speed serial I/O drivers (multi-Gbps per link) benefit from the higher ft/fmax of short-channel transistors, enabling the aggregate bandwidth (Tbps scale for large detectors) needed for trigger-less or data-driven readout architectures
Advanced nodes offer more metal layers and tighter pitch interconnect, easing the routing of high-density data buses within the pixel matrix
Timing Resolution
Sub-100 ps (and increasingly sub-10 ps for 4D tracking) timing requires fast slewing front-end circuits and low-jitter discriminators, both of which benefit from the higher transconductance-to-current ratio (gm/ID) and reduced Cgate of advanced nodes
Time-to-Digital Converters (TDCs) embedded per pixel or per column require fine delay cells; the shorter gate delays in FinFETs/FD-SOI allow higher TDC resolution without excessive area or power
Reduced threshold voltage mismatch lowers timing walk and improves hit-time uniformity across large pixel arrays
Power Budget
Power-per-channel reduction despite increasing functionality
Advanced nodes operate at lower supply voltages reducing dynamic power quadratically (P ∝ CV²f)
The improved Ion/Ioff ratio in FinFETs reduces leakage in large arrays of idle pixels, which dominate static power at high pixel counts
Radiation Tolerance
Total ionizing dose (TID) >1 Grad generally robust but node-to-node variations to be evaluated.
SEU, SET and SEL robustness

## Slide 26: High Energy Physics Implications
Long Design Cycle 5-10 Years
Specification → tape-out: 3–5 yrs
System integration → physics: 3–5 yrs
Node must remain accessible & supported
Radiation Environment
TID: 1 Mrad–1 Grad (inner trackers)
SEU, SET, SEL robust RADHARD-by-design (RHBD) techniques
System-on-Chip Complexity
Analog front-end + ADC + DSP + I/O
Multi-function mixed-signal SoC
Full custom + standard cell co-design
Volume & Economics
Prototype: 100 ~1k die / MPW
Production: 10k–100k die
Product Cost is driven by Foundry NRE: $1.5M–$10M at (28nm to 7nm)
EDA Tool Complexity
PDK complexity grows with node
Mixed-signal design closure challenges
IP reuse: limited — often full-custom
Formal verification mandatory
Foundry Access
Foundry long term engagement
Regular affordable MPWs is essential
HEP is NOT the Consumer Market — Key Differences

## Slide 27: Mask set NRE cost
log scale

## Slide 28: Wafer Production cost by process node

## Slide 29: NRE amortization

## Slide 30: Product development cost in Industry
https://testflowinc.com/blog/2nm-chip-development-cost-725-million-analysis
Moore's Law isn't just about transistor density—it's about economics.

## Slide 31: The 16nm → 7nm Cost Cliff
The 16nm → 7nm step is not a single increase — it is the simultaneous collision of multiple independent cost drivers.
▲
Mask set cost
16nm: ~$12M
7nm: ~$42M
EUV masks need reflective multilayer optics
Features at 7nm have far more OPC polygons — up to 100× more per layer. Inverse Lithography Technology is computational intensive. E-beam inspection of masks (slower than optical)
HEP: one failed prototype iteration can consume an entire collaboration's annual hardware budget.
◆
Wafer cost
16nm: ~$5K/wafer
7nm: ~$10K/wafer
Lithography complexity. More mask layers. A 7nm process can require 80–100+ mask layers vs. ~50–60 for 16nm.. Lower yield, especially at project ramp. Defect density scales unfavorably with feature size.
■
DRC complexity
16nm: ~5,000 rules
7nm: 30,000+ rules
Full DRC on a large ASICs takes days.
HEP: small design teams cannot absorb the specialist effort to debug tens of thousands of interacting coloring and patterning rules.
●
Design methodology
16nm: schematic-driven
7nm: gridded / RDR
Free-form custom layout replaced by mandatory manufacturing grids and restricted design rules (RDR). Parasitic-aware layout in the loop is mandatory — open-loop design then extract gives wrong answers at 7nm pitches. Mixed-signal co-simulation requires FastSPICE at scale.
HEP: no existing IP at 16nm or 7nm. The methodology itself must be learnt from scratch.
★
Metal stack changes
16nm: relaxed / familiar
7nm: gridded / coloured
A new local interconnect layer (M0/LIG) between contacts and M1 has no equivalent at 16nm. Via rules forbid many combinations; mandatory via arrays replace single vias. M1–M3 are fully unidirectional and coloring-constrained at 28–36 nm pitch. Need powerfull PnR..
HEP: coloring-constrained routing and local interconnect are skills absent in our community.
✦
Signoff, closure & EDA
16nm: standard flow
7nm: specialist infrastr.
Full 3D parasitic extraction on every layer. IR-drop, EM and thermal co-simulated. PVT corners double. Multi-patterning coloring inside Calibre — a new discipline entirely. LVS needs updated device decks for FinFET fin counts and well proximity. Tool licences at 7nm cost significantly more; much higher compute runtimes.
HEP: no trained staff nor compute infrastructure for this flow exists in our groups.
!
Bottom line for HEP
Companies that absorbed this cliff — Apple, Qualcomm, NVIDIA — sell hundreds of millions of units, amortising $249M NRE across a product lifetime. A HEP collaboration producing 10–100k ASICs cannot. 28nm remains the highest-volume node in the industry a decade after introduction — the pragmatic ceiling for our community unless a clear physics mandate and industrial partnership justify the step to 7 nm.

## Slide 32: Node Comparison for HEP ASICs
Key candidate nodes — pros, cons, and HEP relevance
Node | Architecture | Strengths for HEP | Challenges | HEP use
28nm | Planar + HKMG shrink node | Mature PDK, MPW readily available, affordable NRE, excellent radiation behavior. HEP Design Kit and design methodology are validated. | Power and density advantages vs. 65nm, limited analog IP ecosystem. | PicoPIX
22nm | Planar + HKMG shrink node | Ultra Low Leakage devices. 10% area reduction, >10% speed gain, or 20% power reduction compared to 28nm. Heavily promoted node by the foundry. | Build HEP Design Kit and design methodology. Build analog IP ecosystem. Validate TID performance. | Backup to 28nm
22nm FD-SOI | FD-SOI (buried oxide) | Body biasing → dynamic VT tuning, excellent low-power, good analog | (GF, STmicro), cost ↑ vs. bulk, TID<10MRad, 10x more robust for SEE | Recommended: for low power, high frequency, application in low TID radiation field, Monolithic sensors (?)
16/14nm | FinFET (3D gate) | High logic density, >200 GHz fT, ML-edge possible. | High NRE ($2–5M), EDA complexity, design methodology gap | Recommended: adopt only with clear physics mandate. Regular MPWs & mini@sics
7nm | FinFET (dense) | Maximum density & performance, AI on-chip | Very high NRE (>$5M), EDA complexity, severe design methodology gap | Recommended: adopt only with clear physics mandate and budgetary considerations Regular MPWs

## Slide 33: Power Performance Area per selected nodes
Parameter | 130nm | 65nm | 28nm | 22nm ULL | 16nm | 7nm
Process type | Bulk planar | Bulk planar | Bulk HKMG | Bulk HKMG | FinFET | FinFET
Vdd nominal (V) | 1.2 – 1.5 | 1.0 – 1.2 | 0.9 – 1.0 | 0.8 – 0.9 | 0.8 – 0.9 | 0.7 – 0.8
Vdd low-power (V) | 1.0 | 0.9 | 0.8 | 0.7 – 0.75 | 0.72 | 0.65
Fmax typical (GHz) | 0.3 – 0.5 | 0.8 – 1.2 | 1.5 – 2.5 | ~1.0 – 1.5 | 2.5 – 4.0 | 4.0 – 6.0
Dynamic power (norm.) | 16× | 8× | 2× | ~1.5× | 1.3× | 1×
Leakage power (norm.) | 1× | 10× – 20x | 50× – 100× | ~5× – 15× | ~20× – 40× | ~30× – 60×
Logic density (MTx/mm²) | ~0.5 | ~2 | ~10 | ~15 | ~30 | ~90
SRAM cell size (μm²) | ~1.0 | ~0.42 | ~0.127 | ~0.10 | ~0.070 | ~0.027
Metal layers | 6 – 8 | 7 – 9 | 8 – 10 | 8 – 10 | 10 – 13 | 13 – 17
M1 pitch (nm) | 320 | 180 | 90 | 90 | 64 | 40

## Slide 34: finFET offerings within reach
Via Europractice/IMEC
  Regular MPW runs for 16 nm and 7 nm
  Regular mini@sics runs for 16 nm
  Special University Program
    16nm: 60kEur/4mm2
    7nm: 50kEur/2mm2
    https://europractice-ic.com/tsmc-university-finfet-program/#PricesTSMCfinfet
Technologies and IP availability

## Slide 35: Foundry economics
Bottom line: The foundry is pushing their 500+ customers hard into the FinFET era and that will again change the foundry landscape.
The trillion dollar question is: What will happen to the mature (non-FinFET) nodes in the not too distant future? And more importantly, what will do the foundries that did not make the jump to FinFETs?

## Slide 36: Conclusions & Take-Aways
The technology landscape is driven by AI/ML, IoT, 5G and automotive HEP benefits as a passenger on this roadmap and must be selective about which nodes to ride.
Advanced CMOS below 28nm is justified for HEP by hit-rate, pixel pitch, bandwidth and timing demands — particularly for HL-LHC and beyond.
HEP specifics (long design cycles, radiation, economics, foundry access) strongly constrain the candidate set — 7nm is currently out of scope for most collaborations.
Sweet spots: 28nm bulk (primary), 22nm (backup), 14nm FinFET (high-density/high performance). Engage foundries; build expertise.

## Slide 37
Thank You

## Slide 38: Power Performance Area per node (28nm baseline)
Planar CMOS
FinFET
GAA Nanosheet
● Foundry-announced
○ Estimated / ITRS
Node
Architecture
Lithography
Density
(×28nm)
Perf
(×28nm iso-pwr)
Power
(÷28nm iso-freq)
Perf/W/mm²
(×28nm)
Key innovation
130nm
2002
Planar
248nm KrF
● 0.06×
● 0.48×
● 0.31×
● 0.01×
Cu interconnect, low-k dielectric — pre-baseline reference
90nm
2004
Planar
193nm ArF
○ 0.13×
○ 0.57×
○ 0.41×
○ 0.03×
Strained Si channel; first 193nm ArF generation
65nm
2006
Planar
193nm ArF
● 0.25×
● 0.67×
● 0.53×
● 0.09×
2× gate density vs 90nm; 30–50% speed gain (TSMC datasheet)
45/40nm
2008
Planar
193nm immersion
○ 0.50×
○ 0.81×
○ 0.69×
○ 0.28×
Immersion litho; HKMG introduced (Intel 45nm); leakage reduction
28nm ⭐
2011
Planar + HKMG
193nm immersion
● 1.0×
● 1.0×
● 1.0×
● 1×
Full HKMG universally adopted; VDD scaling resumes — BASELINE
16/14nm
2014
FinFET
193nm immersion+SADP
● 2.0×
● 1.5×
● 2.5×
● 7.6×
FinFET: ~50% speed or ~60% power vs 28nm (TSMC N16)
10nm
2017
FinFET
193nm SAQP
● 4.0×
● 1.8×
● 3.8×
● 26×
~15% speed or ~35% power vs 16nm; 2× density (TSMC N10)
7nm
2018
FinFET
EUV (partial)
● 6.3×
● 2.1×
● 6.3×
● 81×
~20% speed or ~40% power vs 10nm; EUV for critical layers (TSMC N7)
5nm
2020
FinFET
EUV
● 11×
● 2.4×
● 9.1×
● 246×
~15% speed or ~30% power vs 7nm; 1.8× density (TSMC N5)
3nm
2022
FinFET / GAA*
EUV
● 19×
● 2.8×
● 13×
● 675×
~12% speed or ~28% power vs 5nm; 1.7× density (TSMC N3E)
2nm
2025
GAA Nanosheet
EUV + High-NA
● 22×
● 3.2×
● 18×
● 1,267×
~15% speed or ~30% power vs 3nm; GAA nanosheet (TSMC N2, IEDM 2024)
● Foundry-announced ○ Estimated / ITRS roadmap interpolation *GAA at Samsung 3nm; TSMC N3 remains FinFET
Sources: TSMC process announcements (N16–N2); ITRS (130nm–28nm); StatNano / NPD (65nm); Wikipedia; SemiEngineering; IC Knowledge / Handel Jones