## Slide 1: Cryogenic modeling and Process Design Kit for a CMOS 28-nm bulk technology
Luca castellani – FEE 2026 Paris

## Slide 2: Reason for cryogenic pdk development
Cryogenic ICs  cryogenic particle detectors readout and quantum computing control
Dark matter/neutrino detectors  scalability quantum processors  interconnect
Si Foundries  PDK (Process Design Kits) for a CMOS tech node. Valid only down to -40° C
Cryogenic Designs  custom models
Thesis Goal
Darkside20k liquid Ar cryo-TPC
in construction @LNGS, Italy
[1] DarkSide-20k sensitivity to light dark matter particles, Acerbi et al. 2024
[1]
Goal : establish a cryo characterization and extraction methodology for a 28nm bulk CMOS technology  partial cryo-PDK
Example of fixed cryo-T dilution cryostat for quantum computing prototypes

## Slide 3: cryogenic phenomena - cmos electronics
Threshold voltage increases
Subthreshold swing () decreases  slope increases
Mobility increases (phonon scatt. red.)
Dopant freeze-out
Built-in potentials increrase  PN junction depletion regions widen
Thermal noise reduction
(+ short channel effects!)
[1] “Characterization and Modeling of 28 nm Bulk CMOS Technology down to 4.2K” Beckers et al., 2018
[1]
[1]
[1]
[1]

## Slide 4: 28-nm Bulk CMOS
Mature commercial tech, 2011
Balance of cost, power consumption and performance
Dominant in many applications (Detector ASICs, Analog/Mixed-Signal Ics, scientific R&D)
One of the last av. planar CMOS nodes
Technology Overview @cryo T
BULK vs FD-SOI @CRYO:
No control ()
Freeze out
Cost effective
Less self heating
Bulk CMOS schematic
FD-SOI CMOS schematic

## Slide 5: Cryogenic measurement setup Forschungszentrum juelich

## Slide 6: sample DUT
Courtesy of Giulio Borghello – DRD7, CERN
pMOS and nMOS Test-transistors on p-sub
Intended for Total Ionizing Dose (TID) tests
28-nm, 16 pads per Column
28-nm CMOS multi-geometry chip for needle probing
1 mm

## Slide 7: Attodry800 dry cryostat workstation
Probing Screen
Control PC
N2 Bottle
Cryostat
Vacuum Circuit
Fischer Lines
Microscope
Piezo Modules

## Slide 8: attodry800 cryostat setup
AttoDRY800 dry cryostat @FZJ
Configuration with 3 Piezo Positioners, mounting a needle probe
DC signal through Fischer Lines
Outer shield: thermalized at 60K
Probes, Fischer slots and sample chip thermalized @8K
Heater and T sensor under sample base
Needle Probing Configuration
Cold Plate
Thermal Contact w/ Cold Plate
DUT Chip
3 Probes used:
  Left and right Probe: 4 Needles
  Upper Probe: 1 Needle

## Slide 9: Cryogenic temperature dependence characterization Forschungszentrum juelich

## Slide 10: Transfer currents
Measured @ 300K, 77K, 30K, 18K, 8K
Different geometries and threshold flavours (svt, lvt, ulvt)
Example: Standard nMOS 180/30
Dashed lines – log scale; solid lines – lin scale
Evident increase of subthreshold slope @cryo T
T
T

## Slide 11: Transfer currents
Measured @ 300K, 77K, 30K, 18K, 8K
Different geometries and threshold flavours (svt, lvt, ulvt)
Example: Ultra-low MOS 100/40
Dashed lines – log scale; solid lines – lin scale
Evident increase of subthreshold slope @cryo T
T

## Slide 12: Thresholds
LE (Linear Extrapolation) Method
Threshold increase of more than 100mV @cryo T observed for every device
[1] “Revisiting MOSFET threshold voltage extraction methods” Ortiz-Conde et al., 2013
[1]

## Slide 13: Free-carrier mobilities
where is the gate-oxide capacitance and is fitted at (strong inversion) (linear region)
Jazaeri method
[1] „Free Carrier Mobility Extraction in FETs”, F. Jazaeri et al., 2017
[1]

## Slide 14: Threshold adjustment in bulk technology Forschungszentrum juelich

## Slide 15: Forward body biasing for TUNING
[1]
In a Bulk Tech: increasing the Source-Bulk potential: Forward body biasing (FBB) Compensation of (bigger tech nodes)
Demonstrated in 40 nm Tech  possible because of increasing built-in potentials and depletion regions at cryo T [1]
First time test on 28-nm, only pMOS FBB
[1] TU Delft : Cryogenic-Aware Forward Body Biasing in Bulk CMOS, Overwater et al. 2024

## Slide 16: Forward Body biasing limits and leakages
All off/on leakages monitored, swept until S-B diode turned on (beyond tech limits at 8K)
Significant rev-leakage current reduction  ulvt more viable (of interest because of lower and lower doping  less freeze-out impact)
Example UL threshold pMOS 310/40 @T=8K
T |  |  | 
8K | 0V | 900mV | 100mV
30K | 0V | 800mV | 100mV
77K | 0V | 800mV | 100mV
T |  |  | 
8K | 0V | 900mV | 100mV
30K | 0V | 800mV | 100mV
77K | 0V | 800mV | 100mV

## Slide 17: Forward Body biasing results
Color legend: , , ,
Transfer and strong inversion output characteristics shown, exhibiting threshold decrease and output current increase
Example UL threshold pMOS 310/40 @T=8K

## Slide 18: Forward Body biasing results
Color legend: , , ,
Transfer and strong inversion output characteristics shown, exhibiting threshold decrease and output current increase
Example UL threshold pMOS 310/40 @T=8K

## Slide 19: Forward Body biasing tuning
with LE (Linear Extrapolation) Method
For no measured device reached room T level of operation
A significant threshold voltage reduction of is obtained, similarly at every temperature
Example UL threshold pMOS 310/40
Vth @ T=300K, Vsb = 0
[1]
[1] “Revisiting MOSFET threshold voltage extraction methods” Ortiz-Conde et al., 2013

## Slide 20: Experimental Data – in a nutshell
T Characterization Data
Measured short-channel devices:
9 nMOS and 9 pMOS svt
8 nMOS and 8 pMOS lvt
8 nMOS and 8 pMOS ulvt
Different W/L
Measurement repeated at 8K, 18K, 30K 77K and 300K
For each device:
6 transfer curves @
10 output curves @
Leakage acquired during each measurement
FBB Data
For each device:
6 transfer curves @
10 output curves @
Leakage acquired during each measurement
Measurement repeated at 8K, 30K and 77K
Measurement repeated @ (or compliance)
Measured short-channel devices:
4 pMOS lvt
4 pMOS ulvt
Different W/L

## Slide 21
Method for cryogenic cmos model extension
INFN TORINO

## Slide 22: The partial cryo-PDK procedure
Software Setup
SW Setup: Cadence Spectre + Python possible thanks to pyspectre interface
Model: BSIM-BULK (former BSIM-6)
Workspace was tested @ FZJ and setup @ INFN Torino
Goal: partial PDK establish a procedure to create cryo-corners in 28-nm, valid at fixed thermal states
[1] “PySpectre: Python interface for Cadence Spectre” GitHub repository. Y. Uhlmann., Version 1.2.0. 2024
[2] “BSIM-BULK 107.2.1 MOSFET Compact Model”. Berkeley, CA, 2025
[2]
[1]
5 BSIM-BULK T dependent parameters chosen
Additive components in custom model files 
Custom model files accessible via pyspectre

## Slide 23: The Parameter extraction PROCESS
Pyspectre flow
Netlist loaded
Netlist loaded
|Ids| vs Vgs simulation @ different Vds
Measured vs simulated metric check
Algorithm changes 5 additive parameters in model files
START
Parameters
Metric unsatisfied
Metric satisfied

## Slide 24: Metric and multiple fitting algorithm
svt pMOS W/L = 100/35
Procedure tested on a single svt pMOS W/L = 100/35
Chosen metric  mean square error sum with weightintg: moderate (50x) in strong inversion, heavy (150x) in sharp moderate inversion, light (0.5x) for sub-threshold noise
Algorithms  two multidim tested: Levenberg-Marquardt and Nelder-Mead

## Slide 25: Metric and multiple fitting algorithm
svt pMOS W/L = 100/35
Procedure tested on a single svt pMOS W/L = 100/35
Chosen metric  mean square error sum with weightintg: moderate (50x) in strong inversion, heavy (150x) in sharp moderate inversion, light (0.5x) for sub-threshold noise
Algorithms  two multidim tested: Levenberg-Marquardt and Nelder-Mead
Freeze-out kinks

## Slide 26: Sim vs meas data – 8K
svt pMOS W/L = 100/35

## Slide 27: PARTIAL CRYO-PDK – in a nutshell
Foundry BSIM complete model (.scs) files
Transistor netlist (.scs)
Custom BSIM transistor model (.scs) files with
Multiple fitting procedure run (python scripts)
INCLUDED
INCLUDED
Experimental data
pyspectre interface
Custom BSIM transistor model (.scs) files with
OBTAINED
Repeated @ W/L of nMOS-pMOS
Partial cryo-PDK files valid @ fixed T
Enhance the PDK to cover continuous T ranges
Cryo CMOS IP libraries

## Slide 28: Conclusions and outlook
Collaborative research between UniTO, INFN and FZJ; 4 months on site at Julich for cryogenic data extraction.
Implementation of a partial cryo-PDK for a 28-nm bulk CMOS technology, using experimental data at 8-18-30-77K and state-of-the-art methodology for a model extension at fixed temperatures.
First test of the cyo-FBB technique (used for trimming the device ) on a bulk 28nm CMOS technology node.
Conclusions
Outlook
Development of a new cryogenic device model allowing for simulation over a continuous temperature range (instead of fixed thermal states), in collaboration with TU Graz (Austria).
Design of a new DUT (bulk-28nm, other techs) optimised for cryogenic measurements – current measurement campaign used a DUT developed for radiation hardness studies.
Design of a cryo-IP (bulk 28-nm) prototype using the partial PDK developed and available for the complete demonstration of the cryo-PDK.

## Slide 29: REFERENCEs
“DarkSide-20k sensitivity to light dark matter particles” Acerbi et al. 2024
“Characterization and Modeling of 28 nm Bulk CMOS Technology down to 4.2K” Beckers et al., 2018
“Revisiting MOSFET threshold voltage extraction methods” Ortiz-Conde et al., 2013
“BSIM-BULK 107.2.1 MOSFET Compact Model”. Berkeley, CA, 2025.
“PySpectre: Python interface for Cadence Spectre” GitHub repository. Y. Uhlmann., Version 1.2.0. 2024
Presentation references
“Free Carrier Mobility Extraction in FETs”, F. Jazaeri et al., 2017
“Characterization and modeling of 28-nm FDSOI CMOS technology down to cryogenic temperatures” Beckers et al. 2019
“Cryogenic-Aware Forward Body Biasing in Bulk CMOS” Overwater et al. 2024

## Slide 30: Backup - discarded setup
TID damage live monitoring: many devices contacted on the same cycle
Contact @CERN: 2 entire columns sim. !!
16L + 16R Needle Probes
Tried but discarded:
Hard repeated contacts @cryo
Vertical bending @cryo
Lack of cryostat feedthroughs
Heavy T load

## Slide 31: Backup - transconductances

## Slide 32: Backup - Mobilities
[1]
[1] “Characterization and Modeling of 28 nm Bulk CMOS Technology down to 4.2K” Beckers et al., 2018

## Slide 33: Backup – short channel effects
Drain-induced barrier lowering
Halo dopings

## Slide 34: BACKUP - FD-SOI backgate tuning of
Increase of in cryo
Adjusted with
One of the advantages of SOI for cryo ICs
[1]
[1] Characterization and modeling of 28-nm FDSOI CMOS technology down to cryogenic temperatures, Beckers et al. 2019

## Slide 35: backup - PMOS FBB
Only pMOS FBB because:
Substrate in contact with the cold plate
CERN Chip: no triple well nMOS devices
 Ground Loop
 -> ESD Diode on S
Cu Alloy Cold Plate
DUT Chip
Ag Glue

## Slide 36: Backup – Statystical testing
svt pMOS W/L = 100/35, Levenberg Marquardt algorithm

## Slide 37: Backup – Statystical testing
svt pMOS W/L = 100/35, Levenberg Marquardt algorithm
not passed  model extension weakness in linear region

## Slide 38: Backup – Statystical testing
svt pMOS W/L = 100/35, Levenberg Marquardt algorithm
passed, or barely not (low regime)

## Slide 39: Backup – Statystical testing
Freeze-out kinks
Max noise levels

## Slide 40: Backup - Algorithms comparison
8K optimization 5 parameters
Same initial guess, same 5 pars
Same target RMS  adherence sim-meas
Levenberg-Marquardt
Total time: 30.43 s
Function evals: 29
Time per eval: 1.05 s
Final cost: 9.4e-07
Final RMS: 3.5e-05
Quadratic
Faster but more sensitive to loc. min. and initial guess
Nelder-Mead
Total time: 113.50 s
Function evals: 149
Time per eval: 0.46 s
Final cost: 9.4e-07
Final RMS: 3.5e-05
Linear
Less sensitive to loc. min. and initial guess but slower