## Slide 1: Front-end ASICs for high resolution imaging spectroscopy in space
David Baudin et.al.

## Slide 2: Summary
Astrophysic Context: Existing missions and future needs
Noise optimisation for high resolution
  CMOS Amplifier
  Non Stationnary Noise Suppressor
Matrix based optimisation
  Double CR-RC stage
  AC link with low noise leakage current generation
Packaging and interconnexion
Results and conclusion

## Slide 3: Astrophysic Context: Existing missions and future needs
1

## Slide 4: Summary of astrophysic context: Solar physics
Solar orbiter:
  Fourier-transform imaging
  Stackup of CdTe – ASIC – Supplies
  12 Pixels per modules
  30 modules – Caliste-SO
  IDEF-X HD ASICs (one per module)
Study the electron acceleration in coronal emission (Solar Orbiter)
Measure the electron distribution and polarisation
Flux and transient phenomena measurements
Science Case:
Space missions (on-flight):
Padre:
  Direct measurement
  4 modules – Caliste-SO
  IDEF-X HD ASICs
Future Needs:
Highly pixelated integrated circuit:
  < 250 x 250 µm²
  > 32 x 32 pixels
Energy resolution < 2 keV @ 30 keV
< 40 el.rms
Flux: ~200 kHz/mm²
Fig1: Sum picture in UV and X-Ray taken by Solar Orbiter
Fig 2: Padre nano satellite
Fig 3: Solar orbiter imaging system, focal plane, flux variation with time, Caliste So module

## Slide 5: Summary of astrophysic context: Extra galactic [SNR, Gamma ray burst]
Science Case:
Space missions (on-flight):
Future Needs:
Highly pixelated integrated circuit (for polarisation):
  < 250 x 250 µm²
  > 32 x 32 pixels
Energy resolution < 1 keV @ 30 keV < 20 el.rms
Study the metal generation on stellar generation
  56Ni → 56Co at 156 keV
  57Co → 57Fe at 122 keV
Study polarization and energy distribution of Gamma ray bursts
SVOM:
  Coded mask imaging
  Stackup of CdTe – ASIC – Supplies
  32 Pixels per modules
  25 modules
  IDEF-X Eclairs
Comcube:
  Coded mask imaging
  SDD detector
  Constellation of 27 nano-satelittes
  4 ASICs
  IDEF-X HDBD
Fig 4: Cas-A picture (chandra-X)
Fig 5: Simulated flux from SNR
Fig 6: Comcube ballon launch and payload
Fig 7: SVOM eclair coded mask aperture, focal plane, image of GRB

## Slide 6: ASICs Developped at Saclay List and Specification
ASIC | Energy resolution eV @ 60 keV | Number of Pixels / channels | Size of pixels / channels (µm x µm) | Power density (mW/mm²) (mW/channel) | Options / Technology
IDeF-X HDBD | 526 [17 el.rms] | 32 | 150 x 2000 | 2,7 0,8 | Bidirectionnal AMS 0.35 µm
IDeF-X S | 474 [10 el.rms] | 32 | 150 x 2500 | 2,2 0,8 | Common mode rejection AMS 0.35 µm
D2R1 | 666 [29 el.rms] | 16 x 16 | 300 x 300 | 2,7 0,25 | CDS XFAB 0.18 µm
D2R2 | 910 [54 el.rms] | 32 x 32 | 250 x 250 | 4,8 0,3 | XFAB 0.18 µm
ANAQIN-X | NA [17 el.rms] | 4 x 4 | 250 x 250 | 4,8 0,3 | Prototype XFAB 0.18 µm
Fig 8: ASICs Developped at Saclay

## Slide 7: General structure of our ASICs
Amplification:
  CSA with continuous reset
Filtering:
  Analog CR-RCn filter with transistors copy
Maximum detection:
  Peak detector with or without pileup detection
Triggering:
  Tunable threshold with baseline rejection
Some options used in some designs:
Non stationnary noise suppressor
Multi-Stage CR-RC
CMOS amplifier
Fig 9: IDEFX-HD picture
Fig 10: General spectroscopic instrumentation chain schematic

## Slide 8: Noise optimisation for high resolution
2

## Slide 9: A- CMOS architecture for Charge Sensitive Amplifier
Circuit:
Classical folded cascode architecture
Both P and N mosfet are connected together
A current regulation set the current state
  In our case its a « mirror » version of the CSA that generate voltage reference for « current regulation »
Hypothesis: - Strong Inversion region
- Ln = Lp = Lmin
Thermal Noise optimization
Flicker Noise optimization
Optimum for:
Optimum for:
Fig 11: CMOS CSA

## Slide 10: A- CMOS architecture for Charge Sensitive Amplifier
Optimisation is found as:
  a = b for both Flicker and Thermal
  Then, depending on optimisation ( or ) => and
We can fix some parameter to help us identify noise ratios
Noise ratio with respect to NMOS for thermal and Flicker for PMOS can be found as:
Noise Type | NMOS | PMOS | CMOS
Flicker |  |  | 
Thermal |  |  | 
Noise Type | NMOS | PMOS | CMOS
Flicker |  |  | 
Thermal |  |  | 
Technology | NMOS | PMOS | CMOS
Thermal AMS035 | 1 | 1,3 | 0,93
Thermal AMS018 | 1 | 0,5 | 0,95
Thermal XFAB018 | 1 | 1,5 | 0,95
Thermal TSMC0065 | 1 | 1,1 | 0,89
Noise Type | NMOS | PMOS | CMOS
Thermal AMS035 | 1 | 1,3 | 0,93
Flicker AMS035 | 1,1 | 1 | 0,95

## Slide 11: A- CMOS architecture for Charge Sensitive Amplifier
Several ASIC have been done with this circuit, one of the latest is:
  IDEF-X HDBD:
Coupled with a Silicon drift detector (Cdet = 120 fF)
  Resolution: 227 eV @ 5,9 keV
  Threshold: 1,2 keV
  Power: 26 mW
  Channel: 32
Fig 14:
Fig 13: IDEF-X HDBD picture mounted with INAF-Triestre & Roma SDD
Fig 12: IDEF-X HDBD noise variation with peaking time and capacitance

## Slide 12: B- Non stationnary noise suppressor
Our design are often base on a continuous reset done with a MOS transistor in subthreshold region.
When signal amplifies high value charges:
  CSA output increases
  Source voltage increase
  Reset transistor is non longer in subthreshold region during that time
Consequences:
  Reset goes faster (could generates ballistic deficit)
  Noise increase temporarily
We implemented a special filter at CSA’s output
Advantages:
  Supress gm variation with charges
Drawbacks:
  Increase Reset time
  Generates oscillation when Ileak increases if low pass)
Fig 15: Single stage CR-RC in continuous reset
Fig 16: Double Stage CR-RC in continuous reset
[Geronimo et.al], “A CMOS fully compensated continuous reset system,” IEEE Transactions on Nuclear Science, vol. 47, no. 4, pp. 1458–1462, Aug. 2000

## Slide 13: B- Non stationnary noise suppressor
Filter is based on a small differential pair with a zero and pole path done with « R » and « C ».
R is based on an inverted diode with small potential accross in order to reach Tohms values
Avoids having oscillation a high leakage, if design with a correct pole and zero, one can be always stable (if Ileak < 10 fA).
One ASIC has implemented a version where we can turn on / off this features: D2R2
Fig 18: Oscilloscope output of a 27 kel equivalent pulse
Fig 17: NSNS Structure
Fig 19: ENC variation with injected charge

## Slide 14: Matrix based optimisation
3

## Slide 15: A- Double CR-RC stage
One Stage CR-RC
Double Stage CR-RC
We add a resistor to add a « free pole »:
We can vary peaking time by varying R (N) or Cx
Varying Cx allows to reduce amplifier throughput
Noise:
  One stage:
  Double stage:
For low noise: should be high
Fig 20: Schematic of single stage and double stage continuous reset architecture (left) and resulting AC bode diagram (right)

## Slide 16: A- Double CR-RC stage
Fig 21: Plot of the mathematical representation of area ratio between two architecture, taking into acount transistors area together with capacitance area for Cdensity = 2,35 fF/µm²

## Slide 17: AC link with low noise leakage current generation
With Continuous reset circuit:
  If Ileak increases, noise will increase both due to schot noise in detector but also with thermal noise produced by the reset
With radiation, detectors (Silicon) tends to have increasing leakage current
We wanted to decouple inside the ASIC (for matrix connection) reset and detector bias => AC link
Feedback capacitance outside of AC link loops helps to provide
And amplification of Cac to be able to have 30 pF
with only 1 pF internal capacitance
Reset can be done with N transistor in diode which allows:
Fig 22: Semi-AC reset architecture.
[Perić, Ivan et.al.] « High-voltage pixel detectors in commercial CMOS technologies for ATLAS, CLIC and Mu3e experiments ». Nuclear Instruments and Methods in Physics Research Section A: Accelerators, Spectrometers, Detectors and Associated Equipment, PIXEL 2012, vol. 731 (décembre 2013): 131‑36. https://doi.org/10.1016/j.nima.2013.05.006.

## Slide 18: AC link with low noise leakage current generation
Optimum point for 7 diodes
12.7 pA
Optimum point for 3 diodes
55 pA
2
3
4
5
6
7
Number of Diodes
Ileak (pA)
100
20
50
We implemented this on two pixels of ANAQIN chip with possibility to change number of diodes
Capacitance (pF)
Normalised Gain
We reach with 1 pF and equivalent gain of 30 pF
Leakage current is controlled with voltage reference
We have seen an improvement with 1 – 2 transistors
Larger number of transistors have shown issues in the leakage current generation
Fig 23: Gain measured with or without « semi - AC » architecture
Fig 24: Simulated optimal point by variying both Tpeak and number of diode in series

## Slide 19: AC link with low noise leakage current generation
We implemented this on two pixels of ANAQIN chip with possibility to change number of diodes
Capacitance (pF)
Normalised Gain
We reach with 1 pF and equivalent gain of 30 pF
Leakage current is controlled with voltage reference
We have seen an improvement with 1 – 2 transistors
Larger number of transistors have shown issues in the leakage current generation
Fig 23: Gain measured with or without « semi - AC » architecture
Fig 25: Measure of total noise with Varying Leakage current

## Slide 20: Packaging and interconnection
4

## Slide 21: A- Packaging and interconnexion From 3D interconnection to 2D
Detector
Interconnection
Molding
Laser routing
Step 1: chip molded in siliciced resin
Step 2: copper deposition and lithography
Step 3: gold stud deposition
Step 4: serigraphy with stencil and Ag epoxy
Step 6: Gold wire insertion for « TPV »
Step 5: detector deposition
Detector
IDeF-X HD
Power supply / decoupling
PGA outputs
Fig 26: X-Ray Photography of a Caliste - HD
Fig 27: 2D interconnection process steps

## Slide 22: Results and conclusion
5

## Slide 23: A- D2R2 ASIC
Fig 30: IDeF-X D2R2 picture
Fig 29: IDeF-X D²R2 Pixel Layout
Fig 28: Schematic of one pixel
250 µm
250 µm
8500 µm
8500 µm

## Slide 24: A- D2R2 ASIC
Fig 31: Readout Strategy

## Slide 25: B- D2R2 ASIC results
Fig 32: Gain Map
Fig 33: ENC Map
Mean value: 31 µV/el
Standard deviation: 271 nV/el
Mean value: 74 el.rms [12 expected]
Minimum: 42 el.rms
Standard deviation: 21 el.rms
[CSA + Internal shaper / All pixels]

## Slide 26: C- Packaging and interconnexion
Energy (keV)
Normalised intensity
Fig 33: Hybrid made by Imagine-X Japan, hit map above threshold, and sum spectrum
Fig 34: Hybrid made « inhouse », and count map.
Noise with detector is similar than without (77 vs 74).
Issue with excess of noise in the circuit (74 vs 14)
Custom interconnects still needs improvement:
  Not 100 % of full connection
  Different gain seen in the pixels (not seen with IMAGIN-X hybrids)

## Slide 27: C- ANAQIN ASIC results
Fig 35: Picture of ANAQIN-X ASIC
Reference pixel (nelna)
Nelna with 300 µm length
NMOS standard
PMOS Base CSA
AC-Based CSA
Fig 36: ENC versus peaking time for PMOS based CSA (top) and NMOS based CSA (bottom)

## Slide 28: Conclusion
I tried to show the different solutions we developped for reduction of:
  Noise: CMOS amplifier, NSNS, semi-AC link
  Interconnexion: packaging with custom WDoD
  Space: Double stage CR-RC
With ANAQIN-X we managed to find a pixel with a correct working point
Future Matrix « CESAR » is planned to be taped out on july 2026
  Pixel selected from ANAQIN-X measurements
  Reduction of interfaces (136 pads to 64)
    DACs for reference
    Serialized mode for output
In parallel, module is beeing built
Fig 37: Layout of CESAR ASIC

## Slide 29: Thank You and thanks to the team
Xavier Coppolani, Pascal Couderc, Olivier Gevin, Olivier Limousin, Florent Bouyjou, Hugo Allaire, Diana Renaud, Marin Prieur, Aline Meuris, Fabrice Soufflet, Jean-Michel Guinet, Eric Tan, Noemie Belin, Jérémy Chauveau, Olivier Garel, Hervé Bervas, Denis Chesnais,…

## Slide 30: Backups

## Slide 31: Oscillations with low pass NSNS
If Low pass:
Ileak ↑  oscillation
Solution:

## Slide 32: Simulation optimisation with XFAB018 and nelna
GOL = 8000 V/V
GCL = 6.2 µV/el
Trise = 50 ns
W = 90 µm
L = 180 nm
ENCFloor = 14 el.rms with Ideal CR-RC filter
Noise | NMOS | PMOS | CMOS
Flicker | 0.38 | 1 | 0.5
Thermal | 1 | 1.44 | 0.94
XFAB 0.18 µm:
= 0.23
= 1.55

## Slide 33: Measurement D2R2
Gain: 6.3 µV/el
ENCfloor: 36 el.rms at Tpeak = 9.5 µs [CSA + External filter]
(14 el.rms expected)
Variation with capacitance: 300 el/pF at Tpeak = 4 µs
(20 el/pF expected)
« Flat » slope
1/f noise ?
Vary with Icsa
Tpeak = 12 µs
Tpeak = 18 µs
Tpeak = 54 µs
Tpeak = 153 µs
Tpeak = 1200 µs
Cdet = 0 pF
Cdet = 1.5 pF
Cdet = 3.4 pF
Cdet = 5.2 pF
Cdet = 7 pF
Cdet = 8.8 pF
Tpeak = 12 µs
Tpeak = 18 µs
Tpeak = 54 µs
Tpeak = 153 µs
Tpeak = 1200 µs
CSA + External Shaper
Cdet

## Slide 34: Measurement D2R2
Linearity
  2.6 % [For all range high gain]
  0.24 % [For 0-110 keV range high gain]

## Slide 35: Measurement D2R2

## Slide 36: Measurement D2R2
Minimum threshold:
  1.5 keV
Noise contribution
From Discriminator:
  < 30 el.rms
Discriminator

## Slide 37: Measurement D2R2
Noise Distribution

## Slide 38: Measurement D2R2
Filter Area
Filter Function

## Slide 39: Measurement D2R2
Why?:
Parallel noise:
WI:
SI:
How?:
Low pass:
Stability:
How?:
3rd Order system:
Stability:

## Slide 40: Technology validation
For finding appropriate technology we have done several test matrices of CSA’s in:
  AMS 0,18 µm
    Pmos
    Nmos
  XFAB 0,18 µm
    Pmos
    Nmos
    Nmos « low noise »
    Pmos 3,3V
    Pmos « low noise »
Chart: AMS 0.18: PMOS 100/0.18, 10µA
| 1.1000000000000001 | 1.8 | 3 | 5.0999999999999996 | 6.9 | 10.5 | 18 | 52 | 150
Cadd=22pF | 1258.75 | 1091.43 | 934.375 | 789.7 | 704.213 | 599.635 | 619.7242 | 529.0464 | 534.8179
Cadd=15pF | 977.459 | 853.439 | 731.51 | 647.212 | 570.223 | 477.946 | 450.2659 | 401.6266 | 394.7587
Cadd=10pF | 721.79 | 632.386 | 529.047 | 449.71 | 402.986 | 339.744 | 346.439 | 334.7366 | 349.3949
Cadd=0pF | 183.113 | 148.89 | 125.25 | 109.41 | 103.18 | 96.33 | 125.0688 | 153.744 | 191.856
10pFfit | 748.9735 | 621.4849 | 513.0056 | 431.7264 | 394.7256 | 350.4252 | 326.8206 | 306.6329 | 323.7285
Cadd=4.7pF | 463.75 | 378.57 | 316.758 | 257 | 233.824 | 192.9 | 201.6 | 194.88 | 218.0026
No bonding | 24.1086 | 18.9352 | 14.9377 | 12.406 | 11.1235 | 9.5129 | 10.1931 | 10.6768 | 12.7925
15 pF fit | 1049.6816 | 841.3486 | 697.7723 | 583.7435 | 537.2063 | 478.6324 | 448.161 | 414.393 | 420.8932
22pF fit | 1398.4657 | 1141.8072 | 945.5349 | 796.4221 | 742.3607 | 669.5136 | 617.6984 | 568.0207 | 562.7811
4.7pFfit | 457.1767 | 377.5615 | 312.0239 | 263.0058 | 238.5712 | 210.8228 | 198.9438 | 197.3765 | 231.4371
0pF fit | 189.0778 | 157.8843 | 128.3466 | 107.2574 | 98.8084 | 91.9364 | 92.6508 | 115.7886 | 173.9358
no bonding fit | 23.2122 | 19.1282 | 15.2993 | 12.5327 | 11.3477 | 10.0956 | 9.6294 | 10.2138 | 13.2396
Chart: Tpeak (µs)
| 0.98699999999999999 | 1.35 | 2.27 | 4 | 5.8 | 10.5
XFAB 100/0.45 | 36.463 | 28.9 | 21.6 | 17 | 14.6 | 12.1
AMS 100/0.45 | 28.1504 | 21.2667 | 15.9457 | 12.5188 | 11.0239 | 8.9422
Conclusion:
  AMS 0,18 µm have shown better results
  Both chip have been irradiated up to 1 Mrad and 300 krad (see next)
  We unfortunately have been forced to stop ams 0.18 (OSRAM has reserved the foundry)

## Slide 41: C- Technlogy validation
Irradiation: With a 60Co source
XFAB
AMS
XFAB:
  We followed the previous development to characterize different types of transistor in a chip: ANAQIN