## Slide 1: Electroplated Ni Targets for ⁶¹Cu/⁶⁴Cu Production in Clinical Cyclotrons
Jose Daniel Campos Mendez
Thomas Sounalet
Erick Mora Ramirez
Ferid Haddad

## Slide 4
Enriched 61Ni 64Ni
61Cu
64Cu

## Slide 5
Jose Daniel Campos Mendez
2nd year PhD Candidate
Cyclotron 18 MeV
University of Costa Rica
Costa Rica
Cyclotron 18 MeV
GIP ARRONAX
Nantes, France

## Slide 6: 61Cu and 64Cu
Therapy and diagnosis (theragnosis) of cancer
Prostatic
Breast
Neuroendocrine
Production in a medical cyclotron by proton irradiation
Enriched Ni target
Most of Ni is not activated

## Slide 7: Having a cyclotron means the patients will have Cu benefits?
Benefits of Cu theragnosis options.
Medical Cyclotron could produce this isotopes.
Enriched Ni is really expensive.
Most of the Ni is wasted in the production.
The costs of the production are too high.

## Slide 8: Process optimization
Ni target
Electroplating
Target Irradiation
Separation of Cu
Ni Recycling
Enriched 64Ni or 61Ni
64Cu / 61Cu

## Slide 9: Process optimization
Ni target
Electroplating
Target Irradiation
Separation of Cu
Ni Recycling
Enriched 64Ni or 61Ni
64Cu / 61Cu

## Slide 10: Ni Electroplating
Ni source | NiSO4 | NiCl2 | NiCl2
Buffer | 2M NH3 / 1M (NH4)2SO4 | 2M NH3 / 1M (NH4)2SO4 | 2M NH3 / 1M NH4Cl
Current density (mA/cm2) | -8 -20 -50 | -10 -20 | -10 -20
pH controller | NH3 | NH3 | NH3
pH range | 10 – 8,5 |  | 
Support | Au (1mm) |  | 
Temperature (°C) | ≈30 |  | 

## Slide 11
10 g/L
6 g/L
4 g/L
Sulfate
Sulfate-Chloride
Chloride
5 g/L
4 g/L
1 cm
Reusing an electrolyte solution
Ni Concentration
≈ 35 µm

## Slide 12
10 g/L
6 g/L
4 g/L
Sulfate
Sulfate-Chloride
Chloride
5 g/L
4 g/L
1 cm
pH within the range
Reusing an electrolyte solution
Ni Concentration
≈ 35 µm

## Slide 13
10 g/L
6 g/L
4 g/L
Sulfate
Sulfate-Chloride
Chloride
5 g/L
4 g/L
1 cm
pH within the range
Current efficiency above 90 %
Reusing an electrolyte solution
Ni Concentration
≈ 35 µm

## Slide 14
10 g/L
6 g/L
4 g/L
Sulfate
Sulfate-Chloride
Chloride
5 g/L
4 g/L
1 cm
pH within the range
Current efficiency above 90 %
Homogeneous deposits
Reusing an electrolyte solution
Ni Concentration
≈ 35 µm

## Slide 15
10 g/L
6 g/L
4 g/L
Sulfate
Sulfate-Chloride
Chloride
5 g/L
4 g/L
1 cm
Ni Concentration
pH within the range
Current efficiency above 90 %
Homogeneous deposits
Morphology changed
Reusing an electrolyte solution
≈ 35 µm

## Slide 16
10 g/L
6 g/L
4 g/L
Sulfate
Sulfate-Chloride
Chloride
5 g/L
4 g/L
1 cm
pH within the range
Current efficiency above 90 %
Homogeneous deposits
Morphology changed
Low current efficiency
Reusing an electrolyte solution
Ni Concentration
≈ 35 µm

## Slide 17
10 g/L
6 g/L
4 g/L
Sulfate
Sulfate-Chloride
Chloride
5 g/L
4 g/L
1 cm
pH within the range
Current efficiency above 90 %
Homogeneous deposits
Morphology changed
Low current efficiency
Reusing an electrolyte solution
Ni Concentration
≈ 35 µm

## Slide 18
SEM / EDS
18
Ni
Ni

## Slide 19
Energy range and cross section

## Slide 20
Energy range and cross section

## Slide 21
Produced Isotope | Cu61 /Cu64 | 
Energy range (MeV) | 5-18 | 
Research center | CICANUM | ARRONAX
Tilt from beam axis (°) | 90 | 6
Apparent thickness (µm) | 583 | 583
Real thickness (µm) | 583 | 61
Target mass (mg) | 1631 | 409
Goal target thickness
9,6 cm
1,0 cm
1,0 cm
6°
M. Sitarz, Radionuclide Yield Calculator. Nantes, France: GIP ARRONAX, (2018). [Online]. Available: http://www.cyclotron-nantes.fr/.
Real thickness
Apparent thickness

## Slide 22
Produced Isotope | Cu61 /Cu64 | 
Energy range (MeV) | 5-18 → 9-16 | 
Research center | CICANUM | ARRONAX
Tilt from beam axis (°) | 90 | 6
Apparent thickness (µm) | 583 → 352 | 583 → 352
Real thickness (µm) | 583 → 352 | 61 → 37
Target mass (mg) | 1631 → 985 | 409 → 247
Goal target thickness
9,6 cm
1,0 cm
1,0 cm
6°
M. Sitarz, Radionuclide Yield Calculator. Nantes, France: GIP ARRONAX, (2018). [Online]. Available: http://www.cyclotron-nantes.fr/.
Real thickness
Apparent thickness

## Slide 23
Produced Isotope | Cu61 /Cu64 | 
Energy range (MeV) | 5-18 → 9-16 | 
Research center | CICANUM | ARRONAX
Tilt from beam axis (°) | 90 | 6
Apparent thickness (µm) | 583 → 352 | 583 → 352
Real thickness (µm) | 583 → 352 | 61 → 37
Target mass (mg) | 1631 → 985 | 409 → 247
Goal target thickness
9,6 cm
1,0 cm
1,0 cm
6°
M. Sitarz, Radionuclide Yield Calculator. Nantes, France: GIP ARRONAX, (2018). [Online]. Available: http://www.cyclotron-nantes.fr/.
Real thickness
Apparent thickness

## Slide 24: Thick targets
1st layer
25 h
288 µm
CE 93,7%
2nd layer
27 h
600 µm
CE 93,5%

## Slide 25: Ni recovery (still in study)
Ni electrolyte after target deposit
Electroplating
Ni electrolyte waste
< 5 mg
> 97%

## Slide 26: Conclusions
Nickel Chloride electrolyte is a good option for electroplating.
Color changing comes from morphology variations.
Thick targets until 600 µm can be produced.
Electroplating for Ni recovery looks promising.

## Slide 27
ARRONAX / SUBATECH
CICANUM
Organizers of GDR Mi2B
Contact information:
campos@subatech.in2p3.fr
jose.camposmendez@ucr.ac.cr