## Slide 1
Andreea Radu (Mitu)
Nicoleta Florea, Florin Crisiacu, Denise Piatti, Mihaela Bacalum, Ion Burducea, Gheorghe Ciocan, Celina Damian, Cristina Gheorghiu, Decebal Iancu, Victor Leca, Paul Mereuta, Daniel Tofan, Adrian Toma
Horia Hulubei National Institute for Physics and Nuclear Engineering,
30 Reactorului Street, P.O. Box MG-6, Bucharest–Magurele, Romania
www.nipne.ro
Activity at the target laboratory of IFIN-HH

## Slide 2
Overview:
Improvement of already available fabrication techniques
Target preparation and characterization procedures
Sharing of knowledge - Basic Training School Euro-labs 2026

## Slide 3
Fully equipped target laboratory:
Target Preparation Laboratory
Methods for target preparation:
Physical Vapor Deposition Methods (PVD)
  resistive heating
  electron-beam gun evaporation
Mechanical reshaping and powder processing
  cold-rolling
  tablet pressing
Laser-based
  PLD (INFLPR)
Anodization – implemented in 2025
  Preparation of Ta218O5 - oxygen targets
High Energy Vibrational Powder Plating (HIVIPP) – in development
  Preparation of targets from isotopically enriched powdered material
N.M. Florea et. all, JRNC, 305, (2015)
A. Mitu et. all, EPJ Web of Conferences, 229, 03001, 2020
Elements featured in the nuclear targets

## Slide 4
  known isotopic composition, to allow for measurable yields
  Known stoichiometry, to allow for accurate beam energy loss calculations
  known thickness, to sustain high beam currents over extended periods of time
  nuclear reactions in inverse kinematics
  nuclear astrophysics studies
Development of the novel anodization set-up
A. Caciolli et al.” Eur. Phys. J. A, 48, 144 (2012)
Manufacturing of isotopically enriched oxygen (Ta218O5) targets for:
Requirements for oxygen solid targets imposed by experiment:

## Slide 5
Electrochemical process that electrolytically passivates the surface of different metals (Al, Ti, Mg, Zn, Ta, Zr, Hf, Nb), forming on its surface a very uniform and compact oxide layer.
This is typically done to:
  enhance durability,
  increase corrosion resistance
  improved surface hardness
  provides aesthetic options through a variety of colours
  offers better adhesion for paints and adhesives
  creates an electrically insulating surface.
In our case it will be used to
prepare isotopically enriched oxygen Ta218O5 targets
What is anodization? How it works?
Ta218O5 target
Mathias Kamp et al. / Energy Procedia 67 ( 2015 ) 70 – 75
H2SO4, H2CrO4, H3PO4, etc.
Al
Ti

## Slide 6
1. Cylindrical Teflon cavity (outer diameter 100 mm, inner diameter and height 25 mm) - defines the volume of the anodization cell were the electrolyte (H218O) is introduced (2-5ml), which can be recovered and reused for further target production
2. Cylindrical stainless-steel base
3. Tantalum disk to be anodized (the anode)
4. Gold filament (99.999%) with dia. 2 cm (cathode)
5. Water cooling system
6. Constant power supply with voltage (0-600V) and current (0 - 350 mA)
1
5
2
4
2
1
3
5
6
A. Caciolli et al.” Eur. Phys. J. A, 48, 144 (2012)
Eng. Florin Crisiacu
5
Setup
Denise Piatti

## Slide 7
Ta218O5 preparation and characterization
Target 1 - 200 V → green layer, ~ 345 nm, 25 oC , 2 mA ; Target 2 - 400 V → purple layer, ~ 699 nm, 25 oC , 2 mA; Target 3- 550 V → brown layer, ~ 994 nm, 25 oC , 2 mA.
The influence of the anodization voltage on the Ta218O5 oxide layer thickness:
SEM analyses
Different anodization phases:
200 V
400 V
100 V

## Slide 8
Preparation of Isotopically Enriched Oxygen Targets (Ta218O5) for Nuclear Reactions in Inverse Kinematics and Nuclear Astrophysics Studies
*Andreea Radu, *Nicoleta Florea, *Florin Crisiacu, Denise Piatti, Ion Burducea, Gheorghe Ciocan, Cristina Gheorghiu, Decebal Iancu, Victor Leca, Paul Mereuta, Daniel Tofan, Adrian Toma

## Slide 9
14N, 48Ca, 24Mg, 50Ti, 61Ni, 78Se, 100Mo, 108,114,116Cd, 115,117,119,120,124Sn, 128Te, 147Sm, 208Pb, 176Yb, 91Zr, InCl3
61Ni
108,114,116Cd
50Cr
100 Mo
12C
natB
Target preparation and characterization

## Slide 10
115,117,119,120Sn/Ta

## Slide 11
176 Yb
Element | Net Counts | Weight % | Weight % Error | Atom % | Atom % Error
C | 9745 | 5.98 | ± 0.07 | 43.64 | ± 1.05
O | 6407 | 1.76 | ± 0.07 | 9.65 | ± 0.81
Yb | 371011 | 92.26 | ± 0.42 | 46.71 | ± 0.43
Total |  | 100.00 |  | 100.00 | 
SEM/EDX

## Slide 12
50Ti
91Zr
Preparation of metallic 50Ti and 91Zr targets

## Slide 13
before
experiment
after
experiment
Preparation of 48Ca target

## Slide 14
• MgO enriched to 98.5%
• 24Mg pressed into a disc:
20 mm diameter,
0.75 mm thickness
422 mg mass
24Mg(n,n’)@n_TOF
high purity metal form of the isotope to be pressed
Experimental Setup
• “Spider” detector mount @ EAR 1 capture
position.
• Five Lanthanum-Bromide (LaBr3) detectors
• Three of 1.5x1.5” (diameter, depth)
• Two of 1.5x2”
• distance of 17 cm and 125 degrees
• Total campaign was ~10 days
• ~2 days for finalizing the configuration.
• ~6 days of stable beam time.
• ~2 days for 16O test.
24Mg(n,n’)@n_TOF
Cross section results

## Slide 15
¹²⁴Sn (n, 𝛄) reaction @ n_TOF EAR2
Experimental setup in EAR2 of n_TOF facility (CERN)
• ¹²⁴Sn enriched to 97.4 % (thin foils)
• ¹²⁴Sn targets pressed into disc shape with:
20 mm diameter
0.5 g, 1 g and 3 g masses
Preliminary results:
Neutron Capture resonances for ¹²⁴Sn nuclei

## Slide 16
Preparation of Plunger Cr targets
0.5 mg/cm2Cr on Au
Cr on Ag
Cr on Au
Good Cr target – used in the experiment
Cr deposited on Au at 350 0C, 2h
Cr deposited on Au at 350 0C, 3h
Cr deposition during heating the Ag substrate at 350 0C, 2h
50Cr target
Made by K.O.Zell
Natural Cr metallic pieces
50Cr metallic material (partially oxidised)

## Slide 17
Thickness determination methods
Quartz crystal monitor
Weighting method
Rutherford Backscattering Spectrometry (RBS)
Alpha transmission
Microstructure characterization
X-ray Diffraction (XRD)
Morphological characterization
Optical Microscopy (OM)
Atomic Force Microscopy (AFM)
Scanning Electron Microscopy (SEM)
Energy Dispersive X-ray Spectroscopy (EDX)
Target characterization

## Slide 18
Future Developments:
High Energy Vibrational Powder Plating (HIVIPP) set-up
Starting material: metal powder
Low amount of starting
material is needed
Efficiency >95%: material losses < 1mg
Two targets are deposited simultanously
The IFIN-HH HIVIPP set-up
designed by eng. F. Crisiacu
Schematic representation of the HIVIPP technique:
inspired by LARAMED group of INFN–LNL, Italy https://web.infn.it/LARAMED/hivipp/
Cisternino, S et al Upgrade of the HIVIPP Deposition Apparatus for Nuclear Physics Thin Targets Manufacturing. Instruments 2022, 6, 23
Cisternino, S. et al Cryomilling of Isotope-Enriched Ti Powders for HIVIPP Deposition to Manufacture Targets for Nuclear Cross Section Measurement. Materials 2023, 16, 3926
LARAMED group of INFN–LNL, Italy

## Slide 19
Sharing of knowledge

## Slide 20
Hands-on target preparation

## Slide 21
SEM/EDS
RBS
Characterization techniques

## Slide 22
Conclusions
In the Target Preparation Laboratory of IFIN-HH, the targets are prepared by:
      PVD, Cold Rolling, Tablet pressing, Anodization
The target characterization in terms of thickness, uniformity, purity, surface morphology and roughness achieved by:
      SEM/EDX, AFM, XRD, RBS
The combination of manufacturing processes and characterization techniques enables innovative target development methods.

## Slide 23
Thank you!