## Slide 1
Cyclotron solid target manufacturing techniques for medical radionuclide production:
R&D within LARAMED project at INFN-LNL
Sara Cisternino, Alisa Kotliarenko, Gaja Piteo, Gaia Pupillo, Liliana Mou, Lucia De Dominicis, Juan Esposito
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS
National Institute for Nuclear Physics – Legnaro National Laboratories (Italy)
18–19 May 2026
GSI Helmholtzzentrum für Schwerionenforschung, Darmstadt

## Slide 2
Sara Cisternino, 18/05/2026
Innovative radiopharmaceuticals for medical advancements…
Need for innovative
radiopharmaceuticals
useful for solving still open
clinical problems
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS

## Slide 3
…with emerging medical radionuclides
Longer half-life periods for immuno-PET
Multimodal Imaging PET/MRI
Theranostic pair  ‘matched pair’
89Zr
78.41 h
β+
52Mn
5.59 d
β+
43Sc
3.9 h
β+ 1.2
γ 373
44Sc
4 h
β+ 1.5
γ 1157
47Sc
3.35 h
β - 0.4, 0.6
γ 159
61Cu
3.3 h
β+
ε
64Cu
12.7 h
β+ 0.7 β- 0.6
γ 1364
67Cu
68.8 h
β - 0.4, 0.6
γ 1852, 93, 91
155Tb
5.3 d
ε
γ 87, 105, 180
e-
152Tb
17.5 h
ε
β+ 3.0, 2.6, 2.0
γ 344, 271, 586
149Tb
4.1 h
α 3.97, ε
β+ 1.4
γ 352, 165
161Tb
6.95 d
β- 0.5, 0.6
γ 26, 49, 75
e-
Kostelnik and Orvig, Chemical Reviews 2019
https://www.iaea.org/projects/crp/f22071
J.M. Pyles, et al., Applied Radiation and Isotopes, 2021
Radzina M. et al., EJNMMI Radiopharmacy and Chemistry, (2024)
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS

## Slide 4
INFN-LNL: LARAMED projects and network
SPES cyclotron at INFN-LNL
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS

## Slide 5
Cyclotron production cycle
Radioisotope of Interest
Dissolution
Extraction/
separation
Purification
Pure radioisotope
Radio-
pharmaceutical
preparation
Target activation
Target recovery
Target
preparation
Radiochemistry
process
Quality Control
Cyclotron irradiation
Nuclear physics studies
Contaminants
“The art of target preparation is a cross between chemistry, physics and technical as well as manual skills. “
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS

## Slide 6
Thin targets for nuclear XS studies
Magnetron Sputtering (MS)
Spark Plasma Sintering (SPS)
High Energy Vibrational Powder Plating (HIVIPP)
INFN-LNL R&D on target manufacturing techniques
Thick targets for production
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS

## Slide 7
Thin targets for nuclear XS studies
Magnetron Sputtering (MS)
Spark Plasma Sintering (SPS)
High Energy Vibrational Powder Plating (HIVIPP)
INFN-LNL R&D on target manufacturing techniques
High Energy Vibrational Powder Plating (HIVIPP)
Thick targets for production
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS

## Slide 8
Advantages
Starting material powder
Efficiency 95-98% no losses of material
Low amount of starting material is needed
Thickness: 0.1-20 µm
Two targets are deposited simultaneously
Process duration 10-40 h
Requirements:
Metal substrates
Metal powder (irregular shape and small size <20 µm)
This deposition technique exploits the phenomenon of vibrational motion of metallic powder in a static electric field
I. Sugai, Nuclear Instruments and Methods, 1997
High Energy Vibrational Powder Plating (HIVIPP)
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS
Typical experimental conditions:
Voltage 10-15 kV
Current < 80 µA
Time 10-40 h

## Slide 9
High Energy Vibrational Powder Plating (HIVIPP)
HIVIPP set up at LNL
- Vacuum system
Glove bag
High voltage power supply (PS)
Automatic control of PS
New sample holder
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS
H. Skliarova, S. Cisternino, et al., Nuclear Instruments and Methods A, 2020
S. Cisternino, et al., Instruments, 2022
S. Cisternino, et al., Materials, 2023
exps repeatibility
uniform deposition
recovery efficiency >95%

## Slide 10
…for nuclear cross-section measurements of the xxTi(p,x)47Sc / xxTi(d,x)47Sc reactions at energy 10-70 MeV
L. Mou, et al., EPJ Web Conf. 2024; G. Pupillo, et al., Radioanalytical and Nuclear Chemistry 2024;
L. D. Dominicis, et al., J. Phys.: Conf. Ser. 2023;
L. D. Dominicis, et al., Applied Radiation and Isotopes, 2025;
L. Canton et al., Applied Radiation and Isotopes, 2025
Irradiation at ARRONAX and Bern medical cyclotron facility
HIVIPP: xxTi targets…
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS
Cross-section SEM analysis
Ion Beam Analysis
Surface SEM analysis

## Slide 11
Thin targets for nuclear XS studies
Thick targets for production
Magnetron Sputtering
Spark Plasma Sintering (SPS)
High Energy Vibrational Powder Plating (HIVIPP)
INFN-LNL R&D on target manufacturing techniques
High Energy Vibrational Powder Plating (HIVIPP)
Magnetron Sputtering (MS)
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS

## Slide 12
Magnetron Sputtering (MS)
Advantages:
Deposition of metals or oxide
High adhesion to substrate
High-purity thin/thick film
H. Skliarova, S. Cisternino et al. Molecules 2019
Y
Nb
Main problem:
high losses of the material during deposition…
Physical vapor deposition technique: target atom extraction due to ionized inert gas bombarding the material
p+ beam
Heat power density
1 kW/cm2
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS
INFN Patent
WO 2019/053570

## Slide 13
Magnetron Sputtering (MS)
Material-saving approach of sputtering technique
magneTron sputtering cyclOtron TargEt Manufacturing
In collaboration with
New MS configuration to reduce the
target loss
ZnO
A. Kotliarenko et al., Applied Science, 2021
A. Kotliarenko et al., Materials, 2023
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS

## Slide 14
Thin targets for nuclear XS studies
Thick targets for production
Magnetron Sputtering
Spark Plasma Sintering (SPS)
High Energy Vibrational Powder Plating (HIVIPP)
INFN-LNL R&D on target manufacturing techniques
High Energy Vibrational Powder Plating (HIVIPP)
Magnetron Sputtering (MS)
Spark Plasma Sintering (SPS)
INFN-LNL first group to propose this technique for solid targets manufacturing for medical radionuclide production
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS

## Slide 15
Spark Plasma Sintering (SPS)
Hu et., Materials & Design, 2020
Kelly and Graeve, The Minerals, Metals & Materials Society, 2014
Masao Tokita, Ceramics, 2021
fast and versatile technique used for several applications in different fields
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS

## Slide 16
Spark Plasma Sintering (SPS)
Sintering by simultaneous application of uniaxial force and DC or AC current
Typical experimental conditions:
Voltage 5-10 V
Current intensity 103-104 A
Pressure 5-100 MPa
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS

## Slide 17
Spark Plasma Sintering (SPS)
Sintering by simultaneous application of uniaxial force and DC or AC current
Typical experimental conditions:
Voltage 5-10 V
Current intensity 103-104 A
Pressure 5-100 MPa
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS

## Slide 18
Spark Plasma Sintering (SPS)
Sintering by simultaneous application of uniaxial force and DC or AC current
Different kind of materials can be processed
High energy efficiency
Easy operation
Typical experimental conditions:
Voltage 5-10 V
Current intensity 103-104 A
Pressure 5-100 MPa
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS

## Slide 19
Spark Plasma Sintering (SPS)
What’s happening:
Micro-spark discharge in the gap between neighboring powder particles.
Three stages:
Plasma heating
Electrical discharge between particles causes localized and momentary heating of particles to high temperatures
The particle surface is purified due to evaporation of impurities due to high localized temperatures
The purified surface layers fuse to each other forming necks.
     The material becomes softer due to heating and neck growth and applied pressure causes plastic deformation
     Plastic flow and faster diffusion result 100% densification.
Joule heating
     The current flows from particle to particle through the necks and results Joules heating.
     The joule heat results enhanced diffusion and neck growth.
    Plastic deformation
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS

## Slide 20
Spark Plasma Sintering (SPS)
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS
Components:
water-cooled vacuum chamber
vacuum system
vertical single-axis hydraulic press
specially designed water-cooled punch electrodes
AC generator
temperature and other sensors
PLC controlling all the sintering parameters
custom graphite punches and die
Lab-scale SPS machine tailored for target manufacturing
Very fast process cycle
Customizable tooling
Easy to use and maintain
Affordability
Vacuum chamber
Collaboration with
prof. U. Anselmi-Tamburini,
S. Bortolussi and
V. Vercesi
fits the requirements for a suitable solid target
desired target material density
negligible material losses
Can be applied to different materials
SPS advantages

## Slide 21
Spark Plasma Sintering (SPS) targets so far…
Y targets for 89Zr
52Cr targets for 52Mn
xxZnO targets for 6xCu
155Gd2O3 targets for 155Tb
Tb2O3 targets
for 155Tb
(indirect production)
Heat power
density 1 kW/cm2 during irradiation
G. Sciacca et al., Molecules 2021
Cisternino et al., Nuclear Medicine and Biology, 2022
F. Porto et al., EJNMMI Radiopharmacy and Chemistry 2024
Cisternino et al., Ceramics International, 2025
Piteo et al., Ceramics International, 2026
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS

## Slide 22
Spark Plasma Sintering (SPS) targets so far…
Y targets for 89Zr
xxZnO targets for 6xCu
155Gd2O3 targets for 155Tb
Tb2O3 targets
for 155Tb
(indirect production)
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS

## Slide 23
Cryomilling
Material preparation process
Material recovery - Powder synthesis
After milling
Original powder
Cryomill
Reduction of the powder size through the milling at liquid nitrogen temperature to avoid melting
Liquid nitrogen is not in contact with the material of interest to avoid contamination
Small jar to reduce/avoid the contamination from the jar and sphere materials
Recovery of enriched Zn material after irradiation and dissolution for the extraction of radionuclide of interest
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS

## Slide 24
Material characterization
Accurate sample preparation based on the material to analyse
Scanning Electron Microscope (SEM)
Energy Dispersive X-ray Spectrometry (EDS)
X-ray diffraction (XRD)
Rutherford Backscattering Spectrometry or Elastic Backscattering Spectrometry (EBS)
Metallurgical interface analysis at DII University of Padova
examples
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS

## Slide 25
Target manufacturing techniques for medical RI production available at LNL
Magnetron Sputtering
Spark Plasma Sintering
High Energy Vibrational Powder Plating
Completion of radiochemistry and target laboratories layout definition and acquisition of furniture
R&D on the realization of different size and configurations for high power target station
Conclusions and perspectives
Sara Cisternino, 18/05/2026
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS
Material preparation and characterization

## Slide 26
Thank you for the attention!
sara.cisternino@lnl.infn.it
https://web.infn.it/LARAMED/
Which is the best target manufacturing technique?
It is a critical technological challenge!
Second Meeting on “Targets for Nuclear Physics” within EURO-LABS

## Slide 27
Additional slides

## Slide 28
Solid targets for medical application: requirements and design
Target material to be irradiated
Often isotopically enriched material
very expensive how is it provided?(powder, crystal bar, foils..)
For production
For nuclear cross section
based on nuclear physics reaction for the production of the specific RN
Usually >150 µm
to exploit the optimal energy range to maximize production
1-10 µm (100s µg/cm2)
The information on the exact amount is mandatory
easily handled for safe radiochemistry process in hot-cell
easily handled for safety during the dismount after the irradiation
Selected backing material
Chemical inertness
High thermal conductivity
Mechanical strenght
Low activation under the beam
Material used as monitor foil (e.g., Al foil 25 µm thick)
Target system
thermo-mechanical strenght to withstand the thermal power deposited during the irradiation
Ø and thickness based on the cyclotron target station
Optimal thickness

## Slide 29
Chart: Time [min]
Target production by SPS: ZnO pellet on backing
Chart: Time [min]
Chart: Time [min]
Pellet sintering and
Au adhesion
Backing preparation:
Au-Nb
Target:
ZnO-Au/Au-Nb
3 steps for target preparation total time 130 min
Sintering of 3 pellets simultaneously (in series) with Au foil adhesion
TOP
CENTRAL
BOTTOM
Cross-section view
The densities and the microstructure are compared to the one-pellet-sintered
The density measured by weight and size is comparable to the density measured by Archimede’s method

## Slide 30
Efficiency of the HIVIPP technique
Total no. of HIVIPP depositions = 20
49Ti and 50Ti powder (cryomilled powder size <10 µm)
HIVIPP parameters: 10-12 kV, 10-15 h
#targets = 40  Mass thickness = 552.9±120.1 µg/cm2
powder recovered
powder deposited
powder lost
For each exp.
Starting material was 19.5 mg (100%)
Succesfully reused it!
Chart: 
| % recovered | % deposited | % losses
 | 86.0146 | 8.6797 | 5.3057
8.7±2.4%
5.3±3.0%
86.0±5.3%

## Slide 31
Design of a dissolution system
Prototype by G. Cicoria
G. Sciacca et al. Molecules 2021
System installed on commercial modules
at Sacro Cuore Don Calabria Hospital (since 2022)

## Slide 32
Spark Plasma Sintering (SPS)
155Gd target for 155Tb production
natGd2O3 MICRO powder, Alfa Aesar
155Gd2O3 ISOFLEX
90.2%
SPS parameters optimization with natGd2O3
micro powder
N of EXP | Starting mass [mg] | Results |  |  |  | 
N of EXP | Mass [mg] | Mass Gd2O3 after [mg] | mass lost [mg] | Thickness Gd2O3 [µm] – [mg/cm2] | density [g/cm3] | %bulk density
(n=5) | 174.6±4.4 | 168.8±3.2 | 5.8±4.1 | 333.8±20.8 µm 214.9±4.0 mg/cm2 | 6.5±0.5 | 87.2±6.3
(n=6) | 116.8±1.3 | 115.8±3.6 | 2.0±1.0 | 266.0±11.4 µm 147.5±4.6 mg/cm2 | 5.5±0.3 | 75.0±3.9
(n=13) | 86.2±2.0 | 84.3±2.2 | 2.1±0.9 | 217.5±25.2- 107.4±2.8 | 5.0±0.5 | 67.3±6.7
Optimal thickness from theoretical evaluation
and nuclear cross section measurements
Sintering and simultaneous adhesion to metal foil for mechanical stability Pt

## Slide 33
Spark Plasma Sintering (SPS)
155Gd target for 155Tb production
Preparation of Pt-Nb backings
Sintering of the pellet with Pt foil
Cleaning pellet in UB
Signing the Pt-Nb with target number
Adhesion Gd2O3-Pt with Pt-Nb
Coin-shaped target manufacturing
Irradiation
HCl 6 M, 80°C /
HNO3 7M, 80°C, N2 flux
Separation/purification
C. Favaretto et al., EJNMMI radiopharm. chem., 2021
Dissolution
Target material recovery
Metallurgical cross-section analysis

## Slide 34
Spark Plasma Sintering (SPS)
70Zn target for 67Cu production
#4 irradiations 15-25-35-50 µA; 19 MeV; 5 min
Irradiation
Separation
Dissolution
1.8 ml 6 M HCl, 80 °C
Labelling
natZnO target
Yield 99%
61Cu
Cisternino et al., Ceramics International, 2025
Target material recovery
natZnO material was succesfully tested
70ZnO
December 2025
2026 first pre-clinical test with novel radiopharmaceutical (in collaboration with IOV)

## Slide 35
Starting materials powder or foil
97% efficiency No loss of isotope-enriched material
Directly bonding of different materials (target and backing)
  protective thin layer in between instead of costly inert material backings
150 m - mm thickness pellet targets for production
Sintering of high melting point materials (metal or oxide)
Spark Plasma Sintering (SPS)
Advantages:
Considerations:
Need to know the powder shape to optimize the parameters with the most similar natural powder  cryomilling process can be implemented
Tailored recovery process to obtain the same starting material (metal or oxide) is necessary when working with isotopically enriched materials
Sara Cisternino – University of Wisconsin, Madison, USA – 16/09/2025

## Slide 36
Conclusions: LNL target technologies to produce radiometals
High Energy Vibrational Powder Plating (HIVIPP) for xs measurement targets
HIVIPP advantages:
Starting material: metal powder
Low amount of starting material is needed
Two targets are deposited simultanously
Skliarova et al., NIMA 2020; Cisternino et al., Instruments 2022; Cisternino et al., Materials 2023
Magnetron sputtering (MS) for thin and thick targets
MS advantages:
Deposition onto any support material
Excellent adhesion on substrate
High thickness range (0.1 µm – 1 mm)
High deposition uniformity
INFN patent WO/2019/053570, 2019; Skliarova et al., Instruments 2019;
Skliarova Molecules 2019; Kotliarenko et al., Materials 2023
SPS advantages:
High Tm material sintering
Starting materials: powder or foils
Adhesion of different materials
Skliarova et al., J. Phys.: Conf. Ser., 2020; Sciacca et al., Molecules 2021; Cisternino et al., NMB 2022; Cisternino et al., Ceramics International, 2025
Spark Plasma Sintering (SPS) for thick target >300 µm

## Slide 37
X5 TIMES
250 mg ZnO + 1.8 mL HCl 6M + 1 mL H2O milliQ
POWDER DISSOLUTION
EVAPORATION:
ZnCl2 salt remains
DILUTION IN 25 mL di HCl 0.005M
(to simulate WASTE 1):
ICE BATH
T= 0°C
ADDING NaOH 5M drop by drop to reach pH about 12:
Test with 1.2-1.3 mL
Test with 1.4-1.5 mL
CENTRIFUGATION (15 min, 4000 rpm)
Zn(OH)2 precipitate accumulates on the bottom of the falcon, the supernatant is discarded. The precipitate is washed with milliQ water to eliminate residual chlorides (chloride assay) and re-centrifugated.
TRANSFER IN A UN CRYSTALLISER  STOVE 150°C 1h  MUFFLE 300°C, 3h
MILLING IN A MORTAR
Precipitation with sodium hydroxide at 0°C with different amount of NaOH (1.2-1.5 mL)

## Slide 38
Spark Plasma Sintering (SPS)
Other application in Pavia University
I. Barisic et al., Applied materials today, 2024