## Slide 1
Activity for the nuclear target development within NUMEN
Daniela Calvo – INFN Torino
on behalf of
M. Campostrini, M. Cavallaro, A. Comite, P. De Remigis, M. Giovannini, A. Massara, F. Morello, F. Picollo, B. Reshma, V. Rigato, O. Sgouros, V. Soukeras, S. Sturari

## Slide 2
Institutions

## Slide 3
Outline
Motivations for the study of new substrates for target deposition
Commercial C-material foils
First custom C-material foils
Preliminary results from measurements of radiation damage

## Slide 4
Activity for nuclear targets
The activity finds its motivation in the study of targets for the NUMEN experiment
  Target of isotopes candidates for 0nbb decays
  20Ne and 18O ion beams with 15-60 MeV/u energy and up to 1013 pps
      → more than 105 W/cm3 power density in the target
      → high thermal stress

## Slide 5
Custom solution for the target
The thermal stress of the target is addressed with a highly thermally conductive substrate that dissipates heat toward a heat sink.
The isotope is evaporated on the substrate by e-beam evaporation or thermal evaporation
Highly Oriented Pyrolytic Graphite (HOPG) and Multilayer Graphene (MLG) featuring higher thermal conductivity (k//=1500-1900 Wm-1K-1), produced in mm-thick foils, are good candidates
Ion beam
Target element
Substrate
Heat sink

## Slide 6
Commercial C-material foils

## Slide 7
Commercial Carbon foils
HOPG – Optigraph
MLG - Kaneka
MLG – ACF/Nanotech
CVD + HT HP annealing
Pyrolysis of polyimide film
GO and rGO
Material | Calculated density [g/cm3 ] | Purity degree /cristallinity | Thickness [mm] | Thermal diffusivity [mm2/s] | Thermal conductivity [W/(m · K)] | Thickness uniformity by APT (@LNS)
HOPG | 2.265 | 99.9 %/HO | 2 | 1550 | 2.3 | poor
MLG - K | 2.272 | 99 %/HO | 1.6 | 1200 | 2.0 (l.) | good
MLG - A | 2.02 | Fair | 1-3 | 1308 | 1.93 (l.) | good
Thermal conductivity measurements till now FAILED!
Only HOPG was measured with the laser flash method

## Slide 8
Commercial Carbon foils
HOPG – Optigraph
MLG - Kaneka
MLG – ACF/Nanotech
Material | Measured Electrical Conductivity [S/m] | Literature value [S/m]
HOPG | 3.05 · 106 | 2.10 ·106
MLG - Kaneka | 2.12 · 104 | 1.00 ·103 to 1.00·104
MLG - ACF | 2.03 ·106 | 1.00 ·106

## Slide 9
Custom C-material foils

## Slide 10
Custom MLG foil production
Filtration of graphene dispersion
Carbonization followed by graphitization of polyimide film (Kapton)
Reduction of graphene oxide (GO) to reduced graphene oxide rGO

## Slide 11
MLG foil production by filtration
Filters: Nylon Polytetrafluoroethylene-PTFE, Mixed cellulose ester -MCE, Polypropylene-PP
Sonicator
Sonicator
E-graphene dispersion
Concentration 2-3 mg/ml
10 mins
Known volume (Vd) of dispersion diluted with water
few mins
Filtration
Procedure
reshma.babu@edu.unige.it
Foils separated from filters
either by peeling off
or by pyrolysis at different temperatures (up to 700 °C)
20 x 20 mm2

## Slide 12
Custom vs Commercial foils – XRD analysis
(002)
(004)
A post-annealing treatment of 700 °C for just 10 minutes improves cristallinity

## Slide 13
Custom vs Commercial foils – Raman analysis
D peak
MLG Genova
MLG Kaneka
G peak
MLG Nanotech

## Slide 14
Custom vs Commercial foils – EBS analysis
EBS of a sample without annealing at 700°C
MLG Kaneka
MLG Genova
MLG Genova
EBS of a sample with annealing at 700°C
The non-uniformity of MLG Genova
doubles compared to MLG Kaneka

## Slide 15
Preliminary results from measurements
of radiation damage

## Slide 16
Irradiated samples @ GANIL
HOPG
Pre-irradiation
HOPG
Post-irradiation
ID/IG  0.23
MLG Kaneka
Post-irradiation
ID/IG  0.31
MLG Kaneka
Post-irradiation
Irradiation with 20Ne9+ beam, 14 MeV/u
Each sample is inside a target holder at room temperature
HOPG, 140 min. with a 245 enA beam current
MLG Kaneka 2, 135 min. with a  245 enA beam current
MLG Kaneka 1, 120 min. with a  125 enA beam current
Thanks to Henning Lebius for the continuous support at GANIL

## Slide 17
Irradiated sample @ GANIL
Irradiation with 20Ne9+ beam, 14 MeV/u
Sample inside a target holder kept at cryogenic temperature
MLG Kaneka, 27 hours with a  200 enA beam current
Thanks to Henning Lebius for the continuous support at GANIL
MLG Kaneka
Not-irradiated area
MLG Kaneka
Irradiated area
ID/IG  0.75

## Slide 18
Irradiated sample @ CERN
Irradiation with a 24 GeV/c proton beam ( 7.5 · 1011 p/spill)
Fluence: 2.4 · 1015 p/cm2
Sample inside a target holder at room temperature
HOPG
Post-irradiation

## Slide 19
Conclusion and Future work
The first samples produced in Genova are encouraging
Post-annealing treatment of MLG Genova improves crystallinity
Production of new samples with a longer post-annealing
Applying pressure during the synthesis
The peak D was measured in the ion-irradiated samples
The peak D was not measured in the proton-irradiated sample
Correlation between the induced defects and the thermal conductivity
Solve the problem of measuring the thermal conductivity!

## Slide 20
SPARES

## Slide 21
RBS of MLG Kaneka
Se target
MLG

## Slide 22
Temperature of heated samples
Chart: Temperature [°C] Optical Power [W * 10 2]
| PANASONIC | OPTIGRAPH | KANEKA | NANOTECH
Optical Power [W *100] | 720 | 760 | 750 | 760
Temperature [°C] | 38 | 263 | 152 | 940
PGS- PANASONIC ~1700 W/(m·K)
HOPG-OPTIGRAPH ~1900 W/(m·K)
MLG-KANEKA ~1800 W/(m·K)
MLG-NANOTECH(ACF) ~1500-1900 W/(m·K)
Graphyte PANASONIC: 10 mm thick
HOPG OPTIGRAPH: 2 mm thick
MLG KANEKA: 1.5 mm thin
MLG NANOTECH, MLG ACF: 1.5 mm thin
ACF

## Slide 23
Cooled samples
Se +MLG-KANEKA
MLG-KANEKA (n. 4)
MLG-KANEKA
Pyrolytic graphite-
PANASONIC
Pyrolytic graphite-
PANASONIC
Target holder-
copper
Target holder-
copper
Se

## Slide 24
Samples at room temperature
MLG-KANEKA (n. 3)
MLG-KANEKA (n. 2)
HOPG (n. 1)
MLG-KANEKA or HOPG
Target holder-
aluminum

## Slide 25
Experimental setup installed at GANIL