## Slide 2: Radiation hardness of CVD diamond detectors efficiency, defects and annealing
Robin Molle
Robin Molle – robin.molle@diamfab.com – GdR Di2i 2026

## Slide 3
Study of detector behavior in extreme conditions
Spatial
High Energy Physics
Medical applications
Why Radiation Tolerance ?
Notes: Why radiation tolerance ? (clic)
Multiple fields where radations are important to take into account or even are the targetted physics : spatial, high energy physics, or medical applications. I participate to a detector development for beam monitoring, particularly for high flux of light ions for radiation therapy (clic). In conventinal radiotherapy, X rays are used. They irradiate healthy tissues before and after targetted tissues, the tumor. Light ions got a peaked dose deposition that helps to not preserve healthy tissues.

## Slide 4: DIAMMONI detector
DIAMMONI detector : a radiation detector for light ion beams at high flux and fluences (40 250 MeV)
Particle energy : 70 MeV (H-D-He)
Beam intensity
ARRONAX cyclotron :
ARRONAX AX casemate
ARRONAX beam
prototype for ARRONAX cyclotron
Beam structure :
Train duration : 50µs (« dt »)
Bunch duration : 4ns ON, ~29ns OFF
Robin Molle – robin.molle@diamfab.com – GdR Di2i 2026

## Slide 5: diamond among other semiconductors
Diamond (C)
Cost, production
Small area
Radiation hard, low Z,
High breakdown field, Fast
Germanium (Ge)
Need to be cooled down
Compactness
Excellent energy resolution
Large volume
Silicon Carbide (SiC)
Mechanical fragility
High Breakdown Field
Cost
Silicon (Si)
Low breakdown field
Low radiation hardness
Easy to produce,
Cost, knowledge

## Slide 6: Solid State ionizing Chamber
Robin Molle – robin.molle@diamfab.com – GdR Di2i 2026
Diamond
+
+
-
Readout electronic
Ionizing particle
Ramo, S. (1939). Currents induced by electron motion. Proceedings of the IRE, 27(9), 584-585.
Shockley, W. (1938). Currents to conductors induced by a moving point charge. Journal of applied physics, 9(10), 635-636.
Charge collection efficiency:

## Slide 7: Fluence measurements
Robin Molle – robin.molle@diamfab.com – GdR Di2i 2026
Charge collection efficiency:
Empirical model as a function of fluence
k: damage constant
d: thickness
: fluence
1st method:
Bäni, L., Alexopoulos, A., Artuso, M., Bachmair, F., Bartosik, M., Beck, H., ... & RD42 Collaboration. (2019). A study of the radiation tolerance of poly-crystalline and single-crystalline CVD diamond to 800 MeV and 24 GeV protons. Journal of Physics D: Applied Physics, 52(46), 465103.
Measure the k of diamond under ions
Irradiation
CCE measurement
CCE
2nd method :
Irradiation & CCE measurement
CCE calculated for each train
Fluence relate to the history of the device
(particle/cm²)

## Slide 8: Fluence experiments
Single crystal CVD Diamond
sCVD – 550µm thick
Single crystal CVD Diamonds
1 diamond cut in 4
150 µm thick
Helium
64 MeV
Proton
68 MeV
Spectroscopie alpha
XBIC - ESRF
Raman-PL
Annealing
Robin Molle – robin.molle@diamfab.com – GdR Di2i 2026
Polycristalline CVD Diamond
300 µm thick
Single crystal CVD Diamond
550 µm thick
Proton
68 MeV
Proton
68 MeV

## Slide 9: Experimental setup
68 MeV proton range in diamond :
Robin Molle – robin.molle@diamfab.com – GdR Di2i 2026
Experimental setup for 68 MeV H+
Irradiation of the whole diamond surface
Homogeneous irradiation
No scattering

## Slide 10: Diamond response to proton fluence
Robin Molle – robin.molle@diamfab.com – GdR Di2i 2026
M1 = control sample
Frenkel defects created with irradiation
Vacancies trap charge carriers

## Slide 11: Diamond response to proton fluence
Robin Molle – robin.molle@diamfab.com – GdR Di2i 2026
Electron and hole are not equivalent with irradiation
Annealing = increase of CCE

## Slide 12: Diamond response to proton fluence
Robin Molle – robin.molle@diamfab.com – GdR Di2i 2026
H19 creation : annealing
Vacancies = GR1
GR1 = vacancies : Raman sensivity > 2e14 vac./cm²
No NV centers created

## Slide 13: Model of CCE with fluence
Initial overall crystal quality
Trap filling
Heterogeneity of point defect distribution
Accumulation of irradiation-induced defects
Robin Molle – robin.molle@diamfab.com – Réseau Semi-conducteur 2026

## Slide 14: To be published
Diamond and Related Materials

## Slide 15
And now ?
  Start-up created in 2019
Based on more than 30 years of
R&D developed at Intstitut Néel- CNRS
+ 8 patents and know-how
  26 People
+ 5 advisors
Power electronics
Quantum application
Hardened electronics (space, nuclear and high temperature)
  Business targeted
Substrate
High Value-added Diamond Wafer
Diamond Electronic Devices
Diamfab unique know-how :
EPITAXY, DOPING, DEVICE DESIGN & PrOCESSING
GrenOBLE
FRANCE
IF you want to work with us, don’t hesitate to contact me !
robin.molle@diamfab.com
Robin Molle
Notes: So, at Diamfab we fabricate diamond.
Our solution is based on a technology developed for more than 30 years at CNRS Grenoble and protected with 8 patents and secrets know-how.
Today, Diamfab is 26 people and 5 world recognised advisors
We target power electronics and hardened electronics market as well as quantum market
Our unique know-how is to grow electronic grade doped diamond as a semiconductor on a diamond substrate and our expertise is to design and process devices.
Therefore, we have a dual model model allowing us to offer either High value-added wafer solution or bare die devices solution

## Slide 16: Thank you for your attention

## Slide 17: Back-Up

## Slide 18: Diamond response to Helium fluence
Robin Molle – robin.molle@diamfab.com – GdR Di2i 2026
18
XBIC map
Frenkel defects
Vacancies  NV centers
Annealing: 6h / 1000°C
64 MeV helium
irradiation
XBIC map
XBIC map

## Slide 19: Diamond response to Helium fluence
Robin Molle – robin.molle@diamfab.com – GdR Di2i 2026
19
Annealing = increase of CCE
Frenkel defects created with irradiation
Electron and hole are not equivalent with irradiation
Vacancies (GR1 centers) trap charge carriers
GR1 converted with annealing in NV centers
After irradiation
Before annealing
After irradiation
After annealing