## Slide 1
Study of the influence of radiolysis of an aqueous solution at the interface with 316L stainless-steel
Brice Lathuilière
Under the supervision of N. Moncoffre and N. Bérerd, within the MATiCE group

## Slide 2
General context
Pressurized water reactor (PWR) in France
Aging of reactor vessel steels

## Slide 3
General context
Lectures by Jean-Luc Béchade, Emir&A thematic school, 02/2025
Assemblies
reactor vessel
Reactor internals
Nitrited stainless steel 316L
The control rod cladding is made of 316L stainless steel

## Slide 4
Water radiolysis
S. Le Caër, Water, 3 (2011), 235
Stable and metastable products
Short-life products
Radiolysis Products Time µs

## Slide 5
Water radiolysis
S. Le Caër, Water, 3 (2011), 235
Reducing species
Oxidizing species
Electrochemical methods
How can the impact of these redox species be measured?
Radiolytic yields depend on the energy deposited in water

## Slide 6
Material Study: 316L Stainless Steel
Chromium (III) oxide layer - very dense
1
Iron hydroxide layer (low density)
2
G. Okamoto, Corrosion science 13 (1973), 471
Degradation of the film
Irradiation
Passive film
Passive layer (duplex oxide)  2-5 nm
Bound water
Metal
2
1
Amorphous structure Slows down oxidizing species and metal cations diffusion
Bound water oxidizing radicals directly within the passive film
Electrolyte

## Slide 7
Objective of the thesis
How to study passive film under extreme conditions?
How does the steel/solution interface evolve at the nanometric scale under extreme conditions?
Experimentally simulate irradiation at interfaces
Characterization and description of the passive film
Physicochemical characterization:
Film composition: Ion beam analysis (IBA)
Chemical speciation: X-ray photoelectron spectroscopy (XPS)
Thickness: XPS, ellipsometry and IBA
Two transportable irradiation devices:
Parameters: Dose deposited at the interface
Variation of the beam energy
Variation of the irradiation time
Experimentally simulate irradiation at interfaces
Electrochemical measurement:
Modeling of the passive film
Thickness, capacitance, resistivity profiles, passivity domain, and corrosion potential

## Slide 8
Extreme conditions simulation:
electrochemical cells
PATRICIA
Study of the effect of irradiation on the sample and radiolysis products
H+
Sample
Solution
45 mm
PhD thesis of Philippe Martinet (2021)
A. Eynard
R. Fillol

## Slide 9
RADEAU
Allows selection of whether to irradiate the interface or not: study of the diffusion of radiolytic species
H+
Sample
Solution
5,7 mm
Extreme conditions simulation:
electrochemical cells
A. Eynard
R. Fillol

## Slide 10
Objective of the thesis
How to study passive film under extreme conditions?
How does the steel/solution interface evolve at the nanometric scale under extreme conditions?
Experimentally simulate irradiation at interfaces
Characterization and description of the passive film
Physicochemical characterization:
Film composition: Ion beam analysis (IBA)
Chemical speciation: X-ray photoelectron spectroscopy (XPS)
Thickness: XPS, ellipsometry and IBA
Electrochemical measurement:
Modeling of the passive film
Thickness, capacitance, resistivity profiles, passivity domain, and corrosion potential
Two transportable irradiation devices:
Parameters: Dose deposited at the interface
Variation of the beam energy
Variation of the irradiation time

## Slide 11
Two variables: the electrochemical potential and the current density
Lectures by V. Vivier, SIEDERAL thematic school, 09/2024
Platinum electrode
316L stainless steel
Mercurous sulfate electrode (MSE)
Na₂SO₄ 0.02 M
In situ measurements of the evolution of the passive film
Passive film study:
electrochemical setup

## Slide 12
  Electrochemical potential measurement Ei:
  - Linked to free enthalpy rG  thermodynamic parameter
  - Related to the activities of chemical species ai (Nernst law)
  Measurement of current density ( j ):
  - Related to the kinetic of electrochemical transformations
  E(O/R) = E°(O/R) + ln
  R.T
  n.F
  aOx 1.aOx2…
  aRed1.aRed2…
  E°(O/R): standard potential of the reaction
  R: ideal gas constant
  T: temperature
  F: Faraday constant
  n: number of moles of electrons exchanged
  j = n.F.(ka.[Red]el – kc.[Ox]el)
  ka: rate constant of the oxidation reaction
  kc: rate constant of the reduction reaction
  [Red]el: concentration of the reducing agent at the electrode surface
  [Ox]el: concentration of the oxidizing agent at the electrode surface
  Example of a half electrochemical reaction:
  Ox + n.e-  Red
Reaction rate at the interface
Spontaneous direction of the electrochemical reaction
Thermodynamic and kinetic interpretation
of electrochemical measurements

## Slide 13
2
1
Steady state (kinetic equilibrium)
Radiolysis products (stable)
Thermodynamic equilibrium
Time (s)
Radiolysis products influence the system equilibrium
Potential (V vs MSE)
Effect of irradiation on the system’s equilibrium state as measured by the open-circuit potential
B. Normand, N. Bérerd et al., Corrosion Science 176 (2020) 108945
Radiolysis products (short-life + stable)
Notes: Le plateau 3 peut s’explique par la présence en solution de produits de recombinaisons des radicaux, tel que H2O2.
En effet, plus la concentration d’une espèce oxydante est élevée comparativement aux autres, plus elle impose son propre potentiel standard.

## Slide 14
How to characterize the 316L stainless
steel/electrolyte system? : Polarisation curve
2
3
1
4
  2 Cr3+ + 3 H2O  Cr2O3 (s) + 6 H+
  Cr2O3 (s) + 4 H2O  Cr2O72-(aq)+ 8 H+ + 6 e-
  Water reduction
  2 H2O + 2 e-  2 OH- + H2
  Water oxidation
  2 H2O  O2 + 4 H+ + 4 e-
  Corrosion protection
  Cr  Cr3+ + 3 e-
1
4
3
Passive domain
What is the impact of irradiation on our system (stainless steel / aqueous solution)?
Ecor = -0,84 V
2
Dissolution in solution

## Slide 15
Nyquist
Bode magnitude and Bode phase
Different models
Lectures by V. Vivier, SIEDERAL thematic school, 09/2024
In situ nanometric-scale characterization of the passive layer
Evolution of the passive layer properties and interfacial charge-transfer kinetics using electrochemical impedance spectroscopy
Modeling of the film using a non-ideal capacitor  CPE

## Slide 16
Bode plots before, during, and after irradiation: Patricia cell
Irradiation: Cyclotron at CEMHTI Orléans
Electrolyte
Steel
H+, 16 MeV
Metal interface Corrosion Diffusion
Passive film <90° film no
ideal CPE
Which properties of the passive film can be inferred from the diagram?

## Slide 17
Determination of passive film properties
Irradiation: Cyclotron at CEMHTI Orléans
Under irradiation, the passive film becomes thicker while offering more reliable corrosion protection
Adimensionnal thickness ()
Adimensionnal thickness
ρ / Ω cm
ρ / Ω cm
Before irradiation
Under irradiation
After irradiation
Irradiation conditions | Re (Ω.cm²) | C (F.cm-²) | e (nm)
Before | 217 ± 3 | (2,4 ± 0,2)e-6 | 4,4 ± 0,4
Under | 247 ± 4 | (1,2 ± 0,4)e-6 | 8 ± 3
After | 244 ± 3 | (4,2 ± 0,3)e-6 | 2,5 ± 0,2
Power-law model for the resistivity profile of the passive film
=0

## Slide 18
Energy deposited at the interface alters the properties of the passive film and influences the governing processes at low frequencies
16 MeV
20 MeV
30 MeV
Evolution of the bode diagram with
incident proton energy
Parameters: Dose deposited at the interface
Variation of the beam energy

## Slide 19
Influence of the deposited dose at the interface: as the dose increases, the chromium oxide layer becomes less protective against corrosion
Evolution of the resistivity profile with
incident proton energy
ρ / Ω cm
Adimensionnal thickness
ρ / Ω cm
LET at the interface: 11 keV/µm
LET at the interface: 22 keV/µm
LET at the interface: 44 keV/µm
Parameters: Dose deposited at the interface
Variation of the beam energy
Adimensionnal thickness ()
=0

## Slide 20
Passive domain
Under irradiation, the corrosion potential is located in the passive domain, with an increase in current density
Entrance window
Stability of the passive film as a function
of incident proton energy
Parameters: Dose deposited at the interface
Variation of the beam energy

## Slide 21
Irradiation energy alters the passive film/electrolyte interface and affects the governing processes at low frequencies
Preliminary results
Evolution of the bode diagram with
incident proton energy
Entrance window
Parameters: Dose deposited at the interface
Variation of the beam energy

## Slide 22
Objective of the thesis
How to study passive film under extreme conditions?
How does the steel/solution interface evolve at the nanometric scale under extreme conditions?
Experimentally simulate irradiation at interfaces
Characterization and description of the passive film
Physicochemical characterization:
Film composition: Ion beam analysis (IBA)
Chemical speciation: X-ray photoelectron spectroscopy (XPS)
Thickness: XPS, ellipsometry and IBA
Electrochemical measurement:
Modeling of the passive film
Thickness, capacitance, resistivity profiles, passivity domain, and corrosion potential
Two transportable irradiation devices:
Parameters: Dose deposited at the interface
Variation of the beam energy
Variation of the irradiation time

## Slide 23
Chemical speciation of elements
in the passive film
X-ray photoelectron spectroscopy
Almost no influence of irradiation dose on element chemical speciation
Parameters: Dose deposited at the interface
Variation of the irradiation time

## Slide 24
Hydrogen profile of the passive film
1H(15N, αγ)12C
Slight influence of irradiation dose on hydrogen concentration
15N + p  16O *  12C * + α
12C + γ

γ = 4,43 MeV
Parameters: Dose deposited at the interface
Variation of the irradiation time
Nuclear Resonant Reaction
Hydrogen profile
Resonance E (MeV) | 6,385
Width Γ (keV) | 1,8
Cross section σr ​ (mbarn) | 1650
Hydrogen analysis

## Slide 25
Conclusion and perspectives
Conclusion:
Radiolysis species strongly affect corrosion mechanisms
The passive film remains stable under irradiation, although its protective properties are progressively degraded
The evolution of the passive film is strongly driven by energy deposition at the interface
Part of my first year was devoted to the development of experimental devices
Perspectives:
Further modeling of the passive film, particularly in the low-frequency domain
Further acquisition of experimental data under irradiation conditions
Physicochemical characterization of the passive film using additional analytical techniques, such as RBS, MEIS, ellipsometry, …
Implementation of pulsed radiolysis experiments to investigate short-lived radiolysis species
Modeling of passive film evolution mechanisms (Thesis, 2026)

## Slide 26
Thank you for listening